# Supporting Information

MOF Derived Oxygen-Vacancy-Rich ZrO2/UiO-66-NH2 for Efficient Visible-Light-Driven Oxidation of Benzyl Alcohol

Yanyan Song1,2· Zhichao Sun1,2 · Jiamin Sun3 · Ying-Ya Liu1,2 · Anjie Wang1,2 · Chong Peng1,2

1State Key Laboratory of Fine Chemicals, School of Chemical Engineering, Dalian University of Technology, Dalian 116024, China

2Liaoning Key Laboratory of Petrochemical Technology and Equipment, Dalian University of Technology, Dalian 116024, China

3Department of Chemistry, Division of Molecular Imaging and Photonics, KU Leuven, 3001, Leuven, Belgium

EPR analysis

Superoxide radical (•O₂⁻) Detection Procedure

5 mg sample was ultrasonically dispersed in 1 mL of anhydrous methanol for 5 min using a bath sonicator. The resulting suspension was subsequently treated with 40 μL of 5,5-dimethyl-1-pyrroline-N-oxide (DMPO) spin trap agent, followed by additional ultrasonication (3 min) to ensure complete homogenization. Approximately 50 μL of the homogeneous mixture was transferred into a capillary tube (0.5 mm i.d.) using a microsyringe, sealed with high-vacuum grease, and mounted in a 4 mm OD quartz EPR tube for measurement at 298 K.

Carbon-Centered Radical Testing Procedure

5 mg sample was ultrasonically dispersed in a benzyl alcohol/ acetonitrile (1:4 v/v) solution. Then, 40 μL of DMPO was added to the dispersion, followed by additional ultrasonication of 3 min to ensure homogeneity. Approximately 50 μL of the homogeneous mixture was transferred into a capillary tube (0.5 mm i.d.) using a microsyringe, sealed with high-vacuum grease, and mounted in a 4 mm OD quartz EPR tube for measurement at 298 K.

Fig. S1 The N2 adsorption-desorption isotherms of a UiO-66-NH2, b–d UiO-66-NH2-1h–3h and e UiO-66-NH2-24h; f Pore size distribution of the sample series

Table S1 Specific surface content data of UiO-66-NH2, UiO-66-NH2-2h and UiO-66-NH2-24h

| Sample | C 1s (atomic %) | N 1s (atomic %) | Zr 3d (atomic %) | O 1s (atomic %) |
| --- | --- | --- | --- | --- |
| UiO-66-NH2 | 61.40 | 5.92 | 4.23 | 28.45 |
| UiO-66-NH2-2h | 57.96 | 4.80 | 6.29 | 30.95 |
| UiO-66-NH2-24h | 42.80 | 3.57 | 13.20 | 40.43 |

Fig. S2 The high resolution XPS spectra for C 1s in UiO-66-NH2, UiO-66-NH2-2h, UiO-66-NH2-24h

Fig. S3 EPR spectra of samples under solvothermal and calcination treatment

Fig. S4 TGA profiles of UiO-66-NH2 and UiO-66-NH2-2h

Fig. S5 The time-dependent performance profile of UiO-66-NH2-2h

Fig. S6. PL emission spectra of UiO-66-NH2, UiO-66-NH2-2h, UiO-66-NH2-24h (λex=367 nm)

Table S2 Comparison of the performance of photocatalytic benzyl alcohol oxidation based on MOFs related catalysts

| Catalyst | Reaction condition | Atmosphere | Light source | Conv. (%) | Sel. (%) | Ref. |
| --- | --- | --- | --- | --- | --- | --- |
| MIL-53-NH2@ZnIn2S4 | 50 mg, 0.5 mmol benzyl alcohol, 20 mL toluene, 4 h | O2 | 300 W Xe lamp 400~780 nm | 56 | >99 | [1] |
| ZnFe2O4/UiO-66-NH2 | 20 mg, 0.2 mmol benzyl alcohol, 2 mL trifluorotoluene, 5 h | O2 | 300 W Xe lamp λ＞420 nm | 72 | 99 | [2] |
| CoFe2O4/Ce-UiO-66 | 100 mg, 1.0 mmol benzyl alcohol, 20 mL n-hexane, 6 h | air | visible-light | 75 | >99 | [3] |
| Bi3.43Fe0.57O6/MIL-53 | 30 mg, 0.2 mmol benzyl alcohol, 3 mL acetonitrile, 3 h | O2 | 300 W Xe lamp λ≥400 nm | 58.5 | >99 | [4] |
| PANI/FeUiO-66 | 5 mg, 0.2 mmol benzyl alcohol, 6 mL ethyl acetate, 5 h | O2 | 300 W Xe lamp λ≥400 nm | 61 | 99 | [5] |
| NH2-MIL-125@TAPB-PDA | 20 mg, 0.2 mmol benzyl alcohol, 3 mL acetonitrile, 30 h | O2 | 5 W LED 420~780nm 150 mW/cm2 | 94.7 | 99 | [6] |
| 0.1%Cu/Cu@UiO-66 | 32 mg, 0.2 mmol benzyl alcohol, 3 mL acetonitrile, 3 h | O2 | 300 W Xe lamp λ≥400 nm | 49.5 | 99 | [7] |
| Au/UIO-66-NH2 Pt/UIO-66-NH2 Pd/UIO-66-NH2 Ag/UIO-66-NH2 | 100 mg, 1 mmol benzyl alcohol, 20 mL toluene, 4 h | O2 | 300 W Xe lamp 350~780 nm | 30.5 9.3 30.3 19.4 | 95 | [8] |
| CdS-UiO-66(NH2) | 8 mg, 0.1 mmol benzyl alcohol, 1.5 mL trifluorotoluene, 4 h | O2 | 300 W Xe lamp λ≥420 nm | 30.12 | 99 | [9] |
| Ni-doped NH2-MIL-125 | 50 mg, 0.3 mmol benzyl alcohol. 6 mL trifluorotoluene, 10 h | O2 | 300 W Xe lamp 420≤λ≤800 nm | 43.2 | >99 | [10] |
| Fe2Co-MOF | 30 mg, 0.21 mmol benzyl alcohol, 2 mL acetonitrile, 12 h | TBHP (75 mg 70% in water) | 100 W LED 380~780 nm | 93.5 | >99 | [11] |
| CdS/Ni@NC(5) | 40 mg, 1mmol benzyl alcohol, 50 mL H2O, 12 h | air | 300 W Xe lamp λ≥420 nm | 78.1 | ~100 | [12] |
| UiO-66-NH2-2h | 50 mg, 0.3 mmol benzyl alcohol, 5 mL acetonitrile, 5 h | O2 | 30 W LED 420~800 nm 89 mW/cm2 | 74.1 | >99 | This work |

References

1.	Zhang L, Qiu J, Xia G et al. (2023) Constructing a Z-scheme Fe-MOF-based heterostructure for visible-light-driven oxidation of aromatic alcohol in ambient air. J Mater Sci Technol, 138: 214–220

2.	Liu J, Sun X, Jiang B et al. (2022) UiO-66-NH2 octahedral nanocrystals decorated with ZnFe2O4 nanoparticles for photocatalytic alcohol oxidation. ACS Appl Nano Mater, 5(2): 2231–2240

3.	Khosroshahi N, Karimi M, Taghvaei T et al. (2021) Ultrasound-assisted synthesis of CoFe2O4/Ce-UiO-66 nanocomposite for photocatalytic aerobic oxidation of aliphatic alcohols. Materials Today Chemistry, 22: 100582

4.	Zhang Q, Liu J-B, Chen L et al. (2020) An etching and re-growth method for the synthesis of bismuth ferrite/MIL-53(Fe) nanocomposite as efficient photocatalyst for selective oxidation of aromatic alcohols. App Catal B: Environ, 264: 118529

5.	Xu X, Liu R, Cui Y et al. (2017) PANI/FeUiO-66 nanohybrids with enhanced visible-light promoted photocatalytic activity for the selectively aerobic oxidation of aromatic alcohols. App Catal B: Environ, 210: 484–494

6.	Lu G, Huang X, Li Y et al. (2020) Covalently integrated core-shell MOF@COF hybrids as efficient visible-light-driven photocatalysts for selective oxidation of alcohols. Journal of Energy Chemistry, 43: 8–15

7.	Xiao L, Zhang Q, Chen P et al. (2019) Copper-mediated metal-organic framework as efficient photocatalyst for the partial oxidation of aromatic alcohols under visible-light irradiation: Synergism of plasmonic effect and schottky junction. App Catal B: Environ, 248: 380–387

8.	Qiu J, Zhang X, Xie K et al. (2019) Noble metal nanoparticle-functionalized Zr-metal organic frameworks with excellent photocatalytic performance. J Colloid Interface Sci, 538: 569–577

9.	Shen L, Liang S, Wu W et al. (2013) CdS-decorated UiO–66(NH2) nanocomposites fabricated by a facile photodeposition process: an efficient and stable visible-light-driven photocatalyst for selective oxidation of alcohols. Journal of Materials Chemistry A, 1(37): 11473–11482

10.	Fu Y, Sun L, Yang H et al. (2016) Visible-light-induced aerobic photocatalytic oxidation of aromatic alcohols to aldehydes over Ni-doped NH2-MIL-125(Ti). Applied Catalysis B: Environmental, 187: 212–217

11.	Ghasempour H, Zarekarizi F, Habibi B et al. (2025) Sustainable synthesis of a mixed-metal MOF: a visible light responsive photocatalyst for the selective oxidation of benzyl alcohols. CrystEngComm, 27: 4826–4834

12.	Yang H, Xia Y, Guo J et al. (2025) Highly-dispersed CdS nanoparticles coating hierarchical Ni@NC derived from ultrathin nanosheets NMOF-Ni: photocatalytic hydrogen evolution coupled with alcohol oxidation. Applied Catalysis B-Environment and Energy, 362: 124700