Research Article

Aromatic Ring-Coordinated g-C3N4 Nanotubes for Enhanced Photocatalytic H2 Evolution

Chongze Cai · Huaiyu Lu · Cheng Cheng* · Wengao Zeng · Xiangjiu Guan* · Liuhao Mao · Li Tian · Jinwen Shi* · Liejin Guo

International Research Center for Renewable Energy, State Key Laboratory of Multiphase Flow in Power Engineering, Xi’an Jiaotong University, Xi’an 710049, China

Received: 12 September 2025 / Revised: 12 October 2025 / Accepted: 20 October 2025 / Published online:

* Correspondence to Cheng Cheng, E-mail: ccheng-xjtu@xjtu.edu.cn; Xiangjiu Guan, E-mail: xj-guan@mail.xjtu.edu.cn; Jinwen Shi, E-mail: jinwen_shi@mail.xjtu.edu.cn

Chemical Materials

Melamine (C3H6N6, 99%), 2-bromo-5-chlorobenzoic acid (C7H4BrClO2, 98%), triethanolamine (C6H15NO3, 99%), ethanol (C2H5OH, 99%) and benzoic acid (C7H6O2, 98%) were received from Sinopharm Chemical Reagent Co., Ltd. Hexachloroplatinic acid (H2PtCl6·6H2O, 99%) was procured from Alfa Aesar. 2,5-Dibromobenzoic acid (C7H4Br2O2, 96%) and 2,5-dichlorobenzoic acid (C7H4Cl2O2, 98%) were both sourced from Shanghai Mairui Biotechnology Co., Ltd.

All of the reagents were used without any further purification.

Characterization

X-ray diffraction (XRD) patterns were recorded by a diffractometer (PANalytical X'pert MPD Pro, Netherlands) with a step size of 0.05° in the 2θ range of 5–80° at 40 kV and 40 mA under Ni-filtered Cu Kα irradiation (λ = 1.5406 Å). Fourier-transform infrared (FT-IR) spectra were obtained from an FT-IR spectrophotometer (Bruker Vertex70, Germany) in the wavenumber range of 4000–400 cm−1. X-ray photoelectron spectroscopy (XPS) analysis was performed by an X-ray photoelectron spectroscope (Kratos Axis Ultra DLD, Japan) with a monochromatic Al Kα line source (hν = 1486.69 eV), and the binding energy was calibrated with adventitious C 1s peak (284.8 eV) as reference. Elemental analysis (EA) was performed by an elemental analyzer (Euro EA3000, Italy). Thermogravimetric (TG) curves were obtained via a thermal analyzer (NETZSCH STA 449 C, Germany) under the conditions of nitrogen atmosphere, gas flow rate of 10 mL/min, heating rate of 10 ℃/min, and heating range of 25–800 ℃. Scanning electron microscopy (SEM) images were obtained from a field-emission scanning electron microscope (JEOL JSM-7800F, Japan). Transmission electron microscopy (TEM) images were obtained from a transmission electron microscope (FEI Tecnai G2 F30 S-Twin, USA). Surface area and porosity measurement was carried out by N2 adsorption on a surface area and porosity analyzer (Micromeritics ASAP 2020, USA). All samples were degassed at 393 K under vacuum for 12 h before test. Ultraviolet-visible (UV–Vis) absorption spectra were recorded by a UV–Vis-NIR spectrophotometer (Agilent Cary 5000, USA) under diffuse reflection mode with a BaSO4 reference in the range of 300–800 nm. Steady-state photoluminescence (PL) spectra were recorded by a fluorescence spectrophotometer (PTI QuantaMaster 40, USA) with an excitation wavelength of 339 nm at room temperature. Transient photoluminescence (PL) was recorded by a fluorescence spectrophotometer (Edinburgh FLS1000, UK) with an excitation wavelength of 375 nm at room temperature. Electron paramagnetic resonance (EPR) analysis was performed by an electron-paramagnetic-resonance instrument (Bruker EMX X-band, Germany). Zeta potential test was carried out by a nanoparticle potentiometer (Malvern Zetasizer Nano ZS90, UK).

Electrochemical Measurements

Electrochemical measurements were carried out on an electrochemical workstation (CH Instruments CHI 760D, USA) in a three-electrode system using Ag/AgCl electrode as the reference electrode and Pt foil as the counter electrode. A 500 W xenon lamp coupled with an AM 1.5 filter was used as the light source and the light intensity was set at 100 mW/cm2. Na2SO4 (0.5 mol/L) was employed as electrolyte. The transient photocurrent densities were obtained at an applied voltage (+0.6 V vs. Ag/AgCl).

Electrochemical impedance spectroscopy (EIS) was measured at the same bias voltage with the frequency ranging from 100 to 1 Hz with a 5 mV AC dither.

Photocatalytic Measurements

Photocatalytic H2 evolution experiments were carried out in a Pyrex glass reactor with a side window for light irradiation from a 300 W Xe lamp (Perfect light PLS-SXE300, China) equipped with a UV-cutoff filter (λ > 400 nm). The H2 evolution rate is recorded by a gas chromatography (13X zeolite column, thermal conductivity detector, Ar as carrier gas).

Calculation Method

Tauc plot was obtained by Kubelka–Munk (K–M) transformation：

FR=1-R22R#1

where R is the relative reflectivity of sample and F(R) is the K–M function.

FR=A(hν -Eg)n∕2#2

where h is the Planck constant; ν is the photon frequency; A is the proportional constant; Eg is the band gap value of sample; and n represents the transition type of semiconductor (for g-C3N4, n = 1). Tauc plot was obtained by plotting the curve with hν as the abscissa and (F(R)hν)1/2 as the ordinate. The abscissa of the intersection point of the horizontal axis and the tangent of the linear part of the curve is Eg.

A double exponential fitting model was used to fit the transient PL attenuation curves:

It=A1ⅇ-t∕τ1+A2e-t∕τ2#3

where I(t) is the PL intensity at time t; A1 and A2 are the amplitudes of each attenuation component; and τ1 and τ2 are the lifetimes corresponding to each attenuation component. The average lifetimes (τavg) was obtained through Eq.(4).

τavg=A1τ1+A2τ2A1+A2#4

The apparent quantum yields (AQY) for photocatalytic H2 evolution were measured under the above Xe arc lamp with different band-pass filter (λ = 380, 400, 420, 470, 500, 520 and 600 nm), and calculated according to Eq.(5).

AQY (%) =Number of reacted electronsNumber of incident photons× 100%

= Number of H2 evolved ×2Number of incident photons× 100%#5

Result and Discussion

Fig. S1 a XRD patterns and b FT-IR spectra of the g-C3N4 samples

The X-ray diffraction (XRD) patterns of CN-XXB are shown in Fig. S1a. All CN-XXB samples showed similar XRD diffraction peaks corresponding to the (100) and (002) planes of the g-C3N4 structure appeared around 13.2° and 27.4°, respectively [1]. The results indicated that the introduction of aromatic small molecules during the hydrothermal process had a negligible effect on the construction of crystal structure for g-C3N4.

Figure S1b presents the Fourier-transform infrared (FT-IR) spectra of CN-XXB sample. The absorption peak near 800 cm−1 corresponded to the ring stretching vibration of the triazine ring system, while the absorption peaks in the range of 1100–1750 cm−1 corresponded to the bending vibration of the C–N heterocyclic structure [2]. The absorption peaks in the range of 3000–3700 cm−1 corresponded to the stretching vibration of the N–H bonds of the uncondensed amino groups and the water molecules adsorbed from the air [3]. In conjunction with the XRD analysis, it could be concluded that the introduction of different aromatic small molecules did not damage the fundamental framework of g-C3N4.

Fig. S2 TG curves of precursors MCN-p and CN-BCB-p

Fig. S3 SEM images of a, b MCN-p and c, d CN-BCB-p. Scale bar: a 100 μm, b, c, d 10 μm

Fig. S4 SEM images of a CN-BBB, b CN-CCB, and c CN-BCB. Scale bar: 1 μm

Fig. S5 TEM images of a, b CN-BBB and c CN-CCB. Scale bar: a 1 μm, b, c 50 nm

Fig. S6 a N2 adsorption-desorption isotherms of the g-C3N4 samples; b BJH pore size distribution curves of the g-C3N4 samples

Fig. S7 XRD patterns of CN-BCB and CN-BCB-R (CN-BCB after 18 h stability test)

The CN-BCB after the 18 h stability test was recovered for XRD analysis and named as CN-BCB-R. It can be seen from Fig. S7 that the XRD peaks of CN-BCB and CN-BCB-R are not much different, which means that its crystal structure did not change much.

Table S1 BET specific surface areas, pore volumes and average pore sizes of the g-C3N4 samples

| Sample | Surface area (m2/g) | Pore volume (cm3/g) | Average pore size (nm) |
| --- | --- | --- | --- |
| MCN | 18.0 | 0.061 | 14.2 |
| CN-BBB | 26.4 | 0.097 | 15.1 |
| CN-CCB | 33.9 | 0.129 | 19.1 |
| CN-BCB | 30.4 | 0.166 | 31.7 |

References

[1] Maeda K, Wang XC, Nishihara Y et al (2009) Photocatalytic activities of graphitic carbon nitride powder for water reduction and oxidation under visible light. J Phys Chem C 113(12):4940–4947

[2] Wang ZC, Di BH, Gong SQ et al (2025) Piezoelectric field and TENG co-promoted photocatalytic degradation of HCHO on BaTiO3/g-C3N4/PTFE/Cu for self-cleaning and air-purification. Appl Catal B Environ 364:124859

[3] Sadanandan AM, Fawaz M, Dharmarajan NP et al (2025) Mesoporous C-doped C3N5 as a superior photocatalyst for CO2 reduction. Appl Catal B Environ 362:124701