Table S1. ANOVA Tables for Reduced Quadratic Models (Particle Size, PDI, Zeta Potential, and Encapsulation Efficiency)

(a) Response 1: Particle Size (nm)

| Source | Sum of Squares | df | Mean Square | F-value | p-value |  |
| --- | --- | --- | --- | --- | --- | --- |
| Model | 5068.09 | 5 | 1013.62 | 76.45 | < 0.0001 | significant |
| A-BSA | 83.85 | 1 | 83.85 | 6.32 | 0.0287 |  |
| B-RSV:BSA | 1272.60 | 1 | 1272.60 | 95.98 | < 0.0001 |  |
| C-PC:BSA | 3256.24 | 1 | 3256.24 | 245.59 | < 0.0001 |  |
| BC | 93.12 | 1 | 93.12 | 7.02 | 0.0226 |  |
| B² | 362.27 | 1 | 362.27 | 27.32 | 0.0003 |  |
| Residual | 145.85 | 11 | 13.26 |  |  |  |
| Lack of Fit | 145.85 | 7 | 20.84 |  |  |  |
| Pure Error | 0.0000 | 4 | 0.0000 |  |  |  |
| Cor Total | 5213.94 | 16 |  |  |  |  |

R² = 0.9720; Adjusted R² ≈ 0.956

(b) Response 2: PDI

| Source | Sum of Squares | df | Mean Square | F-value | p-value |  |
| --- | --- | --- | --- | --- | --- | --- |
| Model | 0.0116 | 5 | 0.0023 | 48.64 | < 0.0001 | significant |
| A-BSA | 0.0005 | 1 | 0.0005 | 11.04 | 0.0068 |  |
| B-RSV:BSA | 0.0046 | 1 | 0.0046 | 95.30 | < 0.0001 |  |
| C-PC:BSA | 0.0041 | 1 | 0.0041 | 86.53 | < 0.0001 |  |
| B² | 0.0021 | 1 | 0.0021 | 44.41 | < 0.0001 |  |
| Residual | 0.0005 | 11 | 0.0000 |  |  |  |
| Lack of Fit | 0.0005 | 7 | 0.0001 |  |  |  |
| Pure Error | 0.0000 | 4 | 0.0000 |  |  |  |
| Cor Total | 0.0122 | 16 |  |  |  |  |

R² = 0.9582

(c) Response 3: Zeta Potential (mV)

| Source | Sum of Squares | df | Mean Square | F-value | p-value |  |
| --- | --- | --- | --- | --- | --- | --- |
| Model | 407.19 | 6 | 67.86 | 28.14 | < 0.0001 | significant |
| A-BSA | 19.53 | 1 | 19.53 | 8.10 | 0.0174 |  |
| B-RSV:BSA | 79.38 | 1 | 79.38 | 32.92 | 0.0002 |  |
| C-PC:BSA | 225.78 | 1 | 225.78 | 93.63 | < 0.0001 |  |
| AB | 14.06 | 1 | 14.06 | 5.83 | 0.0364 |  |
| A² | 13.88 | 1 | 13.88 | 5.76 | 0.0374 |  |
| B² | 51.37 | 1 | 51.37 | 21.30 | 0.0010 |  |
| Residual | 24.11 | 10 | 2.41 |  |  |  |
| Lack of Fit | 24.11 | 6 | 4.02 |  |  |  |
| Pure Error | 0.0000 | 4 | 0.0000 |  |  |  |
| Cor Total | 431.30 | 16 |  |  |  |  |

R² = 0.9441

(d) Response 4: Entrapment Efficiency (%)

| Source | Sum of Squares | df | Mean Square | F-value | p-value |  |
| --- | --- | --- | --- | --- | --- | --- |
| Model | 702.91 | 5 | 140.58 | 46.82 | < 0.0001 | significant |
| A-BSA | 54.60 | 1 | 54.60 | 18.19 | 0.0013 |  |
| B-RSV:BSA | 310.00 | 1 | 310.00 | 103.25 | < 0.0001 |  |
| C-PC:BSA | 181.45 | 1 | 181.45 | 60.43 | < 0.0001 |  |
| B² | 131.23 | 1 | 131.23 | 43.71 | < 0.0001 |  |
| C² | 19.52 | 1 | 19.52 | 6.50 | 0.0270 |  |
| Residual | 33.03 | 11 | 3.00 |  |  |  |
| Lack of Fit | 33.03 | 7 | 4.72 |  |  |  |
| Pure Error | 0.0000 | 4 | 0.0000 |  |  |  |
| Cor Total | 735.94 | 16 |  |  |  |  |

R² = 0.9551

Figure S1. Diagnostic plots confirming the validity of the reduced quadratic models for (a) Particle Size, (b) PDI, (c) Zeta Potential, and (d) Encapsulation Efficiency. In each case: (i) normal probability plot of residuals (showing linearity, confirming normality), (ii) residuals versus predicted values (random scatter, confirming constant variance), and (iii) residuals versus run order (no trends, confirming independence).