Influence of Formulation Composition and Rheological Properties on the Stability of PnPP19 Peptide in Thermoresponsive Hydrogels

FROHLICH, Anna Luciaa,b; MOREIRA, Magali Portelaa, TRINDADE, Camilla Nunes dos Reisc; NEVES, Gabriela Westerlund Peixotoc; LACATIVA, Paulo Gustavoc; PAESE, Karinad; AGUIRRE, Tanira Alessandra Silveiraa,b,*

aGrupo de Pesquisa em Nanomedicina – TANANO,  Universidade Federal de Ciências da Saúde de Porto Alegre. 90050-170, Porto Alegre, RS, Brasil.

bPrograma de Pós-Graduação em Biociências, Universidade Federal de Ciências da Saúde de Porto Alegre. 90050-170, Porto Alegre, RS, Brasil.

c Biozeus Biopharmaceutical S.A. Rua Visconde de Pirajá 623, 9 andar. 22410-003, Rio de Janeiro, RJ, Brasil.

dPrograma de Pós-Graduação em Ciências Farmacêuticas, Faculdade de Farmácia, Universidade Federal do Rio Grande do Sul. 90610-001, Porto Alegre, RS, Brasil.

*Corresponding author: tanira@ufcspa.edu.br

Supplementary  Material

Figure S1: Mean linearity curve. Data fitted with a linear mathematical model. Range 10-100 µg mL-1.

Table S1: Precision, accuracy, work range, limit of detection (LOD), and limit of quantification (LOQ) values.

| Precision (%RSD ± SD) | Inter-day (n=7) | 1.55% ± 0.06 |
| --- | --- | --- |
|  | Intra-day (n=14) | 1.66% ± 0.19 |
| Accuracy (mean ± SD) | Low (25 µg mL-1) (n=3) | 101.18% ± 2.70 |
|  | Medium (50 µg mL-1) (n=3) | 99.75% ± 0.48 |
|  | High (75 µg mL-1) (n=3) | 101.01% ± 1.25 |
| Range |  | 10 – 100 µg mL-1 |
| LOQ |  | 10 µg mL-1 |
| LOD |  | 3.33 µg mL-1 |

Table S2: Statistical analysis of 14F-PEHG, 16F-PEHG, and 17F-PEHG after 1, 3 and 6 months at 25 ºC.

| Time (Month) | Comparison |  | p-value* |
| --- | --- | --- | --- |
| 1 | 17F-PEHG | 14F-PEHG | 0.0175 |
|  | 17F-PEHG | 16F-PEHG | 0.5775 |
|  | 14F-PEHG | 16F-PEHG | 0.0376 |
| 3 | 17F-PEHG | 14F-PEHG | 0.0003 |
|  | 17F-PEHG | 16F-PEHG | <0.0001 |
|  | 14F-PEHG | 16F-PEHG | 0.6771 |
| 6 | 17F-PEHG | 14F-PEHG | 0.1655 |
|  | 17F-PEHG | 16F-PEHG | 0.8321 |
|  | 14F-PEHG | 16F-PEHG | 0.2446 |

*ANOVA one-way unpaired with Tukey post-hoc.

Table S3: Statistical analysis of 14S-PEHG vs. 14F-PEHG and 16S-PEHG vs. 16F-PEHG up to 9 months at 25 ºC.

|  | p-value* |  |
| --- | --- | --- |
| Time (Month) | 14S-PEHG vs. 14F-PEHG | 16S-PEHG vs. 16F-PEHG |
| 1 | 0.4149 | 0.0256 |
| 2 | 0.0035 | <0.0001 |
| 3 | 0.1733 | 0.0024 |
| 4 | <0.0001 | 0.0002 |
| 5 | 0.0004 | 0.0003 |
| 6 | 0.0034 | 0.0004 |
| 9 | 0.0028 | 0.0009 |

*Unpaired t-test with Welch’s correction of p value.

Figure S2: Degradation behavior of selected formulations at 25 ºC.

Table S4: Statistical analysis of 10S-PEHG vs. 16F-PEHG up to 9 months at 25 ºC.

| Time (Month) | p-value* |
| --- | --- |
| 1 | 0.0011 |
| 2 | 0.0003 |
| 3 | 0.0021 |
| 4 | 0.0004 |
| 5 | 0.0289 |
| 6 | 0.0170 |
| 9 | 0.0053 |

*Unpaired t-test with Welch’s correction of p value

Figure S3: Cumulative percentage degradation of the peptide in formulations 10S-PEHG and 16F-PEHG at 5 (A), 25 (B), and 40 °C (C).

Figure S4: Dynamic light scattering (DLS) size distributions of 10S-PEHG and 16F-PEHG at 5, 25, and 40 °C. Size distributions are presented by intensity, number, and volume. Samples were analyzed without dilution using backscatter detection at 173° (n = 3).

Table S5: Dynamic light scattering (DLS) characterization of 10S-PEHG and 16F-PEHG at 5, 25, and 40 °C. Hydrodynamic size distributions are reported by intensity, number, and volume, together with the polydispersity index (PDI). Results are expressed as mean ± standard deviation (n = 3). Samples were analyzed without dilution.

| Formulation 10S-PEHG |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Temperature |  |  |  | Hydrodynamic diameter (nm) |  |  |  |  |  |  |  |  |
| (⁰C) | PDI |  |  | Intensity |  |  | Number |  |  | Volume |  |  |
| 5 | 0.82 | ± | 0.02 | 112.0 | ± | 162.2 | 10.3 | ± | 0.7 | 13.1 | ± | 0.5 |
| 25 | 0.92 | ± | 0.06 | 128.5 | ± | 176.2 | 9.6 | ± | 0.6 | 12.5 | ± | 0.7 |
| 40 | 0.53 | ± | 0.03 | 19.2 | ± | 1.3 | 9.7 | ± | 0.1 | 12.5 | ± | 0.1 |
| Formulation 16F-PEHG |  |  |  |  |  |  |  |  |  |  |  |  |
| Temperature |  |  |  | Hydrodynamic diameter (nm) |  |  |  |  |  |  |  |  |
| (⁰C) | PDI |  |  | Intensity |  |  | Number |  |  | Volume |  |  |
| 5 | 0.61 | ± | 0.04 | 4.4 | ± | 1.1 | 3.9 | ± | 1.1 | 4.2 | ± | 1.1 |
| 25 | 0.13 | ± | 0.01 | 8.2 | ± | 0.1 | 5.0 | ± | 0.2 | 6.2 | ± | 0.2 |
| 40 | 0.30 | ± | 0.17 | 12.3 | ± | 0.4 | 6.3 | ± | 0.6 | 8.0 | ± | 0.5 |