Supplemtary material Table 3. Removal efficiency corresponding to the studied rocks, grain size, synthetic solutions, and groundwater samples

| water type | sample rock used | grain size (mm) | Initial concentrations of the synthetic solution (mg/L) | The highest removal efficiency (%) | water type | sample rock used | grain size (mm) | Initial concentrations of the synthetic solution (mg/L) | The highest removal efficiency (%) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| synthetic solutions of fluoride | DD1705 | <0.05 | 7.2 | 34.39 | high fluoride contents in groundwater | DD1705 | <0.05 | 7.2 | 23.73 |
|  | DD1705 | <0.05 | 2.8 | 32.68 |  | DD1705 | <0.05 | 2.8 | 17.69 |
|  | DD1705 | 0.50-1.41 | 7.2 | 13.99 |  | DD1705 | 0.50-1.41 | 7.2 | 9.05 |
|  | DD1705 | 0.50-1.41 | 2.8 | 17.3 |  | DD1705 | 0.50-1.41 | 2.8 | 17.25 |
| synthetic solutions of arsenic | DD1705 | <0.05 | 7.2 | 94.6 | high arsenic contents in groundwater | DD1705 | <0.05 | 7.2 | 56.16 |
|  | DD1705 | <0.05 | 2.8 | 94.08 |  | DD1705 | <0.05 | 2.8 | 45 |
|  | DD1705 | 0.50-1.41 | 7.2 | 85.16 |  | DD1705 | 0.50-1.41 | 7.2 | 24.66 |
|  | DD1705 | 0.50-1.41 | 2.8 | 82.84 |  | DD1705 | 0.50-1.41 | 2.8 | 20.83 |