Online Resource 2

Chemical composition of glass reference materials as published (after Adlington 2017) and analysed. The analysed result is the average of four analyses in wt% determined by EDS analyses. ‘-’ indicates ‘not published’ in the published data or not analysed.

| Glass standard | Na2O | MgO | Al2O3 | SiO2 | P2O5 | SO3 | Cl | K2O | CaO | TiO2 | MnO | Fe2O3 | CuO | Sb2O5 | BaO | PbO |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Corning A (published) | 14.3 | 2.66 | 1.00 | 66.6 | 0.08 | 0.14 | 0.09 | 2.87 | 5.03 | 0.79 | 1.00 | 1.09 | 1.17 | 1.75 | 0.46 | 0.07 |
| Measured (Average) | 14.31 | 2.52 | 0.95 | 69.42 | - | - | - | 2.75 | 4.94 | 0.74 | 0.96 | 1.04 | 1.19 | 1.79 | - | - |
| St. Dev. | 2.05 | 0.19 | 0.06 | 2.86 | - | - | - | 0.12 | 0.23 | 0.06 | 0.05 | 0.05 | 0.10 | 0.07 | - | - |
| Corning B (published) | 17.0 | 1.03 | 4.36 | 61.6 | 0.82 | 0.49 | 0.16 | 1.00 | 8.56 | 0.09 | 0.25 | 0.34 | 2.66 | 0.46 | 0.08 | 0.61 |
| Measured (Average) | 17.17 | 0.94 | 4.21 | 64.88 | 0.74 | 0.63 | 0.16 | 1.03 | 8.51 | - | 0.24 | 0.31 | 2.65 | - | - | - |
| St. Dev. | 0.23 | 0.06 | 0.14 | 2.44 | 0.06 | 0.08 | 0.04 | 0.06 | 0.12 | - | 0.05 | 0.04 | 0.01 | - | - | - |
| Corning C (published) | 1.07 | 2.76 | 0.87 | 34.9 | 0.07 | 0.1 | 0.1 | 2.84 | 5.07 | 0.79 | - | 0.34 | 1.13 | - | 11.4 | 36.7 |
| Measured (Average) | 1.41 | 2.58 | 0.88 | 35.09 | - | - | - | 2.72 | 4.89 | - | - | 0.27 | 1.21 | - | 11.39 | 36.79 |
| St. Dev. | 0.17 | 0.10 | 0.06 | 0.07 | - | - | - | 0.11 | 0.15 | - | - | 0.08 | 0.18 | - | 0.02 | 0.06 |
| Corning D (published) | 1.20 | 3.94 | 5.30 | 55.2 | 3.93 | 0.23 | 0.16 | 11.3 | 14.8 | 0.38 | 0.55 | 0.52 | 0.38 | 0.97 | 0.29 | 0.24 |
| Measured (Average) | 1.54 | 3.90 | 5.20 | 58.28 | 3.85 | - | - | 11.10 | 14.45 | 0.37 | 0.53 | 0.51 | 0.36 | - | - | - |
| St. Dev. | 0.20 | 0.13 | 0.18 | 0.54 | 0.15 | - | - | 0.39 | 0.46 | 0.04 | 0.04 | 0.04 | 0.06 | - | - | - |