Online Resource 4: Trace elements of 40 objects from SPA, by PIXE. Results are organised by sites and burials. Unknown cemeteries and burials are indicated with the symbol "-". Limit of detection for each reading are presented in grey, with the symbol "<". Three objects were sampled twice: popm005-006, popm013-014 and popm039-040.Major and light elements are presented in %, not ppm. (*) Light elements relate to surface dirt from the soil and/or corrosion.

|  |  |  |  | Major elements (wt%) |  |  | Trace elements (ppm) |  |  |  |  |  |  |  |  | Light elements (wt%)* |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Filter: | HE1 | HE3 | HE1 | BE0 | HE1 | HE1 | BE0 | HE3 | HE1 | HE1 | HE1 | HE3 | BE0 | BE0 | BE0 | BE0 | BE0 |
| Dose | N° Id Lab | Site | Burial | Cu | Ag | Au #L | Ti | Mn | Fe | Ni | Zn | Ga | Hg #L | Pb #L | W #L | Si | S | Cl | K | Ca |
| 600000 | popm002 | C. Parr. | 7 | 2.1 | 28.7 | 61.5 | < 60 | < 1200 | < 720 | < 29 | 520 | < 81 | < 3300 | < 160 | < 180 | < 0.5 | 2.5 | 4.9 | < 0.1 | 0.1 |
| 15000000 | popm003 | C. Parr. | 7 | 2.7 | 24.9 | 71.7 | < 26 | < 990 | < 590 | < 95 | 1190 | < 210 | < 2700 | < 190 | < 380 | < 0.3 | < 0.2 | 0.6 | < 0.1 | < 0.04 |
| 12000000 | popm008 | C. Parr. | 7 | 1.4 | 20.6 | 77.0 | < 150 | < 1000 | 1300 | 300 | 960 | < 210 | < 3500 | < 16 | < 150 | < 1.2 | < 0.5 | 0.8 | < 0.1 | < 0.1 |
| 600000 | popm009 | C. Parr. | 7 | 2.8 | 28.9 | 66.9 | < 50 | < 580 | < 640 | 81 | 750 | 500 | < 3900 | < 290 | < 480 | < 0.2 | < 0.1 | 1.2 | < 0.1 | 0.1 |
| 1000000 | popm011 | C. Parr. | 7 | 1.8 | 21.0 | 76.2 | < 38 | < 1200 | 960 | < 42 | 690 | < 83 | < 1500 | < 160 | < 640 | < 0.2 | 0.5 | 0.1 | < 0.1 | 0.1 |
| 600000 | popm001 | C. Parr. | 8 | 1.9 | 57.7 | 36.3 | < 100 | < 1000 | < 780 | < 38 | 610 | < 66 | < 1700 | < 130 | 200 | 3.0 | 0.6 | 0.3 | < 0.1 | 0.2 |
| 12000000 | popm010 | C. Parr. | 8 | 2.3 | 58.6 | 33.5 | 190 | < 870 | 1700 | < 20 | 600 | 140 | < 2100 | < 110 | < 540 | 2.9 | 0.9 | 1.4 | < 0.1 | 0.3 |
| 12000000 | popm007 | C. Parr. | 16 | 0.9 | 78.0 | 21.1 | < 3300 | < 770 | < 160 | < 3100 | 730 | 140 | < 1100 | < 75 | < 110 | < 27.2 | < 1.9 | < 0.7 | < 0.9 | < 0.3 |
| 600000 | popm047 | C. Parr. | 16 | 1.1 | 35.2 | 62.6 | < 110 | < 420 | 1700 | < 62 | 1500 | < 96 | < 3500 | < 180 | < 1000 | < 1.0 | 0.6 | < 0.1 | < 0.1 | 0.1 |
| 12000000 | popm017 | C. Parr. | 18 | 0.4 | 27.1 | 68.5 | 390 | < 660 | 1900 | < 57 | 800 | < 140 | < 4000 | < 140 | < 1000 | 2.4 | 0.9 | 0.2 | < 0.1 | 0.3 |
| 12000000 | popm018 | C. Parr. | 18 | 0.7 | 28.0 | 66.7 | 230 | < 1500 | 3000 | < 48 | 800 | < 190 | < 4000 | < 200 | < 940 | 2.4 | 1.2 | 0.2 | 0.2 | 0.2 |
| 600000 | popm043 | Coyo-3 | 11 | 0.4 | 49.4 | 0.6 | < 220 | 3000 | < 1400 | < 82 | 380 | 60 | 600 | 150 | < 440 | < 2.4 | 0.6 | 1.7 | < 0.2 | 46.9 |
| 15000000 | popm036 | Larache | 1714 | 0.2 | 13.3 | 82.7 | < 84 | < 620 | 2700 | 170 | 800 | < 180 | < 3900 | < 380 | < 990 | 2.4 | < 0.4 | 0.5 | 0.4 | 0.2 |
| 1000000 | popm035 | Larache | 1714 | 5.6 | 38.3 | 55.0 | 400 | < 870 | 1110 | < 23 | < 410 | < 62 | < 1000 | < 86 | < 110 | < 0.6 | 0.5 | 0.3 | < 0.02 | 0.2 |
| 12000000 | popm014 | Larache | 6-6 | 2.1 | 40.5 | 57.2 | < 40 | < 1200 | < 640 | < 25 | 550 | < 77 | < 2900 | < 150 | < 1100 | < 0.9 | < 0.2 | 0.1 | < 0.1 | 0.1 |
| 12000000 | popm013 | Larache | 6-6 | 1.9 | 42.1 | 55.6 | < 23 | < 960 | 1020 | 160 | 650 | < 63 | < 970 | < 110 | < 140 | < 0.9 | < 0.2 | 0.2 | < 0.1 | 0.1 |
| 600000 | popm012 | Larache | 7-8 | 6.0 | 16.0 | 77.4 | < 51 | < 900 | 1400 | 240 | < 210 | < 70 | < 1200 | < 63 | < 640 | < 0.7 | < 0.2 | 0.2 | 0.2 | 0.1 |
| 12000000 | popm019 | Larache | 7-8 | 1.8 | 15.6 | 77.0 | 8100 | < 790 | 4400 | < 83 | < 780 | < 180 | < 4000 | 8100 | < 820 | 2.4 | < 0.1 | 1.0 | < 0.1 | 0.2 |
| 12000000 | popm023 | Q5 or S3 | - | 2.2 | 10.6 | 78.6 | 490 | < 1200 | 5900 | < 63 | 650 | < 140 | < 5000 | < 190 | < 500 | 5.3 | < 0.2 | 1.5 | 0.7 | 0.3 |
| 1000000 | popm028 | Q5 or S3 | - | 1.2 | 23.5 | 74.8 | < 130 | < 1100 | 2100 | 170 | < 510 | < 70 | < 3500 | < 160 | < 810 | < 1.0 | < 0.3 | 0.1 | < 0.1 | 0.1 |
| 12000000 | popm005 | Quitor-1 | - | 1.1 | 68.3 | 27.1 | 430 | < 1000 | < 400 | < 37 | 690 | < 53 | < 1500 | < 100 | < 370 | 1.6 | 1.7 | < 0.1 | < 0.1 | 0.2 |
| 600000 | popm006 | Quitor-1 | - | 1.3 | 71.5 | 26.8 | < 76 | < 790 | < 230 | < 20 | 740 | < 47 | < 590 | < 71 | < 590 | < 0.6 | 0.3 | < 0.1 | < 0.1 | 0.1 |
| 12000000 | popm032 | Quitor-1 | 889 | 1.0 | 64.9 | 30.4 | 630 | < 560 | < 510 | < 22 | 660 | < 51 | < 1700 | < 92 | < 810 | 1.6 | 1.3 | 0.4 | < 0.1 | 0.3 |
| 12000000 | popm033 | Quitor-1 | 889 | 1.0 | 61.4 | 31.6 | 360 | < 520 | 2200 | < 18 | 620 | < 50 | < 1700 | < 91 | < 520 | 3.5 | 1.7 | 0.2 | < 0.1 | 0.4 |
| 12000000 | popm034 | Quitor-1 | 889 | 0.8 | 61.6 | 34.7 | 102 | < 670 | 780 | < 26 | 640 | < 40 | < 1400 | < 78 | < 690 | 1.1 | 1.2 | 0.3 | < 0.1 | 0.2 |
| 15000000 | popm037 | Quitor-1 | 889 | 0.8 | 58.6 | 32.5 | 430 | < 750 | 3400 | < 38 | 1010 | < 86 | < 1600 | < 32 | < 830 | 2.8 | 3.8 | 0.4 | < 0.1 | 0.6 |
| 15000000 | popm039 | Quitor-1 | 889 | 0.9 | 56.4 | 41.5 | 570 | < 830 | < 650 | < 48 | 800 | < 83 | < 2000 | < 150 | < 710 | < 0.5 | 0.4 | 0.5 | < 0.1 | 0.1 |
| 15000000 | popm040 | Quitor-1 | 889 | 1.1 | 51.2 | 43.6 | 450 | < 1200 | 1600 | < 59 | 600 | < 77 | < 1800 | < 150 | < 720 | < 1.1 | 2.7 | 0.6 | < 0.04 | 0.6 |
| 600000 | popm026 | Quitor-5 | 2003 | 1.4 | 13.6 | 78.9 | 400 | < 710 | 3200 | < 42 | < 390 | < 65 | < 4200 | < 160 | < 1500 | 2.9 | 1.1 | 0.7 | 0.3 | 0.8 |
| 1000000 | popm030 | Quitor-5 | - | 2.6 | 33.0 | 58.7 | 500 | < 1300 | 940 | < 56 | < 360 | < 160 | < 3200 | < 170 | < 410 | 1.2 | 3.5 | 0.7 | < 0.1 | 0.3 |
| 12000000 | popm027 | Quitor-5? | - | 47.9 | 3.9 | 46.9 | < 51 | < 750 | < 560 | 113 | 1700 | 820 | < 960 | 740 | < 2000 | < 0.2 | 0.3 | 0.4 | 0.2 | 0.1 |
| 12000000 | popm015 | Seq. Al. | 767 | 0.7 | 7.5 | 89.0 | 230 | < 1300 | 2800 | 110 | < 450 | < 170 | < 5300 | < 190 | < 920 | 2.2 | < 0.5 | 0.2 | 0.2 | 0.2 |
| 1000000 | popm016 | Seq. Al. | no burial | 1.4 | 8.3 | 83.9 | 250 | < 640 | 6700 | < 38 | < 480 | < 79 | < 3600 | < 82 | < 1000 | 4.8 | < 0.3 | 0.2 | 0.4 | 0.3 |
| 1000000 | popm020 | - | - | < 0.02 | 5.8 | 90.0 | 210 | < 610 | 3400 | 104 | 790 | < 140 | < 3300 | < 140 | < 450 | 2.7 | < 0.1 | 0.5 | 0.4 | 0.3 |
| 12000000 | popm021 | - | - | 2.8 | 24.4 | 70.5 | < 46 | < 1000 | < 770 | < 32 | < 390 | < 74 | < 1200 | < 120 | < 760 | < 0.8 | 0.6 | 1.7 | < 0.04 | 0.1 |
| 1000000 | popm022 | - | - | 2.5 | 25.0 | 70.7 | < 72 | < 1100 | < 770 | < 24 | < 480 | < 80 | < 2600 | < 130 | < 580 | < 0.2 | < 0.3 | 1.7 | < 0.05 | 0.1 |
| 12000000 | popm024 | - | - | 0.9 | 54.5 | 40.0 | 310 | < 690 | 1500 | 84 | 660 | < 99 | < 2500 | < 120 | < 450 | < 1.3 | 3.6 | 0.4 | < 0.1 | 0.4 |
| 1000000 | popm025 | - | - | 1.3 | 49.4 | 48.2 | < 100 | < 370 | < 450 | < 25 | 490 | < 80 | < 1100 | < 150 | < 400 | < 0.2 | 0.8 | 0.2 | < 0.1 | 0.1 |
| 600000 | popm029 | - | - | 1.8 | 27.0 | 69.8 | < 49 | < 970 | < 690 | < 26 | < 460 | < 67 | < 1100 | < 110 | < 940 | < 0.3 | < 0.1 | 1.4 | < 0.04 | 0.1 |
| 15000000 | popm038 | - | - | 1.1 | 29.4 | 66.2 | < 130 | < 790 | 1500 | < 77 | 840 | < 90 | < 1400 | < 140 | < 1000 | < 1.2 | < 0.5 | 2.9 | < 0.1 | 0.2 |
| 600000 | popm041 | - | - | 6.4 | 48.0 | 37.0 | < 68 | < 1200 | < 470 | < 46 | < 460 | < 76 | < 2300 | < 130 | < 810 | < 0.9 | 0.9 | 7.1 | < 0.1 | 0.2 |
| 600000 | popm045 | - | - | 0.04 | 7.2 | 90.1 | < 70 | < 500 | 1700 | < 62 | 890 | < 120 | < 3400 | < 160 | < 710 | 1.7 | < 0.2 | 0.3 | 0.2 | 0.2 |

In the 38 samples analysed, PIXE detected nine elements at trace levels (<0.1%): Fe, Zn, Ti, Ni, Ga, Pb, Hg, Mn and W (full results in Online Resource 3). Most of the samples share similar elements, mainly Zn, Fe and Ti. Overall, no evident groups are found by trace elements but some patterns helped in the identification of specific batches, supporting the information obtained by the pXRF and SEM-EDS. Light elements were also detected: Si, K, Ca, S and Cl. Si are probably associated with quartz inclusions in the metal or on the surface, whereas K and Ca result from surface contamination (except in popm43 where ~46%Ca is part of the corrosion layer). The levels of S and Cl are relatively high in some objects, probably resulting from corrosion processes. Objects with high silver content tend to present high S levels.

Unfortunately, published data on trace elements in native gold from the south-central Andes for comparative use is extremely limited. Alarcón and Fornari (1994) report traces of Cu, As and Sb in specific deposits from Bolivia; while others contain Bi, Fe, Ti, Te, Sn and Hg as well. However, there is no mention of Ni or Zn, the latter a common element in the SPA assemblage. Data from placer deposits in Sandia Province (south Peru) reports a placer with Sn concentration between 0.1–1% (Chinihuaya); while two have <100ppm of Sn: Vetasmayo and Sandia (Petersen 1970). Interestingly, the Sandia placer contained As (100–1000ppm), and Ni, Zn, Ti, Pb, Bi and Cr in concentrations <100ppm. The latter elements are similar to the traces and the composition of the complex phases detected in some objects from SPA (popm12, 15, 20, 24–25; see below). This dataset, with notable absences in Chile and Bolivia, makes an attempt at sourcing metals based on trace elements impossible for now.

The most common impurities detected by PIXE in SPA are Zn, Fe, Ti, some containing Ni, Ga, Pb and Hg; as complex micro-inclusions, the SEM-EDS added Sn, Bi and As. Similarly, the axe from CP analysed by ICP-AES contained 0.1%Al, 0.2%Pb, 0.5%Sn, 0.9%Zn, and 1.6%Fe, besides its Ag-Au-Cu content (Salazar et al. 2011). Data on impurities in gold and silver archaeological objects of the region, either as micro-inclusions or as trace elements, is very limited. Based on the few results published to date, the SPA assemblage is similar to Argentinean finds. Gold ornaments from La Isla de Tilcara and Pueblo Viejo de la Cueva (Humahuaca) contain traces of Fe (by SEM-EDS; Tarragó et al. 2010). From the same region, Angiorama (2001) describes a silver object with 0.6%Fe and 2.4%Zn. While in Salta, González (2004a, p. 333) reports a gold and copper diadem with important amounts of Fe, Zn and Ni (≤5.3%), but with no detectable silver. The Fe-Zn-Ni combination is also found in tin-bronze objects from the puna (Angiorama 2001). These impurities differ from those detected by Schlosser et al. (2009) in Nasca, Paracas and Chavin gold objects, analysed by LA-ICP-MS. They identify traces of PGE in concentrations ~1000ppm in gold objects from the central and north coast of Peru (Chavin), while in the south coast (Paracas, Nasca) objects have low PGE traces (<100ppm). Authors consider two objects from the south coast ‘uncommon’: a Paracas object high in Ni (which is usually <10ppm), and a Nasca artefact high in As and Sn (Schlosser et al. 2009). Traces of Fe, Sn and Sb were detected in Inca gold objects of unknown contexts by Rovira, who also found Fe, Sn, Sb and Pb in Inca silver objects (Rovira 2004). Nevertheless, this data is insufficient and there is no available information on objects from Bolivia, therefore these comparisons are inconclusive.

Technology, life histories and circulation of gold objects during the Middle Period (AD 400–1000). A perspective from the Atacama Desert, Chile; Archaeological and Anthropological Sciences; M.T. Plaza, V. Figueroa-Larre and M. Martinón-Torres*; *corresponding author: Department of Archaeology, University of Cambridge, United Kingdom. M.Martinon-Torres@arch.cam.ac.uk