Table S1: Chemical composition of glass reference materials as analysed and published. Expected values are mainly from Brill (1999) with additional information from Adlington (2017). The analysed result is the average of five analyses in wt% determined by SEM-EDS. Empty cells indicates ‘not published’ on the published data or below detection limit on the analysed data.

|  | Na2O | MgO | Al2O3 | SiO2 | P2O5 | SO3 | K2O | CaO | TiO2 | MnO | Fe2O3 | CoO | CuO | ZnO | SnO2 | Sb2O3 | BaO | PbO |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Corning A |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Mean | 13.7 | 2.55 | 0.86 | 66.1 |  | 0.28 | 2.95 | 5.07 | 0.83 | 1.04 | 1.10 | 0.18 | 1.22 |  | 0.29 | 1.87 | 0.50 | 0.08 |
| sd | 0.28 | 0.07 | 0.03 | 1.44 |  | 0.04 | 0.07 | 0.12 | 0.04 | 0.05 | 0.04 | 0.03 | 0.05 |  | 0.09 | 0.10 | 0.06 | 0.06 |
| Expected | 14.3 | 2.66 | 1.00 | 66.6 | 0.08 | 0.14 | 2.87 | 5.03 | 0.79 | 1.00 | 1.09 | 0.17 | 1.17 | 0.04 | 0.19 | 1.75 | 0.46 | 0.07 |
| Absolute error | -0.56 | -0.11 | -0.14 | -0.45 |  | 0.14 | 0.08 | 0.04 | 0.04 | 0.04 | 0.01 | 0.01 | 0.05 |  | 0.10 | 0.12 | 0.04 | 0.01 |
| Corning B |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Mean | 16.1 | 0.99 | 4.04 | 60.4 | 0.77 | 0.71 | 1.09 | 8.62 | 0.12 | 0.25 | 0.34 | 0.05 | 2.71 | 0.20 | 0.11 | 0.61 | 0.07 | 0.52 |
| sd | 0.35 | 0.04 | 0.09 | 1.08 | 0.05 | 0.04 | 0.03 | 0.15 | 0.03 | 0.03 | 0.03 | 0.03 | 0.07 | 0.05 | 0.07 | 0.08 | 0.04 | 0.05 |
| Expected | 17.0 | 1.03 | 4.36 | 61.6 | 0.82 | 0.49 | 1.00 | 8.56 | 0.09 | 0.25 | 0.34 | 0.05 | 2.66 | 0.19 | 0.02 | 0.46 | 0.08 | 0.61 |
| Absolute error | -0.90 | -0.04 | -0.32 | -1.11 | -0.05 | 0.22 | 0.09 | 0.06 | 0.03 | 0.00 | 0.00 | 0.01 | 0.05 | 0.01 | 0.09 | 0.15 | 0.00 | -0.09 |
| Corning C |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Mean | 0.99 | 2.56 | 0.77 | 33.0 | 0.02 | -0.63 | 2.84 | 4.93 | 0.86 |  | 0.31 | 0.17 | 1.15 | 0.05 | 0.21 |  | 12.0 | 38.5 |
| sd | 0.05 | 0.06 | 0.03 | 0.55 | 0.05 | 0.09 | 0.06 | 0.09 | 0.08 |  | 0.05 | 0.04 | 0.07 | 0.07 | 0.10 |  | 0.20 | 0.50 |
| Expected | 1.07 | 2.76 | 0.87 | 34.9 | 0.07 | 0.10 | 2.84 | 5.07 | 0.79 |  | 0.34 | 0.18 | 1.13 | 0.05 | 0.19 |  | 11.4 | 36.7 |
| Absolute error | -0.08 | -0.20 | -0.10 | -1.88 | -0.05 | -0.73 | 0.00 | -0.14 | 0.07 |  | -0.03 | -0.01 | 0.01 | -0.01 | 0.02 |  | 0.58 | 1.76 |
| Corning D |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Mean | 1.30 | 3.92 | 5.08 | 55.1 | 3.99 | 0.33 | 11.6 | 14.9 | 0.41 | 0.56 | 0.48 | 0.02 | 0.38 | 0.10 | 0.32 | 1.17 | 0.32 | 0.26 |
| sd | 0.04 | 0.08 | 0.07 | 0.84 | 0.11 | 0.05 | 0.20 | 0.23 | 0.04 | 0.03 | 0.04 | 0.04 | 0.04 | 0.05 | 0.10 | 0.11 | 0.06 | 0.06 |
| Expected | 1.20 | 3.94 | 5.30 | 55.2 | 3.93 | 0.23 | 11.3 | 14.8 | 0.38 | 0.55 | 0.52 | 0.02 | 0.38 | 0.10 | 0.10 | 0.97 | 0.29 | 0.24 |
| Absolute error | 0.10 | -0.02 | -0.22 | -0.18 | 0.06 | 0.10 | 0.29 | 0.12 | 0.03 | 0.01 | -0.04 | -0.01 | 0.00 | 0.00 | 0.22 | 0.20 | 0.02 | 0.02 |