Table S1: Chemical composition of glass reference materials as analysed and published. Expected values are mainly from Brill (1999) with additional information from Adlington (2017). The analysed result is the average of five analyses in wt% determined by SEM-EDS. Empty cells indicates ‘not published’ on the published data or below detection limit on the analysed data.

	
	Na2O
	MgO
	Al2O3
	SiO2
	P2O5
	SO3
	K2O
	CaO
	TiO2
	MnO
	Fe2O3
	CoO
	CuO
	ZnO
	SnO2
	Sb2O3
	BaO
	PbO

	Corning A
	
	
	
	
	
	
	
	
	
	
	
	
	
	
	
	
	
	

	Mean
	13.7
	2.55
	0.86
	66.1
	
	0.28
	2.95
	5.07
	0.83
	1.04
	1.10
	0.18
	1.22
	
	0.29
	1.87
	0.50
	0.08

	sd
	0.28
	0.07
	0.03
	1.44
	
	0.04
	0.07
	0.12
	0.04
	0.05
	0.04
	0.03
	0.05
	
	0.09
	0.10
	0.06
	0.06

	Expected
	14.3
	2.66
	1.00
	66.6
	0.08
	0.14
	2.87
	5.03
	0.79
	1.00
	1.09
	0.17
	1.17
	0.04
	0.19
	1.75
	0.46
	0.07

	Absolute error
	-0.56
	-0.11
	-0.14
	-0.45
	
	0.14
	0.08
	0.04
	0.04
	0.04
	0.01
	0.01
	0.05
	
	0.10
	0.12
	0.04
	0.01

	Corning B
	
	
	
	
	
	
	
	
	
	
	
	
	
	
	
	
	
	

	Mean
	16.1
	0.99
	4.04
	60.4
	0.77
	0.71
	1.09
	8.62
	0.12
	0.25
	0.34
	0.05
	2.71
	0.20
	0.11
	0.61
	0.07
	0.52

	sd
	0.35
	0.04
	0.09
	1.08
	0.05
	0.04
	0.03
	0.15
	0.03
	0.03
	0.03
	0.03
	0.07
	0.05
	0.07
	0.08
	0.04
	0.05

	Expected
	17.0
	1.03
	4.36
	61.6
	0.82
	0.49
	1.00
	8.56
	0.09
	0.25
	0.34
	0.05
	2.66
	0.19
	0.02
	0.46
	0.08
	0.61

	Absolute error
	-0.90
	-0.04
	-0.32
	-1.11
	-0.05
	0.22
	0.09
	0.06
	0.03
	0.00
	0.00
	0.01
	0.05
	0.01
	0.09
	0.15
	0.00
	-0.09

	Corning C
	
	
	
	
	
	
	
	
	
	
	
	
	
	
	
	
	
	

	Mean
	0.99
	2.56
	0.77
	33.0
	0.02
	-0.63
	2.84
	4.93
	0.86
	
	0.31
	0.17
	1.15
	0.05
	0.21
	
	12.0
	38.5

	sd
	0.05
	0.06
	0.03
	0.55
	0.05
	0.09
	0.06
	0.09
	0.08
	
	0.05
	0.04
	0.07
	0.07
	0.10
	
	0.20
	0.50

	Expected
	1.07
	2.76
	0.87
	34.9
	0.07
	0.10
	2.84
	5.07
	0.79
	
	0.34
	0.18
	1.13
	0.05
	0.19
	
	11.4
	36.7

	Absolute error
	-0.08
	-0.20
	-0.10
	-1.88
	-0.05
	-0.73
	0.00
	-0.14
	0.07
	
	-0.03
	-0.01
	0.01
	-0.01
	0.02
	
	0.58
	1.76

	Corning D
	
	
	
	
	
	
	
	
	
	
	
	
	
	
	
	
	
	

	Mean
	1.30
	3.92
	5.08
	55.1
	3.99
	0.33
	11.6
	14.9
	0.41
	0.56
	0.48
	0.02
	0.38
	0.10
	0.32
	1.17
	0.32
	0.26

	sd
	0.04
	0.08
	0.07
	0.84
	0.11
	0.05
	0.20
	0.23
	0.04
	0.03
	0.04
	0.04
	0.04
	0.05
	0.10
	0.11
	0.06
	0.06

	Expected
	1.20
	3.94
	5.30
	55.2
	3.93
	0.23
	11.3
	14.8
	0.38
	0.55
	0.52
	0.02
	0.38
	0.10
	0.10
	0.97
	0.29
	0.24

	Absolute error
	0.10
	-0.02
	-0.22
	-0.18
	0.06
	0.10
	0.29
	0.12
	0.03
	0.01
	-0.04
	-0.01
	0.00
	0.00
	0.22
	0.20
	0.02
	0.02



