Supplementary information 1

- Instrumentation conditions for analysis

GC-MS

Organic compounds were identified by a Thermo Scientific Trace 1300 chromatogram coupled to a TSQ 9000 mass spectrometer. The capillary column used for separation was an Agilent DB-5 ms (30 m length, 0,25 mm internal diameter, 0,25μm film thickness). The conditions of method utilization for GC were: column oven temperature (50ºC), injection temperature 250ºC in splitless injection mode and a sampling time of 1 minute. The carrier gas was He (prim. Press. 300-500) with linear velocity of 62.4 (cm/sec). Pressure was set at 31.5 kPa with a total flow of 152.5 mL/min and the column flow 1.48 mL/min. Purge flow was 3 mL/min and split ratio -1.0. The temperature program was was held at 50°C for 2 min, then ramped at 250°C/min until 300°C, followed by a 2-minute hold at that temperature, for an approximate total of 40 minutes. The ion source was set on 240 °C and the interphase temperate on 280 °C. The mass spectrometer was programmed to acquire data between 40 and 850 m/z. Identification and peak assignment were done using a FAME mix standard (Supelco C8-C24) and by comparisson with the National Institute of Standards and Technology (NIST) and Wiley mass spectra libraries through the Chromaleon 7 software (Thermo).

GC-C-IRMS

Samples were rederivatized and dissolved in hexane and analyzed in duplicate using a Delta V Plus mass spectrometer connected with an Iso-link interface to a Thermo 1310 gas chromatograph at the University of North Carolina, Wilmington. The chromatogram used a 60 m TG-5 SILMS colum; the temperature program was was held at 50°C for 2 min, then ramped at 10°C/min until 350°C, followed by a 10-minute hold at that temperature.

Elution times of compounds of interest were determined in relation to relative elution time observed by GC-MS. Compounds with an amplitude below 100 mV for molecular weights 44, 45, and 46 were not analyzed, due to low linearity. Stable carbon values for derivatizing agents were determined by direct injection of the BSTFA and methanol into a Thermo Flash HT Plus Elemental Analyzer linked to the Delta V Plus MS. During compound-speciﬁc runs of archaeological samples, the instrument was calibrated after every four samples using injections of IU Alkane B5 mixture (Indiana University Stable Isotope Reference Materials), with hexane blank runs after every three samples to ensure that the column and autosampler solvent was clean. Data was analyzed using the Qtegra Software. 
The standard deviation for the calibrated reference gas standards run throughout the project was 0.3 ‰. All errors through the sampling process, including errors on measurement of the derivatizing agents, measurement of reference gases, and sampling variation
within multiple runs of the same sample were combined and propagated utilizing a modiﬁed version of the spreadsheet published by Polissar and D’Andrea (2014). The results were a series of pooled standard deviations for compounds within the study that were larger than the sampling variations, but which captured all sources of variation and error within the instrumental sampling process, including all recorded compounds of interest analyzed. The pooled standard deviation of all compounds of interest for samples run using the solvent extraction methodology was 0.5 ‰.

EA-IRMS

For the analysis of food crusts, sherds with visible adhered charred residues were sampled using a clean scalpel and stored in clean glassware until EA-IRMS analysis. A Finnegan Delta Plus mass spectrometer equipped with a Carlo-Erba elemental analyzer and a Conflo II interface was used at the Center for Environmental and Science and Technology (CEST), University of Notre Dame. Carbon and nitrogen isotopes were measured simultaneously. Results were standardized to USGS 43, USGS 40, sucrose, and protein standard OAS (elemental microanalysis) using a mass balance equation.

- Materials

| Site | ID sample | Room | Techno group | Function |
| --- | --- | --- | --- | --- |
| LB-LB1-U14 | 1 | R04 | Coarse red | Pot |
| LB-LB1-U14 | 2 | x | Coarse red | Pot |
| LB-LB1-U14 | 3 | x | Coarse red | Pot |
| LB-LB1-U14 | 4 | x | Coarse red | Pot |
| LB-LB1-U14 | 5 | x | Coarse red | Pot |
| LB-LB1-U14 | 6 | r01 | Fine grey | Bowl |
| LB-LB1-U14 | 7 | x | Coarse red | Bowl/Jar |
| LB-LB1-U14 | 8 | r6 | Coarse red | Pot |
| LB-LB1-U14 | 9 | r6 | Coarse red | Pot |
| LB-LB1-U14 | 10 | r6 | Coarse red | Pot |
| LB-LB1-U14 | 11 | r6 | Coarse red | Pot |
| LB-LB1-U14 | 12 | r6 | Coarse red | SEPot |
| LB-LB1-U14 | 13 | R01 | Coarse red | Pot |
| LB-LB1-U14 | 14 | r4 | Coarse red | Pot |
| LB-LB1-U14 | 15 | r6 | Fine grey | Bowl |
| LB-LB1-U14 | 16 | r6 | Coarse red | Bowl |
| LB-LB1-U14 | 17 | r6 | Coarse red | Pot |
| LB-LB1-U14 | 18 | r6 | Coarse red | Pot |
| LB-LB1-U14 | 19 | r01 | Coarse red | Bowl |
| LB-LB1-U14 | 20 | r01 | Coarse red | Pot |
| LB-LB1-U14 | 21 | r1 | Fine red | Bowl |
| LB-LB1-U14 | 22 |  | Fine red | Bolw |
| LB-LB1-U14 | 23 | r1 | Coarse red | Pot |
| LB-LB1-U14 | 24 | r6 | Fine grey | Bowl |
| LB-LB1-U14 | 25 | r1 | Coarse red | Pot |
| LB-LB1-U14 | 26 | r1 | Coarse red | Pot |
| LB-LB1-U14 | 27 | R1 | Fine grey | Bowl |
| LB-LB1-U14 | 28 | R1 | Coarse red | Pot |
| LB-LB1-U14 | 29 | r1 | Fine grey | Bowl |
| LB-LB1-U14 | 30 | R1 | Fine red | Pot |
| LB-LB1-U14 | 31 | R1 | Fine red | Pot |
| LB-LB1-U14 | 32 | R1 | Coarse red | Pot |
| LB-LB1-U14 | 33 | r1 | Coarse red | Pot |
| LB-LB1-U14 | 34 | R1 | Coarse red | Pot |
| LB-LB1-U14 | 35 | r1 | Fine red | Bowl |
| LB-LB1-U14 | 36 | R1 | Coarse red | Pot |
| LB-LB1-U14 | 37 | r1 | Coarse red | Pot |
| LB-LB1-U14 | 38 | r1 | Fine grey | Bowl |
| LB-LB1-U14 | 39 | R1 | Fine grey | Bowl |
| LB-LB1-U14 | 40 | R1 | Fine red | Bowl |
| LB-LB1-U14 | 41 | R1 | Coarse red | Pot |
| LB-LB1-U14 | 42 | R1 | Fine grey | Bowl |
| LB-LB1-U14 | 43 | R1 | Coarse red | Pot |
| LB-LB1-U14 | 44 | r1 | Coarse red | Pot |
| LB-LB1-U14 | 45 | R1 | Coarse red | Pot |
| LB-LB1-U14 | 46 | R01 | Coarse red | Pot |
| LB-LB1-U14 | 47 | R6 | Coarse red | Pot |
| LB-LB1-U14 | 48 | R01 | Coarse red | Pot |
| LB-LB1-U14 | 49 | R6 | Coarse red | Pot |
| LB-LB1-U14 | 50 | R1 | Coarse red | Pot |
| LB-LB1-U14 | 51 | R1 | Fine red | Pot |
| LB-LB1-U14 | 52 | R6 | Fine red | Pot |
| LB-LB1-U14 | 53 | R6 | Coarse red | Pot |
| LB-LB1-U14 | 54 | R1 | Fine grey | Bowl |
| LB-LB1-U14 | 55 | R6 | Coarse red | Pot |
| LB-LB1-U14 | 56 | R6 | Coarse red | Pot |
| LB-LB1-U14 | 57 | R6 | Coarse red | Pot |
| LB-LB1-U14 | 02b | R1 | Fine grey | Bowl |
| LB-LB1-U14 | 03b | R1 | Fine grey | Bowl |
| LB-LB1-U14 | 04b | R1 | Fine grey | Bowl |
| LB-LB1-U14 | 01b | R1 | Coarse red | Bowl |
| LC-SC-U02 | 1 | R01 | Fine red | Bowl |
| LC-SC-U02 | 2 | R01 | Coarse red | Pot |
| LC-SC-U02 | 3 | R01 | Coarse red | Pot |
| LC-SC-U02 | 4 | R01 | Fine grey | Bowl |
| LC-SC-U02 | 5 | R01 | Fine red | Bowl |
| LC-SC-U02 | 6 | R01 | Coarse red | Pot |
| LC-SC-U02 | 7 | R01 | Coarse red | Jar |
| LC-SC-U02 | 8 | R01 | Fine grey | Bowl |
| LC-SC-U02 | 9 | R01 | Coarse red | Pot |
| LC-SC-U02 | 10 | R01 | Coarse red | Pot |
| LC-SC-U02 | 11 | R01 | Coarse red | Pot |
| LC-SC-U02 | 12 | R01 | Coarse red | Pot |
| LC-SC-U02 | 13 | R01 | Fine grey | Bowl |
| LC-SC-U02 | 14 | R01 | Coarse red | Pot |
| LC-SC-U02 | 15 | R01 | Coarse red w/ slip | Pot |
| LC-SC-U02 | 16 | R01 | Coarse red | Plate |
| LC-SC-U02 | 17 | R01 | Coarse red | Pot |
| LC-SC-U02 | 18 | R01 | Coarse red | Pot |
| LC-SC-U02 | 19 | R01 | Coarse red | Pot |
| LC-SC-U02 | 20 | R01 | Coarse red | Pot |
| LC-SC-U02 | 21 | R01 | Coarse red | Pot |
| LC-SC-U02 | 22 | R01 | Coarse red | Pot |
| LC-SC-U02 | 23 | R01 | Fine red | Bowl |
| LC-SC-U02 | 24 | R01 | Coarse red | Pot |
| LC-SC-U02 | 25 | R01 | Coarse red | Pot |
| LC-SC-U02 | 26 | R01 | Coarse red w/ slip | Pot |
| LC-SC-U02 | 27 | R01 | Coarse red | Pot |
| LC-SC-U02 | 28 | R01 | Coarse red | Pot |
| LC-SC-U02 | 29 | R01 | Coarse red | Pot |
| LC-SC-U02 | 30 | R01 | Coarse red | Pot |
| LC-SC-U02 | 31 | R01 | Coarse red | Pot |
| LC-SC-U02 | 32 | R01 | Coarse red | Pot |
| LC-SC-U02 | 33 | R01 | Fine red | Pot |
| LC-SC-U02 | 34 | R01 | Coarse red | Pot |
| LC-SC-U02 | 35 | R01 | Coarse red | Pot |
| LC-SC-U02 | 36 | R01 | Coarse red | Pot |
| LC-SC-U02 | 37 | R01 | Coarse red | Pot |
| LC-SC-U02 | 38 | R01 | Coarse red | Pot |
| LC-SC-U02 | 39 | R01 | Coarse red | Plate |
| LC-SC-U02 | 40 | R01 | Coarse red | Bowl |
| LC-SC-U02 | 41 | R01 | Coarse red | Jar |
| LC-SC-U02 | 42 | R01 | Fine grey | Bowl |
| LC-SC-U02 | 43 | R01 | Coarse red | Pot |
| LC-SC-U02 | 44 | R01 | Coarse red | Bowl |
| LC-SC-U02 | 45 | R01 | Coarse red | Pot |
| LC-SC-U02 | 46 | R01 | Coarse red | Bowl |
| LC-SC-U02 | 47 | R01 | Coarse red | Pot |
| LC-SC-U02 | 48 | R01 | Coarse red | Pot |
| LC-SC-U02 | 49 | R01 | Coarse red | Pot |
| LC-SC-U02 | 50 | R01 | Coarse red | Pot |
| LC-SC-U02 | 51 | R01 | Coarse red | Pot |
| LC-SC-U02 | 52 | R01 | Coarse red | Bowl |
| LC-SC-U02 | 53 | R01 | Coarse red | Pot |
| LC-SC-U02 | 54 | R01 | Coarse red | Pot |
| LC-SC-U02 | 55 | R01 | Coarse red | Pot |
| LC-SC-U02 | 56 | R01 | Coarse red | Pot |
| LC-LDM-U18 | 10 | R89 | Coarse red | Bowl |
| LC-LDM-U18 | 30 | R89 | Coarse red | Pot |
| LC-LDM-U18 | 53 | R89 | Coarse red | Pot |
| LC-LDM-U18 | 4 | R89 | Coarse red | Pot |
| LC-LDM-U18 | 45 | R89 | Coarse red | Bowl |
| LC-LDM-U18 | 7 | R89 | Coarse red | Pot |
| LC-LDM-U18 | 46 | R89 | Coarse red | Pot |
| LC-LDM-U18 | 24 | R89 | Coarse red | Pot |
| LC-LDM-U18 | 19 | R89 | Coarse red | Pot |
| LC-LDM-U18 | 13 | R89 | Coarse red | Pot |
| LC-LDM-U18 | 25 | R89 | Coarse red | Pot |
| LC-LDM-U18 | 18 | R89 | Coarse red | Pot |
| LC-LDM-U18 | 9 | R89 | Fine red | Bowl |
| LC-LDM-U18 | 39 | R89 | Coarse red | Pot |
| LC-LDM-U18 | 34 | R89 | Coarse red | Pot |
| LC-LDM-U18 | 28 | R89 | Coarse red | Pot |
| LC-LDM-U18 | 26 | R89 | Coarse red | Pot |
| LC-LDM-U18 | 23 | R89 | Coarse red | Pot |
| LC-LDM-U18 | 17 | R89 | Coarse red | Pot |
| LC-LDM-U18 | 20 | R89 | Coarse red | Pot |
| LC-LDM-U18 | 12 | R89 | Coarse red | Bowl |
| LC-LDM-U18 | 36 | R89 | Fine grey | Bowl |
| LC-LDM-U18 | 32 | R89 | Coarse red | Pot |
| LC-LDM-U18 | 11 | R89 | Coarse red | Pot |
| LC-LDM-U18 | 15 | R89 | Coarse red | Pot |
| LC-LDM-U18 | 38 | R89 | Coarse red | Pot |
| LC-LDM-U18 | 33 | R89 | Coarse red | Pot |
| LC-LDM-U18 | 5 | R89 | Fine grey | Bowl |
| LC-LDM-U18 | 41 | R89 | Coarse red | Pot |
| LC-LDM-U18 | 40 | R89 | Coarse red | Pot |
| LC-LDM-U18 | 35 | R89 | Coarse red | Bowl |
| LC-LDM-U18 | 31 | R89 | Coarse grey | Pot |
| LC-LDM-U18 | 8 | R89 | Coarse red | Pot |
| LC-LDM-U18 | 3 | R89 | Fine grey | Bowl |
| LC-LDM-U18 | 1 | R89 | Coarse red | Pot |
| LC-LDM-U18 | 47 | R89 | Coarse red | Bowl |
| LC-LDM-U18 | 22 | R89 | Coarse red | Pot |
| LC-LDM-U18 | 50 | R89 | Coarse red | Bowl |
| LC-LDM-U18 | 51 | R89 | Coarse red | Bowl |
| LC-LDM-U18 | 52 | R89 | Coarse red | Bowl |
| LC-LDM-U18 | 42 | R89 | Coarse red | Pot |
| LC-LDM-U18 | 29 | R89 | Coarse red | Jar |
| LC-LDM-U18 | 6 | R89 | Fine grey | Jar |
| LC-LDM-U18 | 37 | R89 | Coarse red | Pot |
| LC-LDM-U18 | 14 | R89 | Coarse red | Pot |
| LC-LDM-U18 | 27 | R89 | Coarse red | Pot |
| LC-LDM-U18 | 44 | R89 | Fine grey | Bowl |
| LC-LDM-U18 | 16 | R89 | Coarse red | Pot |
| LC-LDM-U18 | 42 | R89 | Coarse red | Pot |
| LC-LDM-U18 | 2 | R89 | Coarse red | Pot |
| LC-LDM-U18 | 21 | R89 | Coarse red | Pot |
| LC-LDM-U18 | 1 | R91 | Fine grey | Bowl |
| LC-LDM-U18 | 2 | R91 | Fine grey | Bowl |
| LC-LDM-U18 | 3 | R91 | Fine grey | Bowl |
| LC-LDM-U18 | 4 | R91 | Fine grey | Bowl |