	Macro-fabric
	Fracture Description
	Void Frequency & Type
	Inclusions
	Samples

	PA1
	Rough to the touch, red, medium-high hardness and compactness
	Low frequency, irregularly shaped
	White (high freq., small–medium, often perforated); Black (rare, small); Transparent (low freq., small, angular–rounded)
	GA1-11; GA15-GA18; GA20; GA22-23; GA25-26; GA28-38; GA42-43; GA47-55; GA57; GA59-63; GA66-70; GA74-90; GA92; PB1-2; PB4-13; PB16-25; PB27; PB29-32; PZA8?, PZA11

	PA2
	Rough to the touch, dark grey, medium-high hardness and compactness
	Low frequency, irregularly shaped
	Same as PA1; differs only in body colour
	GA12; GA14; GA19; GA21; GA24; GA27; GA39; GA41; GA44; GA56; GA58; GA64; GA72—73; GA91; PB3; PB15; PB26 

	PA3
	Fracture fairly smooth to the touch, red/orange in colour, medium-high hardness and compactness
	Low frequency, with irregular shapes
	White (medium-high frequency, small to medium size); transparent (medium frequency, angular and rounded shapes). Overall appearance is similar to PA1 and PA2 but with fewer white inclusions, which are not perforated in the center
	GA71; GA93

	IFR5
	Well-cleaned, smooth, white/beige, high hardness, medium-high compactness
	Medium frequency (small round); medium-low frequency (medium-sized)
	White (low freq., small–medium); Transparent (low freq., small–medium)
	GA97; GA105.

	IFR8
	Powdery to the touch, white/beige, medium hardness and compactness
	Medium frequency, irregularly shaped
	White (low freq., small); Transparent (high freq., small, angular–rounded)
	GA102; GA104; GA107; GA108; GA109; PB34.

	IFR16
	Rough to the touch, light pink, medium hardness, medium-high compactness
	Low frequency, irregularly shaped
	White (medium-low freq., small); Black (rare, small); Transparent (high freq., small–medium, angular–rounded)
	GA94; GA95; GA98; GA99; GA103; GA106; GA110; GA111; PB33.

	IFR46
	Fracture fairly smooth to the touch, light pink, medium- high hardness and compactness
	Medium-law frequency, irregularly shaped
	White (medium freq., small); Black (rare, small); Transparent (medium-high freq., small, angular-rounded)
	GA96

	IFR64
	Smooth to the touch, light pink, high hardness and compactness
	Low frequency, small, irregularly shaped
	White (low freq., small, sometimes perforated); Transparent (medium-high freq., small, angular–rounded)
	GA101.

	IFR89
	Rough to the touch, light pink center (Munsell 2.5YR 8/4), light grey surfaces (Munsell 5Y 8/2)
	Low frequency, small and medium-sized
	Transparent (high freq., small–medium, rounded); Black (rare, small)
	PV6?

	EG47
	Rough to the touch, pink (Munsell 5YR 8/4), medium-high hardness and compactness
	Medium-low frequency, small, irregularly shaped
	White (medium-high freq., small); Transparent (medium freq., small, angular)
	GA100.

	SR1
	Rough to the touch, red near surface, brown/dark red core, medium-high hardness and compactness
	Low frequency, irregular and elongated
	White (high freq., medium, sometimes perforated); Transparent (rare, medium); Fine gold (few)
	SIR1; SIR2; SIR3; SIR4; SIR5; SIR6; SIR7; SIR8; SIR9; SIR10; SIR11; SIR12. 

	AGR1
	Rough to the touch, red near surface, pale red or red core with greenish patches, medium hardness and compactness
	Low frequency, irregular and elongated
	White (medium freq., small–medium, often perforated); Transparent (low–medium freq., small–medium); Black (rare, medium); Fine gold (medium freq.)
	AG2; AG3; AG4; AG5; AG6; AG8; AG9; AG10.

	AGR2
	Rough to the touch, red near surface, pale red with greenish patches, medium hardness and compactness
	Low frequency, irregular and elongated
	White (medium freq., small–medium, often perforated); Transparent (low–medium freq., small–medium); Fine gold (medium freq.)
Note: Same fabric as AGR1 with a different firing
	AG1; AG7.

	PZAR1
	Rough and slightly powdery to the touch, beige to pink, low hardness, medium compactness
	Medium frequency, irregular and elongated
	Transparent (high freq., small–medium); White (rare, medium); Black (rare, small); Red (rare–low, small); Fine gold (low–medium freq.)
	PZA1; PZA2?; PZA3; PZA4; PZA5; PZA6; PZA7; PZA9; PZA10; PZA12; PZA13; PZA14; PZA15; PZA16.

	CDPT1
	Rough to the touch, beige in the core and close to the surfaces, pink with red stripes in the rest
	Low to medium frequency, small, irregularly shaped, very few elongated 
	Transparent (high freq., small–medium, rounded); white (low freq., medium size some with a void inside); red (rare, medium and big size); grey (low freq., medium size)
	CDP3

	CDPT2
	Rough to the touch, light pink/grey in the core, red and then beige close to the surface
	Medium freq., elongated and irregular
	Transparent (high freq., small–medium, rounded); white (medium freq., medium size some with a void inside); black (low freq., medium size)
	CDP2

	CDPT3
	Rough to the touch, beige, pink or dark pink with a thin beige layer close to one of the surfaces
	Medium freq. of irregular, low freq. of elongated
	Transparent (high freq., small–medium, rounded); white (medium freq., medium size some with a void inside); red (rare, medium and big size);
	CDP1; CDP4?; CDP5; CDP6.
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