Supplementary Materials

EDS major element composition of mineral phases of the investigated pozzolana samples (CL, LP, SAV).

Alkali feldspars (Fig.1a) are sanidine with the following compositions: CL (An2Ab18Or80), LP (An0-2Ab17-18Or80-82), SAV (An3-7Ab14-27Or68-84). Plagioclases (Fig.1a) are observed only in LP and CL samples and identified as bytownite and labradorite: CL (An83Ab14Or2), LP (An56-75Ab38-21Or4-6).

The pyroxenes (Fig.1b) (Fe calculated following Papike et al. 2005) are diopside (Wo49En44Fs7 for CL sample, Wo49En38Fs13 for the LP sample and Wo46-47En36-48Fs16 for SAV sample).

The identified mineral phases are consistent with those from Phlegraean Fields products (Morra et al. 2010 and references therein).

Fig.1 (a) Composition of the analyzed feldspar and plagioclase; (b) composition of the analyzed pyroxenes. Compositional areas of Phlegraean Fields feldspar, plagioclase and pyroxenes are from Morra et al. 2010 and references therein

Major elements EDS data of alkali feldspars (wt.%).

| Sample | CL | CL | CL | SAV | SAV | SAV | LP | LP |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| SiO2 | 64.71 | 64.06 | 62.04 | 62.77 | 63.31 | 62.20 | 65.39 | 63.22 |
| Al2O3 | 19.01 | 19.17 | 18.44 | 19.86 | 19.17 | 19.52 | 19.23 | 19.51 |
| FeO | 0.32 | 0.14 | 0.28 | 0.50 | 0.15 | 0.37 | 0.34 | 0.40 |
| CaO | 0.42 | 0.46 | 0.47 | 1.13 | 0.59 | 1.16 | - | 0.44 |
| Na2O | 2.20 | 2.07 | 2.02 | 3.10 | 1.61 | 2.95 | 2.04 | 1.93 |
| K2O | 13.03 | 12.91 | 12.51 | 10.54 | 13.53 | 10.48 | 12.94 | 11.97 |
| BaO | 0.15 | 0.38 | 0.24 | 0.49 | 0.44 | 0.19 | 0.24 | 0.72 |
| SrO | - | - | - | 0.86 | 0.40 | 0.70 | - | 1.23 |
| Total | 99.84 | 99.19 | 96.00 | 99.25 | 99.20 | 97.57 | 100.18 | 99.42 |
|  | cation based on 32 oxygens |  |  |  |  |  |  |  |
| Si | 11.63 | 11.61 | 11.61 | 11.40 | 11.51 | 11.47 | 11.74 | 11.56 |
| Al | 4.07 | 4.14 | 4.11 | 4.30 | 4.16 | 4.29 | 4.12 | 4.25 |
| Fe | 0.05 | 0.02 | 0.04 | 0.08 | 0.02 | 0.06 | 0.05 | 0.06 |
| Ca | 0.08 | 0.09 | 0.10 | 0.22 | 0.12 | 0.23 | - | 0.09 |
| Na | 0.78 | 0.74 | 0.74 | 1.10 | 0.57 | 1.07 | 0.72 | 0.69 |
| K | 3.38 | 3.38 | 3.38 | 2.76 | 3.55 | 2.79 | 3.36 | 3.16 |
| Ba | 0.01 | 0.03 | 0.02 | 0.04 | 0.03 | 0.01 | 0.02 | 0.05 |
| Sr | - | - | - | 0.09 | 0.04 | 0.08 | - | 0.13 |
| Total | 20.00 | 20.00 | 20.00 | 20.00 | 20.00 | 20.00 | 20.00 | 20.00 |
| An% | 1.93 | 2.15 | 2.26 | 5.44 | 2.74 | 5.67 | - | 2.21 |
| Ab% | 18.30 | 17.50 | 17.58 | 27.00 | 13.53 | 26.09 | 17.64 | 17.57 |
| Or% | 79.77 | 80.35 | 80.16 | 67.57 | 83.72 | 68.24 | 82.36 | 80.22 |

An%: anorthite mol%; Ab%= albite mol%; Or%= orthoclase mol%

Major elements EDS data of plagioclase  (wt.%)

| Sample | CL | LP | LP |
| --- | --- | --- | --- |
| SiO2 | 46.41 | 53.69 | 48.47 |
| Al2O3 | 32.91 | 29.16 | 31.67 |
| FeO | 0.82 | 1.18 | 0.88 |
| CaO | 16.70 | 11.30 | 14.65 |
| Na2O | 1.58 | 4.27 | 2.30 |
| K2O | 0.36 | 0.93 | 0.56 |
| BaO | 0.64 | 0.41 | 0.35 |
| SrO | - | - | 0.07 |
| Total | 99.42 | 100.94 | 98.95 |
|  | cation based on 32 oxygens |  |  |
| Si | 8.57 | 9.62 | 8.95 |
| Al | 7.25 | 6.23 | 6.97 |
| Fe | 0.13 | 0.18 | 0.14 |
| Ca | 3.34 | 2.20 | 2.93 |
| Na | 0.57 | 1.50 | 0.83 |
| K | 0.10 | 0.24 | 0.15 |
| Ba | 0.05 | 0.03 | 0.03 |
| Sr | - | - | 0.01 |
| Total | 20.00 | 20.00 | 20.00 |
| An% | 83.34 | 55.76 | 74.91 |
| Ab% | 14.27 | 38.13 | 21.28 |
| Or% | 2.39 | 6.11 | 3.81 |

An%: anorthite mol%; Ab%= albite mol%; Or%= orthoclase mol%

Major elements EDS data of pyroxenes (wt.%)

| Sample | CL | SAV | SAV | SAV | SAV | LP |
| --- | --- | --- | --- | --- | --- | --- |
| SiO2 | 54.18 | 52.89 | 48.88 | 53.84 | 49.83 | 50.09 |
| TiO2 | 0.45 | 0.30 | 0.74 | 0.86 | 0.54 | 0.59 |
| Al2O3 | 2.44 | 2.22 | 2.90 | 15.15 | 2.55 | 3.33 |
| Fe2O3 | 4.97 | 3.28 | 10.3 | 7.82 | 10.01 | 8.87 |
| MnO | 0.16 | 0.28 | 0.35 | 0.29 | 0.52 | 0.25 |
| MgO | 15.99 | 17.3 | 11.97 | 0.69 | 12.19 | 12.68 |
| CaO | 24.6 | 22.69 | 21.55 | 2.15 | 21.75 | 23.06 |
| Na2O | 0.28 | 0.25 | 0.51 | 6.30 | 0.47 | 0.44 |
| K2O | 0.06 | 0.05 | 0.16 | 4.90 | 0.17 | 0.07 |
| Total | 103.13 | 99.26 | 97.36 | 92.00 | 98.03 | 99.38 |
|  | cation based on 6 oxygens |  |  |  |  |  |
| Si | 1.96 | 1.97 | 1.94 | 2.38 | 1.95 | 1.93 |
| Ti | 0.01 | 0.01 | 0.02 | 0.03 | 0.02 | 0.02 |
| IVAl | 0.04 | 0.03 | 0.06 | - | 0.05 | 0.07 |
| VIAl | 0.01 | 0.02 | - | 0.78 | 0.01 | 0.01 |
| Fe3+ | 0.01 | 0.01 | 0.04 | - | 0.02 | 0.04 |
| Fe2+ | 0.14 | 0.09 | 0.31 | 1.24 | 0.31 | 0.25 |
| Mn | - | 0.01 | 0.01 | 0.01 | 0.01 | 0.01 |
| Mg | 0.86 | 0.96 | 0.71 | 0.05 | 0.71 | 0.73 |
| Ca | 0.95 | 0.90 | 0.91 | 0.10 | 0.91 | 0.95 |
| Na | 0.01 | 0.01 | 0.02 | 0.27 | 0.02 | 0.02 |
| Total | 4.01 | 4.00 | 4.02 | 3.52 | 4.01 | 4.02 |
| Wo% | 48.69 | 46.08 | 47.23 | 7.30 | 46.97 | 49.23 |
| En% | 44.02 | 48.86 | 36.49 | 3.26 | 36.61 | 37.65 |
| Fs% | 7.29 | 5.06 | 16.29 | 89.43 | 16.42 | 13.11 |

Wo%: wollastonite mol%; En%= enstatite mol%; Fs%= ferrosilite mol%;  IVAl calculated by difference with Si; Fe3+ and Fe2+ were calculated following Papike et al. (2005)