Supplementary material

Effects of Sc additions on annealing behavior of heavily cold-rolled Al-Cu-Mn alloys

Xiaoyu Huang a, Tianlin Huang a,b,*, Yueyue Zhu a, Guilin Wu a , Yongzhong Zhangc, Xiaoxu Huang a,b, Oleg V. Mishin d,*

a International Joint Laboratory for Light Alloys (MOE), College of Materials Science and Engineering, Chongqing University, Chongqing 400044, China

b Electron Microscopy Center of Chongqing University, Chongqing University, Chongqing 400044, China

c National Engineering & Technology Research Center for Non-Ferrous Metals Composites, GRINM Group Co., Ltd., Beijing 101407, China

d Department of Civil and Mechanical Engineering, Technical University of Denmark, 2800 Kgs. Lyngby, Denmark

*corresponding authors: Tianlin Huang (E-mail: huangtl@cqu.edu.cn); Oleg V. Mishin (E-mail: olmi@dtu.dk)

Fig. S1:  STEM image showing particles and the corresponding distributions of Cu, Mn and Sc in the Al-Cu-Mn-0.2Sc sample annealed at 300 °C for 100 h. The arrows in the STEM image show some examples of AlxCuySc and AlxMn particles (the latter are most likely Al12Mn particles). Note that the marked AlxCuySc particles precipitated along a boundary between two recrystallized grains.