Temperature and particle-size effects on the formation of silica gels from silica sols

Christian Sögaard1, Magnus Hagström2, and Zareen Abbas1*

- Department of Chemistry and Molecular Biology, University of Gothenburg, Kemigården 4, 41296, Gothenburg, Sweden

- Nouryon, SE-44580, Bohus, Sweden

*Corresponding author

E-mail: zareen.abbas@gu.se

Tel: +46766229015

Figure S1: Calculation of activation energy in this case for aggregation of CS30-236. The slope of the inserted trend line is equal to Ea/R.

ES-SMPS Results

Figure S2: Normalized particle size distribution for CS30-236 gelling at 10°C. The 25%, 50% and 75% is the percentage of total gel time at which ES-SMPS measurements were made.

Figure S3: Normalized particle size distribution for CS30-236 gelling at 20°C. The 25%, 50% and 75% is the percentage of total gel time at which ES-SMPS measurements were made.

Figure S4: Normalized particle size distribution for CS30-236 gelling at 30°C. The 25%, 50% and 75% is the percentage of total gel time at which ES-SMPS measurements were made.

Figure S5: Normalized particle size distribution for CS40-222 gelling at 10°C. The 25%, 50% and 75% is the percentage of total gel time at which ES-SMPS measurements were made.

Figure S6: Normalized particle size distribution for CS40-222 gelling at 20°C. The 25%, 50% and 75% is the percentage of total gel time at which ES-SMPS measurements were made.

Figure S7: Normalized particle size distribution for CS40-222 gelling at 30°C. The 25%, 50% and 75% is the percentage of total gel time at which ES-SMPS measurements were made.

Figure S8: Normalized particle size distribution for CS40-213 gelling at 10°C. The 25%, 50% and 75% is the percentage of total gel time at which ES-SMPS measurements were made.

Figure S9: Normalized particle size distribution for CS40-213 gelling at 20°C. The 25%, 50% and 75% is the percentage of total gel time at which ES-SMPS measurements were made.

Figure S10: Normalized particle size distribution for CS40-213 gelling at 30°C. The 25%, 50% and 75% is the percentage of total gel time at which ES-SMPS measurements were made.

Figure S11: Normalized particle size distribution for TM40, CB17, and CS40-213 silica sols. These distributions are valid for the sols before aggregation is initiated.

Table S1: The results of the ES-SMPS measurements for CS30-236 sol. The Nd is also included as calculated from equation 1 using the number average particle sizes in column 6. The % gelled is with reference to the gel time at each temperature when sample has been taken from the aggregating sol and fed into the ES-SMPS.

| Sol | Temp °C | % gelled | Time (min) | Number average particle size (nm) | Nd (calculated from equation 1) |
| --- | --- | --- | --- | --- | --- |
| CS30-236 | Ambient | 0 | 0 | 16.82 | 1.00 |
| CS30-236 | 10 | 25 | 4.75 | 19.78 | 1.41 |
| CS30-236 | 10 | 50 | 9.50 | 22.64 | 1.87 |
| CS30-236 | 10 | 75 | 14.25 | 24.64 | 2.23 |
| CS30-236 | 20 | 25 | 4.58 | 21.03 | 1.60 |
| CS30-236 | 20 | 50 | 9.17 | 23.75 | 2.06 |
| CS30-236 | 20 | 75 | 13.75 | 26.61 | 2.62 |
| CS30-236 | 30 | 25 | 3.25 | 21.16 | 1.62 |
| CS30-236 | 30 | 50 | 6.50 | 24.02 | 2.11 |
| CS30-236 | 30 | 75 | 9.75 | 26.08 | 2.51 |

Table S2: The results of the ES-SMPS measurements for CS40-222 sol. The Nd is also included as calculated from equation 1 using the number average particle sizes in column 6. The % gelled is with reference to the gel time at each temperature when sample has been taken from the aggregating sol and fed into the ES-SMPS.

| Sol | Temp °C | % gelled | Time (min) | Number average particle size (nm) | Nd (calculated from equation 1) |
| --- | --- | --- | --- | --- | --- |
| CS40-222 | Ambient | 0 | 0 | 21.67 | 1.00 |
| CS40-222 | 10 | 25 | 25.25 | 26.81 | 1.56 |
| CS40-222 | 10 | 50 | 50.50 | 31.05 | 2.13 |
| CS40-222 | 10 | 75 | 75.75 | 33.56 | 2.51 |
| CS40-222 | 20 | 25 | 19.92 | 27.25 | 1.62 |
| CS40-222 | 20 | 50 | 39.84 | 31.58 | 2.21 |
| CS40-222 | 20 | 75 | 59.75 | 34.72 | 2.69 |
| CS40-222 | 30 | 25 | 13.08 | 27.74 | 1.68 |
| CS40-222 | 30 | 50 | 26.17 | 31.94 | 2.26 |
| CS40-222 | 30 | 75 | 39.25 | 36.84 | 3.04 |

Table S3: The results of the ES-SMPS measurements for CS40-213 sol. The Nd is also included as calculated from equation 1 using the number average particle sizes in column 6. The % gelled is with reference to the gel time at each temperature when sample has been taken from the aggregating sol and fed into the ES-SMPS.

| Sol | Temp °C | % gelled | Time (min) | Number average particle size (nm) | Nd (calculated from equation 1) |
| --- | --- | --- | --- | --- | --- |
| CS40-213 | Ambient | 0 | 0 | 33.78 | 1.00 |
| CS40-213 | 10 | 25 | 166.33 | 41.41 | 1.53 |
| CS40-213 | 10 | 50 | 332.67 | 48.03 | 2.09 |
| CS40-213 | 10 | 75 | 479.00 | 51.08 | 2.38 |
| CS40-213 | 20 | 25 | 105.17 | 40.83 | 1.49 |
| CS40-213 | 20 | 50 | 210.34 | 46.48 | 1.95 |
| CS40-213 | 20 | 75 | 315.50 | 52.56 | 2.53 |
| CS40-213 | 30 | 25 | 51.83 | 39.00 | 1.35 |
| CS40-213 | 30 | 50 | 103.67 | 43.94 | 1.74 |
| CS40-213 | 30 | 75 | 155.50 | 48.25 | 2.11 |