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UV Spectra of PAMAM dendrimers from G0.5 to G2.5:
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Figure S1: UV-Vis spectra of PAMAM dendrimers from G0.5 to G2.5.

FTIR Spectra of PAMAM dendrimers
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Figure S2: FTIR spectra of PAMAM dendrimers from G0.5 to G2.0.
Table S1: Zeta Potential values of PAMAM Dendrimers.

	Generations of dendrimer
	Zeta Potential (mV)

	G0.5
	1.82

	G1.0
	-0. 309

	G1.5
	1.69

	G2.0
	-0.543

	G2.5
	0.168


