Deoxycholic Acid-Grafted Chitosan Nanocarriers for Enhancing Oral Bioavailability and Hepatoprotection of Silybin

Swarali Kadam1, Gasper Fernandes1, Naitik Jain1, Srinivas Mutalik1*

1 Department of Pharmaceutics, Manipal College of Pharmaceutical Sciences, Manipal Academy of Higher Education, Manipal 576104, Karnataka, India

*Corresponding Author

Dr Srinivas Mutalik

Professor and Principal

Manipal College of Pharmaceutical Sciences

Manipal Academy of Higher Education

Manipal 576104, Karnataka, India

Email: ss.mutalik@manipal.edu

Figures

Fig S1. (A) FTIR spectra (B) DSC spectra of chitosan, deoxycholic acid (DOCA) and deoxycholic acid modified chitosan (DCS).

Fig S2. DSC spectra of Physical Mixture and DCS-LC NPs

Tables

Table S1. Responses obtained during Optimization of independent variables involved in synthesis of DCS-LC NPs

| S. No. | Amount of DCS (mg) | Amount of Lipid (mg) | % of Surfactant |
| --- | --- | --- | --- |
| 1. | 17.5 | 200 | 0.6 |
| 2. | 30 | 125 | 0.6 |
| 3. | 17.5 | 125 | 0.35 |
| 4. | 5 | 50 | 0.35 |
| 5. | 5 | 125 | 0.1 |
| 6. | 5 | 125 | 0.6 |
| 7. | 17.5 | 125 | 0.35 |
| 8. | 1.5 | 125 | 0.35 |
| 9. | 17.5 | 125 | 0.35 |
| 10. | 5 | 200 | 0.35 |
| 11. | 17.5 | 125 | 0.35 |
| 12. | 30 | 50 | 0.35 |
| 13. | 17.5 | 50 | 0.1 |
| 14. | 17.5 | 50 | 0.6 |
| 15. | 17.5 | 200 | 0.1 |
| 16. | 30 | 125 | 0.1 |
| 17. | 30 | 200 | 0.35 |

Table S2. ANOVA table for the Quadratic model of the two responses (Particle size and Entrapment efficiency).

| Content | Particle Size |  | Entrapment Efficiency |  |
| --- | --- | --- | --- | --- |
| Source | Sum of squares | Status | Sum of squares | Status |
| Model | 57067.45 | Significant | 328.36 | Significant |
| A-Amount Of Chitosan | 7335.03 |  | 23.46 |  |
| B- Amount Of Lipid | 375.93 |  | 304.18 |  |
| C- Amount Of Surfactant | 2450.00 |  | 0.7140 |  |
| Ab | 16312.40 |  | 43.42 |  |
| Ac | 12611.29 |  | 33.98 |  |
| Bc | 17982.81 |  | 9.44 |  |
| Residual | 6361.13 |  | 371.77 |  |
| Lack Of Fit | 3863.19 | Not Significant (p= 0.5121) | 33.98 | Not Significant (p= 0.3435) |

Table S3. Actual and predicted values of optimized formulation

|  | ### Independent variables |  |  |  | ### Responses |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Amount of DCS (mg) | Amount of Lipid (mg) |  | ### Amount of Surfactant (%) | Particle size (nm) | Entrapment efficiency (%) |
| Composition suggested by the software | ### 18 | ### 50 | ### 0.6 |  | ### 99.37 | ### 87.65 |
| Practically performed composition (SIL = 5mg) | ### 18 | ### 50 | ### 0.6 |  | ### 95.83 | ### 85.03 |
| Residual error (%) | ### - | ### - | ### - |  | ### 3.56 | ### 2.98 |

Table S4. Observed values of particle size, Zeta potential and PDI of DCS-LC NPs

| Formulation | Amount of SIL (mg) | Particle Size (nm) | PDI | Zeta potential (mV) | % EE |
| --- | --- | --- | --- | --- | --- |
| Blank DCS-LC NPs | - | 90.2 | 0.24 | 25.6 | - |
| DCS-LC NPs | 5 | 95.83 | 0.26 | 17.2 | 85.03 % |
| DCS-LC NPs | 7.5 | 187.2 | 0.20 | 18.6 | 89.54 % |

Table S5: Kinetic modeling of in vitro drug release from DCS-LC NPs.

| Model | DCS-LC NPs |  |  |
| --- | --- | --- | --- |
|  | pH 1.2 | pH 6.8 | pH 7.4 |
| Zero order | R2 = 0.8516 | R2 = 0.4724 | R2 = 0.4726 |
| First order | R2 = 0.9374 | R2 = 0.5992 | R2 = 0.7026 |
| Higuchi | R2 = 0.9782 | R2 = 0.6838 | R2 = 0.6756 |
| Korsmeyer-Peppas | R2 = 0.9776 n = 0.53 | R2 = 0.9981 n = 1.1 | R2 = 1 n = 1.2 |