SUPPLEMENTAL DATA

Fig. 1: Plot of Ct/Co versus contact time of CuO-kaolinite composite used for the calculation of mass transfer rates

Table 1: Mass transfer rates for CuO-kaolinite composite derived from Fig. 1

| Slope I(hr-1) | SlopeII(hr-1) | Exposed Surface Area (cm-1) | KfI (cmhr-1) | KfII (cmhr-1) |
| --- | --- | --- | --- | --- |
| 0.0345 | 0.0184 | 4700 | 7.34^-6 | 3.91^-6 |

Fig. 2: Adsorption capacity versus initial metal concentration of CuO-kaolinite composite [pH=4, 2g/L solid concentration, 10 mg/L Pb2+ concentration]

Fig. 3: Plot of adsorption capacity versus particle concentration (Cp) [pH=4]

Fig. 4: Adsorption capacity versus residence time for CuO-kaolinite composite [pH=4,2 g/L solid concentration, 10mgL-1 Pb2+ concentration]

Fig. 5: Plot of adsorption capacity versus initial pH for CuO-kaolinite composite [2 g/L solid concentration, 10mgL-1 Pb2+ concentration]