Water disinfection using durable ceramic filter coated with silver nanoparticles synthesized using actinomycetes

Supplementary data

Table S1. Comparison between the antibacterial efficiency of pristine and AgNPs-decorated ceramic filter

| Testing water | E. coli MTCC 739 |  | P. aeruginosa MTCC 2453 |  | S. aureus MTCC 96 |  | B. subtilis MTCC 736 |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | CFU/100ml | Efficiency (%) | CFU/100ml | Efficiency (%) | CFU/100ml | Efficiency (%) | CFU/100ml | Efficiency (%) |
| Spiked water before filtration | 1.1 x 106 | - | 1.3 x 106 | - | 5 x 105 | - | 3.8 x 105 | - |
| Filtered by a modified filter | 0 | 100 | 0 | 100 | 0 | 100 | 0 | 100 |
| Filtered by pristine filter | 5 x 103 | 99.5 | 7 x 103 | 99.4 | 4 x 103 | 99.2 | 3 x 103 | 99.2 |

Table S2. The concentrations of the dissolved Ag every day in the outlet

| Day | Concentration of the Ag | Day | Concentration of the Ag |
| --- | --- | --- | --- |
| 1 | 31.2 | 31 | 28.2 |
| 2 | 32.8 | 32 | 35.1 |
| 3 | 30.1 | 33 | 32.5 |
| 4 | 32.4 | 34 | 27.6 |
| 5 | 38.6 | 35 | 24.8 |
| 6 | 35.3 | 36 | 30.2 |
| 7 | 32.9 | 37 | 29.5 |
| 8 | 35.4 | 38 | 32.7 |
| 9 | 38.4 | 39 | 35.7 |
| 10 | 37.6 | 40 | 34.5 |
| 11 | 40.6 | 41 | 30.2 |
| 12 | 37.8 | 42 | 37.6 |
| 13 | 32.3 | 43 | 32.8 |
| 14 | 30.7 | 44 | 30.9 |
| 15 | 35.6 | 45 | 36.3 |
| 16 | 33.5 | 46 | 25.6 |
| 17 | 34.6 | 47 | 29.2 |
| 18 | 35.7 | 48 | 38.4 |
| 19 | 29.8 | 49 | 33.2 |
| 20 | 32.1 | 50 | 30.8 |
| 21 | 33.3 | 51 | 29.3 |
| 22 | 39.4 | 52 | 33.3 |
| 23 | 36.5 | 53 | 35.6 |
| 24 | 30.2 | 54 | 34.9 |
| 25 | 42.8 | 55 | 28.5 |
| 26 | 29.6 | 56 | 37.5 |
| 27 | 35.4 | 57 | 30.8 |
| 28 | 34.1 | 58 | 30.1 |
| 29 | 32.3 | 59 | 39.6 |
| 30 | 41.2 | 60 | 33.2 |
| Day | Concentration of the Ag | Day | Concentration of the Ag |
| 61 | 35.2 | 76 | 33.2 |
| 62 | 30.4 | 77 | 30.5 |
| 63 | 35.6 | 78 | 39.5 |
| 64 | 35.2 | 79 | 37.5 |
| 65 | 30.2 | 80 | 38.1 |
| 66 | 28.9 | 81 | 39.5 |
| 67 | 33.5 | 82 | 38.5 |
| 68 | 35.6 | 83 | 35.6 |
| 69 | 36.4 | 84 | 31.2 |
| 70 | 25.6 | 85 | 36.5 |
| 71 | 30.2 | 86 | 37.1 |
| 72 | 36.4 | 87 | 40.5 |
| 73 | 29.8 | 88 | 33.9 |
| 74 | 39.5 | 89 | 30.8 |
| 75 | 32.4 | 90 | 36.5 |

Fig S1. Phylogenetic dendrogram based on 16S rRNA gene sequence analysis showing the phylogenetic position of Streptomyces parvulus strain k2 OK446664.1

Fig. S2. UV-Vis spectrum of biosynthesized AgNPs. The inset indicates the color difference of AgNO3 (a), cell free supernatant (b), and AgNPs (c).

Fig. S3. Digital photo of blank (a) and modified ceramic filter (b).