Supporting information

Magnetic pomegranate peels activated carbon (MG-PPAC) composite for Acid Orange 7 dye removal from wastewater

Abbreviations

| Abbreviation | Full Name |
| --- | --- |
| AO7 | Acid orange 7 |
| MG-PPAC | Magnetic pomegranate peels activated carbon |
| BET | Brunauer–Emmett–Teller |
| SEM | Scanning electron microscopy |
| EDX | Energy-dispersive X-ray analysis |
| XRD | X-ray diffraction |
| VSM | Vibrating sample magnetometer |
| PFOM | Pseudo first order kinetic model |
| PSOM | Pseudo second order kinetic model |
| IPDM | Intraparticle diffusion model |
| FDM | Film diffusion |
| RLP | Leaf powder of rubber |
| MB | Methylene blue |
| RT | Room temperature |
| LIM | Langmuir isotherm model |
| FIM | Freundlich isotherm model |
| TIM | Tempkin isotherm model |

Table S1: Impact of temperature on PPAC Surface area and volume of pores.

| Method | Temperature (°C) | BET |  |  |
| --- | --- | --- | --- | --- |
| Sample |  | SBET (m2 g) | VT (cm3/g) | DP (nm) |
| PPAC | 600 | 315.59 | 0.1775 | 2.2499 |
|  | 700 | 922.14 | 0.5669 | 2.4588 |
|  | 800 | 753.27 | 0.4791 | 2.5438 |
|  | 900 | 779.05 | 0.5121 | 2.6292 |

Table S2: Effect of impregnation ratio on the surface area analysis of the preparation of PPAC at 700°C.

| ZnCl2 : PP (W:W) ratio | BET |  |  |
| --- | --- | --- | --- |
|  | SBET (m2/ g) | VT (cm3/g) | DP (nm) |
| 1:1 | 378.74 | 0.1902 | 2.0089 |
| 1:2 | 193.06 | 918.04 | 1.9021 |
| 2:1 | 922.14 | 0.5669 | 2.4588 |

Table S3: The SBET, volume of total pores (VT) and mean diameter of pores (DP) of MG-PPAC.

| MG-PPAC | BET |  |  |
| --- | --- | --- | --- |
|  | SBET (m2/ g) | VT (cm3/g) | DP (nm) |
| 1:1 | 513.34 | 0.4025 | 3.1364 |

Figure S1. Synthesis scheme of the magnetic pomegranate peels activated carbon.

Table S4. Evaluation of the PFOM and PSOM constants and qe calculated and experimental values of diverse C0 of AO7 dye and MG-PPAC doses.

| Parameter |  |  | PFOM |  |  | PSOM |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Carbon Conc. | AO (mg L–1) | qe (exp.) | qe (calc.) | k1 x 103 | R2 | qe (calc.) | k2 x 103 | h | R2 |
|  | 150 | 191.22 | 44.62 | 27.8663 | 0.985 | 196.08 | 1.36 | 52095.12 | 1.000 |
| 0.75 g/L | 200 | 239.66 | 99.84 | 25.1027 | 0.967 | 250.00 | 0.49 | 30562.50 | 1.000 |
|  | 300 | 267.72 | 96.81 | 17.7331 | 0.983 | 277.78 | 0.36 | 28086.46 | 0.999 |
|  | 400 | 338.72 | 156.78 | 11.0544 | 0.895 | 357.14 | 0.15 | 19005.12 | 0.985 |
|  | 500 | 339.18 | 75.88 | 3.6848 | 0.968 | 333.33 | 0.26 | 28888.83 | 0.986 |
|  | 150 | 147.98 | 18.17 | 34.78 | 0.858 | 149.25 | 5.22 | 116277.99 | 1.000 |
| 1g/L | 200 | 195.60 | 38.99 | 38.92 | 0.914 | 196.08 | 2.86 | 109880.33 | 1.000 |
|  | 300 | 262.97 | 72.85 | 28.56 | 0.971 | 270.27 | 0.76 | 55551.39 | 1.000 |
|  | 400 | 292.63 | 112.02 | 21.65 | 0.992 | 303.03 | 0.38 | 34802.50 | 1.000 |
|  | 500 | 296.50 | 98.70 | 6.45 | 0.737 | 294.12 | 0.25 | 22024.12 | 0.983 |
|  | 150 | 59.90 | 0.88 | 22.57 | 0.857 | 59.88 | 73.39 | 263155.41 | 1.000 |
| 2.5 g/L | 200 | 79.81 | 2.93 | 27.18 | 0.963 | 70.92 | 1.10 | 5512.65 | 0.993 |
|  | 300 | 119.50 | 1.44 | 24.18 | 0.917 | 119.05 | 44.10 | 624999.80 | 1.000 |
|  | 400 | 158.85 | 9.48 | 30.17 | 0.870 | 158.73 | 8.44 | 212763.49 | 1.000 |
|  | 500 | 178.21 | 56.12 | 20.50 | 0.966 | 185.19 | 0.72 | 24813.74 | 1.000 |
|  | 150 | 49.95 | 0.49 | 20.96 | 0.939 | 50.00 | 114.29 | 285714.25 | 1.000 |
| 3 g/L | 200 | 66.55 | 1.68 | 29.94 | 0.994 | 66.67 | 44.12 | 196077.83 | 1.000 |
|  | 300 | 99.81 | 1.61 | 26.25 | 0.950 | 100.00 | 43.48 | 434783.00 | 1.000 |
|  | 400 | 132.98 | 2.63 | 33.39 | 0.966 | 133.33 | 29.61 | 526310.85 | 1.000 |
|  | 500 | 159.81 | 70.45 | 39.38 | 0.830 | 163.93 | 1.67 | 44826.43 | 1.000 |
|  | 150 | 42.84 | 0.29 | 16.35 | 0.961 | 42.92 | 164.51 | 303023.66 | 1.000 |
| 3.5 g/L | 200 | 57.10 | 0.58 | 21.42 | 0.946 | 57.14 | 95.70 | 312498.97 | 1.000 |
|  | 300 | 85.59 | 1.04 | 23.26 | 0.912 | 85.47 | 59.52 | 434800.80 | 1.000 |
|  | 400 | 113.94 | 1.31 | 27.29 | 0.857 | 113.64 | 40.76 | 526316.19 | 1.000 |
|  | 500 | 141.08 | 16.22 | 24.64 | 0.987 | 142.86 | 3.53 | 71938.63 | 1.000 |

Table S5. Assessment of the EM, IPDM and FDM kinetic models.

| Sorbent dose | AO7 conc. | EM |  |  | EPDM |  |  | FDM |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | β | α | R2 | Kdif | C | R2 | KFD | C | R2 |
|  | 150 | 0.077 | 2.33E+05 | 0.928 | 3.09 | 154.56 | 0.814 | 0.0407 | 0.77 | 0.870 |
| 0.75 g/L | 200 | 0.041 | 2.52E+03 | 0.986 | 6.16 | 163.38 | 0.954 | 0.0427 | 0.06 | 0.799 |
|  | 300 | 0.030 | 5.74E+02 | 0.983 | 8.25 | 164.08 | 0.916 | 0.0392 | 0.13 | 0.694 |
|  | 400 | 0.020 | 1.49E+02 | 0.928 | 13.09 | 155.38 | 0.934 | 0.0022 | 0.61 | 0.908 |
|  | 500 | 0.025 | 6.16E+02 | 0.822 | 9.93 | 192.99 | 0.765 | 0.0357 | 0.35 | 0.503 |
|  | 150 | 0.165 | 2.99E+09 | 0.906 | 0.99 | 136.40 | 0.707 | 0.0380 | 2.10 | 0.858 |
| 1g/L | 200 | 0.207 | 1.22E+16 | 0.916 | 1.81 | 174.55 | 0.717 | 0.0388 | 1.61 | 0.914 |
|  | 300 | 0.043 | 1.32E+04 | 0.918 | 5.56 | 197.87 | 0.800 | 0.0420 | 0.56 | 0.863 |
|  | 400 | 0.029 | 1.15E+03 | 0.982 | 8.33 | 189.72 | 0.910 | 0.0429 | 0.17 | 0.737 |
|  | 500 | 0.026 | 3.17E+02 | 0.869 | 9.44 | 156.69 | 0.836 | 0.0363 | 0.49 | 0.504 |
|  | 150 | 5.342 | 8.40E+135 | 0.966 | 0.05 | 59.28 | 0.951 | 0.0226 | 4.22 | 0.857 |
| 2.5 g/L | 200 | 1.353 | 3.74E+44 | 0.963 | 0.18 | 77.63 | 0.873 | 0.0271 | 3.30 | 0.963 |
|  | 300 | 1.276 | 1.49E+64 | 0.921 | 0.13 | 118.01 | 0.705 | 0.0241 | 4.42 | 0.917 |
|  | 400 | 0.703 | 2.66E+46 | 0.865 | 0.71 | 150.65 | 0.606 | 0.0301 | 2.82 | 0.870 |
|  | 500 | 0.049 | 9.02E+02 | 0.915 | 4.83 | 119.48 | 0.805 | 0.0386 | 0.19 | 0.756 |
|  | 150 | 8.547 | 1.48E+182 | 0.954 | 0.03 | 49.56 | 0.948 | 0.0210 | 4.62 | 0.939 |
| 3 g/L | 200 | 2.145 | 3.37E+59 | 0.930 | 0.11 | 65.24 | 0.818 | 0.0300 | 3.68 | 0.994 |
|  | 300 | 2.483 | 1.06E+105 | 0.927 | 0.10 | 98.61 | 0.834 | 0.0263 | 4.13 | 0.950 |
|  | 400 | 2.503 | 9.75E+141 | 0.888 | 0.21 | 130.55 | 0.586 | 0.0335 | 3.92 | 0.966 |
|  | 500 | 0.097 | 3.78E+05 | 0.923 | 2.46 | 130.38 | 0.810 | 0.0394 | 0.82 | 0.830 |
|  | 150 | 13.193 | 8.97E+241 | 0.941 | 0.02 | 42.57 | 0.975 | 0.0164 | 5.00 | 0.961 |
| 3.5 g/L | 200 | 7.022 | 1.03E+171 | 0.968 | 0.04 | 56.63 | 0.972 | 0.0215 | 4.59 | 0.946 |
|  | 300 | 4.545 | 9.89E+165 | 0.950 | 0.06 | 84.85 | 0.971 | 0.0232 | 4.41 | 0.912 |
|  | 400 | 4.044 | 1.48E+197 | 0.955 | 0.14 | 112.31 | 0.597 | 0.0263 | 4.15 | 0.883 |
|  | 500 | 0.190 | 1.65E+10 | 0.932 | 1.25 | 126.08 | 0.821 | 0.0352 | 1.60 | 0.880 |