Elimination of Cd2+ from Synthetic and Real Polluted Water by Optimized Acacia nilotica Biographene

Nourhan El-Maghrabi1,2*, Manal Fawzy1,2,3 , and Alaa El Din Mahmoud1,2

1 Environmental Sciences Department, Faculty of Science, Alexandria University, 21511 Alexandria, Egypt.

2 Green Technology Group, Faculty of Science, Alexandria University, 21511 Alexandria, Egypt

3 National Biotechnology Network of Expertise (NBNE), Academy of Scientific Research and Technology (ASRT), Egypt

*Corresponding author: nourhan.elmaghrabi@alexu.edu.eg      orcid: 0000-0001-6097-3208

Supplemental Information

Fig. S1 TEM images of graphene synthesized at 250℃ for 1h (A), at 250℃ for 3h  (B), at 450℃ for 1h (C), and at 450℃ for 3h (D).

Fig. S2. Elemental analysis of the fabricated graphene at 250℃ for 1h (A), at 250℃ for 3h (B), at 450℃ for 1h (C), and at 450℃ for 3h (D).

D

D

C

C

B

B

A

A

Fig. S3. Zeta potential of the prepared graphene at 250℃ for 1h (A), at 250℃ for 3h (B), at 450℃ for 1h (C), and at 450℃ for 3h (D).

B

A

B

Fig. S4. The reusability of biographene (A), the removal of cadmium from real wastewater (B).

Table S1

The elemental analysis of the synthesized graphene at 250℃ for 1 hour (G250-1h), 250℃ for 3 hours (G250-3h), 450℃ for 1 hour (G450-1h), and 450℃ for 3 hours (G450-3h) in atomic%

| The element | G250-1h | G250-3h | G450-1h | G450-3h |
| --- | --- | --- | --- | --- |
| C | 53.64 | 93.87 | 81.76 | 95.38 |
| O | 27.57 | 5.91 | 12.32 | 4.00 |
| Al | 7.83 | - | - | - |
| Si | 8.69 | 0.10 | 0.15 | 0.31 |
| K | 2.26 | 0.12 | 1.53 | - |
| Mg | - | - | 0.97 | - |
| P | - | - | 0.17 | - |
| S | - | - | 0.13 | 0.10 |
| Cl | - | - | 0.06 | 0.11 |
| Ca | - | - | 2.90 | 0.10 |

Table S2

Kinetic and isotherm parameters of G450-3h

Kinetic Parameters

|  | Pseudo-first-order |  |  |  | Pseudo-second-order |  |  |  | Elovich |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| qe, expa (mg g-1) | K1 (min-1) | qe, cal (mg g-1) | R2 |  | K2 (g mg-1 min-1) | qe, cal (mg g-1) | R2 |  | β (g mg-1) | α (g mg-1 min-1) | R2 |
| 21.3 | 0.1 | 0.9 | 0.95 |  | 0.003 | 24.33 | 0.99 |  | 0.2 | 1.2 | 0.96 |

a = experimental data at initial Cd(II)concentration of 15 mg L-1

Isotherm Parameters

|  | Langmuir |  |  |  |  | Freundlich |  |  |  | Temkin |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| qm* (mg g-1) | KL (L mg-1) | RL | R2 |  | KF (L mg-1) |  | 1/n | R2 |  | BT (J mol-1) | KT (L mg-1) | R2 |
| 122.3 | 9.6 | 0.02 | 0.99 |  | 3.34 |  | 0.5 | 0.96 |  | 16.3 | 1.18 | 0.95 |

* qm is the calculated maximum adsorption capacity by Langmuir model.

Table S3

Physicochemical parameters of the real wastewater sample

| Parameter | Concentration |
| --- | --- |
| pH | 6 |
| Cadmium (mg/L) | 1.18 |
| TDS (ppm) | 345 |
| BOD (mg/L) | 127 |
| COD (mg/L) | 54 |
| EC (µS cm-1) | 677 |