Supplementary information

Fig. S1 Fluoride ion removal rate of A-00, A-02, A-04, and A-06 (initial concentration (Cinit) = 20 ppm, adsorbent dose = 3 mg/ml, adsorption time = overnight).

Fig. S2 Comparison of fluoride ion removal capacity between Ca(OH)2, commercial AlOOH (c-AlOOH) and A-04 (Cinit = 20 ppm, adsorbent dose = 0.4 mg/ml, adsorption time = 120 min).

Fig. S3 Powder X-ray diffraction patterns of A-00, A-02, A-04, and A-06.

Fig. S4 Al 2p X-ray photoelectron spectroscopy (XPS) spectra of (a) A-00, (b) A-02, (c) A-04, and (d) A-06 (grey: experimental data, purple: fitted curve, green: background, blue: Al-OH, and red: Al-O).

Table S1 Al 2p XPS peak parameters for A-00, A-02, A-04, and A-06 adsorbents.

|  | Binding energy (eV) | A-00 | A-02 | A-04 | A-06 |
| --- | --- | --- | --- | --- | --- |
| Al-OH | 74.6 | 13.71 % | 32.67 % | 47.23 % | 66.00 % |
| Al-O | 74.1 | 86.29 % | 67.34 % | 52.77 % | 34.00 % |
| Area ratio of Al-OH to Al-O | - | 0.16 | 0.49 | 0.89 | 1.94 |

Fig. S5 N2 isotherm of A-00, A-02, A-04, and A-06 at 77 K.

Table S2 Brunauer-Emmett-Teller (BET) surface area of A-00, A-02, A-04, and A-06 (calculated from N2 isotherm measurement at 77 K).

| AlOOH powders | BET surface area (m2/g) |
| --- | --- |
| A-00 | 166 |
| A-02 | 203 |
| A-04 | 207 |
| A-06 | 204 |

Fig. S6 (a) The fluoride ion removal adsorption capacity of A-04 as a function of initial fluoride ion concentrations (solid line = pseudo-first order fitting, dashed line = pseudo-second order fitting, adsorbent dose = 0.4 mg/ml) and (b) its Langmuir fit (red solid line).

Table S3 Pseudo-first order, pseudo-second order kinetics and Langmuir isotherm model parameters for fluoride ion adsorption on A-04 with different initial fluoride ion concentrations.

| Experimental values |  |  |  |
| --- | --- | --- | --- |
| parameters | values |  |  |
| Cinit | 10 ppm | 20 ppm | 50 ppm |
| qe (mg/g) | 13.00 | 17.75 | 27.00 |
| Pseudo-first order |  |  |  |
| parameters | values |  |  |
| Cinit | 10 ppm | 20 ppm | 50 ppm |
| qe (mg/g) | 12.40 | 17.94 | 26.84 |
| k1 (min-1) | 0.14 | 0.13 | 0.09 |
| R2 | 0.98 | 0.99 | 0.99 |
| Pseudo-second order |  |  |  |
| parameters | values |  |  |
| Cinit | 10 ppm | 20 ppm | 50 ppm |
| qe (mg/g) | 13.33 | 19.17 | 29.82 |
| k2 (g/mg*min) | 0.02 | 0.13 | 0.01 |
| R2 | 0.99 | 0.98 | 0.98 |
| Langmuir isotherm |  |  |  |
| qmax (mg/ml) |  | 34.17 |  |
| KL (L/mg) |  | 0.13 |  |
| R2 |  | 0.94 |  |

Table S4 Comparison of maximum adsorption capacities (qmax) of various Al-based powder-type adsorbents and paper-type adsorbents for fluoride ions.

| Adsorbent type | Name | qmax (mg/g) | References |
| --- | --- | --- | --- |
| Powder | Activated alumina | 16.34 | (Ku and Chiou 2002) |
|  | Amorphous AlOOH | 41.9 | (Gai et al. 2021) |
|  | Bayerite/boehmite | 56.8 | (Jia et al. 2015) |
|  | Al2O3 nanoparticles | 9.73 | (Tangsir et al. 2016) |
|  | Nano-AlOOH | 3.259 | (Wang et al. 2009) |
|  | Hydrous-manganese oxide-coated alumina | 7.09 | (Maliyekkal et al. 2006) |
|  | A-04 | 34.17 | This study |
| Paper | CBM/UF/MMM | 5.00 | (Chatterjee et al. 2020) |
|  | ABN/TPU-NFM | 1.90 | (Suriyaraj et al. 2015) |
|  | MFS-AA-PVDF | 5.30 | (Meng et al. 2020) |
|  | PA-1.25 | 6.26 | This study |

Fig. S7 N2 isotherm of polyvinylidene fluoride (PVDF) film with the different volumetric ratio of N,N-dimethylformamide (DMF) and acetone at 77 K.

Table S5 BET surface area of PVDF film with the different volumetric ratio of DMF and acetone.

| The composition of the PVDF solution | BET surface area (m2/g) |
| --- | --- |
| DMF 100 : Acetone 0 | 5 |
| DMF 75 : Acetone 25 | 7 |
| DMF 50 : Acetone 50 | 17 |
| DMF 25 : Acetone 75 | 14 |

Fig. S8 Thermogravimetric analysis of PA-1.25 (a mass loss of approximately 2.8 wt% occurs as AlOOH changes to Al2O3 between 200 °C and 320 °C).

Fig. S9 N2 isotherm of A-04-incorporated paper-type adsorbent with different mass ratio of A-04 to PVDF at 77 K.

Table S6 BET surface area of A-04-incorporated PVDF paper-type adsorbent with different mass ratio of A-04 to PVDF.

| Mass ratio of A-04 to PVDF | BET surface area (m2/g) |
| --- | --- |
| 0.00 | 17 |
| 0.50 | 60 |
| 1.00 | 86 |
| 1.25 | 88 |
| 1.50 | 90 |

Table S7 Pseudo-first order, pseudo-second order kinetics and Langmuir isotherm model parameters for fluoride ion adsorption on PA-1.25 with different initial fluoride ion concentrations.

| Experimental values |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| parameters | values |  |  |  |  |  |  |  |  |  |
| Cinit | 10 ppm |  | 20 ppm |  |  | 30 ppm |  | 40 ppm |  | 50 ppm |
| qe (mg/g) | 2.17 |  | 3.80 |  |  | 4.90 |  | 4.67 |  | 5.42 |
| Pseudo-first order |  |  |  |  |  |  |  |  |  |  |
| parameters | values |  |  |  |  |  |  |  |  |  |
| Cinit | 10 ppm | 20 ppm |  |  | 30 ppm |  | 40 ppm |  | 50 ppm |  |
| qe (mg/g) | 2.11 | 4.03 |  |  | 4.41 |  | 5.03 |  | 5.49 |  |
| k1 (min-1) | 0.03 | 0.03 |  |  | 0.04 |  | 0.04 |  | 0.04 |  |
| R2 | 0.98 | 0.99 |  |  | 0.99 |  | 0.98 |  | 0.99 |  |
| Pseudo-second order |  |  |  |  |  |  |  |  |  |  |
| parameters | values |  |  |  |  |  |  |  |  |  |
| Cinit | 10 ppm | 20 ppm |  |  | 30 ppm |  | 40 ppm |  | 50 ppm |  |
| qe (mg/g) | 2.37 | 4.55 |  |  | 4.90 |  | 5.51 |  | 6.04 |  |
| k2 (g/mg*min) | 0.01 | 0.01 |  |  | 0.01 |  | 0.01 |  | 0.01 |  |
| R2 | 0.98 | 0.97 |  |  | 0.99 |  | 0.99 |  | 0.99 |  |
| Langmuir isotherm |  |  |  |  |  |  |  |  |  |  |
| qmax (mg/ml) |  |  |  | 6.26 |  |  |  |  |  |  |
| KL (L/mg) |  |  |  | 0.16 |  |  |  |  |  |  |
| R2 |  |  |  | 0.98 |  |  |  |  |  |  |

Fig. S10 (a) Water flux of PA-1.25 at 0.2, 0.4, 0.6, 0.8, and 1.0 bar and (b) linear fit of water flux as a function of pressure.

Fig. S11 XPS (a) C 1s, (b) F 1s (c) Al 2p, and (d) O 1s spectra of PA-1.25 before and after fluoride ion adsorption (Cinit = 50 ppm, adsorbent dose = 3 mg/ml, t = 120 min).

Table S8 XPS peak parameters of PA-1.25 before and after fluoride ion adsorption.

| Electrons | Peak | Binding energy (eV) | Before adsorption | After adsorption |
| --- | --- | --- | --- | --- |
|  |  |  | Concentration (Atomic %) |  |
| Al 2p | Al-CH2CH2 | 73.2 | 11.10 | 1.61 |
|  | Al-O | 73.8 | 12.00 | 11.79 |
|  | Al-OH | 74.6 | 76.90 | 50.98 |
|  | Al-F | 75.3 | 0.00 | 35.62 |
| O 1s | Al-O | 530.9 | 13.28 | 14.39 |
|  | Al-OH | 532.0 | 76.58 | 58.37 |
|  | H2O | 533.0 | 10.14 | 27.24 |

References

Ku, Y. & Chiou, H.-M. (2002) The adsorption of fluoride ion from aqueous solution by activated alumina Water Air Soil Pollut 133: 349-361 doi:https://doi.org/10.1023/A:1012929900113

Gai, W.-Z., Zhang, S.-H., Yang, Y., Zhang, X. & Deng, Z.-Y. (2021) Separation of excess fluoride from water using amorphous and crystalline AlOOH adsorbents ACS omega 6: 16488-16497 doi:https://doi.org/10.1021/acsomega.1c01620

Jia, Y. et al. (2015) Fluoride removal mechanism of bayerite/boehmite nanocomposites: roles of the surface hydroxyl groups and the nitrate anions J Colloid Interface Sci 440: 60-67 doi:https://doi.org/10.1016/j.jcis.2014.10.069

Tangsir, S. et al. (2016) Water defluoridation using Al2O3 nanoparticles synthesized by flame spray pyrolysis (FSP) method Chem Eng J 288: 198-206 doi:https://doi.org/10.1016/j.cej.2015.11.097

Wang, S. G., Ma, Y., Shi, Y. J. & Gong, W. X. (2009) Defluoridation performance and mechanism of nano‐scale aluminum oxide hydroxide in aqueous solution J Chem Technol Biotechnol 84: 1043-1050 doi:https://doi.org/10.1002/jctb.2131

Maliyekkal, S. M., Sharma, A. K. & Philip, L. (2006) Manganese-oxide-coated alumina: a promising sorbent for defluoridation of water Water Res 40: 3497-3506 doi:https://doi.org/10.1016/j.watres.2006.08.007

Chatterjee, S., Mukherjee, M. & De, S. (2020) Groundwater defluoridation and disinfection using carbonized bone meal impregnated polysulfone mixed matrix hollow-fiber membranes J Water Process Eng 33: 101002 doi:https://doi.org/10.1016/j.jwpe.2019.101002

Suriyaraj, S., Bhattacharyya, A. & Selvakumar, R. (2015) Hybrid Al 2 O 3/bio-TiO 2 nanocomposite impregnated thermoplastic polyurethane (TPU) nanofibrous membrane for fluoride removal from aqueous solutions RSC Adv 5: 26905-26912 doi:https://doi.org/10.1039/C5RA02523K

Meng, C., Zheng, X., Hou, J. & Wang, C. (2020) Preparation and defluoridation effectiveness of composite membrane sorbent MFS-AA-PVDF Water Air Soil Pollut 231: 1-10 doi:https://doi.org/10.1007/s11270-019-4351-2