Table S1. EDX elemental analysis of CMC and MOF: Fe (Ⅱ)-CMC sorbent.

| Element | CMC (wt %) | MOF (wt %) |
| --- | --- | --- |
| C | 28.78 | 28. 25 |
| N | 22.91 | 32.50 |
| O | 48.16 | 36.25 |
| S | 0.02 | 0.1 |
| Fe | _ | 2.90 |

Fig.S1. Equilibrium isotherms for the adsorptive uptake of MB, CV and MG onto (MOF: Fe (Ⅱ)-CMC) sorbent.

Fig. S2. Zeta Potential distribution of MOF: Fe (Ⅱ)-CMC nanocomposite structure.

Fig. S3.  Diagrammatic representation of the synthesis of MOF:Fe(Ⅱ)-CMC nanocomposite and the dye adsorption process