Table S1. EDX elemental analysis of CMC and MOF: Fe (Ⅱ)-CMC sorbent.  
	Element
	CMC (wt %)
	MOF (wt %)

	C
	28.78
	28. 25

	N
	22.91
	32.50

	O
	48.16
	36.25

	S
	0.02
	0.1

	Fe
	_
	2.90
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Fig.S1. Equilibrium isotherms for the adsorptive uptake of MB, CV and MG onto (MOF: Fe (Ⅱ)-CMC) sorbent. 
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Fig. S2. Zeta Potential distribution of MOF: Fe (Ⅱ)-CMC nanocomposite structure.




























[bookmark: _GoBack]Fig. S3.  Diagrammatic representation of the synthesis of MOF:Fe(Ⅱ)-CMC nanocomposite and the dye adsorption process    
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