Supplementary Information.

Transhydrogenation of C5H12/C6H10 over CrOx/Al2O3 and Potassium-doped CrOx/Al2O3 Catalysts.

Mustapha D. Garba and S. David Jackson*

Centre for Catalysis Research, School of Chemistry, University of Glasgow, Glasgow G12 8QQ, Scotland, UK.

e-mail: david.jackson@glasgow.ac.uk

The yield of each product formed, assuming no interaction between the species, was calculated from the individual run and summed as the theoretical yield:

Palone + 1HYalone= 1HY Theory

This was then compared to the mixed feed runs termed as transhydrogenation yield, which was used to understand the effect of the transhydrogenation occurring during reaction.

XRD spectra for the alumina support and the catalyst.  Only alumina reflections are observed.

Table S1: Products yield of the transhydrogenation over CrOx/Al2O3 at 773 K

|  | P | 1HY | P+1HY | P+1HY Theory |
| --- | --- | --- | --- | --- |
|  | Conversion [%] |  |  |  |
| Pentane[P] | 11 |  | 19 | 11 |
| Hexyne[1HY] |  | 98 | 96 | 98 |
|  | Yield [%] |  |  |  |
| Iso-pentane | 1.0 |  | 0.2 | 1.0 |
| Pentene |  |  | 0.9 | 0 |
| Trans-2-pentene | 8.6 |  |  | 8.6 |
| Hexane |  | 1.6 | 2.1 | 1.6 |
| Hexene |  | 1.0 | 0.7 | 1.0 |
| 2-Hexene |  | 0.6 | 1.6 | 0.6 |
| 3-Hexene |  | 1.6 | 1.9 | 1.6 |
| Methyl-2-pentene |  | 3.2 | 4.2 | 3.2 |
| 3-Methylpentyne |  | 5.2 | 3.3 | 5.2 |
| 3-methyl-1-hexene |  | 7.5 | 5.1 | 7.5 |
| 3-Methylhexane |  | 2.5 | 5.4 | 2.5 |
| 2-Methyl-1,3-pentadiene |  | 1.4 | 9.2 | 1.4 |
| 1,4-Hexadiene |  | 13.5 | 16.9 | 13.5 |
| 2-methyl-1-hexene |  | 7.4 | 5.1 | 7.4 |
| methylcyclohexane | 0.6 | 8.8 | 1.6 | 9.4 |
| Ethylcyclopentane | 0.4 |  |  | 0.4 |

Table S2: Products yield of the transhydrogenation over CrOx/Al2O3 at 673 K

|  | P | 1HY | P+1HY | P+1HY Theory |
| --- | --- | --- | --- | --- |
|  | Conversion [%] |  |  |  |
| Pentane[P] | 08 |  | 13 | 08 |
| Hexyne[1HY] |  | 97 | 86 | 97 |
|  | Yield [%] |  |  |  |
| Iso-pentane | 0.46 |  | 0.11 | 0.46 |
| Pentene |  |  | 0.01 | 0 |
| Trans-2-Pentene | 0.53 |  |  | 0.53 |
| hexane |  | 0.38 | 1.95 | 0.38 |
| Hexene |  |  | 0.27 | 0 |
| 2-Hexene |  | 0.9 | 6.08 | 0.9 |
| 3-Hexene |  |  | 0.42 | 0 |
| Methyl-2-pentene |  | 3.42 | 4.61 | 3.42 |
| 3-Methylpentyne |  | 7.49 | 10.28 | 7.49 |
| 3-methyl-1-hexene |  | 1.67 | 1.97 | 1.67 |
| 3-Methylhexane |  | 6.17 | 1.36 | 6.17 |
| 2-Methyl-1,3-pentadiene |  | 7.49 | 0.27 | 7.49 |
| 1,4-Hexadiene |  | 31.42 | 25.18 | 31.42 |
| methylcyclohexane | 3.91 | 1.8 |  | 5.17 |

Table S3: Products yield of the transhydrogenation over CrOx/Al2O3 at 623 K

|  | P | 1HY | P+1HY | P+1HY Theory |
| --- | --- | --- | --- | --- |
|  | Conversion [%] |  |  |  |
| Pentane[P] | 10 |  | 26 | 10 |
| Hexyne[1HY] |  | 95 | 87 | 95 |
|  | Yield [%] |  |  |  |
| Pentene |  |  | 0.19 | 0 |
| Trans-2-Pentene | 0.08 |  |  | 0.08 |
| Haxane |  |  | 0.52 | 0 |
| Hexene |  | 0.33 | 1.81 | 0.33 |
| 2-Hexene |  | 1.21 | 2.06 | 1.21 |
| 3-Hexene |  |  | 1.46 | 0 |
| Methyl-2-pentene |  | 2.17 | 2.22 | 2.17 |
| 3-Methylpentyne |  | 11.6 | 19.24 | 11.6 |
| 3-methyl-1-hexene |  | 1.29 | 1.70 | 1.29 |
| 3-Methylhexane |  | 0.55 | 1.38 | 0.55 |
| 2-Methyl-1,3-pentadiene |  |  | 2.14 | 0 |
| 1,4-Hexadiene |  | 20.95 | 19.38 | 20.95 |
| methylcyclohexane | 5.23 | 15.19 | 2.42 | 20.42 |
| Ethylcyclopentane | 1.25 | 2.77 | 1.12 | 3.92 |

Table S4: Products yield of the transhydrogenation over CrOx/Al2O3 at 573 K

|  | P | 1HY | P+1HY | P+1HY Theory |
| --- | --- | --- | --- | --- |
|  | Conversion [%] |  |  |  |
| Pentane[P] | 04 |  | 20 | 04 |
| Hexyne[1HY] |  | 42 | 48 | 42 |
|  | Yield [%] |  |  |  |
| Iso-pentane |  |  | 0.05 | 0 |
| Pentene |  |  | 0.10 | 0 |
| Trans-2-Pentene | 0.02 |  |  | 0.02 |
| hexane |  | 0.05 | 0.88 | 0.05 |
| Hexene |  | 1.07 | 3.06 | 1.07 |
| 2-Hexene |  | 0.2 | 3.08 | 0.2 |
| 3-Hexene |  |  | 3.44 | 0 |
| Methyl-2-pentene |  |  | 0.28 | 0 |
| 3-Methylpentyne |  | 6.18 | 7.75 | 6.18 |
| 3-methyl-1-hexene |  | 1.13 | 0.65 | 1.03 |
| 3-Methylhexane |  | 0.45 | 0.34 | 0.41 |
| 2-Methyl-1,3-pentadiene |  | 0.17 | 0.66 | 0.17 |
| 1,4-Hexadiene |  | 9.41 | 5.32 | 9.41 |
| methylcyclohexane | 0.22 | 3.87 | 1.24 | 3.99 |
| Ethylcyclopentane | 0.39 | 1.36 | 0.89 | 1.75 |

Table S5: Products yield of the transhydrogenation over CrOx/Al2O3 at 523 K

|  | P | H | P+H | P+H Theory |
| --- | --- | --- | --- | --- |
|  | Conversion [%] |  |  |  |
| Pentane[P] | 0.9 |  | 20 | 0.9 |
| Hexyne[1HY] |  | 47 | 46 | 47 |
|  | Yield [%] |  |  |  |
| Iso-pentane |  |  | 0 | 0 |
| Pentene |  |  |  | 0 |
| Trans-2-Pentene | 0.008 |  |  | 0.008 |
| Hexane |  | 0 | 0 | 0 |
| Hexene |  | 0.12 | 0 | 0.12 |
| 2-Hexene |  | 0 | 0 | 0 |
| 3-Hexene |  | 0 | 0.09 | 0 |
| Methyl-2-pentene |  | 0.56 | 1.45 | 0.56 |
| 3-Methylpentyne |  | 10.55 | 0 | 10.55 |
| 3-methyl-1-hexene |  | 1.65 | 1.81 | 1.5 |
| 3-Methylhexane |  | 0.46 | 0.31 | 0.42 |
| 2-Methyl-1,3-pentadiene |  | 1.64 | 1.58 | 1.64 |
| 1,4-Hexadiene |  | 11.51 | 0.56 | 11.51 |
| 2-methyl-1-1hexene |  | 1.36 | 2.24 | 1.364 |
| methylcyclohexane |  | 11.18 | 2.41 | 11.187 |

Figure S1.  Profile of the evolved gases over CrOx/Al2O3 using pentane only at 523 K.

Figure S2.  Profile of the evolved gases over CrOx/Al2O3 using 1-hexyne only at 523 K.

Figure S3.  Profile of the evolved gases over CrOx/Al2O3 using pentane/1-hexyne at 523 K.

The TPR/TGA for K-CrOx/Al2O3.  There are hydrogen up-takes at 540 K and 760 K’

Table S6. Product yield of  trans-hydrogenation over K-CrOx/Al2O3 at 773K

|  | P | H | P+H | P+H Theory |
| --- | --- | --- | --- | --- |
|  | Conversion (%) |  |  |  |
| Pentane(P) | 35.7 |  | 91 | 35.7 |
| Hexyne(1HY) |  | 98 | 97 | 98 |
|  | Yield (%) |  |  |  |
| Iso-pentane | 10.48 |  | 0.21 | 0.48 |
| Pentene |  |  | 1.81 | 0 |
| Trans-2-Pentene | 0.2 |  |  | 0.2 |
| 4-Methylpentene |  | 0.03 |  | 0.03 |
| Hexane |  | 0.77 | 0.66 | 0.77 |
| 1-Hexene |  | 2.58 | 1.60 | 2.58 |
| 2-Hexene |  | 0.9 | 3.56 | 0.9 |
| 3-Hexene |  | 3.24 | 4.04 | 3.24 |
| Methyl-2-pentene |  | 10.65 | 8.58 | 10.65 |
| 3-Methyl-1-hexene |  | 21.06 | 15.29 | 21.06 |
| Benzene |  | 4.09 | 2.86 | 4.09 |
| 3-Methylhexane |  | 6.27 | 4.59 | 6.27 |
| 2-Methyl-1,3-pentadiene |  | 23.3 | 17.05 | 23.3 |
| methylcyclohexane | 17.69 | 6.20 | 18.94 | 23.89 |

Table S7. Product yield of trans-hydrogenation over K-CrOx/Al2O3 at 673K

|  | P | H | P+H | P+H Theory |
| --- | --- | --- | --- | --- |
|  | Conversion (%) |  |  |  |
| Pentane(P) | 43.58 |  | 87 | 43.58 |
| Hexyne(1HY) |  | 97 | 100 | 97 |
|  | Yield (%) |  |  |  |
| Iso-pentane |  |  | 0.04 | 0 |
| Pentene | 22.82 |  |  | 22.82 |
| Trans-2-Pentene | 0.22 |  |  | 0.22 |
| Cis-2-pentene | 0.57 |  |  | 0.57 |
| Hexane |  | 0.4 | 10.76 | 0.4 |
| 1-Hexene |  | 1.3 | 2.72 | 1.3 |
| 2-Hexene |  | 0.22 | 5.29 | 0.22 |
| 3-Hexene |  | 1.23 | 12.35 | 1.23 |
| Methyl-2-pentene |  | 9.89 | 1.26 | 9.89 |
| 3-Methyl-1-hexene |  | 28.16 | 14.64 | 28.16 |
| Benzene |  | 1.45 | 0.52 | 1.45 |
| 3-Methylhexane |  | 6.88 | 1.28 | 6.88 |
| 2-Methyl-1,3-pentadiene |  | 27.7 | 4.96 | 27.7 |
| Methylcyclohexane | 11.6 | 2.58 | 14.06 | 14.18 |

Table S8. Product yield of trans-hydrogenation over K-CrOx/Al2O3 at 623K

|  | P | H | P+H | P+H Theory |
| --- | --- | --- | --- | --- |
|  | Conversion (%) |  |  |  |
| Pentane(P) | 37.58 |  | 85 | 85 |
| Hexyne(1HY) |  | 97 | 99 | 99 |
|  | Yield (%) |  |  |  |
| Iso-pentane | 10.38 |  | 0.07 | 10.38 |
| Pentene |  |  | 0.27 | 0 |
| Trans-2-Pentene | 0.46 |  | 0.42 | 0.46 |
| Cis-2-pentene | 0.33 |  | 0.14 | 0.33 |
| Hexane |  | 0.75 | 0.34 | 0.75 |
| 1-Hexene |  |  | 0.49 | 0 |
| 2-Hexene |  |  | 5.17 | 0 |
| 3-Hexene |  |  | 0.72 | 0 |
| Methyl-2-pentene |  | 3.55 | 5.58 | 3.55 |
| 3-Methyl-1-hexene |  | 17.32 | 16.17 | 17.32 |
| Benzene |  | 1.45 | 1.03 | 1.45 |
| 3-Methylhexane |  | 4.86 | 3.28 | 0 |
| 2-Methyl-1,3-pentadiene |  | 6.8 | 15.00 | 6.8 |
| 1,4-Hexadiene |  | 31.67 |  | 31.67 |
| Methylcyclohexane | 11.76 | 10.95 | 16.45 | 22.71 |

Table S9. Product yield of trans-hydrogenation over K-CrOx/Al2O3 at 573K

|  | P | H | P+H | P+H Theory |
| --- | --- | --- | --- | --- |
|  | Conversion (%) |  |  |  |
| Pentane(P) | 36.59 |  | 77 | 36.59 |
| Hexyne(1HY) |  | 98 | 99 | 98 |
|  | Yield (%) |  |  |  |
| Iso-pentane | 10.38 |  | 0.18 | 10.38 |
| Pentene |  |  | 0.10 | 0 |
| Trans-2-Pentene | 0.42 |  |  | 0.42 |
| Cis-2-pentene | 0.71 |  |  | 0.71 |
| Hexane |  |  | 0.80 | 0 |
| 1-Hexene |  |  | 0.13 | 0 |
| 2-Hexene |  |  | 3.17 | 0 |
| 3-Hexene |  | 0.4 | 0.63 | 0.4 |
| Methyl-2-pentene |  | 4.47 | 2.35 | 4.47 |
| 3-Methyl-1-hexene |  | 18.5 | 17.05 | 18.5 |
| Benzene |  | 5.3 | 0 | 5.3 |
| 3-Methylhexane |  |  | 2.03 | 0 |
| 2-Methyl-1,3-pentadiene |  | 16.13 | 9.07 | 16.13 |
| 2-Methyl-1-1hexene |  |  | 0.89 | 0 |
| 1,4-Hexadiene |  | 35.56 | 0 | 35.56 |
| Methylcyclohexane | 13.37 | 12.54 | 14.87 | 15.91 |

Table S10.  Product yield of trans-hydrogenation over K-CrOx/Al2O3 at 523K

|  | P | H | P+H | P+H Theory |
| --- | --- | --- | --- | --- |
|  | Conversion (%) |  |  |  |
| Pentane(P) | 38.22 |  | 73 | 38.22 |
| Hexyne(1HY) |  | 94 | 98 | 94 |
|  | Yield (%) |  |  |  |
| Iso-pentane | 26.74 |  |  | 26.74 |
| Pentene | 8.12 |  | 0.06 | 8.12 |
| Trans-2-Pentene |  |  | 0.26 | 0 |
| Cis-2-pentene |  |  | 0.42 | 0 |
| Hexane |  |  | 0.29 | 0 |
| 1-Hexene |  |  | 0.20 | 0 |
| 2-Hexene |  |  | 0.07 | 0 |
| 3-Hexene |  |  | 0.27 | 0 |
| Methyl-2-pentene |  | 6.23 | 6.25 | 6.23 |
| 3-Methylpentyne |  | 33.42 |  | 33.42 |
| 3-Methyl-1-hexene |  |  | 19.36 | 0 |
| 3-Methylhexane |  | 3.91 | 3.16 | 3.91 |
| 2-Methyl-1,3-pentadiene |  | 25.89 | 16.43 | 25.89 |
| Methylcyclohexane | 3.72 | 11.86 | 13.19 | 3.7236 |