Supplementary Information

Eric Y. Dua, b, H.T. Kim Duonga, M.A. Kristine Tolentinoa, b, Jacinta L. Hounga, b, Panthipa S Eric Y. Dua,b, H.T. Kim Duonga,b, M.A. Kristine Tolentinoa, b, Jacinta L. Hounga, b, Panthipa Suwannakota,b, Kristel C. Tjandraa, Duyen H.T. Nguyena,b, Richard D. Tilleya, c, J. Justin Goodinga, b*

a School of Chemistry, The University of New South Wales, 2032

b Australian Centre for Nanomedicine, The University of New South Wales, 2032

c Electron Microscopy Unit, Mark Wainwright Analytical Centre, The University of New South Wales, 2032

* Corresponding author email address: justin.gooding@unsw.edu.au

Figure S1. The calibration curve generated from glycine standard solution of different concentrations.

Table S1. Concentration of primary amine (mol/g) found in Gelatin Type B from different sources as determined using the calibration curve generated with glycine.

Table S2.  Summary of CPADB conjugation reactions with gelatin type B (bovine skin)

Figure S2. Stacked 1H NMR (400 MHz, D2O) of the CPADB conjugation reaction to gelatin performed at (A) pH 7 and (B) pH 10. The new peak at 7.6 (highlighted yellow) indicates the reaction was successful at pH 10

Figure S3. Stacked 1H NMR (400 MHz, D2O) of the A) Gel-SPMA15, B) Gel-SPMA30, and C) Gel-SPMA45. The methylene (CH2) peak at 2.9 corresponds to the CH2 next to the terminal sulphate group. This peak was used to determine the chain length.

Figure S4. Time sweeps tested for 15 minutes for A) Gel-SPMA15, B) Gel-SPMA30, C) Gel-SPMA45, and D) GelCPADB. All polymers were prepared at 10% w/v and crosslinked with 10% w/v PEG-MAETMA.

E=2G"(1+v)

Equation S1. Formula for calculating Young’s modulus (E) from shear modulus (G”) where v is the Poisson’s ratio (assumed to be 0.5 for gelatin). Data was obtained in oscillatory rheology using a frequency of 0.1 Hz.