How does sutures pattern influence stomach motility after endoscopic sleeve gastroplasty? A computational study

Supplementary Materials

Authors: Alice Berardoa,b , Lino Poleseb,c, Emanuele Luigi Carnielb,d* and Ilaria Toniolob,d,

a Department of Civil, Environmental and Architectural Engineering, University of Padova, Italy

b Centre for Mechanics of Biological Materials, University of Padova, Italy

c Department of Surgery, Oncology and Gastroenterology, University of Padova, Italy

d Department of Industrial Engineering, University of Padova, Italy

* corresponding author: emanueleluigi.carniel@unipd.it

- Suture wires stiffness evaluation

ESG suture wires were tested by means of tensile tests, aiming to evaluate stiffness k (N/mm).

ESG sutures were PLL monofilament non absorbable wires 2-0 FILBLOC (Assut Europe, Rome, Italy).

During the experimental protocol, wires were tight longitudinally, with a constant velocity of 0.05 mm/s. The stiffness was computed as the mean slope of the force-displacement curve. Experimentations were performed on two 100 mm length samples.

Figure SM1 reports the linear regions of the force-displacement curves, together with the linear interpolation and the slopes that were obtained from the fit. The experimental results suggested an average stiffness k of 3.5 N/mm.

Figure SM1: Force-displacement curves from tensile tests on wires and evaluation of wire stiffness.