Supplementary material to Juntke et al.:

Table 1 Particle size measurement of resuspended and nebulized nanocarriers
	Sample
	Measurement
	Z-Average size
[d.nm]
	Polydispersity Index (PdI)

	Average ± SEM
[nm]

	Nanocarrier in KRB
	1
	329,7
	0,434
	374.2 ± 40.77

	
	2
	337,2
	0,449
	

	
	3
	455,6
	0,452
	

	nebulized Nanocarrier in KRB
	1
	318,5
	0,451
	320.8 ± 1.577

	
	2
	320,0
	0,446
	

	
	3
	323,8
	0,470
	


Standard error of the mean (SEM)


Table 2 Recovery rate of nebulized nanocarriers measured with UHPLC
	Sample 
	AUC
	Konz. 1:100
[µM]
	Konz.
[µM]
	Average ± SEM [µM]

	1
	1.1
	4,6293
	2,9386
	293,86
	227,7 ±53,87

	
	1.2
	1,7434
	1,2094
	120,94
	

	
	1.3
	4,201
	2,6820
	268,20
	

	2
	2.1
	4,7676
	3,0215
	302,15
	206,7 ± 68,90

	
	2.2
	3,8131
	2,4496
	244,96
	

	
	2.3
	0,9413
	0,7288
	72,88
	

	3
	3.1
	2,69
	1,7766
	177,66
	269,1 ± 45,89

	
	3.2
	5,0937
	3,2169
	321,69
	

	
	3.3
	4,8647
	3,0797
	307,97
	

	Average ± SEM [µM]
	
	234,5 ± 30,0 

	Recovered amount [%]
	
	67,0  ± 8,6


3 samples (each 1 ml; concentration of 350 µM) were prepared; 200 µl of each sample were nebulized in separate wells of a 12-well plate; triplicates were made


	
	
	

	
	
	

	
	
	



