# Supplementary Information DDTR-D-22-00018

Supplementary Table 1. Summary and comparison of characterization data by NTA and DLS for AuNP

| AuNP Measured Parameter | Supplier Value | TCD Value |
| --- | --- | --- |
| Mean hydrodynamic size (DLS) | 45.5 nm | 42.45 nm |
| Mean hydrodynamic size (NTA) | Not provided | 43.4 nm |
| Polydispersity Index (PDI) (DLS) | Not provided | 0.102 |
| Zeta Potential | -26 mV | -26.4 mV |

Supplementary Table 2. Summary and comparison of characterization data by NTA and DLS for LipImage™815

| LipImage™815 | Supplier Value | TCD Value |
| --- | --- | --- |
| Mean hydrodynamic size (DLS) | 52.2 nm | 50.72 nm |
| Mean hydrodynamic size (NTA) | Not provided | 72.7 nm |
| Polydispersity Index (PDI) (DLS) | <0.102 | 0.11 |

Supplementary Table 3. Summary and comparison of characterization data by NTA and DLS for unloaded PACA

| PACA Measured Parameter | Supplier Value | TCD Value |
| --- | --- | --- |
| Mean hydrodynamic size (DLS) | 134 | 134.8 |
| Mean hydrodynamic size (NTA) | Not provided | 94 |
| Polydispersity Index (PDI) (DLS) | 0.11 | 0.092 |
| Zeta Potential | -3.2 mV | Not provided |

Supplementary Table 4. Summary and comparison of characterization data by NTA and DLS for NR668-PACA

| PACA NR668 Measured Parameter | Supplier Value | TCD Value |
| --- | --- | --- |
| Mean hydrodynamic size (DLS) | 178 | 164.7 |
| Mean hydrodynamic size (NTA) | Not provided | 140 |
| Polydispersity Index (PDI) (DLS) | 0.28 | 0.18 |
| Zeta Potential | -3.6 mV | Not provided |

Supplementary Table 5. Summary and comparison of characterization data by NTA and DLS for CBZ-PACA

| CBZ-PACA Measured Parameter | Supplier Value | TCD Value |
| --- | --- | --- |
| Mean hydrodynamic size (DLS) | 121.8 | N/A |
| Mean hydrodynamic size (NTA) | Not provided | 116.7 |
| Polydispersity Index (PDI) (DLS) | 0.14 | N/A |
| Zeta Potential | -5.5 mV | N/A |

Supplementary Table 6. Significant differences between negative control and test concentrations; AuNP experiments

| Labs |  | NT | EMS | TiO2 | 1 | 5 | 10 | 20 | 30 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 30 min | TCD 1 | ns | **** | ns | ns | ns | ns | ns | ns |
|  | IBE | ns | ns | ns | ns | ns | ns | ns | ns |
|  | TCD 2 | ns | **** | ns | ns | ns | ns | ns | ns |
| 3 h | TCD 1 | ns | **** | ns | ns | ns | ns | ns | ns |
|  | IBE | ns | **** | ns | ns | ns | ns | ns | ns |
|  | TCD 2 | ns | **** | ns | ns | ns | ns | ns | ns |
| 24 h | TCD 1 | ns | **** | ns | ns | ns | ns | ns | ns |
|  | IBE | ns | **** | ns | ns | ns | ns | ns | ns |
|  | TCD 2 | ns | **** | ns | ns | ns | ns | ns | ns |

Supplementary Table 7. Significant differences between negative control and test concentrations; LipImage™815 experiments

|  |  | NT | EMS | TiO2 | 10 | 50 | 100 | 200 | 500 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 30 min | TCD 1 | ns | **** | ns | ns | ns | ns | ns | ns |
|  | IBE | ns | ns | ns | ns | ns | ns | ns | ns |
|  | TCD 2 | ns | **** | * | ns | ns | ns | ns | ns |
| 3 h | TCD 1 | ns | **** | ns | ns | ns | ns | ns | ns |
|  | IBE | ns | **** | ns | ns | ns | ns | ns | ns |
|  | TCD 2 | ns | **** | ns | ns | ns | ns | ns | ns |
| 24 h | TCD 1 | ns | **** | ns | ns | ns | ns | ns | ns |
|  | IBE | ns | **** | ns | ns | ns | ns | ns | ns |
|  | TCD 2 | ns | **** | * | ns | ns | ns | ns | ns |

Supplementary Table 8. Significant differences between negative control and test concentrations; PACA experiments

|  |  | NT | EMS | TiO2 | 10 | 50 | 100 | 200 | 500 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 30 min | TCD 1 | ns | **** | ns | ns | ns | ns | ns | ns |
|  | IBE | ns | ns | ns | ns | ns | ns | ns | ns |
|  | TCD 2 | ns | *** | ns | ns | ns | ns | ns | ns |
| 3 h | TCD 1 | ns | **** | ns | ns | ns | ns | ns | ns |
|  | IBE | ns | **** | ns | ns | ns | ns | ns | ns |
|  | TCD 2 | ns | **** | ns | ns | ns | ns | ns | ns |
| 24 h | TCD 1 | ns | **** | ns | ns | ns | ns | ns | ns |
|  | IBE | ns | **** | ns | ns | ns | ns | ns | ns |
|  | TCD 2 | ns | **** | ns | ns | ns | ns | ns | ns |