- Supplementary to section 3.1: Infliximab microencapsulation

Table 2. Process yield (P.Y) and Encapsulation Efficiency (E.E) of developed formulations.

|  | PEOT-PBT | PLGA RG502 | PLGA RG503 | Technique | P.Y. (%) | E.E (%) |
| --- | --- | --- | --- | --- | --- | --- |
| F1 | 100 % | 0 % | 0 % | UA | 84.2 ± 2.1 | 69.74 ± 3.21 |
| F2 | 65 % | 35 % | 0 % | UA | 94.5 ± 1.9 | 70.32 ± 3.18 |
| F3 | 65 % | 0 % | 35 % | UA | 91.3 ± 1.7 | 80.21 ± 2.97 |
| F4 | 100 % | 0 % | 0 % | Em/Ev | 68.7 ± 2.9 | 22.99 ± 1.90 |
| F5 | 65 % | 35 % | 0 % | Em/Ev | 84.1 ± 3.2 | 17.26 ± 0.92 |
| F6 | 65 % | 0 % | 35 % | Em/Ev | 79.2 ± 3.1 | 21.33 ± 1.02 |

Fig. s1 Langmuir (a) and Freundlich (b) adsorption isotherms of Rose Bengal to the surface of microcapsules fabricated by UA in PBS 100 mM, pH 7.4 at 20ºC: F1 (PEOT-PBT), F2 (65:35 PEOT-PBT: PLGA RG502) and F3 (65:35 PEOT-PBT: PLGA RG503).

Supplementary to section 3.5: Surface Hydrophobicity

Fig. S2. DSC thermogram of INF (Remicade®) in solution (PBS 10 mM, pH 7,2). Characteristic endothermic transitions attributed to the denatured variable domain of the protein (Fab) and the CH3 domain of the heavy chains were detected.

Supplementary to section 3.6: Differential Scanning Calorimetry

Fig. S3 DSC thermograms of microparticulate formulations fabricated by UA: Empty F1 (a), F1 (b), Empty F2 (c), F2 (d), Empty F3 (e), F3 (f).

Fig. S5 FTIR spectra of pure Infliximab (a), Polyactive® 1000PEOT70PBT30 (b), Resomer® RG502 (c), Resomer® RG503 (d), empty MCs (e, g, i) and INF-loaded MCs (f, h, j).

Fig. S4 DSC thermograms of Polyactive® 1000PEOT70PBT30 (a), Resomer® RG502 (b), Resomer® RG503 (c), Empty F4 (d), F4 (e), Empty F5 (f), F5 (g), Empty F6 (h), F6 (i).

Supplementary to section 3.7: Fourier Transform Infrared Spectroscopy

Fig. S6 SDS page electrophoresis under reducing (a, b) and non-reducing (c, d) conditions of INF standard (1a, 5b; 1c, 5d), Ultrasonic atomized infliximab (4b; 4d) and INF extracted from microparticulate formulations F1(1b; 1d), F2 (b2; d2),, F3 (b3; d3), F4 (a2, c2), F5 (a3, c3) and F6 (a4, c4).

Supplementary to section 3.9:	Structural stability of infliximab

- Supplementary to section 3.10:	Biological activity of microencapsulated INF

Fig.S7 Dose-response curve obtained for the neutralization of TNF-α produced by THP-1 macrophages after incubation with different concentrations of INF in solution.