PLGA-PEI nanoparticle covered with poly(I:C) for personalised cancer immunotherapy

Drug Delivery and Translational Research (DDTR)

Lorena Gonzalez-Melero1,2†, Edorta Santos-Vizcaino1,2,3†, Rubén Varela-Calvino4, Iria Gomez-Tourino5,6,  Aintzane Asumendi7,8, Maria Dolores Boyano7,8,  Manoli Igartua1,2,3*, Rosa Maria Hernandez1,2,3*

1NanoBioCel Research Group, Laboratory of Pharmaceutics, School of Pharmacy, University of the Basque Country (UPV/EHU), Vitoria-Gasteiz, Spain.

2Bioaraba, NanoBioCel Research Group, Vitoria-Gasteiz, Spain.

3Biomedical Research Networking Centre in Bioengineering, Biomaterials and Nanomedicine (CIBER-BBN). Institute of Health Carlos III, Madrid, Spain.

4Department of Biochemistry and Molecular Biology, School of Pharmacy, University of Santiago de Compostela, Santiago, Spain.

5Centre for Research in Molecular Medicine and Chronic Diseases (CiMUS), University of Santiago de Compostela, Santiago, Spain.

6Health Research Institute of Santiago de Compostela (IDIS), Santiago, Spain.

7Biocruces Bizkaia Health Research Institute, 48903 Barakaldo, Spain.

8Department of Cell Biology and Histology, Faculty of Medicine and Nursing, University of the Basque Country (UPV/EHU), 48940 Leioa, Spain.

*co-correspondings: rosa.hernandez@ehu.eus; manoli.igartua@ehu.eus

†These two authors contributed equally to this work.

Supplementary Table 1.  Mean NP size (Z-average diameter), polydispersity index (PDI) and Z-potential values for NPs covered at pH 4.6 with 0-350 µg/ml poly(I:C) shows high NP sizes and suboptimal PdI values.

| Formulation | Size (nm) | PdI | Zeta potential (mV) |
| --- | --- | --- | --- |
| NP PLGA PEI - pH 4,6 – 0 µg/ml poly(I:C) | 328,9 ± 1,4 | 0,309 ± 0,018 | 8,37 ± 0,17 |
| NP PLGA PEI - pH 4,6 - 150 µg/ml poly(I:C) | 2347,0 ± 388,38 | 0,855 ± 0,108 | -8,59 ± 0,04 |
| NP PLGA PEI - pH 4,6 - 250 µg/ml poly(I:C) | 772,3 ± 52,1 | 0,522 ± 0,066 | -19,70 ± 0,87 |
| NP PLGA PEI - pH 4,6 - 350 µg/ml poly(I:C) | 608,6 ± 47,69 | 0,407 ± 0,003 | -26,71 ± 0,36 |

Supplementary figure 1.  Representative flow cytometry plots from DCs after maturation with 5 µg/ml poly(I:C), NPpoly(I:C) and non-covered NPs.

Supplementary figure 2.  Representative flow cytometry plots from CD14- cells after maturation with        NPpoly(I:C) at 5 µg/ml poly(I:C).

Supplementary figure 3. Flow cytometry gating of PBMCs for the specific response studies of T cells.