Supplementary material
Supplementary material. Outcomes on Eudragit L100-55 mixture with plasticizers Triethyl citrate (TEC) or Polyethylene glycol (PEG) of low molecular weight (PEF 400)
	Ink name
	Eudragit L100-55
	TEC (%)
	PEG (%)
	Printing outcomes

	E1T1
	40
	60
	-
	Too fluid to shape

	E2T2
	50
	50
	-
	Too fluid to shape

	E2T3
	60
	40
	-
	Non extrudable

	E1P1
	40
	-
	60
	Too fluid to shape

	E1P2
	50
	-
	50
	Too fluid to shape

	E1P3
	60
	-
	40
	Too fluid to shape

	E1P4
	70
	-
	30
	Non extrudable
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