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Table S1. Design of experiments. Factors and responses evaluated.
	Experiment
	Ethanol (%)
	AmB (mg/ml)
	Implant Height (mm)
	Drug loading AmB
(%)

	1
	75
	5
	1
	0.203

	2
	75
	2.5
	1
	0.165

	3
	75
	2.5
	2
	0.098

	4
	85
	2.5
	2
	0.029

	5
	75
	5
	2
	0.213

	6
	85
	5
	1
	0.105

	7
	85
	5
	2
	0.036

	8
	85
	2.5
	1
	0.112
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Figure S1. 3D printed support for holding the implant in the drug loading experiments. 
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Figure S2. Receptacle specifically designed for the acetabular cup release experiments. Key: (a) Design and dimensions of the receptacle, front and top views, (b) Images of the 3D printed receptacle alone and with the acetabular cup.


image1.png




image2.png
£
®lg
H

HW





