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Figure S1. Raw mechanical testing data for ND, F1, F2 and F3 filaments.


[bookmark: OLE_LINK1]Table S1. One-way ANOVA for distance at break. 
	ANOVA table
	SS
	DF
	MS
	F (DFn, DFd)
	P value

	Treatment (between columns)
	13.43
	3
	4.477
	F (3, 16) = 5.616
	P=0.0080

	Residual (within columns)
	12.75
	16
	0.7971
	
	

	Total
	26.18
	19
	
	
	





Table S2. Tukey’s multiple comparisons test for distance at break.
	Tukey's multiple comparisons test
	Mean Diff.
	95 % CI
	Adjusted P Value

	ND vs. F1
	0.3308
	-1.285 to 1.946
	0.9349

	ND vs. F2
	-1.501
	-3.117 to 0.1141
	0.0733

	ND vs. F3
	-1.409
	-3.025 to 0.2061
	0.0988

	F1 vs. F2
	-1.832
	-3.448 to -0.2167
	0.0236

	F1 vs. F3
	-1.74
	-3.356 to -0.1247
	0.0326

	F2 vs. F3
	0.092
	-1.523 to 1.707
	0.9984
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Table S3. One-way ANOVA for force. 
	ANOVA table
	SS
	DF
	MS
	F (DFn, DFd)
	P value

	Treatment (between columns)
	77.36
	3
	25.79
	F (3, 16) = 20.08
	P<0.0001

	Residual (within columns)
	20.55
	16
	1.284
	
	

	Total
	97.91
	19
	
	
	




Table S4. Tukey’s multiple comparisons test for force.
	Tukey's multiple comparisons test
	Mean Diff.
	95 % CI
	Adjusted P Value

	ND vs. F1
	2.58
	0.5294 to 4.631
	0.0116

	ND vs. F2
	-2.62
	-4.671 to -0.5694
	0.0103

	ND vs. F3
	1.6
	-0.4506 to 3.651
	0.1567

	F1 vs. F2
	-5.2
	-7.251 to -3.149
	<0.0001

	F1 vs. F3
	-0.98
	-3.031 to 1.071
	0.5362

	F2 vs. F3
	4.22
	2.169 to 6.271
	0.0001




Table S5. Two-way ANOVA for drug release.
	ANOVA table
	SS
	DF
	MS
	F (DFn, DFd)
	P value

	    Interaction
	811.8
	18
	45.1
	F (18, 30) = 2.920
	P=0.0046

	    Row Factor
	4847
	9
	538.6
	F (9, 30) = 34.87
	P<0.0001

	    Column Factor
	34805
	2
	17403
	F (2, 30) = 1127
	P<0.0001

	    Residual
	463.4
	30
	15.45
	 
	 






Table S6. Tukey’s multiple comparisons test between formulations at each dissolution sampling timepoint. 
	Tukey's multiple comparisons test
	Mean Diff.
	95.00% CI of diff.
	Adjusted P Value

	
	
	
	

	  F1
	 
	 
	 

	    5 vs. 10
	0
	-13.41 to 13.41
	>0.9999

	    5 vs. 15
	-1.122
	-14.53 to 12.29
	>0.9999

	    5 vs. 30
	-2.704
	-16.11 to 10.70
	0.9994

	    5 vs. 45
	-3.913
	-17.32 to 9.494
	0.9903

	    5 vs. 60
	-5.37
	-18.78 to 8.037
	0.9281

	    5 vs. 90
	-7.391
	-20.80 to 6.016
	0.6812

	    5 vs. 120
	-10.41
	-23.82 to 2.997
	0.2397

	    5 vs. 240
	-17.14
	-30.54 to -3.728
	0.0047

	    5 vs. 360
	-24.69
	-38.10 to -11.29
	<0.0001

	    10 vs. 15
	-1.122
	-14.53 to 12.29
	>0.9999

	    10 vs. 30
	-2.704
	-16.11 to 10.70
	0.9994

	    10 vs. 45
	-3.913
	-17.32 to 9.494
	0.9903

	    10 vs. 60
	-5.37
	-18.78 to 8.037
	0.9281

	    10 vs. 90
	-7.391
	-20.80 to 6.016
	0.6812

	    10 vs. 120
	-10.41
	-23.82 to 2.997
	0.2397

	    10 vs. 240
	-17.14
	-30.54 to -3.728
	0.0047

	    10 vs. 360
	-24.69
	-38.10 to -11.29
	<0.0001

	    15 vs. 30
	-1.582
	-14.99 to 11.83
	>0.9999

	    15 vs. 45
	-2.791
	-16.20 to 10.62
	0.9992

	    15 vs. 60
	-4.249
	-17.66 to 9.158
	0.983

	    15 vs. 90
	-6.269
	-19.68 to 7.138
	0.8402

	    15 vs. 120
	-9.288
	-22.70 to 4.119
	0.3811

	    15 vs. 240
	-16.01
	-29.42 to -2.606
	0.0099

	    15 vs. 360
	-23.57
	-36.98 to -10.16
	<0.0001

	    30 vs. 45
	-1.209
	-14.62 to 12.20
	>0.9999

	    30 vs. 60
	-2.667
	-16.07 to 10.74
	0.9995

	    30 vs. 90
	-4.687
	-18.09 to 8.720
	0.9679

	    30 vs. 120
	-7.706
	-21.11 to 5.701
	0.6306

	    30 vs. 240
	-14.43
	-27.84 to -1.024
	0.027

	    30 vs. 360
	-21.99
	-35.40 to -8.582
	0.0002

	    45 vs. 60
	-1.457
	-14.86 to 11.95
	>0.9999

	    45 vs. 90
	-3.478
	-16.89 to 9.929
	0.9958

	    45 vs. 120
	-6.497
	-19.90 to 6.910
	0.8117

	    45 vs. 240
	-13.22
	-26.63 to 0.1851
	0.0557

	    45 vs. 360
	-20.78
	-34.19 to -7.372
	0.0004

	    60 vs. 90
	-2.021
	-15.43 to 11.39
	>0.9999

	    60 vs. 120
	-5.039
	-18.45 to 8.368
	0.9502

	    60 vs. 240
	-11.76
	-25.17 to 1.642
	0.1242

	    60 vs. 360
	-19.32
	-32.73 to -5.915
	0.0011

	    90 vs. 120
	-3.019
	-16.43 to 10.39
	0.9986

	    90 vs. 240
	-9.744
	-23.15 to 3.663
	0.3188

	    90 vs. 360
	-17.3
	-30.71 to -3.894
	0.0042

	    120 vs. 240
	-6.725
	-20.13 to 6.682
	0.7809

	    120 vs. 360
	-14.28
	-27.69 to -0.8757
	0.0296

	    240 vs. 360
	-7.557
	-20.96 to 5.850
	0.6547

	
	
	
	

	  F2
	 
	 
	 

	    5 vs. 10
	0
	-13.41 to 13.41
	>0.9999

	    5 vs. 15
	-1.225
	-14.63 to 12.18
	>0.9999

	    5 vs. 30
	-5.165
	-18.57 to 8.242
	0.9424

	    5 vs. 45
	-7.595
	-21.00 to 5.812
	0.6486

	    5 vs. 60
	-10.92
	-24.32 to 2.491
	0.1896

	    5 vs. 90
	-16.04
	-29.44 to -2.630
	0.0097

	    5 vs. 120
	-19.32
	-32.73 to -5.912
	0.0011

	    5 vs. 240
	-27.88
	-41.29 to -14.48
	<0.0001

	    5 vs. 360
	-29.36
	-42.77 to -15.96
	<0.0001

	    10 vs. 15
	-1.225
	-14.63 to 12.18
	>0.9999

	    10 vs. 30
	-5.165
	-18.57 to 8.242
	0.9424

	    10 vs. 45
	-7.595
	-21.00 to 5.812
	0.6486

	    10 vs. 60
	-10.92
	-24.32 to 2.491
	0.1896

	    10 vs. 90
	-16.04
	-29.44 to -2.630
	0.0097

	    10 vs. 120
	-19.32
	-32.73 to -5.912
	0.0011

	    10 vs. 240
	-27.88
	-41.29 to -14.48
	<0.0001

	    10 vs. 360
	-29.36
	-42.77 to -15.96
	<0.0001

	    15 vs. 30
	-3.94
	-17.35 to 9.467
	0.9898

	    15 vs. 45
	-6.37
	-19.78 to 7.037
	0.8279

	    15 vs. 60
	-9.691
	-23.10 to 3.716
	0.3256

	    15 vs. 90
	-14.81
	-28.22 to -1.405
	0.0213

	    15 vs. 120
	-18.09
	-31.50 to -4.687
	0.0025

	    15 vs. 240
	-26.66
	-40.07 to -13.25
	<0.0001

	    15 vs. 360
	-28.14
	-41.54 to -14.73
	<0.0001

	    30 vs. 45
	-2.43
	-15.84 to 10.98
	0.9997

	    30 vs. 60
	-5.751
	-19.16 to 7.656
	0.8959

	    30 vs. 90
	-10.87
	-24.28 to 2.535
	0.1936

	    30 vs. 120
	-14.15
	-27.56 to -0.7464
	0.032

	    30 vs. 240
	-22.72
	-36.13 to -9.312
	<0.0001

	    30 vs. 360
	-24.2
	-37.60 to -10.79
	<0.0001

	    45 vs. 60
	-3.322
	-16.73 to 10.09
	0.997

	    45 vs. 90
	-8.443
	-21.85 to 4.965
	0.5107

	    45 vs. 120
	-11.72
	-25.13 to 1.683
	0.1268

	    45 vs. 240
	-20.29
	-33.70 to -6.882
	0.0005

	    45 vs. 360
	-21.77
	-35.18 to -8.361
	0.0002

	    60 vs. 90
	-5.121
	-18.53 to 8.286
	0.9452

	    60 vs. 120
	-8.402
	-21.81 to 5.005
	0.5172

	    60 vs. 240
	-16.97
	-30.37 to -3.560
	0.0053

	    60 vs. 360
	-18.45
	-31.85 to -5.039
	0.0019

	    90 vs. 120
	-3.281
	-16.69 to 10.13
	0.9973

	    90 vs. 240
	-11.85
	-25.25 to 1.560
	0.119

	    90 vs. 360
	-13.33
	-26.73 to 0.08184
	0.0524

	    120 vs. 240
	-8.565
	-21.97 to 4.842
	0.4911

	    120 vs. 360
	-10.04
	-23.45 to 3.363
	0.2813

	    240 vs. 360
	-1.479
	-14.89 to 11.93
	>0.9999

	
	
	
	

	  ASD Tablet 
	 
	 
	 

	    5 vs. 10
	-9.163
	-22.57 to 4.245
	0.3994

	    5 vs. 15
	-19.54
	-32.94 to -6.129
	0.0009

	    5 vs. 30
	-26.46
	-39.86 to -13.05
	<0.0001

	    5 vs. 45
	-26.86
	-40.27 to -13.46
	<0.0001

	    5 vs. 60
	-29.47
	-42.87 to -16.06
	<0.0001

	    5 vs. 90
	-27.34
	-40.75 to -13.94
	<0.0001

	    5 vs. 120
	-33.52
	-46.93 to -20.11
	<0.0001

	    5 vs. 240
	-33.67
	-47.07 to -20.26
	<0.0001

	    5 vs. 360
	-33.48
	-46.88 to -20.07
	<0.0001

	    10 vs. 15
	-10.37
	-23.78 to 3.034
	0.2437

	    10 vs. 30
	-17.29
	-30.70 to -3.886
	0.0042

	    10 vs. 45
	-17.7
	-31.11 to -4.295
	0.0032

	    10 vs. 60
	-20.3
	-33.71 to -6.897
	0.0005

	    10 vs. 90
	-18.18
	-31.59 to -4.772
	0.0023

	    10 vs. 120
	-24.36
	-37.76 to -10.95
	<0.0001

	    10 vs. 240
	-24.5
	-37.91 to -11.10
	<0.0001

	    10 vs. 360
	-24.31
	-37.72 to -10.91
	<0.0001

	    15 vs. 30
	-6.92
	-20.33 to 6.487
	0.753

	    15 vs. 45
	-7.329
	-20.74 to 6.079
	0.691

	    15 vs. 60
	-9.931
	-23.34 to 3.476
	0.2951

	    15 vs. 90
	-7.806
	-21.21 to 5.601
	0.6143

	    15 vs. 120
	-13.98
	-27.39 to -0.5771
	0.0355

	    15 vs. 240
	-14.13
	-27.54 to -0.7241
	0.0325

	    15 vs. 360
	-13.94
	-27.35 to -0.5333
	0.0364

	    30 vs. 45
	-0.4083
	-13.82 to 13.00
	>0.9999

	    30 vs. 60
	-3.011
	-16.42 to 10.40
	0.9986

	    30 vs. 90
	-0.8862
	-14.29 to 12.52
	>0.9999

	    30 vs. 120
	-7.064
	-20.47 to 6.343
	0.7317

	    30 vs. 240
	-7.211
	-20.62 to 6.196
	0.7093

	    30 vs. 360
	-7.02
	-20.43 to 6.387
	0.7383

	    45 vs. 60
	-2.603
	-16.01 to 10.80
	0.9996

	    45 vs. 90
	-0.4779
	-13.89 to 12.93
	>0.9999

	    45 vs. 120
	-6.656
	-20.06 to 6.751
	0.7905

	    45 vs. 240
	-6.803
	-20.21 to 6.604
	0.77

	    45 vs. 360
	-6.612
	-20.02 to 6.795
	0.7964

	    60 vs. 90
	2.125
	-11.28 to 15.53
	>0.9999

	    60 vs. 120
	-4.053
	-17.46 to 9.354
	0.9877

	    60 vs. 240
	-4.2
	-17.61 to 9.207
	0.9843

	    60 vs. 360
	-4.009
	-17.42 to 9.398
	0.9885

	    90 vs. 120
	-6.178
	-19.58 to 7.229
	0.851

	    90 vs. 240
	-6.325
	-19.73 to 7.082
	0.8335

	    90 vs. 360
	-6.134
	-19.54 to 7.273
	0.856

	    120 vs. 240
	-0.147
	-13.55 to 13.26
	>0.9999

	    120 vs. 360
	0.04376
	-13.36 to 13.45
	>0.9999

	    240 vs. 360
	0.1907
	-13.22 to 13.60
	>0.9999
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