# High Resolution Mass Spectrometry of Polyfluorinated Polyether – based Formulation

# Ian Ken Dimzon,  Xenia Trier, Tobias Frömel, Rick Helmus,

# Thomas P. Knepper and Pim de Voogt

Supplementary Information

Supplementary Information 1

Higher-order mass defect calculation

SI 1a Higher-order mass transformation of selected accurate masses from the mass spectrum of PFPE formulation.

| Accurate Mass, M0 (1) | Relative Intensity (2) | Relation to m/z 1176.9994 |  |  | 1st Order Transformation |  |  | 2nd Order Transformation |  |  | 3rd Order Transformation |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | -C2H4O- (3) | -C2F4O- (4) | -CF2O- (5) | M1 (6) | round(M1,0) (7) | MD1 (8) | M2 (9) | round(M2,0) (10) | MD2 (11) | M3 (12) | round (M3, 0) (13) | MD3 (14) |
| 1176.9994 | 100.0 |  |  |  | 1176.2990 | 1176 | 0.2990 | 3.7130 | 4 | 0.2870 | 0.7018 | 1 | 0.2982 |
| 1088.9465 | 79.5 | -2 |  |  | 1088.2985 | 1088 | 0.2985 | 3.7068 | 4 | 0.2932 | 0.7170 | 1 | 0.2830 |
| 1132.9731 | 78.4 | -1 |  |  | 1132.2989 | 1132 | 0.2989 | 3.7117 | 4 | 0.2883 | 0.7048 | 1 | 0.2952 |
| 1221.0259 | 78.0 | +1 |  |  | 1220.2993 | 1220 | 0.2993 | 3.7167 | 4 | 0.2833 | 0.6927 | 1 | 0.3073 |
| 1265.0523 | 77.9 | +2 |  |  | 1264.2995 | 1264 | 0.2995 | 3.7192 | 4 | 0.2808 | 0.6866 | 1 | 0.3134 |
| 1309.0776 | 76.8 | +3 |  |  | 1308.2986 | 1308 | 0.2986 | 3.7080 | 4 | 0.2920 | 0.7140 | 1 | 0.2860 |
| 945.0236 | 95.4 |  | -2 |  | 944.4612 | 944 | 0.4612 | 5.7280 | 6 | 0.2720 | 0.6651 | 1 | 0.3349 |
| 1061.0114 | 87.0 |  | -1 |  | 1060.3800 | 1060 | 0.3800 | 4.7192 | 5 | 0.2808 | 0.6865 | 1 | 0.3135 |
| 1292.9885 | 85.8 |  | +1 |  | 1292.2190 | 1292 | 0.2190 | 2.7203 | 3 | 0.2797 | 0.6837 | 1 | 0.3163 |
| 1408.9769 | 85.2 |  | +2 |  | 1408.1384 | 1408 | 0.1384 | 1.7190 | 2 | 0.2810 | 0.6869 | 1 | 0.3131 |
| 1045.0156 | 75.6 |  |  | -2 | 1044.3937 | 1044 | 0.3937 | 4.8896 | 5 | 0.1104 | 0.2699 | 0 | 0.2699 |
| 1111.0076 | 74.8 |  |  | -1 | 1110.3464 | 1110 | 0.3464 | 4.3025 | 4 | 0.3025 | 0.7397 | 1 | 0.2603 |
| 1242.9915 | 72.6 |  |  | +1 | 1242.2518 | 1242 | 0.2518 | 3.1271 | 3 | 0.1271 | 0.3108 | 0 | 0.3108 |
| 1308.9835 | 71.2 |  |  | +2 | 1308.2045 | 1308 | 0.2045 | 2.5400 | 2 | 0.5400 | 1.3204 | 1 | 0.3204 |
| Standard deviation of shaded MD |  |  |  |  |  |  | 0.008 |  |  | 0.012 |  |  | 0.020 |

SI 1b Higher-order mass transformation of the selected exact masses of the repeating unit

| Repeating Units | Order | Exact Mass | M1 | round(M1,0) | MD1 | M2 | round(M2,0) | MD2 | M3 | round(M3,0) | MD3 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| -C2H4O- | 1 | 44.0262 | 44.0000 | 44 | 0.00000 | 0.0000 | 0 | 0.0000 | 0 | 0 | 0.0000 |
| -C2F4O- | 2 | 115.9885 | 115.9195 | 116 | 0.08052 | 1.0001 | 1 | 0.0001 | 0.0001 | 0 | 0.0001 |
| -CF2O- | 3 | 65.9917 | 65.9524 | 66 | 0.04757 | 0.5910 | 1 | 0.4090 | 1.0001 | 1 | 0.0001 |

Steps in the calculation of higher-order mass defects used in this study and the generation of the different MD graphs.

1. Accurate masses and their corresponding relative intensities were extracted from the mass spectrum of PFPE formulation (Columns 1 and 2 in SI1a).

2. It was decided that the transformations will be in the following order of the bases (repeating units): -C2H4O-, -C2F4O-, and -CF2O-.

3.  First order transformation (based on the -C2H4O- repeating units):  M0 was multiplied by the ratio 44/44.0262 to obtain M1 (See SI1b). The nominal M1 was obtained by rounding off M1 to the nearest ones.

MD1 = M1 - nominal M1

4. Second order transformation (based on the -C2F4O- repeating units): M2 was calculated by dividing MD1 by the MD1 of -C2F4O- (0.08052). The nominal M2 was obtained by rounding off M2 to the nearest ones.

MD2 = M2 - nominal M2

5. Third order transformation (based on the -CF2O- repeating units): M3 was calculated by dividing MD2 by the MD2 of -CF2O- (0.4090). The nominal M3 was obtained by rounding off M3 to the nearest ones.

MD3 = M3 - nominal M3

6. Different graphs can be generated using SI1a, for example, nominal M0 vs MD1; MD1 vs MD2; etc. The relative intensities can be added in the graph as a third dimension (e.g. size of the points).

Supplementary Information 2

Sample MSn mass spectra of m/z 1176.999.

SI 2a Fragmentation of m/z 1176.9 as precursor ion in the HCD at a normalized collision energy of 25%; recorded in the FTMS mode

SI 2b MS3 with the following precursor ions: 1176.9  1079.0 m/z in the CID at a normalized collision energies of 23% and 20% respectively; recorded in the FTMS mode

SI 2c MS4 with the following precursor ions: 1176.9  990.9  970.9 m/z in the CID at a normalized collision energies of 23%, 20% and 20% respectively; recorded in the ITMS mode

Supplementary Information 3

Summary of fragmentation of some major ions selected by data-dependent acquisition

| Precursor Ion (m/z) (1) | Relation to m/z 1177 |  |  |  | Observed Fragment Ions (m/z) |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | -C2H4O- (2) | -C2F4O- (3) | -CF2- (4) | difference from m/z 1177 (5) | Neutral Loss of 18 m/z (6) | Neutral Loss of 98 m/z (7) | Series of 44 m/z losses starting from the m/z in column (7) (8) |
| 945 |  | -2 |  | -232 | 927 | 847 | 803; 759; 715 |
| 1017 | -1 | -1 |  | -160 | 999 | 919 | 875; 831; 787 |
| 1061 |  | -1 |  | -116 | 1043 | 963 | 919; 875; 831; |
| 1105 | +1 | -1 |  | -72 | 1087 | 1007 | 963; 919; 875; 831 |
| 1111 |  | -1 | +1 | -66 | 1093 | 1013 | 969; 925; 881 |
| 1127 |  |  | -1 | -50 | 1109 | 1029 | - |
| 1133 | -1 |  |  | -44 | 1115 | 1035 | 991; 947 |
| 1155 | +1 | -1 | +1 | -22 | - | 1057 | 1013; 969; 925 |
| 1177 |  |  |  | 0 | 1159 | 1079 | 1035; 991; 947 |
| 1227 |  |  | +1 | 50 | - | 1129 | - |