Supplementary Information (SI)

Inkjet Printed Quantum Dots Color Conversion Layers for Full-color Micro-LED Displays

Feng Qin1, 2, ‡, Cao Liu2, *, ‡, Wenhui Wu2, Wenxiang Peng2, Sitao Huo2, Jiandong Ye1 and Shulin Gu1, *

1 School of Electronic Science & Engineering, Nanjing University, Nanjing 210023, China;

2 Shanghai Tianma Microelectronics Co., Ltd, Shanghai 201201, China;

* Correspondence: cao_liu1@tianma.cn; slgu@nju.edu.cn

‡ These authors contributed equally to this work.

Fig. S1 a The schematic diagram of crosstalk source in QDCC LED; b Transmittance spectrum of gray bank material with 10 μm thickness. Inset show the SEM image of bank material introducing the scattering particle and the tested transmission value for 10 μm thick bank and the calculated value for 20 μm thick bank.

Table S1 The summaries of specific light leakage ratio for scheme (a) and (b) devices.

| Items | R-screen |  |  | G-screen |  |  | B-screen |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Color | R | G | B | R | G | B | R | G | B |
| Scheme (a) distribution | 81.03% | 13.72% | 5.24% | 2.79% | 83.95% | 13.26% | 1.92% | 9.52% | 88.57% |
| Scheme (b) distribution | 98.66% | 1.02% | 0.32% | 0.72% | 92.13% | 7.15% | 0.63% | 6.71% | 92.66% |

Fig. S2 The luminescence spectra of blue backlight with long and short wavelength BLED (467 nm and 455 nm).

Table S2 The summaries of specific light leakage ratio for 467 nm and 455 nm BLED backlights.

| Items | R-screen |  |  | G-screen |  |  | B-screen |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Color | R | G | B | R | G | B | R | G | B |
| BLED (467nm) distribution | 98.66% | 1.02% | 0.32% | 0.72% | 92.13% | 7.15% | 0.63% | 6.71% | 92.66% |
| BLED (455nm) distribution | 99.48% | 0.44% | 0.09% | 0.35% | 96.02% | 3.63% | 0.33% | 4.49% | 95.18% |

Table S3 The performance summaries of QDCC devices with 467 nm and 455 nm BLED backlights.

| Items |  | BLED (467nm) |  | BLED (455nm) |  |
| --- | --- | --- | --- | --- | --- |
| Color coordinates | R | 0.6894 | 0.2986 | 0.6951 | 0.2997 |
|  | G | 0.1651 | 0.5871 | 0.166 | 0.6635 |
|  | B | 0.136 | 0.0504 | 0.1446 | 0.0352 |
| NTSC |  | 91.59% |  | 107.53% |  |

Fig. S3 a The SEM image of G-QDs and the first layer bank after the second layer bank and partial CVD encapsulation layer were stripped. b The peak position of blue Micro LED variation with the temperature rising from 0 to 80 ℃.