Supplementary Material

Impact of Hydrothermal Carbonization on Combustion Properties of Residual Biomass

Lynn Hansen,* Sebastian Fendt,* Hartmut Spliethoff*,†

*Chair of Energy Systems, Technical University of Munich, Boltzmannstraße 15, 85748 Garching, Germany

†ZAE Bayern, Walther-Meißner-Straße 6, 85748 Garching, Germany

E-Mail: lynn.hansen@tum.de

Table S 1: Mass yield, proximate and ultimate analysis of raw feedstock and HTC treated feedstock at different temperatures for a residence time of 0.5 h. 
All values are reported on dry basis.

| Biomass type | HTC conditions | LHV / MJ kg-1 | Mass yield / - | Energy yield / - | Ash content / wt.-% | Volatiles / wt.-% | Fixed-C / wt.-% | C / wt.-% | H / wt.-% | N / wt.-% | S / wt.-% | O / wt.-% | Cl / wt.-% | Molar 2 S/Cl ratio |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| digestate | HTC 180 °C | 19.16 | 0.74 | 0.80 | 9.15 | 77.79 | 13.06 | 51.86 | 5.52 | 1.19 | 0.14 | 32.14 | 0.20 | 1.27 |
|  | HTC 210 °C | 20.63 | 0.67 | 0.78 | 8.70 | 73.69 | 17.61 | 54.97 | 5.35 | 1.51 | 0.15 | 29.31 | 0.22 | 1.24 |
|  | HTC 240 °C | 22.42 | 0.55 | 0.69 | 10.41 | 68.30 | 21.29 | 58.88 | 5.17 | 1.86 | 0.16 | 23.52 | 0.15 | 1.94 |
|  | HTC 270 °C | 26.53 | 0.44 | 0.66 | 14.93 | 60.12 | 24.95 | 67.04 | 5.13 | 2.56 | 0.19 | 10.15 | 0.11 | 3.13 |
| empty fruit bunches | HTC 180 °C | 18.91 | 0.72 | 0.71 | 7.57 | 80.72 | 11.71 | 55.20 | 6.12 | 0.83 | 0.11 | 30.17 | 0.16 | 1.25 |
|  | HTC 210 °C | 21.67 | 0.63 | 0.71 | 6.97 | 76.30 | 16.72 | 59.53 | 6.31 | 0.89 | 0.12 | 26.18 | 0.16 | 1.36 |
|  | HTC 240 °C | 24.86 | 0.56 | 0.73 | 7.60 | 72.88 | 19.52 | 62.33 | 6.30 | 1.01 | 0.13 | 22.64 | 0.12 | 1.97 |
|  | HTC 270 °C | 28.36 | 0.42 | 0.62 | 8.58 | 68.85 | 22.57 | 68.68 | 6.66 | 1.29 | 0.13 | 14.66 | 0.04 | 5.90 |
| lawn cuttings | HTC 180 °C | 21.47 | 0.56 | 0.70 | 10.00 | 68.78 | 21.22 | 55.87 | 5.93 | 2.31 | 0.15 | 25.73 | 0.08 | 3.40 |
|  | HTC 210 °C | 20.72 | 0.55 | 0.67 | 16.58 | 63.13 | 20.29 | 54.86 | 5.43 | 2.04 | 0.15 | 20.94 | 0.11 | 2.47 |
|  | HTC 240 °C | 20.96 | 0.50 | 0.61 | 18.07 | 60.15 | 21.78 | 56.24 | 5.47 | 2.15 | 0.15 | 17.93 | 0.07 | 3.89 |
|  | HTC 270 °C | 23.85 | 0.42 | 0.59 | 20.13 | 56.46 | 23.40 | 58.21 | 5.39 | 2.38 | 0.16 | 13.73 | 0.05 | 5.81 |
| olive pomace | HTC 180 °C | 22.51 | 0.67 | 0.73 | 0.60 | 81.66 | 17.74 | 58.30 | 6.35 | 0.38 | 0.09 | 34.29 | 0.14 | 1.17 |
|  | HTC 210 °C | 24.57 | 0.63 | 0.75 | 0.79 | 77.67 | 21.54 | 63.32 | 6.61 | 0.46 | 0.09 | 28.73 | 0.13 | 1.26 |
|  | HTC 240 °C | 26.58 | 0.57 | 0.73 | 0.60 | 72.41 | 26.99 | 67.98 | 6.76 | 0.51 | 0.09 | 24.05 | 0.13 | 1.26 |
|  | HTC 270 °C | 31.16 | 0.46 | 0.69 | 0.84 | 61.05 | 38.11 | 78.85 | 7.19 | 0.64 | 0.10 | 12.38 | 0.15 | 1.21 |
| sewage sludge | HTC 180 °C | 14.84 | 0.73 | 0.71 | 39.78 | 58.91 | 1.31 | 36.11 | 3.99 | 4.68 | 0.37 | 15.08 | 0.26 | 2.58 |
|  | HTC 210 °C | 13.88 | 0.56 | 0.51 | 51.85 | 49.89 | 0.00 | 33.90 | 3.74 | 2.96 | 0.35 | 7.20 | 0.16 | 3.97 |
|  | HTC 240 °C | 13.88 | 0.54 | 0.49 | 53.75 | 45.91 | 0.34 | 32.84 | 3.47 | 2.45 | 0.34 | 7.15 | 0.16 | 3.86 |
|  | HTC 270 °C | 13.73 | 0.50 | 0.45 | 57.47 | 41.97 | 0.56 | 32.79 | 3.25 | 2.27 | 0.33 | 3.90 | 0.16 | 3.74 |
| spruce bark | HTC 180 °C | 21.11 | 0.70 | 0.77 | 3.49 | 72.93 | 23.58 | 59.29 | 5.66 | 0.43 | 0.07 | 31.06 | ND | ND |
|  | HTC 210 °C | 22.36 | 0.67 | 0.78 | 3.26 | 69.19 | 27.55 | 61.89 | 5.37 | 0.44 | 0.07 | 28.97 | ND | ND |
|  | HTC 240 °C | 23.79 | 0.60 | 0.75 | 3.59 | 65.44 | 30.97 | 65.03 | 5.23 | 0.44 | 0.07 | 25.64 | ND | ND |
|  | HTC 270 °C | 27.66 | 0.48 | 0.69 | 3.63 | 54.95 | 41.41 | 72.95 | 5.06 | 0.54 | 0.08 | 17.74 | ND | ND |
| wheat straw | HTC 180 °C | 17.28 | 0.78 | 0.82 | 11.22 | 76.58 | 12.19 | 47.87 | 4.97 | 0.53 | 0.09 | 35.33 | 0.17 | 0.96 |
|  | HTC 210 °C | 18.73 | 0.64 | 0.73 | 13.36 | 70.27 | 16.36 | 50.80 | 5.00 | 0.50 | 0.08 | 30.26 | 0.15 | 0.97 |
|  | HTC 240 °C | 20.47 | 0.57 | 0.71 | 14.38 | 64.18 | 21.43 | 54.73 | 4.93 | 0.60 | 0.08 | 25.28 | 0.15 | 0.97 |
|  | HTC 270 °C | 24.03 | 0.44 | 0.64 | 17.45 | 51.38 | 31.17 | 62.38 | 4.75 | 0.79 | 0.08 | 14.55 | ND | ND |

*ND: below detection limit

Table S 2: Mass yield, proximate and ultimate analysis of raw feedstock and HTC treated feedstock at different temperatures for a residence time of 4 h. 
All values are reported on dry basis.

| Biomass type | HTC conditions | LHV / MJ kg-1 | Mass yield / - | Energy yield / - | Ash content / wt.-% | Volatiles / wt.-% | Fixed-C / wt.-% | C / wt.-% | H / wt.-% | N / wt.-% | S / wt.-% | O / wt.-% | Cl / wt.-% | Molar 2 S/Cl ratio |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| digestate | HTC 180 °C | 20.00 | 0.71 | 0.80 | 8.84 | 74.66 | 16.50 | 53.56 | 5.52 | 1.19 | 0.14 | 32.14 | 0.20 | 1.27 |
|  | HTC 210 °C | 21.47 | 0.63 | 0.76 | 8.42 | 70.58 | 21.00 | 57.21 | 5.35 | 1.51 | 0.15 | 29.31 | 0.22 | 1.24 |
|  | HTC 240 °C | 25.94 | 0.46 | 0.67 | 12.11 | 60.78 | 27.11 | 65.85 | 5.17 | 1.86 | 0.16 | 23.52 | 0.15 | 1.94 |
|  | HTC 270 °C | 26.73 | 0.40 | 0.60 | 15.68 | 54.74 | 29.58 | 67.28 | 5.13 | 2.56 | 0.19 | 10.15 | 0.11 | 3.13 |
| empty fruit bunches | HTC 180 °C | 21.65 | 0.67 | 0.76 | 6.95 | 78.96 | 14.08 | 56.54 | 6.12 | 0.83 | 0.11 | 30.17 | 0.16 | 1.25 |
|  | HTC 210 °C | 23.00 | 0.60 | 0.72 | 6.84 | 74.40 | 18.77 | 59.52 | 6.31 | 0.89 | 0.12 | 26.18 | 0.16 | 1.36 |
|  | HTC 240 °C | 28.95 | 0.51 | 0.77 | 7.74 | 63.21 | 29.05 | 71.24 | 6.30 | 1.01 | 0.13 | 22.64 | 0.12 | 1.97 |
|  | HTC 270 °C | 26.29 | 0.38 | 0.52 | 7.69 | 67.36 | 24.94 | 66.56 | 6.66 | 1.29 | 0.13 | 14.66 | 0.04 | 5.90 |
| lawn cuttings | HTC 180 °C | 19.93 | 0.64 | 0.75 | 17.84 | 61.58 | 20.57 | 53.28 | 5.93 | 2.31 | 0.15 | 25.73 | 0.08 | 3.40 |
|  | HTC 210 °C | 21.29 | 0.53 | 0.66 | 17.03 | 61.51 | 21.47 | 55.34 | 5.43 | 2.04 | 0.15 | 20.94 | 0.11 | 2.47 |
|  | HTC 240 °C | 23.33 | 0.47 | 0.64 | 20.57 | 56.55 | 22.88 | 58.85 | 5.47 | 2.15 | 0.15 | 17.93 | 0.07 | 3.89 |
|  | HTC 270 °C | 26.07 | 0.37 | 0.56 | 21.81 | 53.26 | 24.93 | 63.18 | 5.39 | 2.38 | 0.16 | 13.73 | 0.05 | 5.81 |
| olive pomace | HTC 180 °C | 23.40 | 0.65 | 0.74 | 0.64 | 78.55 | 20.81 | 61.55 | 6.35 | 0.38 | 0.09 | 34.29 | 0.14 | 1.17 |
|  | HTC 210 °C | 25.31 | 0.62 | 0.76 | 0.63 | 74.00 | 25.37 | 65.75 | 6.61 | 0.46 | 0.09 | 28.73 | 0.13 | 1.26 |
|  | HTC 240 °C | 27.94 | 0.52 | 0.70 | 0.58 | 65.11 | 34.31 | 71.61 | 6.76 | 0.51 | 0.09 | 24.05 | 0.13 | 1.26 |
|  | HTC 270 °C | 30.69 | 0.46 | 0.68 | 0.90 | 58.92 | 40.18 | 77.65 | 7.19 | 0.64 | 0.10 | 12.38 | 0.15 | 1.21 |
| sewage sludge | HTC 180 °C | 14.39 | 0.59 | 0.55 | 48.13 | 52.81 | -0.94 | 34.54 | 3.99 | 4.68 | 0.37 | 15.08 | 0.26 | 2.58 |
|  | HTC 210 °C | 13.68 | 0.54 | 0.48 | 52.36 | 47.39 | 0.25 | 32.96 | 3.74 | 2.96 | 0.35 | 7.20 | 0.16 | 3.97 |
|  | HTC 240 °C | 13.95 | 0.52 | 0.47 | 55.18 | 44.08 | 0.74 | 32.53 | 3.47 | 2.45 | 0.34 | 7.15 | 0.16 | 3.86 |
|  | HTC 270 °C | 14.04 | 0.50 | 0.46 | 57.58 | 41.07 | 1.35 | 31.38 | 3.25 | 2.27 | 0.33 | 3.90 | 0.16 | 3.74 |
| spruce bark | HTC 180 °C | 21.11 | 0.70 | 0.77 | 3.28 | 69.61 | 27.10 | 60.37 | 5.66 | 0.43 | 0.07 | 31.06 | ND | ND |
|  | HTC 210 °C | 22.46 | 0.67 | 0.79 | 3.44 | 66.80 | 29.76 | 63.09 | 5.37 | 0.44 | 0.07 | 28.97 | ND | ND |
|  | HTC 240 °C | 25.34 | 0.54 | 0.72 | 3.81 | 57.54 | 38.65 | 70.20 | 5.23 | 0.44 | 0.07 | 25.64 | ND | ND |
|  | HTC 270 °C | 28.62 | 0.47 | 0.70 | 3.28 | 52.16 | 44.55 | 75.95 | 5.06 | 0.54 | 0.08 | 17.74 | ND | ND |
| wheat straw | HTC 180 °C | 18.46 | 0.69 | 0.78 | 13.17 | 73.59 | 13.25 | 50.34 | 4.97 | 0.53 | 0.09 | 35.33 | 0.17 | 0.96 |
|  | HTC 210 °C | 19.32 | 0.62 | 0.73 | 13.26 | 67.23 | 19.50 | 52.58 | 5.00 | 0.50 | 0.08 | 30.26 | 0.15 | 0.97 |
|  | HTC 240 °C | 23.09 | 0.47 | 0.66 | 16.40 | 52.82 | 30.78 | 60.54 | 4.93 | 0.60 | 0.08 | 25.28 | 0.15 | 0.97 |
|  | HTC 270 °C | 24.85 | 0.43 | 0.65 | 17.49 | 49.19 | 33.32 | 64.54 | 4.75 | 0.79 | 0.08 | 14.55 | ND | ND |

*ND: below detection limit

Table S 3. Elemental ash analysis, ash content and mass yield of untreated digestate and digestate treated by HTC at different temperatures and residence times.

| Feedstock | Condition | Ash Content / wt.-% | Mass Yield / - | Na2O / wt.-% | MgO / wt.-% | Al2O3 / wt.-% | SiO2 / wt.-% | P2O5 / wt.-% | SO3 / wt.-% | K2O / wt.-% | CaO / wt.-% | TiO2 / wt.-% | Fe2O3 / wt.-% | ZnO / wt.-% |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| digestate | raw | 8.90 | 1.00 | 1.32 | 8.48 | 3.00 | 25.76 | 14.33 | 1.90 | 31.78 | 11.76 | 0.00 | 1.66 | 0.00 |
|  | HTC 180 °C, 0.5 h | 8.58 | 0.74 | 0.94 | 9.61 | 3.67 | 27.14 | 20.96 | 2.10 | 14.15 | 18.45 | 0.14 | 2.13 | 0.55 |
|  | HTC 180 °C, 2 h | 8.36 | 0.71 | 0.90 | 8.08 | 3.45 | 25.70 | 24.69 | 2.15 | 15.43 | 16.96 | 0.14 | 1.84 | 0.53 |
|  | HTC 180 °C, 4 h | 9.77 | 0.70 | 1.18 | 7.88 | 3.56 | 27.05 | 25.69 | 1.85 | 12.06 | 18.01 | 0.16 | 1.88 | 0.54 |
|  | HTC 210 °C, 0.5 h | 8.22 | 0.67 | 1.19 | 7.70 | 3.94 | 26.57 | 25.46 | 2.13 | 11.14 | 18.87 | 0.16 | 2.11 | 0.58 |
|  | HTC 210 °C, 2 h | 8.04 | 0.63 | 0.92 | 7.80 | 3.54 | 25.21 | 26.94 | 2.13 | 11.78 | 18.82 | 0.15 | 1.97 | 0.57 |
|  | HTC 210 °C, 4 h | 9.34 | 0.59 | 0.90 | 7.26 | 3.73 | 26.40 | 26.96 | 2.04 | 10.20 | 19.53 | 0.15 | 2.12 | 0.56 |
|  | HTC 240 °C, 0.5 h | 9.97 | 0.55 | 0.93 | 7.85 | 3.93 | 26.90 | 27.01 | 1.84 | 7.67 | 20.65 | 0.16 | 2.28 | 0.62 |
|  | HTC 240 °C, 2 h | 11.56 | 0.46 | 0.60 | 8.08 | 4.02 | 28.93 | 27.28 | 1.66 | 5.94 | 20.41 | 0.17 | 2.19 | 0.60 |
|  | HTC 240 °C, 4 h | 12.78 | 0.44 | 0.67 | 8.51 | 3.75 | 28.41 | 26.81 | 1.76 | 6.18 | 20.76 | 0.17 | 2.21 | 0.61 |
|  | HTC 270 °C, 0.5 h | 14.19 | 0.44 | 0.68 | 9.42 | 3.97 | 29.59 | 25.42 | 1.70 | 5.49 | 20.56 | 0.16 | 2.22 | 0.63 |
|  | HTC 270 °C, 2 h | 14.93 | 0.40 | 0.50 | 10.57 | 3.59 | 31.22 | 24.44 | 1.49 | 4.87 | 20.13 | 0.17 | 2.29 | 0.60 |
|  | HTC 270 °C, 4 h | 15.02 | 0.41 | 0.53 | 10.67 | 3.55 | 31.39 | 24.00 | 1.46 | 5.36 | 19.83 | 0.16 | 2.35 | 0.57 |

Table S 4. Elemental ash analysis, ash content and mass yield of untreated empty fruit bunches and empty fruit bunches treated by HTC at different temperatures and residence times. All values are reported on dry basis.

| Feedstock | Condition | Ash Content / wt.-% | Mass Yield / - | Na2O / wt.-% | MgO / wt.-% | Al2O3 / wt.-% | SiO2 / wt.-% | P2O5 / wt.-% | SO3 / wt.-% | K2O / wt.-% | CaO / wt.-% | TiO2 / wt.-% | Fe2O3 / wt.-% | ZnO / wt.-% |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| EFB | raw | 8.29 | 1.00 | 0.42 | 6.05 | 4.25 | 32.43 | 4.68 | 1.89 | 41.77 | 4.38 | 0.17 | 3.71 | 0.06 |
|  | HTC 180 °C, 0.5 h | 7.24 | 0.72 | 1.59 | 4.40 | 6.90 | 47.15 | 4.97 | 1.81 | 17.86 | 9.61 | 0.29 | 5.05 | 0.12 |
|  | HTC 180 °C, 2 h | 6.67 | 0.67 | 1.32 | 3.54 | 7.53 | 51.96 | 4.36 | 1.60 | 14.41 | 9.90 | 0.24 | 4.58 | 0.39 |
|  | HTC 180 °C, 4 h | 6.91 | 0.66 | 1.10 | 3.68 | 7.39 | 53.04 | 5.74 | 1.50 | 13.09 | 8.39 | 0.26 | 5.49 | 0.10 |
|  | HTC 210 °C, 0.5 h | 6.66 | 0.63 | 1.41 | 3.37 | 7.37 | 51.27 | 7.02 | 1.66 | 12.20 | 10.48 | 0.27 | 4.61 | 0.12 |
|  | HTC 210 °C, 2 h | 6.57 | 0.60 | 0.96 | 3.06 | 7.72 | 49.28 | 8.33 | 1.43 | 10.42 | 12.10 | 0.30 | 5.80 | 0.30 |
|  | HTC 210 °C, 4 h | 6.61 | 0.57 | 0.85 | 3.66 | 7.39 | 49.46 | 9.57 | 1.63 | 12.34 | 9.44 | 0.27 | 5.03 | 0.12 |
|  | HTC 240 °C, 0.5 h | 7.33 | 0.56 | 1.24 | 3.37 | 7.60 | 52.63 | 8.91 | 1.54 | 9.98 | 8.19 | 0.27 | 5.89 | 0.12 |
|  | HTC 240 °C, 2 h | 7.48 | 0.51 | 0.50 | 3.34 | 9.14 | 48.61 | 13.91 | 1.10 | 3.94 | 11.09 | 0.39 | 7.20 | 0.32 |
|  | HTC 240 °C, 4 h | 6.07 | 0.41 | 0.43 | 3.62 | 8.27 | 45.30 | 13.69 | 1.88 | 9.78 | 10.30 | 0.34 | 5.88 | 0.15 |
|  | HTC 270 °C, 0.5 h | 8.29 | 0.42 | 0.65 | 2.88 | 8.90 | 54.61 | 10.26 | 1.29 | 5.96 | 8.29 | 0.32 | 6.39 | 0.15 |
|  | HTC 270 °C, 2 h | 7.45 | 0.38 | 0.76 | 2.99 | 8.15 | 51.61 | 9.42 | 1.47 | 10.36 | 8.84 | 0.29 | 5.64 | 0.14 |
|  | HTC 270 °C, 4 h | 6.87 | 0.40 | 0.38 | 3.56 | 8.61 | 50.20 | 13.33 | 1.00 | 4.60 | 10.18 | 0.32 | 7.26 | 0.17 |

Table S 5. Elemental ash analysis, ash content and mass yield of untreated lawn cuttings and lawn cuttings treated by HTC at different temperatures and residence times. All values are reported on dry basis.

| Feedstock | Condition | Ash Content / wt.-% | Mass Yield / - | Na2O / wt.-% | MgO / wt.-% | Al2O3 / wt.-% | SiO2 / wt.-% | P2O5 / wt.-% | SO3 / wt.-% | K2O / wt.-% | CaO / wt.-% | TiO2 / wt.-% | Fe2O3 / wt.-% | ZnO / wt.-% |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| lawn cuttings | raw | 9.47 | 1.00 | 1.09 | 8.62 | 3.12 | 25.69 | 11.69 | 2.35 | 27.98 | 17.56 | 0.15 | 1.56 | 0.05 |
|  | HTC 180 °C, 0.5 h | 9.45 | 0.56 | 0.34 | 5.64 | 5.41 | 32.45 | 14.76 | 2.10 | 14.08 | 21.76 | 0.22 | 2.89 | 0.10 |
|  | HTC 180 °C, 2 h | 17.03 | 0.64 | 0.67 | 5.86 | 6.21 | 39.70 | 10.68 | 1.54 | 10.40 | 20.97 | 0.28 | 3.36 | 0.07 |
|  | HTC 180 °C, 4 h | 10.48 | 0.54 | 0.70 | 5.77 | 5.10 | 29.75 | 17.61 | 2.09 | 11.04 | 24.54 | 0.23 | 2.82 | 0.09 |
|  | HTC 210 °C, 0.5 h | 15.91 | 0.55 | 0.33 | 5.27 | 6.75 | 40.81 | 11.80 | 1.38 | 6.75 | 22.80 | 0.28 | 3.49 | 0.08 |
|  | HTC 210 °C, 2 h | 16.42 | 0.53 | 0.64 | 5.89 | 6.19 | 39.28 | 10.76 | 1.54 | 10.54 | 21.05 | 0.26 | 3.52 | 0.07 |
|  | HTC 210 °C, 4 h | 11.56 | 0.47 | 0.46 | 5.40 | 5.46 | 30.43 | 18.90 | 1.94 | 7.32 | 26.24 | 0.25 | 3.22 | 0.11 |
|  | HTC 240 °C, 0.5 h | 17.42 | 0.50 | 0.31 | 5.70 | 6.95 | 38.78 | 13.31 | 1.41 | 5.47 | 23.74 | 0.29 | 3.65 | 0.09 |
|  | HTC 240 °C, 2 h | 19.85 | 0.47 | 0.36 | 5.61 | 7.23 | 37.42 | 14.04 | 1.52 | 5.95 | 23.72 | 0.30 | 3.48 | 0.08 |
|  | HTC 240 °C, 4 h | 15.15 | 0.40 | 0.41 | 6.48 | 5.62 | 33.49 | 17.44 | 1.73 | 5.85 | 24.75 | 0.30 | 3.51 | 0.11 |
|  | HTC 270 °C, 0.5 h | 19.50 | 0.42 | 0.22 | 7.67 | 6.60 | 40.30 | 13.02 | 1.35 | 3.61 | 22.66 | 0.30 | 3.87 | 0.09 |
|  | HTC 270 °C, 2 h | 21.03 | 0.37 | 0.28 | 6.96 | 6.77 | 36.60 | 14.50 | 1.65 | 5.60 | 23.44 | 0.29 | 3.50 | 0.08 |
|  | HTC 270 °C, 4 h | 16.33 | 0.33 | 0.14 | 10.28 | 5.17 | 36.86 | 17.05 | 1.50 | 3.17 | 21.50 | 0.27 | 3.60 | 0.13 |

Table S 6. Elemental ash analysis, ash content and mass yield of untreated olive pomace and olive pomace treated by HTC at different temperatures and residence times. All values are reported on dry basis.

| Feedstock | Condition | Ash Content / wt.-% | Mass Yield / - | Na2O / wt.-% | MgO / wt.-% | Al2O3 / wt.-% | SiO2 / wt.-% | P2O5 / wt.-% | SO3 / wt.-% | K2O / wt.-% | CaO / wt.-% | TiO2 / wt.-% | Fe2O3 / wt.-% | ZnO / wt.-% |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| olive pomace | raw | 2.01 | 1.00 | 5.51 | 2.57 | 1.51 | 10.84 | 7.59 | 1.68 | 59.53 | 5.48 | 0.05 | 0.59 | 4.60 |
|  | HTC 180 °C, 0.5 h | 0.58 | 0.67 | 4.75 | 2.14 | 2.17 | 13.84 | 5.89 | 4.07 | 30.79 | 29.64 | 0.10 | 2.72 | 3.60 |
|  | HTC 180 °C, 2 h | 0.62 | 0.65 | 4.16 | 1.97 | 2.37 | 14.17 | 4.94 | 5.16 | 29.32 | 32.35 | 0.10 | 1.80 | 3.50 |
|  | HTC 180 °C, 4 h | 0.44 | 0.63 | 5.64 | 1.77 | 2.03 | 12.24 | 4.56 | 5.68 | 35.48 | 27.04 | 0.08 | 0.71 | 4.69 |
|  | HTC 210 °C, 0.5 h | 0.77 | 0.63 | 6.27 | 1.76 | 2.03 | 13.37 | 9.42 | 3.32 | 24.73 | 28.56 | 0.09 | 3.81 | 6.16 |
|  | HTC 210 °C, 2 h | 0.61 | 0.62 | 7.45 | 1.88 | 2.06 | 13.24 | 13.40 | 4.23 | 28.09 | 16.98 | 0.09 | 2.33 | 9.98 |
|  | HTC 210 °C, 4 h | 0.30 | 0.58 | 6.76 | 1.94 | 1.98 | 11.56 | 9.07 | 5.59 | 48.41 | 5.30 | 0.07 | 1.07 | 8.19 |
|  | HTC 240 °C, 0.5 h | 0.58 | 0.57 | 6.75 | 2.35 | 2.22 | 12.80 | 12.60 | 5.70 | 35.18 | 10.20 | 0.11 | 3.78 | 7.87 |
|  | HTC 240 °C, 2 h | 0.57 | 0.52 | 7.03 | 2.34 | 2.12 | 12.77 | 15.96 | 5.45 | 33.21 | 9.37 | 0.09 | 2.13 | 9.35 |
|  | HTC 240 °C, 4 h | 0.38 | 0.52 | 6.80 | 2.53 | 2.09 | 11.98 | 13.27 | 5.57 | 41.35 | 6.70 | 0.08 | 1.39 | 8.16 |
|  | HTC 270 °C, 0.5 h | 0.77 | 0.46 | 6.18 | 4.01 | 1.90 | 12.20 | 24.15 | 3.84 | 21.95 | 14.50 | 0.10 | 4.13 | 6.39 |
|  | HTC 270 °C, 2 h | 0.86 | 0.46 | 6.69 | 3.98 | 2.02 | 12.81 | 26.56 | 3.50 | 18.76 | 14.46 | 0.10 | 2.23 | 8.48 |
|  | HTC 270 °C, 4 h | 0.70 | 0.48 | 6.77 | 4.66 | 1.74 | 14.52 | 29.12 | 2.08 | 16.02 | 13.69 | 0.10 | 2.05 | 8.82 |

Table S 7. Elemental ash analysis, ash content and mass yield of untreated sewage sludge and sewage sludge treated by HTC at different temperatures and residence times. All values are reported on dry basis.

| Feedstock | Condition | Ash Content / wt.-% | Mass Yield / - | Na2O / wt.-% | MgO / wt.-% | Al2O3 / wt.-% | SiO2 / wt.-% | P2O5 / wt.-% | SO3 / wt.-% | K2O / wt.-% | CaO / wt.-% | TiO2 / wt.-% | Fe2O3 / wt.-% | ZnO / wt.-% |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| sewage sludge | raw | 28.10 | 1.00 | 1.27 | 3.54 | 12.09 | 21.04 | 26.03 | 1.95 | 2.93 | 18.66 | 0.38 | 11.55 | 0.19 |
|  | HTC 180 °C, 0.5 h | 38.07 | 0.73 | 0.71 | 2.86 | 13.18 | 21.34 | 26.87 | 1.31 | 1.93 | 19.18 | 0.38 | 11.64 | 0.19 |
|  | HTC 180 °C, 2 h | 45.24 | 0.59 | 0.41 | 2.86 | 13.70 | 21.21 | 27.49 | 1.18 | 0.98 | 19.63 | 0.41 | 11.52 | 0.19 |
|  | HTC 180 °C, 4 h | 45.76 | 0.58 | 0.47 | 2.85 | 13.74 | 20.95 | 27.54 | 1.10 | 1.03 | 19.64 | 0.40 | 11.66 | 0.20 |
|  | HTC 210 °C, 0.5 h | 48.97 | 0.56 | 0.38 | 2.88 | 13.48 | 21.14 | 27.26 | 1.09 | 0.96 | 20.02 | 0.39 | 11.79 | 0.20 |
|  | HTC 210 °C, 2 h | 50.00 | 0.54 | 0.40 | 2.93 | 13.45 | 20.97 | 27.43 | 1.01 | 0.98 | 19.99 | 0.39 | 11.84 | 0.20 |
|  | HTC 210 °C, 4 h | 51.05 | 0.51 | 0.37 | 2.93 | 13.71 | 20.60 | 27.54 | 0.99 | 0.99 | 20.06 | 0.40 | 11.80 | 0.20 |
|  | HTC 240 °C, 0.5 h | 51.53 | 0.54 | 0.47 | 3.02 | 13.36 | 20.45 | 27.53 | 1.19 | 0.98 | 20.17 | 0.39 | 11.84 | 0.19 |
|  | HTC 240 °C, 2 h | 53.04 | 0.52 | 0.39 | 2.99 | 13.55 | 20.88 | 27.05 | 1.06 | 0.99 | 19.97 | 0.40 | 12.11 | 0.19 |
|  | HTC 240 °C, 4 h | 54.94 | 0.49 | 0.45 | 3.05 | 13.64 | 21.26 | 26.94 | 0.81 | 1.04 | 19.65 | 0.41 | 12.15 | 0.20 |
|  | HTC 270 °C, 0.5 h | 54.88 | 0.50 | 0.41 | 3.04 | 13.57 | 21.03 | 27.16 | 1.01 | 0.96 | 19.94 | 0.41 | 11.85 | 0.19 |
|  | HTC 270 °C, 2 h | 55.84 | 0.50 | 0.34 | 3.04 | 13.68 | 21.14 | 26.41 | 0.87 | 1.10 | 20.14 | 0.40 | 12.26 | 0.20 |
|  | HTC 270 °C, 4 h | 57.78 | 0.49 | 0.44 | 3.09 | 13.71 | 21.45 | 26.17 | 0.79 | 1.09 | 20.03 | 0.43 | 12.18 | 0.20 |

Table S 8. Elemental ash analysis, ash content and mass yield of untreated spruce bark and spruce bark treated by HTC at different temperatures and residence times. All values are reported on dry basis.

| Feedstock | Condition | Ash Content / wt.-% | Mass Yield / - | Na2O / wt.-% | MgO / wt.-% | Al2O3 / wt.-% | SiO2 / wt.-% | P2O5 / wt.-% | SO3 / wt.-% | K2O / wt.-% | CaO / wt.-% | TiO2 / wt.-% | Fe2O3 / wt.-% | ZnO / wt.-% |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| spruce bark | raw | 3.43 | 1.00 | 0.90 | 5.42 | 2.60 | 16.13 | 4.82 | 0.85 | 9.72 | 55.49 | 0.26 | 1.31 | 0.37 |
|  | HTC 180 °C, 0.5 h | 3.23 | 0.70 | 0.64 | 3.05 | 2.89 | 16.53 | 2.56 | 0.98 | 4.47 | 65.86 | 0.21 | 1.13 | 0.28 |
|  | HTC 180 °C, 2 h | 3.08 | 0.70 | 0.66 | 3.25 | 3.07 | 17.29 | 2.68 | 1.31 | 5.02 | 63.65 | 0.19 | 1.12 | 0.31 |
|  | HTC 180 °C, 4 h | 3.20 | 0.70 | 0.60 | 2.82 | 2.94 | 17.27 | 2.19 | 1.03 | 4.58 | 65.14 | 0.20 | 1.42 | 0.31 |
|  | HTC 210 °C, 0.5 h | 3.07 | 0.67 | 0.69 | 2.76 | 3.23 | 17.26 | 3.04 | 1.10 | 3.83 | 64.90 | 0.19 | 1.25 | 0.31 |
|  | HTC 210 °C, 2 h | 3.27 | 0.67 | 0.69 | 2.79 | 3.22 | 16.77 | 4.22 | 1.08 | 3.96 | 63.82 | 0.19 | 1.28 | 0.36 |
|  | HTC 210 °C, 4 h | 3.54 | 0.66 | 0.63 | 2.71 | 3.15 | 17.01 | 4.80 | 1.07 | 3.86 | 63.07 | 0.19 | 1.41 | 0.37 |
|  | HTC 240 °C, 0.5 h | 3.41 | 0.60 | 0.74 | 2.65 | 3.26 | 17.11 | 5.86 | 1.04 | 3.38 | 62.47 | 0.19 | 1.30 | 0.35 |
|  | HTC 240 °C, 2 h | 3.63 | 0.54 | 0.73 | 2.55 | 3.52 | 17.16 | 7.34 | 1.14 | 3.18 | 60.86 | 0.18 | 1.25 | 0.37 |
|  | HTC 240 °C, 4 h | 3.91 | 0.51 | 0.56 | 2.31 | 3.45 | 16.78 | 7.03 | 1.15 | 2.76 | 62.20 | 0.17 | 1.50 | 0.37 |
|  | HTC 270 °C, 0.5 h | 3.48 | 0.48 | 0.72 | 2.60 | 3.83 | 17.73 | 7.97 | 1.27 | 2.75 | 59.55 | 0.19 | 1.38 | 0.34 |
|  | HTC 270 °C, 2 h | 3.12 | 0.47 | 0.77 | 2.86 | 4.50 | 18.10 | 9.81 | 1.43 | 3.40 | 54.92 | 0.20 | 1.78 | 0.42 |
|  | HTC 270 °C, 4 h | 2.88 | 0.46 | 0.82 | 2.88 | 5.24 | 20.03 | 11.18 | 1.55 | 3.00 | 49.70 | 0.24 | 2.71 | 0.54 |

Table S 9. Elemental ash analysis, ash content and mass yield of untreated wheat straw and wheat straw treated by HTC at different temperatures and residence times. All values are reported on dry basis.

| Feedstock | Condition | Ash Content / wt.-% | Mass Yield / - | Na2O / wt.-% | MgO / wt.-% | Al2O3 / wt.-% | SiO2 / wt.-% | P2O5 / wt.-% | SO3 / wt.-% | K2O / wt.-% | CaO / wt.-% | TiO2 / wt.-% | Fe2O3 / wt.-% | ZnO / wt.-% |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| wheat straw | raw | 10.83 | 1.00 | 0.49 | 2.51 | 2.63 | 78.63 | 0.37 | 0.82 | 11.33 | 2.26 | 0.09 | 0.77 | 0.02 |
|  | HTC 180 °C, 0.5 h | 10.70 | 0.78 | 0.12 | 1.85 | 2.22 | 86.20 | 0.00 | 0.51 | 6.90 | 1.49 | 0.07 | 0.54 | 0.03 |
|  | HTC 180 °C, 2 h | 12.56 | 0.69 | 0.00 | 1.23 | 2.27 | 92.07 | 0.00 | 0.35 | 2.84 | 0.56 | 0.08 | 0.53 | 0.02 |
|  | HTC 180 °C, 4 h | 11.77 | 0.87 | 0.00 | 1.19 | 2.23 | 91.68 | 0.00 | 0.35 | 3.03 | 0.89 | 0.07 | 0.49 | 0.02 |
|  | HTC 210 °C, 0.5 h | 12.83 | 0.64 | 0.00 | 1.26 | 2.25 | 92.46 | 0.08 | 0.32 | 2.46 | 0.48 | 0.08 | 0.53 | 0.03 |
|  | HTC 210 °C, 2 h | 12.70 | 0.62 | 0.04 | 1.28 | 2.28 | 92.46 | 0.09 | 0.36 | 2.56 | 0.13 | 0.07 | 0.65 | 0.02 |
|  | HTC 210 °C, 4 h | 13.39 | 0.58 | 0.00 | 1.17 | 2.23 | 93.04 | 0.18 | 0.33 | 2.35 | 0.00 | 0.08 | 0.54 | 0.03 |
|  | HTC 240 °C, 0.5 h | 13.85 | 0.57 | 0.00 | 1.20 | 2.27 | 93.62 | 0.25 | 0.29 | 1.73 | 0.00 | 0.07 | 0.48 | 0.02 |
|  | HTC 240 °C, 2 h | 15.80 | 0.47 | 0.00 | 1.06 | 2.27 | 94.31 | 0.33 | 0.26 | 1.07 | 0.00 | 0.08 | 0.54 | 0.02 |
|  | HTC 240 °C, 4 h | 16.33 | 0.45 | 0.00 | 1.09 | 2.21 | 94.02 | 0.53 | 0.27 | 1.15 | 0.00 | 0.07 | 0.58 | 0.03 |
|  | HTC 270 °C, 0.5 h | 16.85 | 0.44 | 0.00 | 1.03 | 2.31 | 94.69 | 0.24 | 0.20 | 0.77 | 0.00 | 0.08 | 0.61 | 0.02 |
|  | HTC 270 °C, 2 h | 16.79 | 0.43 | 0.00 | 1.07 | 2.27 | 94.56 | 0.43 | 0.22 | 0.82 | 0.00 | 0.08 | 0.47 | 0.02 |
|  | HTC 270 °C, 4 h | 15.17 | 0.38 | 0.00 | 1.23 | 2.15 | 92.33 | 1.33 | 0.32 | 1.24 | 0.72 | 0.08 | 0.52 | 0.03 |

Figure S1: Evolution of molar 2 S/Cl ratio of all treated biomass fuels with increasing treatment temperature at a residence time of 0.5 h (left) and 4 h (right).