Breakthrough studies for the sorption of methylene blue dye from wastewater samples using activated carbon derived from waste banana peels.

Denga Ramutshatsha-Makhwedzhaa*, Alexis Munyengabeb, Mapula Lucey Mavhungua, Richard Mbayaa, Jeffrey Baloyic

aDepartment of Chemical, Metallurgical and Materials Engineering, Tshwane University of Technology, Pretoria West Campus, Private Bag X680, South Africa

bDepartment of Chemistry, Tshwane University of Technology, Arcadia Campus, Pretoria 0001, South Africa

cSmart Places Cluster, Council for Scientific and Industrial Research (CSIR), Pretoria 0001, South Africa

Table S1. T- test and p-value analysis

| Adsorbent mass (g) | DF | T-statistics | Mean | P-Value |
| --- | --- | --- | --- | --- |
| 1 | 19 | -7.80967 | 0.28288 | 2.39 x10-7 |
| 4 | 11 | -3.10417 | 0.71673 | 0.00143 |
| 8 | 26 | -8.42318 | 0.26546 | 6.6388x10-9 |
| Initial concentration (mg/L) |  |  |  |  |
| 40 | 12 | -4.9398 | 0.55679 | 0.000342 |
| 80 | 9 | -3.1041 | 0.7167 | 0.01264 |
| 120 | 10 | -3.89365 | 0.6475 | 0.00299 |

Foot note: DF: Degree of freedom; P-Value: Probability value