Sequestration of chromium by Ananas comosus extract-coated nanotubes: synthesis, characterization, optimization, thermodynamics, kinetics, and antioxidant activities

James Friday Amaku and Raymond Taziwa

Department of Applied Science, Faculty of Science Engineering and Technology, Walter Sisulu University, Old King William Town Road, Potsdam Site, East London 5200, South Africa.

Contact author details:

Name: James Friday Amaku, Tel: ++27-61-7997907, email: famaku@wsu.ac.za

0000-003-4894-0512 (J Amaku)

Sorption kinetic and equilibrium isotherm models

To better understand the mechanism responsible for the uptake of Cr(VI), adsorption kinetics of Cr(VI) onto the MWPJ and MWCNTs were analyzed using various kinetics models as displayed in Table S1. On the other hand, Table S2 provides the list of equilibrium isotherm models that were used to evaluate the sorption of Cr(VI) onto MWPJ and MWCNTs at 298 K, 303 K, 313 K and 318 K solution temperatures .

Table  S1  Kinetics models investigated for the adsorption of Cr(VI) onto the MWPJ and MWCNTs.

| Kinetic models | Equations | Parameters | References |
| --- | --- | --- | --- |
| Pseudo-first order | dqtdt=k1qe-qt | qe,k1 | [43] |
| Pseudo-second order | dqtdt=k2qe-qt2 | k2,qe | [44] |
| Weber-Morris intraparticle diffusion | dqtdt-0.5=kid | kid, l | [45] |
| Elovich | dqtdt=αexp-βqt | α, β | [46] |
| k1, pseudo-first order rate constant (min-1); k2, pseudo-second order rate constant (g mg-1 min-1). kid, intraparticle diffusion rate constant (mg g-1 min0.5); l, is a constant related to the boundary layer thickness (mg g-1);qt, quantity of adsorbate adsorbed at time t (mg g-1); qe, quantity of adsorbate adsorbed at equilibrium (mg g-1); α, adsorption rate constant (mg g-1 min-1); β, desorption rate constant (g mg-1). |  |  |  |

Table  S2  Isotherm models used to describe the uptake of Cr(VI)  onto MWPJ and MWCNT.

| Isotherm model | Equation | Parameters | References |
| --- | --- | --- | --- |
| Langmuir | qe=qmaxbCe1+bCe | qmax, b | [47] |
| Freundlich | qe=KFCe1n | kF, n | [48] |

qeq, adsorption capacity (mg g-1) of MWPJ or MWCNT; Ceq, equilibrium concentration of Cr(VI) in solution (mg dm-3); qmax, maximum monolayer capacity (mg g-1) of MWPJ and MWCNT; b, Langmuir isotherm constant (dm3 mg-1); KF, Freundlich isotherm constant