Supplementary Information tables for:

Utilization of paper sludge in preparation of high-purity calcium formate

Mohammad L. Hassan*, Enas A. Hassan, Wafaa S. Abou-Elseoud, Aisha M. Mostafa

1 Cellulose and Paper Department, National Research Centre, Dokki, Giza 12622, Egypt.

2 Advanced Materials and Nanotechnology Group, Centre of Excellence for Advanced Sciences, National Research Centre, Dokki, Giza 12622, Egypt.

3 Solid State Department, National Research Centre, Dokki, Giza 12622, Egypt.

Corresponding author email: ml.hassan@nrc.sci.eg.

Supplementary Information Table S1. Selected bond lengths (Å) and angles (◦) in the crystal structure of synthetic calcium formate.

|  | Bond length (Å) |  | Bond angle (º) |
| --- | --- | --- | --- |
| Ca-O1 | 2.276(19) | O1–Ca1–O4 | 92.3(6) |
| Ca-O2 | 2.350(18) | O1–Ca1–O4 | 91.8(6) |
| Ca-O2 | 2.417(18) | O2–Ca1–O2 | 155.5(6) |
| Ca-O3 | 2.227(18) | O2–Ca1–O3 | 66.6(6) |
| Ca-O3 | 2.548(20) | O2–Ca1–O3 | 144.2(7) |
| Ca-O4 | 2.449(18) | O2–Ca1–O4 | 122.1(6) |
| Ca-O4 | 2.192(16) | O2–Ca1–O4 | 171.0(6) |
| <Ca-O> | 2.350(18) | O3–Ca1–O2 | 88.5(6) |
| Ca-----O1 | 3.496Å | O3–Ca1–O2 | 69.9(5) |
| C1- O1 | 1.478(58) | O3–Ca1–O3 | 85.2(6) |
| C1-O1 | 1.478(58)Å | O3–Ca1–O4 | 56.0(6) |
| C1 - O2 | 1.334(46) | O3–Ca1–O4 | 95.5(6) |
| C2 - O3 | 1.087(28) | O4–Ca1–O2 | 86.8(5) |
| C2 - O4 | 1.632(24) | O4–Ca1–O2 | 171.0(6) |
| C1 - H1 | 0.965(30) | O4–Ca1–O3 | 55.9(4) |
| C2-H2 | 1.085(24) | O4–Ca1–O3 | 93.5(6) |
| O1–Ca1–O2 | 108.1(6) | O4–Ca1–O4 | 65.9(5) |
| O1–Ca1–O2 | 83.5(6) | O1–C1–O2 | 121.8(10) |
| O1–Ca1–O3 | 92.8(6) | O3–C2–O4 | 117.9(1) |

Supplementary Information Table S2. Selected bond lengths (Å) and angles (◦) in the crystal structure of calcium formate from paper sludge.

|  | Bond length (Å) |  | Bond angle (º) |
| --- | --- | --- | --- |
| Ca-O1 | 2.430(22) | O1–Ca1–O4 | 87. 5(7) |
| Ca-O2 | 2.401(25) | O2–Ca1–O2 | 85.5(8) |
| Ca-O2 | 2.463(24) | O2–Ca1–O3 | 146.9(9) |
| Ca-O3 | 2.192(23) | O2–Ca1–O3 | 67.4 (8) |
| Ca-O3 | 2.555(26) | O2–Ca1–O4 | 154.3(7) |
| Ca-O4 | 2.476(24) | O2–Ca1–O4 | 119.0(8) |
| Ca-O4 | 2.342(22) | O3–Ca1–O2 | 74.5 (8) |
| <Ca-O> | 2.409(23) | O3–Ca1–O2 | 91.1 (8) |
| Ca-----O1 | 3.414 | O3–Ca1–O3 | 86.8(8) |
| C1- O1 | 1.431(54) | O3–Ca1–O4 | 96.2(9) |
| C1-O1 | 2. 750(44) | O3–Ca1–O4 | 125.1 (8) |
| C1 - O2 | 1.432(51) | O4–Ca1–O2 | 84.5(8) |
| C2 - O3 | 1.542(41) | O4–Ca1–O2 | 165. 9(9) |
| C2 - O4 | 1.251(42) | O4–Ca1–O3 | 125.0 (8) |
| C1 - H1 | 0.935(39) | O4–Ca1–O3 | 125.0(8) |
| O1–Ca1–O2 | 80.71(69) | O4–Ca1–O4 | 72.4 (8) |
| O1–C1–O2 | 108.6 (31) | O1–C1–O2 | 130.4 (20) |
| O1–Ca1–O3 | 89.68(61) | O3–C2–O4 | 106.2 (27) |
| O1–Ca1–O3 | 171.8(8) |  |  |