Synthesis of Spherical Carbon Nanoparticles from Orange Peel and Their Surface Modification with Chitosan: Evaluation of Optical Properties, Biocompatibility, Antioxidant and Anti-hemolytic Activity

Asma Ben Amor 1,2, Hadia Hemmami 1,2,, Mohammed Taher Gherbi3,4 , Bachir Ben Seghir1,2, Soumeia Zeghoud 1,2,, Ahlam Hacine Gharbi1,2  , Djihad Chenna 5,6, Ilham Ben Amor1 , Huda Alsaeedi7, David Cornu8, Mikhael Bechelany8,9, Ahmed Barhoum10*

1Department of Process Engineering and Petrochemical, Faculty of Technology, University of El Oued, El Oued 39000, Algeria.

2Renewable Energy Development unit in Arid Zones (UDERZA), University of El Oued, El Oued 39000, Algeria.

3Department of Mechanical Engineering, University of El Oued, El Oued 39000, Algeria

4Laboratory of Applied Chemistry and Environment, Faculty of Exact Sciences, University of El Oued, P.O. Box 789, El Oued 39000, Algeria

5El Oued University, Faculty of Life and Natural Sciences, Department of Molecular and Cellular Biology, Algeria

6El Oued University, Laboratory Biology, Environment, and Health, Algeria

7Department of Chemistry, College of Science, King Saud University, Riyadh 11451, Saudi Arabia

8Institut Européen des Membranes, IEM, UMR-5635, University Montpellier, ENSCM, CNRS, Place Eugene Bataillon, Montpellier, France

9Gulf University for Science and Technology, GUST, Helwan, Kuwait

10NanoStruc Research Group, Chemistry Department, Faculty of Science, Helwan University, Cairo, Egypt

Corresponding author: ahmed.barhoum@science.helwan.edu.eg

Supplementary file

Table S1. FTIR peak assignments of Orange peel, CNPs and Chitosan@CNPs.

| Composite | Peak ( cm⁻¹) | Assignment |
| --- | --- | --- |
| Orange peel | 3280 | OH stretching |
|  | 2917 | C–H bonds |
|  | 1629,1643 | C=O stretches |
|  | 1417 | carboxylic acid groups |
| CNPs | 3281 | O−H stretching |
|  | 1643 | C=O stretching |
|  | 1218 | C−O stretching |
|  | 1566 | N−H vibrations |
|  | 1399 | C=C vibration |
|  | 618 | C-H vibration |
| Chitosan@CNPs | 3004 | N–H stretching |
|  | 2904 | alkane stretching |
|  | 2357 | C≡N stretching |
|  | 1976 | C≡C stretching |
|  | 1018 | C-O stretching |

Table S2. DPPH Radical Scavenging Activity (%) of CNPs and Chitosan@CNPs. Values were expressed as means ± SD (n=3) of three parallel measurements.

| Concentration | DPPH inhibition (%) of Samples |  |
| --- | --- | --- |
|  | Chitosan@CNPs | CNPs |
| 1x10-3 | 59.97±0.7 | 76.31±0.6 |
| 2×10-3 | 56.47±0.5 | 83.66±0.4 |
| 4×10-3 | 56.41±0.4 | 87.33±0.5 |
| 5×10-4 | 52.56±0.4 | 87.51±0.6 |
| 2.5×10-4 | 47.6±0.3 | 89.52±0.4 |

Table S3. Cell Viability (%) of CNPs and Chitosan@CNPs.

| Samples | Percentage of cells (%) |  |
| --- | --- | --- |
|  | Live cells | Dead cells |
| Negative control | 98.2±0.4 | 53.6±0.4 |
| Positive control (100%) | 2.4±0.3 | 97.6±0.5 |
| Positive control (50%) | 53.6±0.6 | 46.4±0.7 |
| CNPs | 97.6±0.7 | 2.4±0.4 |
| Chitosan@CNPs | 91.4±0.8 | 8.6±0.6 |

Table S4. Antihemolytic Activity (%) of CNPs and Chitosan@CNPs Compared to Ascorbic Acid.

| Concentration(mg/ml) | Antihemolytic activity (%) |  |  |
| --- | --- | --- | --- |
|  | CNPs | Chitosan@ CNPs | Ascorbic acid |
| 20 | 70.1±0.3 | 74.4±0.4 | 100±0.1 |
| 10 | 57.1±0.6 | 78.7±0.5 |  |
| 5 | 60.3±0.4 | 63.5±0.7 |  |
| 2.5 | 50.1±0.5 | 65.5±0.4 |  |
| 1.25 | 46.7±0.4 | 58.1±0.3 |  |
| 0.625 | 48.9±0.6 | 55.1±0.5 |  |