Supplementary Materials

Chemical products yielded from different pyrolysis processes of rice waste residues: A comprehensive review

Saad A. El-Sayed

Mechanical Power Engineering Dept.-Zagazig University-Alsharkia-Egypt

Corresponding author Email: shamad53@hotmail.com

Table S1: Bio-yield products, pyrolysis type and experimental devices and experimental conditions of RH and RS.

| Ref. No. | Tested Materials | Experimental Devices | Type | Operating conditions | Yield products |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | Bio-oil | Bio-char | Non-condensable gases |
| [1] | Rice straw(RS) -Sugarcane bagass-coconut shell - < 0.5 mm size - China | Fixed bed reactor, Induction heating –GC/MS-FTIR | Fast pyrolysis | 400-800 oC-HR =100-500 oC/min-Reaction time (Rt)=1-8 min. N2= 1000 cm3/min | RS: 400 oC:5% 500 oC:8% 600 oC:7% 700 oC:6% 800 oC:7% | RS: 400 oC:74% 500 oC:38% 600 oC:27% 700 oC:23% 800 oC:22% | -- |
| [2] | Rice straw-Indonesia | Lab scale baked bed reactor | Slow pyrolysis | 300 to 700 oC- HR= 12 oC/min, Reation time (Rt) =60 min. | Wet basis: 300 oC:30% 400 oC:37% 500 oC:38% 600 oC:40% 700 oC:40% Dry ash free basis: 300 oC:32% 400 oC:42% 500 oC:43% 600 oC: 45% 700 oC:44% | 57% 45% 41% 40.5% 40% 50.5% 33% 28% 25.5% 25% | 13% 17% 20% 20% 21% 18% 24% 28.5% 28% 30% Gases: CO,CO2, H2, C2H4,C2H6, C3H6,C3H8 |
| [3] | Rice straw- < 1 mm size -Egypt | Free fall reactor - | Fast pyrolysis | 450 to 700 oC – Rt= 1.5 s - Feed rate (FR) = 1 kg/h | 450 oC:39% 450 oC:46% 450 oC:44% 450 oC:40% 450 oC:35% | 37% 23% 20% 16% 13% | 23.5% 29.6% 33.5% 42.5% 49.0% Gasses:35.33% H2, 20.80% CO2, 11.67% CO, 16.28% CH4, 1.34% C2H6, 3.11% C2H4, 0.22% C3H8,0.49% C3H6, 0.02% IC4H10, 0.04% C4H10,0.05% C4H8, 0.01% IC5H12, 0.01% C5H12,0.05 %(C6 +), 10.27% (N2), 0.31% (O2) |
| [4] | Rice straw –0.1 - 0.3 mm size – China - cataltysis: ZSM-5,LOSA-1, Gamma, Al2O3, spent FCC poweders of 0.063 and 0.154 mm | Int. inter-connected fluidized bed reactor - GC/MS, GC/FID and GC/ TCD (Thermal conduct. detector) | Catalytic fast pyrolysis | 550 oC - feeding rate (FR) = 44 g/h for 30 min | 23.3% Max. yields of aromatics (12.8%) and C2-C4 olefins (10.5%) with ZSM-5 - yield of un-identified compounds (43.9%) | 32.3% Char and coke is the maximum value (32.3%) with ZSM-5 - Gamma-Al2O3 yields the lowest coke & char (22.7%) | 33.5% Gases: CO (highest concentration), followed by CO2, then CH4. |
| [5] | Rice Straw, Rice husk, Corn Cob-dried < 74 mm size-Thailand | TGA-MS, FTIR | Slow pyrolysis | Room temp. to 600 oC – HR = 10 oC/min - helium flow rate of 50 mL/min | Rice straw 600 oC: 9.6% Rice husk:600 oC: 47% | 30% 11% | 60.4% 42.0% RS Gases:24.4% H2O, 16.4% CO2, 16.3%CO, H2+CH4: 3% RH: 18% H2O, 10%CO2, 12.5% CO, H2+CH4: 1.5% |
| [6] | Rice Straw – <0.295 mm size-China | Bench-scale fixed bed reactor | Slow and fast pyrolysis | 600 to 1000 oC – HR = 10 &300 oC/min – RT=60 min for low HR | - | HR=300oC/min: 600 oC:31.23% 700 oC:29.96% 800 oC:28.69% 900 oC:27.36% 1000 oC: 26.22% HR=10oC/min: 900 oC: 29.33% | - |
| [7] | Rice Straw – air dried -0.425 to 0.85 mm size -Taiwan | Microwave-induced system | Microwave-induced slow pyrolsis | 50 - 500 W - 105 to 563 oC – HR = 5 - 141 oC/min – Rt =7 -30 min –N2 at 50 mL/ min | At 300 W: 22.56% | 28.07% | 49.37% Gases:H2:55%, CO:17%,CO2:13%, CH4:10%, |
| [8] | Rice Straw-air dried 0.425 to 0.85 mm-Tiawan | Microwave-induced oven GC/ TCD | Slow pyrolysis -2000W | N2 = 50 mL/min – 200, 300, 400, 500 W | - | - | Gas compositions: H2=50.67% CO2=22.56%, CO= 16.09%,CH4 =7.42%, 3.27% not detected |
| [9] | Rice straw, maize stalk, cotton straw - < 0.295 mm size - China | TGA-FTIR (4 cm-1 resol.- 32 scans -4000 -400 cm-1) | Slow pyrolysis | 200-900 oC – HR=10 oC/ min – N2 = 100 mL/min – FR= 10 to 15 mg | From 200 to 500 oC, the yield increase from 5% to 44% (fixed from 500 to 800 oC) | From 200 to 500 ◦C, the yield decreases from 95% to 30% (fixed from 500 to 800 oC) | 200 to 500 oC, yield increase from 1% to 25% (fixed from 500 to 800 oC) Gases:CO2, CO, CH4, C2H4, C2H6, CH2O, CH3OH, HCOOH, C3H6O |
| [10] | RH, RS, corn cob -75µm size -Thailand cellulose, organic lignin - acid treated | Drop-tube/ fixed bed reactor -MS –TGA- SEM - sorption analyzer | Fast pyrolysis | 200-850 oC –HR>1000 oC/s to 3 h –N2 at 400 mL/min – 0.5 MPa | - | - | At 850oC : H2, CH4, CO (highest rate), CO2 |
| [11] | paddy rice husks - 355–500 µm size- MFI zeolite ZSM-5 catalyses | Drop type fixed-bed pyrolyzer | Catalytic -Fast pyrolysis | 350 - 600 oC-Rt =10 min – biomass/catalses ratios (0.5–2) | 350 oC:25% 400 oC:27% 450 oC:35% 500 oC:29% 550 oC:28% 600 oC:26% ZSM-5 catalyst: 0.0 :37 % 0.5 :30 % 1.0 :28 % 1.5 :25 % 2.0 :24 % | 57% 48% 39% 37% 37% 31% 40% 50% 48% 41% 37% | 18% 21% 24% 32% 33% 38% 24% 18% 24% 31% 38% Gases for noncatalyst and catalytic(0.0, 0.5, 1.0, 1.5, 2.0): H2: 0.42, 0.56 0.66, 0.69, 0.74% CH4: 2.071, 4.1, 4.45, 4.62, 4.44% CO: 10.25%, 23.85, 27.85, 26.54, 24.15% CO2: 29.05, 33.45, 35.46, 37.85, 39.85% |
| [12] | RH, Todo fir wood-What –man CF11 cellulose powder - <500 µm size | Pulse current heating device and graphite die -700-950 A, 12-16 V GC/ MS | Slow pyrolysis | 300-800℃ - HR = 15 and 20 ℃/s, Rt = = 3 min – Helium = 40.3 mL/min | Raw: 300 oC:5% 400 oC:33% 500 oC:42% 600 oC:32% 700 oC:32% 800 oC:28% | - 85% 44% 37% 35% 34% | 100% 0% 23% 20% 33% 34% |
| [13] | Rice straw, 0.005 mm size - China | Tubular reactor –GC/MS | Fast pyrolysis | 400-900 oC, 10000 K/min, Rt=4 min, N2 = 100 mL/ min | 400 oC:41.5 500 oC:44.0 600 oC:41.5 700 oC:37.5 800 oC:33.0 900 oC:32.5 | 38.5% 32.0% 30.5% 30.7% 30.6% 27.2% | 18.5% 23.5% 27.0% 29.5% 33.0% 37.6% |
| [14] | Rice straw, - dried 40-80 mesh, Shanghai, China | Fixed bed reactor –GC/MS | Slow pyrolysis | 300 to 700 oC, HR= 5 oC/min, Ht=1.5 h | 300 oC:31% 400 oC:37% 500 oC: 38.5% 600 oC: 37.5% 700 oC:37% | 50% 38.75% 36% 33.6% 32.5% | 18.5% 24% 25% 27.5% 28.6% Gases: H2 (2.5% max), CO (16.5% max), CH4(2.5% max), CO2 (27.5% max) |
| [15] | Rice straw, < 2 mm size- China | Muffle furnace | Slow pyrolysis | 250, 300, 350, 400, 450 oC - Rt= 2, 4, 8 h | - | 63% to 26% at 250 oC and 2 hr to 450 oC, 8hr duration | - |
| [16] | Rice straw - dried -20 mm size -China | Tubular furnace | Slow pyrolysis | 300, 400, 500, 600 & 700 oC, HR= 5 oC/min, residence time (1, 2, 3 & 5 h – N2 at 1.0 L/min | - | For Rt=1, 2,3,5: 300-1: 49.5% 300-2: 50.1% 300-3: 49.8% 300-5: 49.1% 400-1: 42.8% 400-2: 42.3% 400-3: 41.1% 400-5: 42.0% 500-1: 39.0% 500-2: 38.6% 500-3: 38.0% 500-5: 38.6% 600-1: 35.7% 600-2: 35.1% 600-3: 36.1% 600-5: 36.3% 700-1: 34.7% 700-2: 33.5% 700-3: 35.2% 700-5: 36.5% | - |
| [17] | RS, cotton, wheat, corn straws, wood shaving, 0.125 mm size- China | Muffle furnace -FTIR | Slow pyrolysis - bio-char | 600 oC, HR =10 oC/min, Ht = 3 h | - | 34.3% alkaline and alkaline earth metals (K+, Ca2+, Mg2+, and Na+) with K+ being the highest | - |
| [18] | RH -hydrochloric acid for leached at 400 ◦C (A-RH) - Argentina | Tubular quartex reactor –GC/MS | Catalytic -Fast Pyrolysis | 300, 400, 500, 600 and 700oC, Ht= 20 min – N2 at 0.1mL/min – Rt= 0.1 s – P = 1 to 5 torr | RH: RH:300 oC:14% 400 oC:34% 500 oC:28% 600 oC:25% 700 oC:27% A-RH: 300 oC:28% 400 oC:47% 500 oC:43% 600 oC: 40% 700 oC: 39% Levoglucosan yields: RH: 300 oC:9% 400 oC:10% 500 oC:13% 600 oC: 19% 700 oC: 10% A-RH: 300 oC:19% 400 oC:22% 500 oC:30% 600 oC: 20% 700 oC: 17% | 45% 29% 21% 23% 19% 46% 34% 19% 22% 25% | 41% 37% 51% 52% 54% 26% 19% 28% 38% 36% |
| [19] | RS, masson pine, fir wood bark, bamboo leaves, etc. 40 mesh China | Fixed-bed tubular reactor (5 L) | Slow pyrolysis | 350 ◦C or 500 ◦C, N2 at 200 ml/min, HR= 5 ◦C /min - Ht = 120 min, | - | 350 oC:47% 500 oC:39% | - |
| [20] | RH, coconut pulp, of <0.30 mm and 0.30 ≤ - <0.50 mm | TGA-N2 at 150 ml/min | Flash pyrolysis | Room temp. to 700 oC, HR= 50 and 80 °C/min | - | At HR=50 oC/min <0.3mm:39.09% >0.3 mm:35.50% | At HR=100 oC/min: <0.3 mm: 37.47% >0.3 mm: 37.49% |
| [21] | sugar cane, eucalyptus, and rice straw | a lab-scale packed bed reactor | Slow pyrolysis | 300, 350, 400, 450, 500, 550, 600, 650, 700°C- HR of 5°C/min – N2 at 2.0 L/min | 300 oC:17% (Wet base) 350 oC:18% 400 oC:23% 450 oC:28% 500 oC:29% 550 oC:30% 600 oC:31% 650 oC:32% 700 oC:33% 300 oC:18% (dry base) 350 oC:20% 400 oC:21% 450 oC:22% 500 oC:23% 550 oC:25% 600 oC:26% 650 oC:27% 700 oC:29% | 50% 47% 45% 41% 39% 37% 36% 33% 32% 43%(dry basis) 42% 41% 40% 38% 36% 35.5% 34.5% 34% | 6% 7% 9% 12% 12.5% 13.5% 15% 16% 17% 8%(dry basis) 9% 10% 12% 13% 14% 15.5% 15% 16.5% |
| [22] | RH - 3.192 mm, sand as bed material of 0.45 mm | Fluidized bed reactor GC–MS | Fast pyrolysis | 420 - 540 oC – FR = 7.32 kg/h – N2 | 420 oC:53% 450 oC:56% 480 oC:56% 510 oC:53% 540 oC:49% | 35% 29% 24% 21% 18% | 12% 15% 20% 26% 33% |
| [23] | Rice husk, 0.63–1 mm size, sand of 0.3–0.63 mm size | Bench-scale plant with a conical spouted bed reactor – GC/MS | Fast pyrolysis | 400, 450, 500, 600 oC - N2 at 10-30 ml/min | 400 oC:67.5 450 oC:70.5 500 oC:69% 600 oC:67% | 32% 26% 25.5% 25% | 1% 5% 6% 10% H2: 1.0% at 400 oC to 7% at 600oC CH4: 0.5% at 400 oC -7% at 600oC CO: 43% at 400 oC -67% at 600oC CO2: 54% at 400oC -17% at 600oC C2-C4:1.0% at 400 oC-6% at 600oC |
| [24] | Rice husk, < 0.18 mm size and 0.28-0.45 mm - catalyst (ZSM-5) | A lab-scale unit + fluidized bed –Py/GC/MS | Catalytic Fast pyrolysis | 400 to 550 oC – samd 0.28-0.45 mm size | Non-cataylatic F.B. for 7 runs , %: 23.2, 39.3, 46.9, 40.0, 33.5, 31.3 Catalytic 40.3% | 42.9, 34.0, 30.0, 34.3, 37.0, 42.2, 46.3% | 33.9, 26.7, 23.1, 25.7, 29.6, 26.6, 13.4% |
| [25] | Rice husk, particle size of <0.50 mm, | Fixed-bed reactor, FTIR, GC-MS | Fast pyrolysis system using induction heating | 400–800 °C, HR of 100–500 °C/min, Ht of 1–8 min, N2 of 500–1500 cm3/min | 400 oC:5% 500 oC:10% 600 oC:6% 700 oC:5% 800 oC:8% Ht (min.): 1.0:8% 2.0:10% 4.0:11% 8.0:8% HR (oC/min): 100:8% 200:9% 300:10% 400:8% 500:7% | 75% 38% 27% 23% 21% 37% 29% 26% 24% 36% 38% 39% 40% 42% | - |
| [26] | Rice husk | Fixed-bed reactor- GC-MS | Slow pyrolysis | 400-600 0C - carrier gas flow rate was 200 ml/min | 400oC:32.5% 450oC:43% 500oC:44% 550oC: 46% 600oC:41% Max 45% at 550 oC | 43% 39.5% 38% 37% 37% max 40% at 400 oC | 12% 16% 17% 16.5% 22% Max 22% at 600 oC |
| [27] | RS, RH, bamboo, sugarcane bagasse, and neem bark -less than dried - <1000 µm | Single stage fixed- bed reactor - GC-MC and FTIR | Fast pyrolysis | 350 to 650 oC - Residence times of 27, 30, 33, and 36 s | 450 oC: 35.5% 500 oC: 37.5% 550 oC:42% 600 oC:38% 650 oC: 34.5% | 46.5% 48% 39.5% 37.5% 37% | 18% 17% 17.5% 23% 27.5% Gases(450 to 650 oC): CO :36.39 -41.39 vol % , CH4:1.96 - 15.45 %, H2: 5.53 -15.55% CO2: 43.48 - 26.89% |
| [28] | RS, Camellia oleifera shell, 0.18 mm size | Continuous fast microwave-assisted pyrolysis system | Fast pyrolysis | 400, 500, and 600 °C and feed rates rice straw: 25,45, and 66 g/min; C.oleifera shell: 100, 200, and 400 g/min | 400 oC, FR(g/min): 24:18.96% 45:20.25% 66:21.46% 500 oC, FR(g/min): 24:31.86% 45:27.03% 66:18.91 600 oC, FR(g/min): 24:16.24% 45:25.72% 66:16.28% | 37.41% 38.67% 39.15% 32.44% 34.83% 41.96% 31.27% 33.14% 34.52% | 62.59% 61.33% 60.85% 67.56% 65.17% 58.04% 68.73% 66.86% 65.48% |
| [29] | RS–Turkey- Dp < 0:224, 0.224 < Dp < 0.425, 0.425 < Dp < 0.850, 0.850 < Dp < 1.250, 1.250 < Dp < 1.800, >1.8 mm | Steel fixed-bed reactor – GC- FTIR | Slow pyrolysis | 673, 773, 823 and 973 K; K HR=5 K/min, N2 of 50, 100, 200 and 400 ml/min, and steam of 0.6, 1.3, 2.7 cm/s | 673 K:23% 773 K:28% 823 K:30% 973 K:23% | 43% 39.5% 38% 37% 37% | 27% 24% 24% 30% |
| [30] | Rice husks – glass bed( 0.42 mm – 0.84 mm) size - Taiwan | Fluidized bed pyrolyzer –GC-MS | Slow pyrolysis | 600 oC - N2 =30 or 40 L/min –10 or 20 g/min raction time (Rt)=30 min | FR=10 g/ min -N2 =30 l/min : 20.42% FR=10 g/ min- N2 =40 l/min : 29.44% FR=20 g/ min- N2 =30 l/min :19.93% FR=20 g/ min- N2 =40 l/min : 27.14% | 30.65% 38.52% 33.63% 31.63% | 48.93% 32.04% 46.54% 41.23% |
| [31] | RH, dried- The size was 8–10 mm long, 2.0–2.5 mm wide and 0.1–0.15 mm thick | Fluidized bed reactor, T, MR, FR and fluidizing medium | Fast pyrolysis | 400, 450, 500, 550 oC, N2 at 3, 4, 5 L/min, FR=1.5, 2.5 g/min | 400 oC:50% 450 oC:51% 500 oC:45% 550 oC:34% N2: 3:45% 4:47% 5:48% FR: 1.5:44% 2.5:49% | 34% 32% 29% 27% 33% 32.% 33.5% 31% 32.5% | 17% 18% 24% 36% 22% 20% 18% 24% 17% |
| [32] | RH –dried - 355 to 500µm – Malaysia -biomass with various ratios of ZSM-5 catalyst (0.5–2) | Drop fixed-bed reactor - GC-MS, FTIR | Catlytic-Fast pyrolysis | 350, 400, 450, 500, 550, 600 °C | 350 oC:24.85% 400 oC:27.5% 450 oC:35.5% 500 oC:28.8% 550 oC:27.8% 600 oC:26% RH-ZSM-5 at 450 oC: 0.0:35.5% 0.5:30.5% 1.0:28.3% 1.5:26.7% 2.0:25.5% | 56.63% 49% 39.5% 37.7% 36.7% 33.35% 40.33% 50.1% 47.6% 42.7% 38.8% | 18.52% 23.5% 25% 33.5% 35.5% 39.35% 24.17% 19.4% 24.1% 30.6% 34.23 Gases (vol%):for non & cat. at loading ratios (0.0,0.5,1.0, 1.5, 2,0) H2: 0.42, 0.56, 0.66, 0.69, 0.74. CH4: 2.071, 4.10, 4.45, 4.62, 4.44. CO: 10.25, 23.85, 27.85, 26.54, 24.1, CO2 29.05, 33.45, 35.46, 37.85, 39.85. |
| [33] | RH | Fluidized bed - capacity 120 kg/h – GC-MS - FTIR | Fast pyrolysis | Rt of pyrolysis vapors < 2 s | The highest bio-oil yield about 50 wt% at 475 oC. Methanol was added into the bio-oil at 5, 10, 15 wt% | The char particles were burned in the combustion chamber to provide heat to the pyrolysis reactor. | CO, CH4 and CO2 |
| [34] | RS, 2-mm sieve. | Bench-scale auger,batch, fluidized bed –GC-MS, FTIR | Slow pyrolysis for Auger + batch Fast for FBR | 500 oC, N2 at 45 L/min | For Auger:25.7% For batch: 31.3% For FBR: 43.4% | For Auger: 44.9% For batch: 47.7% For FBR: 43.4% | For Auger: 13.2% For batch: 11.5% For FBR: 23% N2, O2, CO, CH4, CO2, C2H4, C2H6, C3H6, C3H8 |
| [35] | RS-Indonesia, size of 400 μm | Fixed bed reactor - GC-MS | Fast pyrolysis | 450 to 600 oC, SGR of N2 (1200 to 1582 mL/min), Ht – Rt=1.35 s | 450oC:22.08%, 500oC:31.86%, 550oC:30.84%, 600 oC: 20.4% Ht: 26% at 1.35s, max 27% at 1.53s and 25.5% at 1.78s |  | 63.83% 67.65% 57.18% 56.90% Ht: 67.5% at 1.35s, max 68% at 1.53s and 60% at 1.78s Levoglucosan (LG) (C6H10O5) |
| [36] | RS, wheat straw, corn stover, rape stalk and cotton stalk- 0.90 mm sieve | Tube furnace | Slow pyrolysis | 300-600 oC – HR=10 oC/min – Rt=30 min –N2 | 18.08±1.42% 35.56±0.98% 41.56±0.35% 41.25±0.28% 42.87±0.10% 40.54±0.77% 40.31±0.91% | 62.73±1.52% 46.60±0.24% 41.08±0.22% 37.79±0.16% 35.86±0.68% 35.02±0.21 35.79±1.47 | 7.44±0.39% 10.77±0.17% 14.72±0.21% 18.78±0.13% 19.64±0.43% 22.83±0.42% 24.11±1.58% CO2 (26.59 ± 0.01-73.48 ±0.73) CO (14.72 ± 2.59-51.51 ± 3.64) CH4 (0.16 ± 0.04-27.66 ± 6.21) H2 (1.76 ± 0.45-28.78 ± 1.69) CnHm (0.23 ± 0.06-4.31 ± 0.97) |
| [37] | RH, 10 mm screen size and corn stalk - China | Auger reactor system - speed 12 rpm, which corresponds to a solid residence time of 60 s - GC | Slow pyrolysis | 350, 400, 450, 500, 550 and 600 °C - | 350 oC:44% 400 oC:45% 450 oC:48.5% 500 oC:51% 550 oC:50% 600 oC:47% | 46% 44% 39% 35% 32% 31% | 10% 11% 12.5% 14% 18% 23% The gases consist of CO2, CO, CH4, H2 and some other light HC as: C2H4, C2H6, C3H6, C3H8 and n-C4H10 At 350 oC: 73.36% CO2, 24.15% CO, 74%CH4, 1.74% others At 400 oC: 71.47 % CO2, 24.23% CO, 2.19%CH4, 2.11% others At 450 oC: 66.47 % CO2, 24.46% CO, 6.17%CH4, 2.63% others At 500 oC: 60.57 % CO2, 24.86% CO, 10.13%CH4, 4.18% others, 0.26% H2 At 550 oC: 50.52 % CO2, 27.26% CO, 15.53%CH4, 5.03% others, 1.56% H2 At 600 oC: 41.41 % CO2, 31.06% CO, 17.45%CH4, 5.55% others, 4.53% H2 |
| [38] | RS - 1–1.5 cm long- alkali catalysts ofKOH,NaOH, K2CO3 – pressure of 2 -6 MPa final 18 MPa | a custom-built stainless-steel autoclave, GC-MS | Hydro-thermal lique-faction | 300, 325, 350 ◦C - Rt =30, 60 min, RS/ water (1:1, 1:5, 1:10,1:15 wt%) Methanol/ water (0:100, 25:75, 50:50, 75:25 (vol.%) | Rt=30 min.: 300 oC: 10.8 325 oC: 15.1 350 oC: 12.9 wt% Rt= 60 min: 300oC:12.3wt% 325oC:9.2wt% 350 oC:3.1wt% | 24.6wt% 25.6 wt% 1.4 wt% 24.6wt% 25.6wt% 20.0 wt% | 64.6wt% 59.3wt% 65.7 wt% 62.9wt% 67.9wt% 76.9 wt% |
| [39] | RS - India | Glass tube fixed bed reactor – GC/MS-FTIR | Slow pyrolysis | 300, 350, 400, 450 oC under CO2(50ml/min), N2 HR=20 oC/min, Rt = 1 h | For CO2:300 oC:31.4% 350 oC:34.1% 400 oC:34.5% 450 oC:34.1% For N2: 300 oC:29.2% 350 oC:30.6% 400 oC:31.0% 450 oC:29.8% | 47.0% 42.0% 38.0% 37.0% 39.2% 35.6% 34.2% 33.2% | 21.6% 23.9% 27.5% 28.9% 31.6% 33.8% 34.8% 37.0% |
| [40] | RS, RH, corn cob, wheat straw– india- 0.5 and 2 mm size | Fixed bed reactor- GC/MS-FTIR | Slow pyrolysis | 300-450 oC, N2 of 50 mL /min – HR=20 oC/min –Ht=1 h | RS: 300oC:25.9% 350oC:27.1% 400oC:28.4% 450oC:27.1% RH: 300oC:35.9% 350oC:36.2% 400oC:37.5% 450oC:38.1% | 300oC:35.1% 350oC:35.0% 400oC:33.5% 450oC:33.1% 300oC:43.3% 350oC:37.2% 400oC:35.3% 450oC:35.0% | 300oC:39.0% 350oC:37.9% 400oC:39.1% 450oC:39.8% 300oC:20.8% 350oC:26.6% 400oC:27.2% 450oC:26.9% |
| [41] | RS - 5 mm size | Fluidized bed reactor system 3kg/hr –GC/MC | Slow pyrolysis | 412, 443, 516, 545, 598 oC-Rt= 118, 87, 67, 80 min – FR= 864, 1034, 1397, 1125kg/h | 412 oC:49% 443 oC:47% 516 oC:48% 545 oC:42% 598 oC:37% | 30% 30% 25% 26% 25% | 18% 19% 25% 28% 42% |
| [42] | RS-Torrefaction and dilute acid (Acetonitrile and dimethyl sulfoxide) pretreatment - size of 2 mm | Micro-pyrolysis reactor | Torre-faction and fast pyrolysis | Torref. at 225 °C, 250 °C, 275 °C for 30 min. in a Py-GC/MS reactor. – Pyrolysis at 450, 500, 550 oC – HR=1000 oC/s, Ht=20 s | Pyrolysis: 450 oC:37% 500 oC:39% 550 oC:47% Torrefaction +pyrolysis at 450 oC): 225 oC: 16, 20% 250 oC: 28, 16% 275 oC: 42, 10 % Torrefaction +pyrolysis at 500 oC): 225 oC: 14, 25% 250 oC: 23, 23% 275 oC: 33, 12 % Torrefaction +pyrolysis at 550 oC): 225 oC: 17, 26% 250 oC: 22, 22% 275 oC: 32,13% | Torrefaction: Pyrolysis at 450 oC: 225 oC:82% 250 oC:70% 275 oC:56% Torrefaction: Pyrolysis at 500 oC: 225 oC:84% 250 oC:75% 275 oC:62% Torrefaction: Pyrolysis at 550 oC: 225 oC:82% 250 oC:75% 275 oC:63% Pyrolysis: 450 oC:51% 500 oC:48% 550 oC:37% Pyrolysis at 450 oC and torrefied: 225 oC:51% 250 oC:49% 275 oC:44% Pyrolysis at 500 oC and torrefied: 225 oC:46% 250 oC:44% 275 oC:43% Pyrolysis at 550 oC and torrefied: 225 oC:42% 250 oC:42% 275 oC:43% | Pyrolysis+Torrefaction: 10% (RS) 10+1% 4+1% 2+2% 11%(RS) 12+1% 7+4% 6+4% 13%(RS) 12+1% 10+2% 7+4% |
| [43] | RS-0.6-1.18 mm -dolomite (300 µm) zeolite ZSM-5– Malaysia | Fixed bed reactor –FTIR-CHN-S Analyzer | Catalytic slow pyrolysis | 450 oC- HR = 77.63 oC/min, Ht = 2.61 min - N2 SGR = 100 cm3/min. | Without cat.:27.6% With zeolite ZSM-5: 26.7% With dolomite: 45.7% | Without cat.:26.3% With zeolite ZSM-5:25.3% With dolomite: 48.4% | Without cat.:23.2% With zeolite ZSM-5: 24.8% With dolomite: 52% |
| [44] | Rice straw - 0.5-2 mm size | Fixed bed reactor under prototype hydropyrolysis unit- GC-MS –HNMR and FTIR | Slow pyrolysis | 300, 350, 400, 450 °C and P of 1,10, 20, 30, 40 bar in H2 and N2, Ht =1.0 h - N2 of 50 ml/ min | Slow pyrolysis: 300 oC: 29.2% 350 oC:30.6% 400 oC:31% 450 oC:29.8 % Hydropyrolysis 1 bar: 300 oC: 14.2% 350 oC: 17% 400 oC: 20.3% 450 oC: 16.9% Hydropyrolysis 40 bar: 300 oC: 8.8% 350 oC: 9.2% 400 oC: 9.7% 450 oC: 8% | 39.2% 35.6% 34.2% 33.2% 43.9% 40.1% 35.8% 36.4% 47.3% 41.3% 37.5% 37.8% | 31.6% 33.8% 34.8% 37% 41.2% 42.9% 43.9% 46.7% 43.9% 49.% 52.% 54.% |
| [45] | RS - Acid pretreatment (5vol%HCl), <1.0 mm size | Parr pressure reactor –GC -FTIR | Slow pyrolysis | 500 oC and P = 0.69 MPa, HR=3.4 oC/min | Untreated: 25% Treated,T: 28% | 47% 50% | 17% 15% - Gases for untreated and treated RS: CO:15%, 17%, CO2:51%,48%, CH4:11%, 8%, H2:1%, 0.5%, C2H2: 2%, 1% |
| [46] | RH (280 µm sieve) – Australia | Solar pyrolysis reator (70 kW/m2) – GC/MS | Solar pyrolysis | 500, 600, 700 and 800 °C at a heating rate of 160 ± 6 °C/min | 500 oC:42% 600 oC:40.7% 700 oC:43.1% 800 oC:38.7% | 43.0% 42.86% 36.32% 35.52% | 14.0% 16.42% 20.55% 25.48% Gases:CO2,CO,CH4,C2H4,C2H6, H2 |
| [47] | RH and sawdust - 40 mesh - china | Entrained flow Reactor –gas analyzer | Flash pyrolysi | 700–1000 °C, N2 -residence time of 0.8 s. | 700 oC:35% 800 oC:31% 900 oC:24% 1000 oC:25% | 32% 29% 27% 26% | 35% 40% 50% 51% Gases: CO, CO2, H2, CH4, C2H4 and LHV gases |
| [48] | RS, 1–3 mm size –Australia | Microwave-hydro-thermal carbonization (MIHTC) | Micro-wave hydo-thermal - RSM | 1200 W and temperature of 230 ◦C | - | The hydro-char ranged from 37.95% to optimum 57.89% at 180 oC, 20 min, 1.1.5 (B/W) ratio | - |
| [49] | Rice husk, China, | Continuous downdraft circulating fluidized bed - capacity of 3 t/h - 1.2 and 1.6 mm ceramic balls | Fast pyrolysis | 550oC - helium flow rate 1.0 mL/ min - 1 to 3 t /h | 43.1 - 53.2% Average at different Rt and FR:47. 47.7 ± 2.7 bio-oil peaked at 53.2 wt%. | 27 - 34 wt% 30.6 ± 2.0% | 16.8 - 27.5 wt% 21.8 ± 2.8 wt% Gases:CO2(41.25%), (z)-2-butene (10.97%), acetone(15.55%), methyl formate(4.88%), isobutane (4.16%), acetic acid (10.59%) ammonia (5.17%) |
| [50] | RH – China - 0.25 - 0.4 mm size | Semi fluidized bed–GC/MS | Fast pyrolysis | 400, 500, 600 oC, -N2 at 2.2 m3/hr - | 400oC:<30% 500oC:~34% 600oC:~33% | 400oC:>50% 500oC:~47% 600oC:~40% | 400oC:<17% 500oC:<20% 600oC:<27% |
| [51] | RH - < 0.15 mm, 0.15-0.30 mm, 0.30-0.60 mm, 0.60-1.18 mm and 1.18-1.80 mm. | Fixed bed reactor - GC-MS, FTIR | Slow pyrolysis | 400 and 600°C –HR of 20,40, 60°C/min | 400 oC:22.57% 450 oC:28.7% 500 oC:30.1% 550 oC:29.5% 600 oC:29.05% For dp(mm): <0.15: 22.57% 0.15-0.3:25% 0.3-0.6:27% 0.6-1.18: 30% 1.18-1.8:31.3% HR(oC/min): 20:29.37% 40:30.7% 60:31.78% | 39.98% 37.3% 36.26 % 33.5% 32.53% 34.17 % 36.2% 36.3% 35.5% 36.37% 42.52% 39.0% 36.04% | 32.83% 32.5% 33.5% 36.5% 38.42% 43.26% 38.1% 36.0% 34.1% 32.31% 27.5% 30.0% 32.0% |
| [52] | RH –Taiwan - 1.68 mm to 3.36 mm and dried in a 110 °C | Fluidized bed pyrolyzer-GC/MS | Slow pyrolysis | 500 and 600 oC - carrier gas of N2 – 10, 20 gm/min feeding rate (FR) -superficial gas velocity is 0.225 -0. 425 m - sodium glass beads of size range of 0.42- 0.84 mm – | At 500 oC, FR =10 gm / min: superficial gas velocity(m/s): 0.255:19.5% 0.340:20.5% 0.425:17.9% At 500 oC and FR 20 gm/ min: 0.255:29.4% 0.340:30.4% 0.425:27.6% At 600 oC and FR =10 gm /min: 0.255:18.4% 0.340:19.8% 0.425:14.2% At 600 oC and FR =20 gm/min: 0.255:26.5% 0.340:27.1% 0.425:24.1% | 31.7% 32.2% 31.5% 38.5% 36.1% 34.7% 30.7% 33.6% 32.2% 37.1% 31.6% 33.6% | 48.8% 47.35 50.6% 32.0% 33.5% 37.7% 50.9% 46.5% 53.6% 36.4% 41.2% 42.3% |
| .[53] | RH-Indonesia -0.25-1 mm size | S.-steel tubular reactor | Slow pyrolysis | 450, 500, and 550 °C for 1 h –HR=8 ⁰C/min | 450 oC:16% 500 oC:27% 550 oC:29% | 60% 59.5% 57.5% | 23% 12.5% 12% |
| [54] | RH –Nigeria -1-4 mmm size | Fixed bed reactor | Slow pyrolysis | 500-650 oC – Rt= 30-120min | 24 to 38.49% For 60 runs | 37 to 54.48% 49.5, 44.6 | 21 to 25.21% |
| [55] | RH –Tailand - < 35 mesh size | Fixed bed reactor | Slow pyrolysis | 400, 500 and 600 °C – N2 at 10 L/min - | 400 °C: 38% 500 °C: 40% 600 °C: 30% | 49.5%, 44.6% 38.6 %wt. | 12% 14% 32% |
| [56] | RH – dried 0.5-7 mm size | Fixed bed pyrolysis reactor –GC/MS - FTIR | Slow pyrolysis | 430-580 oC - natural gas at 1.5 L/min -residence time was 1.2 min. – FR=200 gm/h | 430 oC:30% 450 oC:35% 480 oC:40% 500 oC:40% 550 oC:35% 580 oC:30% | 50% 40% 35% 33% 31.5% 30% | 20% 24% 24% 27% 33% 40% |
| [57] | RS, RH, bagasse, corn cob-Vietnam- (0.18 -0.50 mm, 0.50 -1.00 mm, and 1.00 -2.00 mm) sizes | Fluidized bed reactor | Fast pyrolysis | N2 at 4.0 to 7.2 L/ min – 470 to 515 oC | RS: N2 at 6 L/min, 0.18-0.5 mm size: 470 oC:48.5% 480 oC:50% 490 oC:51% 500 oC:52.8% 510 oC:48% 515 oC:48% SGR ( 500 oC, 0.18-0.5 mm size): At 4 L/min, <50%, At 7.2 L/min 50%, max 52% at 6 L/min ( FR=6 L/ min and 500 oC): particle size, mm 0.18-5: 52.76% 0.5-1.0: 50% 1.02.0: 48.52% (6 L/min, 500 oC, 0.18-0.50 mm) RS: 52.76% RH: 55.41% | 34% 33.5% 32% 31% 31% 30% At 4 l/min, ~32% -at 7.2 l/min ~36% 32.24% 33.0% 37.48% 33.12% 32.83% | 16% 15% 14.5% 14% 18.5% 20% At 4 l/min, ~20% and at 7.2 l/min ~13% 15% 17% 14% 14.12% 11.76% |
| [58] | RS, RH, Wheat, maize, - 3 cm length | Mobile bench-scale pyrolyse | Slow pyrolysis | 400 oC, HR =5 oC/min –Rt=2h | RS:25.4% RH:19.1% | RS: 43.8% RH:42.8% | RS:30.8% RH:38.1% |
| [59] | RH -4 different types of sieves (10, 50, 100 and 200 mesh size) | Split-tube furnace feeding rate 20 cm3/min - FTIR | Slow pyrolysis | 500 oC, N2, retention time (15, 30, 60 and 90 min.)-HR=1,2,5,10 oC/min – air rates (AR) of 20, 50,100,200 cm3/min - retention time (Rt) of 15 to 90 min. | 300 oC: 13% 400 oC:17.85% 500 oC:18.72% 600 oC:20% 700 oC:18.8% Rt (min): 15:17.89% 30:18.5% 60:18.0% 90:19.0% HR (oC/min): 1.0:15.45% 2.0: 21.38% 5.0:20.4% 10:20.2% AR(cm3/min): 20:18.72% 50:20.3% 100:22.54% 200:22% Particle size (mesh): <200:24.67% 200-100:20.8% 100-50:19.7% 50-10:18.72% | 57.13% 42.2% 38.8% 37.17% 37.19% 40.58% 39.5% 38.8% 38.06% 39.1% 39.0% 38.6% 37.8% 39.14% 38.2% 37.3% 36.09% 33.96% 37.06% 38.06% 39.14% | 25.64 % 27.95% 36.4% 40.83% 42.50 % 33.87 % 36.9% 38% 38.23 % 37.45% 31.85 % 35% 37% 36.71 % 38.5% 38.7% 39.78 % 35.87% 36.7% 38.87% 35.8% |
| [60] | RH-Argentina acid leach in a HCl (5% v/v) during 1 h, with a ratio of 50 g RH:1 L HCl | lab-scale fast pyrolysis under vacuum conditions (1-5 Torr) –GC/MS | Catalytic fast pyrolysis | 300, 400, 500, 600 and 700 ◦C-reaction time 20 min. | For RH: 300oC:14% 400oC:34% 500oC:28% 600oC:25% 700oC:27% For A-RH: 300oC:28% 400oC:47% 500oC:43% 600oC:40% 700oC:39% | For RH: 300oC:45% 400oC:29% 500oC:21% 600oC:23% 700oC:19% For A-RH: 300oC:46% 400oC:34% 500oC:29% 600oC:22% 700oC:25% | For RH: 300oC:41% 400oC:37% 500oC:51% 600oC:52% 700oC:54% For A-RH: 300oC:26% 400oC:19% 500oC:28% 600oC:38% 700oC:36% |
| [61] | RS-1-2 mm size | Pilot scale entrained flow reactor –Aspen Plus | Fast pyrolysis | 450 to 600o C - N2 =15 to 30 L/ min-Rt= 1-5 s | 27% + 20% water and others | 27% char+ash | 26% |
| [62] | RH-Nigeria – 40 mm mesh – catalytic CuO/ Kaolin | Pyrex glass reactor - GC-MS | Slow pyrolysis | 350 oC - heating rate of 10oC/min – 1 to 5 min. | Raw RH.: 20.42±0.76 % RH+CuO/Kaolin: 21.62±0.83% | 62.33±0.49% 45.02±0.16 | 17.25±0.76% 33.36±0.34% |
| [63] | RH, Coconut and Walnut shell, gracilis, etc.– Iran – 150 μm size | Fixed bed reactor of quartz glass tube | Slow pyrolysis | 500 o C – HR= 100 o C/min, Rt = 30 min.-Argon = 30 mL/min | 44.1% | 33.2% | 23.7% CO2 (45%), CO (27%), H2 (18%), CH4 (7.5%), C2-C4 (2.5%) |
| [64] | RH - <0.25 mm, 0.250 - 0.355 mm and 0.355 – 0.50 mm size | Semi-Batch Reactor- GC/MS- | Slow pyrolysis | 400, 450, and 500˚C, HR of 10, 15, and 20 oC/min, N2 of 100, 300, and 500 mL/min. | Bio-oil:400 oC: <0.25:29.27% 0.25-0.355: 30.17% 0.355-0.5: 31.025% 450 oC: <0.25:30.51% 0.25-0.355: 30.94% 0.355-0.5: 31.82% 500 oC: <0.25:29.91% 0.25-0.355: 30.33% 0.355-0.5: 31.21% 100 ml/min & HR: 10:28.6% 15:31.52% 20:31.82% 300 ml/min &HR: 10:24.28% 15:27.2% 20:27.5% 500 ml/min &HR: 10:23.11% 15:26.03% 20:26.33% | Bio-oil: 100 ml/min &size: <0.25: 30.51% 0.25-0.355: 30.94% 0.355-0.5: 31.82% 300 ml/min&size: <0.25:26.19 % 0.25-0.355: 26.62% 0.355-0.5:27.5% 500 ml/min&size: <0.25:25.03 % 0.25-0.355: 25.45% 0.355-0.5:26.33% 10 oC/min & size: <0.25: 27.29% 0.25-0.355: 27.72% 0.355-0.5:28.6% 15 oC/min & size: <0.25: 30.21% 0.25-0.355: 30.46% 0.355-0.5:31.52% 20 oC/min & size: <0.25: 30.51% 0.25-0.355: 30.94% 0.355-0.5:31.82% No char | Bio-oil: 100 ml/min &temperature: 400oC:31.05% 450oC:31.82% 500oC:31.21% 300 ml/min &temperature: 400oC:26.73% 450oC: 27.5% 500oC:26.89% 500 ml/min &temperature: 400oC:25.65% 450oC:26.33% 500oC:25.73% 10 oC/min &temperature: 400oC:27.83% 450oC:28.5% 500oC:27.99% 15 oC/min &temperature: 400oC:30.75% 450oC:31.52% 500oC:30.91% 20 oC/min &temperature: 400oC:31.05% 450oC:31.82% 500oC:31.21% No gases |
| [65] | RS, RH, corn stover, sugar-cane bagasse, peel, coffee waste,bamboo leave-.297mm | Single-mode microwave oven - 2.45 GHz frequency –GC-MS | Slow pyrolysis | N2 at 50 mL/min – 30 min. | RS: 44% RH: 49% | 20% 22% | 36% 30% RS: 25% H2, 7%, 51%CO, 14% CO2 RH: 25% H2, 7%, 51%CO, 13% CO2 |
| [66] | RS - 10 mm - Biochar with concentration of 5% of the weight feedstock- biochar was produced from MAP of RS at 700-W for 20 min | Solar photovoltaic (PV)-powered microwave heating -1000 W max | Slow pyrolysis | –N2 at 50 mL/min- 300, 500, 700 and 900 W -reaction time (Rt) (15, 20 and 25 min) | Raw RS: Rt of 15 min: 300 W:11% 500 W:16% 700 W:19.5% 900 W:20% Rt of 20 min: 300 W:11.5% 500 W:17.2% 700 W:23.14% 900 W:21.5% Rt of 25 min: 300 W:10% 500 W:17% 700 W:22.5% 900 W:21.5% With add: Rt of 15 min: 300 W:20.2% 500 W:21% 700 W:23.5% 900 W:24% Rt of 20 min: 300 W:23.3% 500 W:21.7% 700 W:25.18% 900 W:25.0% Rt of 25 min: 300 W:22.8% 500 W:23.1% 700 W:24.0% 900 W:24.8% | 46% 42% 40% 37% 42.5% 38.8% 38.20% 37% 37.5% 36% 34% 32.5% 39.8% 37% 35.5% 34.5% 37.7% 36.3% 36.0% 34.5% 34.7% 34.5% 33.0% 33.5% | 43% 42% 39.5% 43% 46% 44% 38.66% 41.5% 52.5% 47% 43.5% 46.5% 40% 42% 41% 41.5% 39% 42 38.82% 40.5 42.5% 42.0% 43.0% 41.7% |
| [67] | RH - 0.16 mm size sodium chloride (NaCl) catalys (1, 2, 3, 4, 5 wt.% of RH)- China | Fixed bed reactor – GC/MS | Ctalytic Slow pyrolysis | 550 °C, a HR of 20 °C/min, N2 flow rate of 300 mL/min | Non-catalytic:53.81 % cayalytic(%RH): 1.0:55.0% 2.0:56.5% 3.0:57.61% 4.0:56.0% 5.0:54.5% | 37.64% 36.64% 36.0% 36.5% 36.5% 36.5% | 8.55 wt.% 8.36% 7.5% 5.89% 7.5% 9.0% Gases: H2, CH4, CO, CO2 CO > CO2 > H2 > CH4 fractions |
| [68] | RS, Pterocar- pus indicus, Cunninghamia lanceolata, etc. | Fluidized bed reactor – 2 kW -3kg/hr – GC/MS | Fast pyrolysis | 723 to 973 K, N2 = 3–6 Nm3/ h , 154 to 250 µm particle size | RS at 773 K, dp = 154–250 µm : 33.7% + 53.5% water | - | - |
| [69] | RH –catalytic ZnO (5, 10, 15, 20 wt.% of raw material) – China - 0.3 < Dp < 0.6 mm - particle size 0.1–0.2 mm of catalytic | Fixed-bed reactor – GC-MS - FTIR | Catalytic -Slow pyrolysis | 400,450,500,550, 600 or 700 °C - heating rate of 25 °C/min was kept constant – N2 of 50, 100, 150, 200, 250, 300 or 400 mL/min at 550 oC | 400 oC:41.51% 450 oC:46% 500 oC:47% 550 oC:49.91 600 oC:48.5% 700 oC:47% N2 (mL/min.): 50:45.48% 100:47.5% 150:49.65% 200:48% 250:46% 300:44.5% 400:42.88% Catalytic (%): 5:47.02% 10:45% 15:42% 20:41.05% | 38.48% 33% 30.5% 27% 26% 25.61% 30% 28% 27% 26.5% 26% 25.5% 25% 31.5% 31% 30% 30.3% | 20.01% 21.5% 22.0% 22.5% 25% 27.41% 24.11% 23% 22% 24% 27% 28% 31.21% 21.38 24.5% 26% 28.74% |
| [70] | Rice husk, 0.15–0.45mm | Vertical tubular fixed-bed reactor – GC-MS | Slow pyrolysis | SGR= 10 mL/min to 500 mL/min - The gas pressures from 0.1 MPa to 5.0 MPa – HR of 15 oC/min - room temperature to 700 oC for Rt of 60 min | Constant gas flow velocity: At Patm 27.50% + water 0.5MPa:19.5% 1.0MPa:18% 3.0MPa:14% 5.0MPa:12.5% Constant volume flow rate: 0.1MPa:36.2% 0.5MPa:23% 1.0MPa:17.5% 3.0MPa:16% 5.0MPa:13.5% | 33.92% 36% 37% 37% 37.3% 33% 36.2% 37% 37.5% 37.5% | 16.10% 17% 17.5% 19.5% 20% 16.3% 18% 20% 20% 20.2% |
| [71] | RH - (100 > dp > 355μm –catalyzed and non-catalyzed | Drop‐type pyrolyzer – GC/MS | Cataltic Fast pyrolysis | 450 oC – 10 min reaction time. | Non-catalyst:20% SAPO‐34 zeolite:10% ferrierite zeolite:12% MCM‐22 Zeolite:10% ITQ‐2 zeolite: 10% ZSM‐5 zeolite: 10% MORD zeolite: 10% (rest is water) | 40% 42% 40% 40% 40% 39% 42% | 25% 28% 28% 29% 29% 27% 28% |
| [72] | Brunei RH - ZSM-5, Al-MCM-41, Al-MSU-F and Brunei rice husk ash (BRHA)( 550 ◦C for 3 h) - 355–849 µm for RH | Fixed-bed reactor for biomass feed, coupled to a secondary fixed-bed reactor for catalyst | Catalytic slow pyrolysis – GC/TCD | Primary reactor: 450 oC – HR=25 oC/min. Secondary reactor: 490–540 ◦C – N2 at 50 cm3/min | Non-catalyst: 39.61% ZSM-5 Al: 38.29% MCM-41: 39.98% Al-MSU-F:39.59% BRHA:38.29% | 41.92% 42.27% 43.15% 43.31% 42.27% | 18.47% 19.45% 18.80% 19.18% 21.62% Gasses: CH4 (vol.%): 2.06, 2.86, 1.72, 1.49, 4.65 CO:9.14, 3.38, 11.28, 7.03, 7.76 CO2: 75.40, 83.19, 74.20, 78.80, 76.33 |
| [73] | RH - zeolite ZSM-5 catalyst - size 0.25–1.0 mm - ize of the catalyst was 0.2 cm diameter | Fluidized bed reactor - bed material quartz sand with a mean diameter of 250 m - feedrate of 0.200 0.015 kg/ h - GC | Catalytic fast pyrolysis – | 400, 450, 500, 550 and 600 oC - Helium gas flow rate of 2 cm3 /min | 400oC:46.5% 450oC:43.5% 500oC:37% 550oC:28.5% 600oC:21.5% rest water Pyrolys / catalytic (%): 500-400oC:7.2% 500-450oC:6.7% 500-500oC:4.4% 500-550oC:3.8% 500-600oC:3.4% | 400oC:33% 450oC:32% 500oC:29% 550oC:26.8% 600oC:25.5% Pyrolys/ catalytic: 500-400oC: 22.2% 500-450oC: 26.6% 500-500oC: 36.2% 500-550oC: 39.7% 500-600oC:41.0% Coke at same T: 12.0%, 10.7%,9.7%, 9.6%, 7.8% | 400oC:6.5 % 450oC:10 % 500oC:17.5% 550oC:25.4% 600oC:34.5% Pyrolys /catalytic (%): 500-400oC:7.2% 500-450oC:6.7% 500-500oC:29.6% 500-550oC:29.5% 500-600oC:29.3% |
| [74] | RS- 40 mesh size - straw washed and stirring with hydro-fluoric acid (48 wt. % HF in H2O) - Korea | Fluidized bed – 300 g/h- slica sand (SiO2 > 99%; 450–550 µm particle size) –GC/MS | Fast pyrolysis | 350, 420, and 500 °C – N2 at 15 L/min - residence time 1.2 s – HR of >1000 °C/s | Raw straw: 350oC:45% 420oC:40% 500oC:35% HF-straw 350oC:54% 420oC:45% 500oC:37% | Raw straw: 350oC:25% 420oC:23% 500oC:19% HF-straw 350oC:18% 420oC:10% 500oC:8% | Raw straw: 350oC:30% 420oC:32% 500oC:50% HF-straw 350oC:28% 420oC:45% 500oC:58% |
| [75] | RH, RS, maize stalk, cotton straw - particle sizes <0.295 mm | Bench-scale fixed- bed pyrolysis system – Gas analyzer-FTIR | Fast pyrolysis – Gas analyzer- FTIR-TCD | 600 to 1000 °C - | Rice straw(ES): 600 oC:45.5% 700 oC:38.5% 800 oC:33% 900 oC:27.7% 1000 oC:27.9% Rice husk(RH): 600 oC:42.8% 700 oC:36.5% 800 oC:31.5% 900 oC:27.5% 1000 oC:27.1% | 31.2% 30% 28.5% 27.7% 26.2% 32.3% 31% 29.2% 28.5% 27.4% | 23.3% 30.5% 37.5% 44.5% 45.9% 24.9% 37.4% 38.8% 44.3% 45.5% Gases (600 to 1000 oC):CO: 42.5% to 54.9% (RS)-45.6 to 59.7% (RH) CH4:7.2 %to 20% (RS)- 15.7 to 21.6% (RH) - CO2:36.5% to 21% (RS) - 39% to 15% (RH) |
| [76] | RS, bamboo sawdust - sizes of 0.6 and 0.85 mm | Bubbling fluidized bed equipped with a char separation system - quartz sand (1.5 kg), the mean particle size of ca. 0.4 mm –GC/MS | Fast pyrolysis | 414, 445, 471, 491, 542 oC in for the rice straw – feed rate (FR) of 1.6, 2.5, 3.3 g/min | 414 oC:45% 445 oC:68% 491 oC:67.5% 542 oC:50% RS of size 5 mm and 491oC: 68.5% RS of size 10 mm and 490oC: 61% FR of 1.6 g/ min and 491oC: 64% FR of 3.3 g/ min and 487 oC: 68% | 45% 18% 18% 25% 17% 20.5% 18% 16% | 13% 13.5% 13.5% 22% 14% 16% 18% 13% Gases at 414-542 0C: CO: 25 - 30%, CO2: 76- 60%, CH4:2 - 6% Other hydro-carbon C1-C4. |
| [77] | RS and corn stover - 1000 µm size-Italy | A lab-scale, cylindrical, and fixed-bed semi-batch reactor | Fast pyrolysis | 250–300, 300–350, 350–400, 400–450, 450– 500, 500–550, and 550–600°C – Rt = 10, 20, 30 s | Rt (s): 10:50.2% 20:53.2% 30:54.7% 250–300oC: 17% 300–350oC:22.5% 350–400oC:33% 400–450oC:41% 450–500oC:51% 500–550oC:48.5% 550–600oC: 45% | 54.3% 53.0% 52.2% 71% 64.5% 53% 42% 31.5% 25.5% 21% | 50.6% 51.2% 51.6% 12% 13% 14% 17% 17.5% 26% 34% At 400-600 oC: (2-5.5%) H2, (4-7.5%) CH4, (40.9-35%) CO, (50.7-46.5%) CO2 |
| [78] | RH, cassava peel, corn stalk - 150 – 180 𝞵m – ratio of mixing (1:1:1, 2:1:1, 1:2:1, 1:1:2wt) | Fixed bed reactor | Co-fast pyrolysis | N2 at 3 mL/min- HR=25 oC/min - 400–600 o C - residence time (∼2s) | Mix 1:1:1: 400 oC: 13% 525 oC: 25% 600 oC: 17% Mix 2:1:1: 400 oC: 25% 525 oC: 55.6% 600 oC: 38% Mix 1:2:1: 400 oC: 11.5% 525 oC: 29% 600 oC: 21.5% Mix 1:1:2: 400 oC: 15% 525 oC: 31% 600 oC: 24.5% | - | - |
| [79] | Raw RH, cellulose removed (hemicellulose + lignin), hemicellulose removed (cellulose + lignin), and lignin removed (cellulose + hemicellulose) – India- NaOH and H2SO4 used for removal | Tubular furnace – 5 g | Slow pyrolysis | 300, 350, 400, 450, 500, and 550℃ - N2 - residence time of 30 min - HR = 4 oC/min | Untreated RH: 300 oC: 22% 550 oC:35.6% Cellulose-removed RH: 300 oC: 12% 550 oC:18.6% Hemicellulose-removed RH: 300 oC: 12% 550 oC: 20.6 % Acid hydro- lyzed RH: 300 oC: 25% 550 oC: 33.6% Alkaline Hydro -lyzed RH: 300 oC:19% 550 oC:32.4% | 300 oC:59.2% 550 oC:46.4% 300 oC:60.0% 550 oC:46.6% 300 oC:58.0% 550 oC:43.0% 300 oC:61.2% 550 oC:42.8% 300 oC:56.4% 550 oC:37.4% | 300 oC:12.0% 550 oC:15.6% 300 oC:29.0% 550 oC:35.6% 300 oC:31.6% 550 oC:35.0%, max 40 % at 400oC 300 oC: 12.6% 550 oC:23.6% 300 oC:23.6% 550 oC:30.2% |
| [80] | RH, (20% of total weight of rice) -particle size of 212 μm | Fixed bed reactor | Slow pyrolysis | HR of 20 °C/min - 300ºC, 400°C and 500ºC at residence times 1, 1,5 and 2h (isothermal process) – N2 of 100 ml/min | 300 oC, HR =5 oC/min, 1 hr: 33.0 % 400 oC, HR =5 oC/min, 1.5h: 32.06 % 500 oC, HR=5 oC/min, 2h: 17.93% 300 oC, HR=10 oC/min, 2h:36.13 % 400 oC, HR=10 oC/min, 1h: 38.08 % 500 oC, HR=10 oC/min, 1.5h: 33.28 % 300 oC, HR=20 oC/min, 1.5h: 30.86 % 400 oC, HR=20 oC/min, 2h: 33.98 % 500 oC, HR=10 oC/min, 1h: 31.88 % | nd nd 5.4% nd nd nd 28.5% 18.22% 30.1% | 11.63 14% 12.4% 51.48% 33.57% 49.56% 38.3% 44.03% 32.7% |
| [81] | RH, wood, forestry wood residue – Malaysia - 1.4 and 2.8 mm for RH | Fixed bed reactor – GC/MS | Fast pyrolysis and slow pyrolysis | 750-1050 °C, under fast pyrolysis at temp. up to 1050 °C, with HR of 300-500 °C/s For slow pyrolysis 850°C at a HR of 10°C /min | RH :Fast Pyrolysis: 750 oC:12.01% 850 oC:10.22% 950 oC:8.13% 1050 oC:6.19% Slow pyrolysis: At 850 oC: 60% | 20.60% 16.21% 15.86% 13.12% 15.0% | 60.43% 66.61% 74.55% 77.43% 23.5% Gasses: CO: 45.01, 46.17, 48.31, 49.40% - H2 :21.84, 25.32, 27.83, 30.3% - CO2:15.06, 12.98, 11.33, 8.65% - CH4:11.92, 10.65, 8.94, 8.67% - C2-C4: 6.17, 4.88 , 3.59, 2.99% |
| [82] | RH – china - raw rice husk (RH), acid washed rice husk(AWRH) | Two stage reactor (pyrolysis zone (stage I) and catalytic zone (stage II)) | Catalytic fast pyrolysis | 500 oC residence time 15 min | With catalytic RH-N: 34.92% With catalytic AWRH-N: 35.14% Without catalytic RH: 24.49% AWRH 24.13% | 37.03% 33.81% 36.08% + 2.18% Coke 33.41% + 2.62% Coke | 28.05% 31.05% 37.25% 39.84% |
| [83] | RH – RH char (RHC)- catalytic – Ni (NO3)2 Fe(NO3)2, Cu(NO3)2, -50 g RH blended with 15 g catalyst | Microwave pyrolysis oven 3600 W -GC/MC-TCD | Catalytic microwaves pyrolysis | 700 W in the N2 atmosphere for 20 min - N2 with 150 L/h | No cat.: 21% RHC: 15% Ni/RHC:10% Fe/RHC:16% Cu/RHC:12% Effect of Ni in catalytic: 0.5Ni/RHC:12.5% 1.0Ni/RHC: 10% 1.5Ni/RHC: 9.2% 2.0Ni/RHC:8.8% | 42.5% 38% 36% 34% 37% 37.5% 35.5% 35.2% 35% | 34.5% 46% 53% 49% 50% 50.0% 53.7% 55.5% 56.5% |
| [84] | RS 0.1–0.3 mm - (ZSM-5, LOSA-1, Gamma-Al2O3 and spent FCC catalyst-.063 and 0.154 mm | Internally interconnected fluidized bed (IIFB), GC/FID | Catalytic fast pyrolysis | 550 oC-N2=2.4 L/min in horizontal tube, N2=1.0 L/min in vertical tube, N2=0.5 L/min for fluidizing gas – FR= 44 g/h for 30 min | 12.8% and 10.5% max. of aromatics and C2-C4 olefins were obtained with ZSM-5 catalyst - aromatic + olefin decreases in the order: ZSM-5 > LOSA-1 > spent FCC catalyst > Gamma-Al2O3. | Max. value (32.3%) with ZSM- Gamma- Al2O yield lowest 22.7% coke and 43.9%undefined compounds - | ZSM-5: 21%CO,12.5%CO2, 1.5% CH4 LOSA-1:17.5%CO, 11.5%CO2, 2.5%CH4 Gamma-Al2O3: 11.5%CO,10%CO2, 2.8%CH4 Spent FCC: 15.5%CO,12.5%CO2, 3.2%CH4 |
| [85] | Pretreatment RH, LTRH, MTRH, STRH for raw rice husk torrefied at diff temp. - acid leaching process performed for raw and torrefied husk | Vertical drop fixed-bed reactor for pre-treatment torrefaction, | Slow pyrolysis | SGR of N2 = 200 mL/min -550 oC -5 min - HR = 10oC/min torrefaction temps. of 210, 240, and 270 C for 1h. | Pyrolysis: RH:40.2% LRH:37.6% MRH:30% SRH:16% Acid washing: W-RH:44.4% W-LRH:40.2% W-MRH:31.5 W-SRH:16.7% Torrefaction+pyrolysis: RH: 40.0% LRH: 37.5% MRH: 35% SRH: 32% Acid washing: W-RH: 45% W-LRH: 40.5 % W-MRH:35.5% W-SRH:33 % | 32.1% 35.4% 45.0% 64.2% 27.5% 32.5% 42.0% 59.5% 32% 32.5% 34% 35.6% 27% 28.5% 31% 32.5% | 27.7% 27.0% 25.0% 19.8% 28.1% 27.3% 26.5% 23.8% 28% 30% 31% 32.4% 26% 28% 31% 33.5% |
| [86] | Rice husk -0.2-0.6 mm | bench-scale fluidized-bed reactor- hot vapor filtration (HVF)–GC/MS-FTIR | Fast pyrolysis | N2 at 60 L/min | bio-oil yield decreased from 41.7% using cyclone alone to 39.5wt% due to HVF(hot vapor filter) | - | H2 (mol.%) 12.8 % before (BHVF)16.9% after (AHVF) CO: (mol.%) 45.2% BHVF, 51.4% AHVF: CO2(mol.%) 13.1% BHVF, 13.4% AHVF, CH4(mol.%): 11.7% BHVF, 13.4% AHVF- C2-C4’sa (mol.%): 17.2 BHVF 4.9%, AHVF (H2, C2H4, C2H6, C3H4, C3H6, C3H8, C4H6, C4H8, C4H10) |
| [87] [43] in the ref. list??? | RS-Tiwan- 0.6–0.425 mm - dried | Radio frequency plasma pyrolysis technology of 2000 W and RF frequency of 13.56 MHz-GC/TCD | RFPT-N system overcomes the problem of tar formation during the pyrolysis of rice straw. | 740, 813, 843 and 880 K with corresponding loading powers of 357, 482, 574 and 664 W at the pressure of 0.9 torr – N2 at 200 mL/min - | 740 ± 5 K (or 357 ± 2 W): 69.3% 813 ± 5 K (or 482 ± 2 W) :43.4% 843 ± 5 K (or 574 ± 2 W): 37.5% 880 ± 5 K (or 664 ± 2 W): 33.5% | 0% 0% 0% 0 | 30.7% 56.6% 62.5% 66.5% Gassses: CO, H2, CH4, C2-C5: At 740 ± 5 K: 27.75% 2.03%, 0.21%, 0.05% At 813 ± 5 K :44.9%, 3.78%, 0.3%, 0.09% At 843 ± 5 K: 56.68%, 3.79%, 0.8%, 0.2% At 880 ± 5 K: 58.54%, 3.88%, 0.65%, 0.96% |
| [88] | RH, oil palm empty fruit bunches (OPEFB) Indonesia-100 mesh size - | Bench scale semi-batch pyrolysis reactor –GC/MS | Slow pyrolysis | 300; 400; 500; 600°C, mass feed of 150; 250; 350; 450 g , N2 =1.5 mL/min | 300oC: 1.18 % 400oC:2.8% 500oC:3.03% 600oC:2.26% At 600 oC: 150g: 1.92% 250g: 2.18% 350g: 1.69% 450g:1.77% | 84.87% 45.67% 49.56% 37.4% 36.83% 36.51% 31.96% 31.39% | 13.95% 51.53% 47.41% 60.34% 61.25% 61.32% 66.35% 66.84% |
| [89] | Rice husk-0.45-1 mm | Fluidized bed GC/MS -FTIR | Fast pyrolysis | 450-550 °C, gas residence time (<1 s) | At o520 C: 46.36% | 29.8% | 24.5% Gasses: CO2, CO and CH4 |
| [90] | RH, olive bagasse, wheat straw -< 2 mm | Bench scale screw reactor | Fast pyrolysis | 480-630 ºC -gas flow rate of 526 mL/min - | 480 oC:45% 530 oC:50% 580 oC:46% 630 oC:31% | 480 oC:37% 530 oC:39% 580 oC:40% 630 oC:30% | 480 oC:20.5% 530 oC:12% 580 oC:14% 630 oC:40.5% |
| [91] | RS -0.3 to0.5 mm size- acid catalysts: Meso-porous Al-SBA-15 with Si/Al | Stainless steel fixed-bed tubular reactor | Catalytic slow pyrolysis | 400–600 ◦C, HR= 20 ◦C /min , SGR= 160 mL/ min | Without catalyst at 550◦C 48.3% With Al-SBA-15 at 550 ◦C: 44.5% With Al-SBA-15 at 450 ◦C: 48.5% Acid. Diatomite: 49% | 29.7% 29.3% 30.0% 30% | 22.0% 26.2% 21.5% 21% |
| [92] | RS- 300-700µ size, -ZSM-5 catalyst of 106-212µm | Fluidized bed reactor (semi-batch reactor)- N2 and N2+H2 preheat at 300 oC – GC/MS | Catalytic slow pyrolysis and hydropyrolysis | Pyrolysis and hydropyrolysis were performed at 500o C and pressure of 1, 5 and 10 bar - N2 and N2 + H2 | For noncatalytic- P (1 to 10 bar): 31.5 to 39 wt.% P (1 to 10 bar): 28 to 42 wt.% a with ZSM-5 catalyst. | 40 to 43, then to 34 wt.% 40% to 33 wt.% with ZSM-5 | NCG was decreased with increase in P from 22.3 to 18.1 wt.%. CH4, C2H6, C3H6 C3H4 and CO, CO2 |
| [93] | RS (2 mm length) -Mesquite saw dust -india | Auger reactor - ratio of sand/ biomass between 1:1, 2:1, 3:1, 4:1 and 5:1 –GC/MS | Fast pyrolysis | 475, 500 and 525 °C - auger speeds=10, 30, 50 rpm -Rt >7 s - 10 kg/h for 3 h – Rt for fast pyrolysis be 1.03 s | 475oC:34.5% 500oC:32% 525oC:28% Biomass to heat carrier ratio: 0:01:28.5% 01:02:35% 01:03:32% Auger speed, rpm: 10:27.5% 30:31.5% 50:34.5% | 475oC:32.5% 500oC:28% 525oC:35% 36% 33% 35.5% 36% 35% 33% | 475oC:32.5% 500oC:38% 525oC:36.5% 35% 33% 32.5% 36% 33% 33% |
| [94] | RS - 1–3 mm size-Australia- Ammonium sulphate (AS), Diammonium phosphate (DAP) for treatment at [0.1, 0.2 and 0.5 mol -1] | TGA-HR of 10 ◦C/min from ambient to pyrolysis temp. - FTIR | Slow pyrolysis | Rt=30 and 60 min - 300, 400, 500, and 600◦C –N2 = 20 mL/min | - | RS bio-cahr: At 30 min., NT RSB: 28% 0.1mol/l AS RSB: 31.5% 0.1mol/l DAP RSB: 40% At 60 min, NT RSB :21.5% 0.1mol/l AS RSB: 28% 0.1M DAP RSB: 37.5% | - |
| [95] | RH- Australia - 280 and 500 μm sieve | Solar pyrolysis system- parabolic dish of 70kW/m2 –Max. power and flux density was 1.5 kW and 12,000 kW /m2 - GC/MS | Solar slow pyrolysis | 500, 600, 700, 800 oC – HR= 160 ± 6 °C/min | 500 oC:42% 600 oC :40.7% 700 oC :43.1% 800 oC:38.7% At 280 µm size: 800 oC:46% 1200 oC:40% 1600 oC:38% At 500 µm size: 800 oC:44% 1200 oC:41% 1600 oC:38% | 43% 42.86% 36.32% 35.82% - 800 oC: 42% 1200 oC: 34% 1600 oC:25 % - 800 oC:37 % 1200 oC: 32% 1600 oC: 25% | 14% 16.42% 20.55% 25.48% - 800 oC: 12% 1200 oC: 26% 1600 oC: 39% - 800 oC: 20% 1200 oC:26 % 1600 oC: 37% Gases CH4, CO2, C2H4, C2H6, H2, CO. At 500oC: 1.1, 5.1, 0.3, 0.4, 0.4 ,3.6% - At 600oC:1.5, 1.3, 0.05, 0.1, 0.3, 2.8% - At 700oC: 0.5, 0.5, 0.05, 0.8, 0.7, 2.2% - At 800oC: 0.3, 0.45, 0.02, 1.5, 2.7% |
| [96] | RH - size (dp) <250µm, 250-500 µm, 500-710 µm) | Semi-batch reactor -L9 Taguchi method was used to design the experiments | Slow pyrolysis | N2 = 100, 300, 500 mL/min - 400, 450, 500oC – HR = 10, 15, 20 oC/min | For N2 (mL/min): 100:36.57% 300:33.79% 500:32.31% For (dp), µm: <250::33.64% 250-500:: 36.57% 500-710: 33.27% For temperature: 400oC:33.41% 450oC:36.28% 500oC:36.57% For HR (oC/min): 10:32.17% 15:33.6% 20:36.57% | - | - |
| [97] | RH and RH pellets, oil palm empty fruit bunch (EFB– 8-9 cm length size | Fixed bed Reactor and BP-125 Microwave oven, 1 kW - 2.45 GHz | Slow + micro-wave pyrolyses | N2=4 L/min – HR=10 oC/min Microwave: 500 and 800°C Rt = 9, 15 min, HR=55°C/min- N2= 4 L/min | Fixed bed: 500 oC:23% 800 oC:12.22% Microwave: 500 oC:30% 800 oC:20.6% | 33% 27% 35% 31% | 42% 60% 35% 48% |
| [98] | RH | HSC Chemistry computer aided code + fixed bed reactor | Slow pyrolysis | 100-1200 °C, P = 1.0,5, 10, 15 bar – N2 – RT= 120 min | liquid yield decreased with increase in reactor temperature from 400°C to 650°C | decrease in char yield was also observed at higher temperature | As Temp. inreases from 450 to 650 oC: H2 (8% to 28%), CO2 (100% to 70%), CO (39% to 20%), CH4, small quantity of aromatic compounds like C6H6, C7H8, C8H10 (ethylbenzene), C8H10 (xylenes) and C6H5 –OH |
| [99] ¦ | RS of 0.4–0.7 mm size, RH of 2.0–3.4 mm size - quartz sand (QS) and red brick (RB) of 0.3–0.4 mm size | Spout-fluid bed reactor and systems for heating using flue gas from diesel | Fast pyrolysis | 400 to 580 oC – N2 - RH1/RS1 to RH8/RS8 are used as mixture – FR = 4 and 7 kg/h - two feed size (0.4–0.7 and 2.0–3.4 mm) | RH: 400 oC:45% 460 oC:48% 520 oC:47% 580 oC:43% RS: 400 oC:47% 460 oC:53% 520 oC:49% 580 oC:46.5% | RH: 400 oC:35% 460 oC:27.5% 520 oC:25% 580 oC:29% RS: 400 oC:33% 460 oC:29% 520 oC:22% 580 oC:21% | RH: 400 oC:20 % 460 oC: 23.5% 520 oC: 27.5% 580 oC:37.5% RS: 400 oC: 21.5% 460 oC:22 % 520 oC: 28% 580 oC: 37% |
| [100] | RS - distilled water washed RS (WRS)- acid washed rice straw (ARS) of 15–0.45 mm | Fixed bed reactor | Slow pyrolysis | HR = 10 °C/min -275 to 725 °C- SGR of argon = 300 mL/min | RS (nearly) 300oC:26% 350oC:40% 400oC:42% 500oC:44% 600oC:43% 700oC:43% ARS 300oC:27% 350oC:40% 400oC:42% 500oC:46% 600oC:47% 700oC:47% | RS (nearly) 300oC:70% 350oC:45% 400oC:40% 500oC:38% 600oC:37% 700oC:35% ARS 300oC:70% 350oC:50% 400oC:43% 500oC:35% 600oC:33% 700oC:32% | RS (nearly) 300oC:4% 350oC:13% 400oC:11% 500oC:16% 600oC:20% 700oC:22% ARS 300oC:3% 350oC:7% 400oC:7% 500oC:9% 600oC:12% 700oC:13% Gasses:H2, CO, CH4, CO2 |
| [101] | RS - 0.6mm –0.425 mm size | Radio-Frequency plasma (RFPT) thermolysis - 2000 W and 13.56 MHz | Fast pyrolysis | N2 = 200 mL/min - 300 to 950 K - input power 137 to 591 W - pressure of 1 torr | RFPT: 0% Normal thermolysis 42.6% | 50% 1.5% | 50% 55.9% Gasses: H2 (3.88–11.06 %), CO (5.21–14.82 %), CH4 (1.38–2.48 %), CO2 (1.51–5.05 %), and C2 (1.5–3.92 %) |
| [102] | RH and corn cob -Thailand - | Fixed-bed reactor | Slow pyrolysis | N2=100 mL/min - 300, 400, 500, 600, and 700 ℃ - HR=10 ℃/min | - | 300 oC:54.81% 400 oC:46.96%, 500 oC:6.18%, 600oC:44.19% 700oC:44.01% | - |
| [103] | (RH) - <2mm, empty fruit bunch | Muffle furnace | Slow pyrolysis | 350, 500, and 650°C - 2 h | - | 350 oC:50.67% 500 oC:34.63% 600 oC:29.02% | - |
| [104] | RS- china -100 mesh sieve size- Modified H-type ZSM-5 (HZSM-5) catalyst | A tandem μ-reactor system connected to (GC – MS, MSD) | Catalytic fast pyrolysis | 40 to 900 °C - 20:1 (catalyst: RS) – Helium- HZ means without CTAB (bare)- HZ and CTAB/ SiO2 molar ratio | At 600 oC, aromatics: HZ: 23% HZ-01: 27% HZ-02: 22.5% HZ-03: 16% HZ-04: 14% HZ-5:14% Olefins:4%, 6%, 7%, 9%, 5%, 5% | Coke: 45% 39% 45% 53% 56% 55% | CO: CO2: 18% 7% 18% 8% 17% 7.5% 13% 5.0% 15% 6.0% 15% 7.0% |
| [105] | RS, wheat straw, and sugarcane bagasse - 0.2 - 0.4 mm, 0.4 - 0.6 mm, and 0.6 - 0.8 mm size | Tubular fixed-bed reactor –GC/MS - FTIR | Slow pyrolysis | 350–650 °C – HR=20 and 100 °C/min –SGR= 30 to 100 mL/min | 0.2–0.4 mm, SGR=30 mL/min, HR=100 oC/min: 350oC:31.5% 450oC:33% 550oC:32% 650oC:32% 450 oC, GR=30 mL/ min, HR=100 oC/min, size (mm): 0.2-0.4:33% 0.4-0.6:25% 0.6-0.8:22% Fot SGR=30 mL/min, HR(oC/min): 20: 27.3% 100: 32.6% | 37% 34% 33% 32% 34.5% 37% 38.5% 46.7% 40.1% | 31.5% 32.5% 34.5% 35% 32% 36% 37.5% 37.45% 38.75% |
| [106] | RS, RH, olive bagasse | Screw auger of 1.2 kW–GC/MS -FID (flame ionization detector) | Fast pyrolysis | N2 = 526 mL/min – Rt=2.8 s | 39.4% From fractional distillation: Light:4.3% Heavy:11.5% Aqueous:46.9% | 34% Charcoal: 37.3% | 26.6% |
| [107] | RH, RS, and others – 150 -250 mm size – treated with 10% HCL and treated with aqueous 5% NaOH | Packed bed pyrolyser | Catalytic Slow pyrolysis | N2- Potassium chloride (KCl) was impregnated into deminer- alized coir pith (D), RH at different concentrations | Untreated RH: 41.2% Demineralized:57.4% With KCl: 35.1% withZnCl2: Demineralized : 57.4% WithK2CO3: 5.5% withZnCO3 :5.5% Untreated: 41.2% Demineralized: 57.4% | 17.3% 24.4% 22.6% 24.4% 28.3% 21.6% 17.3% 24.4% | 41.5% 18.2% 42.3% 18.2% 66.2% 72.9% 41.5% 18.2% |
| [108] | RH - 0.35, 0.60, 0.90, 1.20 and 1.50 mm size - | Fixed-bed reactor –GC/MS | Slow pyrolysis | N2 =100 cm3/min –RSM (Response surface methodology) for optimum yield -300,400,500,600,700 oC-Rt=2-4 min | For HR=50,100 oC/min, dp= 0.6 to 1.2 mm, 400 and 600 oC: 30 to 45% At 500 oC, dp= 0.3,0.9, 1.5 mm HR=25,125,75 oC/min: 30 to 44% At 300 oC, 75 HR, 0.9 dp, Ht= 3min: 26% At 700 oC, 75 oC/min 0.9 dp, Ht= 3min: 36% | - | - |
| [109] | Raw/torrefied RS - 60 to 125 μm size - torrefaction at 240 °C for 1 h in a tubular furnace reactor – catalyized RS | Vertical drop fixed-bed reactor-GC/MS Deminer-alization processes : (a) K; (b) Na; (c) Mg; (d) Ca | Slow pyrolysis – RS/H2O, RS/C2H4O2, RS/HCl Torrified RS: TRS-H2O, TS/ C2H4O2, TS/HCl | l550 °C –N2 = 200 mL/min leaching by deionized water, acetic acid and HCL for deminera-lization of raw/torrefied RS–Rt = 5 min | Torrefied RS: TS:20.77% TS-H2O: 25.47% TS-C2H4O2:27.56% TS-HC:27.98% Raw material: RS-HCl: 24% RS- C2H4O2: 25% RS-H2O: 28% RS:33% | TS:55.23% TS-H2O: 48.53% TS-C2H4O2: 44.44% TS-HC:43.52% RS-HCl: 47% RS- C2H4O2: 46% RS-H2O: 42% RS:29% | TS:24% TS-H2O: 26% TS-C2H4O2: 28% TS-HC: 28.5% RS-HCl: 29% RS- C2H4O2: 29% RS-H2O: 30% RS:38% |
| [110] | RS- catalyst with metal salts (FeCl3, CuCl2, MgCl2 and MnCl2), metal basic oxides (MgO, CaO, MgCO3 and CaCO3), acidic metals (ZnO, ZrO2, CeO2 and TiO2),zeolites (ZSM-5, Y-Zeolite, Mordenite and SBA-15), catalyst amount (5, 10, 15 and 20 wt%) - China | Fixed bed reacto -GC/MS –FTIR | Catalytic Slow pyrolysi | 350, 400, 450 and 500 oC - size 0.3-0.45 mm –HR of 10 oC/min –N2 at 40 ml/min - reaction time of 1 h - | 350 oC:26.7% 400 oC:33.2% 450 oC:38.5% 500 oC:32.5% Metal salts: FeCl3:32.3% C4Cl2:41.5% MgCl2:48.4% MnCl2:45.3% Basic metal oxides: MgO:52.1% CaO: 38.7% MgCO3:42.4% CaCO3:30.5% Acid metalic oxides: ZnO:46.2% ZrO2:48.3% CeO2:52.3% TiO2:48.2% Zeolites catalytics: ZSM-5:47.4% Y-zeolite (%): 55.2% Mordente:49.1 SBA-15:37.3% MgCl2 cat (%): 5:42.1% 10:48.4% 15:47.4% 20:41.5% Mg cataly (%): 5: 44.2% 10:52.1% 15:53.6% 20: 43.3% CeO2 catal (%): 5: 38.2% 10:46.3% 15:43.4% 20:42.1% Y-zeolite (%): 5: 43.7% 10:55.2% 15:46.8% 20: 42.6% | 48.6% 41.4% 37.1% 24.4% 29.3% 25.1% 20.3% 21.5% 27.5% 40.1% 21.2% 38.1% 20.4% 21.3% 18.9% 23.4% 21.2% 18.3% 20.5% 23.2% 24.5% 20.3% 18.8% 16.5% 25.7% 20.0% 19.5% 19.4% 30.4% 18.9% 22.3% 22.8% 26.1% 18.3% 24.9% 22.8% | 38.5% 33.4% 31.3% 33.2% 24.7% 25.4% 24.4% 32.3% 27.5% 21.2% 27.4% 27.5% 33.4% 30.0% 28.8% 36.4% 31.4% 26.5% 30.4% 39.8% 33.4% 31.3% 33.8% 42% 30.1% 27.5% 26.3% 37.3% 31.4% 34.8% 34.3% 35.1% 30.2% 26.5% 28.9% 34.6% |
| [111] | RS - India) – 2 mm size - | Muffle furnace | Slow pyrolysis | (300, 400, 500, 600 ºC - Rt=1, 2, 3 h - HR =10°C/min – N2=1.5L/min | Rt=1 h, HR=10 oC/min: 300 oC: 30.22% 400 oC: 37.5% 500 oC: 39.5% 600 oC: 38.21% Rt=2 h, HR=10 oC/min: 300 oC: 32.02% 400 oC: 38.5% 500 oC: 40.7% 600 oC: 39.94% Rt=3 h, HR=10 oC/min: 300 oC: 33.9% 400 oC: 39.5% 500 oC: 41.7% 600 oC: 40.59% | 57.87% 43.0% 37.3% 34.63 % 50.65% 42.0% 37.0% 32.77 % 46.78% 40.6% 34.77% 31.25 % | 11.91% 19.3% 23.2% 27.16% 17.42% 19.6% 22.6% 27.29% 19.31% 20.35% 23.70% 28.16% For Rt and T ranges: CO: (41.81-29.66%), CO2: (54.01-38.46%),H2: (1.9 -19.22%), CH4: (2.3-10.54%) |
| [112] | RS- 1 mm size- catalytic cracking – alumina (Al2O3) and ZSM-5 | Stainless-steel reactor tube –GC/MS | Catalytic slow pyrolysis | 550°C and p=1.2 atm -N2 of 80 mL/min | Raw RS (average): 35.90% With catalyst composition 100, 90, 80, 70, and 60% of ZSM-5/Al2O3 at 425OC. | 48.36% - | 15.64% - |
| [113] | RS, RH –India | Pyrolysis reactor | Slow pyrolysis | 1 to 1:30 hours, 300 to 500°C. | RH:11.17% RS:4.86% | 54.93% 46.79% | 33.90% 48.35% |
| [114] | RS-pinewood, peanut shell- K2CO3 as the catalyst - 0.2–0.4 mm size | Gas sweeing fixed-bed reactor –GC/MS | Catalytic Slow pyrolysis | 300 °C to 700°C – HR = 10 °C/ min – SGR of argon =300 mL/min – Rt = 2.7 s | Catalyist- K2CO3 loading: 0% : 52% 5.5%: 46% 9.9%: 46% 17.7%:45% | 33% 35% 34% 25% | 15% 19% 20% 30% H2, CO, CO2 highly promoted by K2CO3 and CH4 low at high T. |
| [115] | RS –Malaysia - 0.6 - 1.18 mm size catalysts of dolomite of 300 µm and ZSM-5 | Fixed-bed pyrolysis | Catayltic Slow pyrolysis | 900°C - 8 hrs -pyrolysis temp. at 450 oC- HR =77.63 oC/min- RT=2.61min -N2=100 cm3 /min | No cataclytic: 27.6% For zeolite (ZSM-5): 26.3% For dolomite: 23.2% | 26% 25% 23.5% | 46% 48.5% 52% |
| [116] | RS– India - 5±1 cm size - char | - | Slow pyrolysis | 300℃, 500℃, 700℃, 800℃ - Rt = 30 min | 300 oC:22% 500 oC:27% 700 oC:32% 800 oC:37% | 56% 47% 36% 32% | 22% 26% 31% 31% |
| [117] | RS, sawdust, cotton stalk - powdered (0.6 mm size) and pelletized (4 and 6 mm size and addition of water) | Batch-type fixed-bed reactor - 1-2 kg/batch | Slow pyrolysis | 400 to 500 °C- HR = 10oC/min Rt = 15 to 120 min. – N2= 0 to 10 L/min | RS (0.6 mm) powder: 400 oC: 21.0% 450 oC: 27.0% 500 oC: 24.5% RS (4 mm) pellet size: 400 oC: 31.0% 450 oC: 36% 500 oC: 33% RS (6 mm) pellet size: 400 oC: 37.5% 450 oC: 39.0% 500 oC: 35.0% | 44.0% 36.0% 34.0% 42.0% 35.0% 33.0% 35% 30% 27.5% | 35.0% 37.0% 41.5% 26.0% 25.0% 30.5% 35% 27.5% 37.5% Gasses at 400oC:14.5% H2, 10.8%CO,16.7%CH4, 40.0%CO2 At 450 oC: 15.6%H2,14.6% CO, 17.2%CH4, 34.9%CO2 At 500 oC: 17.2%H2,14.2% CO,18.9%CH4, 31.8%CO2 |
| [118] | Washing RS (WRS) - 250 µm – H2O+ HCl were labeled as H2O-RT-RS, H2O-HT-RS, HCl-RS | TGA and TG-MS techniques | Catalytic -Slow pyrolysis , | N2 = 100 ml/min – HR = 10 oC/min – 30 to 800 oC | For raw RS: 6.9% For HCl-RS: 22.6% | 32.6 % 23.4% | Gases:H2, CH4, CO, CO2, H2O For raw RS (g sample/g gas): H2(Trace),CH4(minor), CO(0.113), CO2(0.207), H2O(0.274) For HCl-RS: H2(Trace),CH4 (minor), CO(0.061), CO2(0.143), H2O(0.235) |
| [119] | Torrefied & pyrolysis pelletized RS -10–15 mm (length) - 0.5–1 mm size-activated carbon at 10 wt.% loading | Microwave-assisted torrefaction reator – Analytical pyrolysis-GC/MS (Py-GC/MS) technique | Micro-wave pyrolysis | 450, 600, and 800 W - final temperature 300, 600, 800◦C | 800 oC, 600 W: 10.5% 600 oC, 600 W: 12.9% 300 oC, 600 W: 10.5% 300 oC, 450 W: 15.2% 300 oC, 800 W: 14.7% 300 oC, 800 W with susceptor: 12.7 % rests: H2O | 33.7% 35.5% 55.6% 50.3% 50.6% 35.3% | 29.5% 25.8% 10.7% 13% 12.2% 26% |
| [120] | RH | ASPEN Plus V8.8 - reactor block for the model is RGIBBS | Slow pyrolysis | 400, 500, 600 oC | Optimum oil yield was 44.2% at 400°C, then drops gradually to 41% at 500°C. Then drops sharply to 32.9% at 600°C. At 600°C, 84.7% acids, 7.9% pyrolytic water, 7.42% aldehyde and traces of alcohol and others were detected. | simulation predictions show a slight increase in char yield with temperature (opposite to experiments) - Though the yield increases from 38.7% to 41.9% at 400°C and 600°C | The gas yield was lowest at 400°C and is about 17.1%. Gas yield increases with increasing temperature. The optimum yield based on the thermodynamic predictions was 25.2% at 600°C |
| [121] | RH -Malaysia -<250 µm – Nickel (RH-N), zeolite (RH-Z), coal ash (RH-C) catalysts of 10% of total mass | TGA/DTA-MS | Catalytic -Slow pyrolysis – no yield | N2 = 00 ml/min - 323 to 1173 K/min –HR = 10, 20, 30, 50 K/min –Rt=10 min | - | - | At 50 K/min RH: H2:28%, CO:32%, CH4:15%, CO2:23% RH-N: H2:40%, CO:26%, CH4: 11%, CO2:21% RH-Z: H2:37.5%, CO:30%, CH4: 13%, CO2:17% RH-C: H2:36%, CO:31%, CH4: 16%, CO2:14% |
| [122] | Co-pyrolysis of RS and polythene waste (PW) –size of < 2mm | Fixed bed pyrolysis LPG heating reactor | Co-fast pyrolysis | 400 to 500 oC –Rt= 8 s – P/RS mass ratios 100:0, 75:25, 50:50 , 25:75, and 0:100 | PW 100%: 80% 25%RS/75%PW: 75% 50%RS/50%PW: 60% 75%RS/25%PW: 40% | 0% 10% 15% 25% | 21% 18% 20% 35% |
| [123] | Co-pyrolysis of rice (RS) and water hyacinth (WH) –china - 0.5 to 2 mm size - RS, WH,RS:WH | Fixed bed reactor-GC-FTIR | Co-slow pyrolysis | 300, 350, 400 to 450 °C –HR = 20 °C/min –N2= 30 mL/min – Rt = 1 h | For RS 300 oC:25% 350 oC:27% 400 oC:28% 450 oC:27% For WH 300 oC:23% 350 oC:23% 400 oC:24% 450 oC:23% For RS:WH 30:70:33% 50:50:44% 70:30:34% | 36% 35% 33% 32.5% 47% 42% 38% 35% 47% 41% 43% | 39% 37% 37% 40% 28% 34% 37% 40% 15% 15% 24% |
| [124] | Polypropyle (PP) plastics /(RS) -0.50 - 2.0 mm RS size -3.0 mm PP (ratio 1:1)-Malaysia | Fixed-bed drop type - GC-TCD (thermal conductivity detector) - GC-FID | Co-slow pyrolysis | 450, 500, 550, 600 °C – N2 –Ht = 20 min – HR=20 °C/min | For RS:PP 450 oC:32% 500 oC:54% 550 oC:69% 600 oC:51% | 21.5% 14.45% 10.5% 9.47% | 46.5% 68.55% 20.5% 39.53% H2 :61%, O2 :1%, N2 :6%,CO:15%, CH4:15%, Unknown:2% |
| [125] | Sewage sludge (SS) and rice straw (RS) –china – SS and RS are ground into 0.25-0.38 mm size | Fixed bed reactor - | Co-slow pyrolysis | 450, 550, 650, 750 and 850 °C N2 = 300 mL/min. – HR = 10 °C/min | - | - | SS (ml/gm): 10 H2 at 450 oC, to 110 max at 850 oC- -5 CO at 450 oC to 45 max at 850 oC – 20 CO2 at 450 oC to 2 at 850 oC - 8 CH4 at 450 oC to 80 at 750oC RS (ml/gm): 5 H2 at 450 oC, to 80 max at 750 oC -55 CO at 450 oC to 180 max. at 850 oC - 25 CO2, at 450 oC to 38 max. at 650 oC-50 CH4 at 450 oC to 225 at 750 oC - For 5, 10, 15, 20, 25 % RS/SS: At 650 oC: H2: 60 max. at10% and min. of 45 at 25% CH4:150 max. at 10% and min. 80 at 25%, CO: 30 min. at 5,25% and 35 max. at 20%, CO2:10 min. at 35% and 30 max. at 10% |
| [126] | RS/ ulva prolifera macroalgae (UPM)-china-<150 mm size- catalysts as (NiFe-LDH, NiFe-LDO, NiFe-LDO/ AC, Ga/NiFe-LDO/AC) – A-UPM acids | vertical dual-bed tubular quartz reactor with electric furnace - GC/MS | Co-slow pyrolysis | 500 oC – SGR of argon = 30 mL/min - a series of nickeliron-layered double oxides (NiFe-LDO) supported on activated bio-char catalysts (activated carbon AC) | RS: 44.73% UPM: 38.84% RS/UPM: 41.25% RS/A-UPM: 46.68% Catalytic (RS/A-UPM):NiFe-LDO: 43.21% NiFe- LDO/AC: 40.20 % 5Ga/NiFe-LDO/AC: 39.13% 10Ga/NiFe-LDO/AC: 38.07% | 24.32% 29.05% 27.32% 23.63% 23.59+ 3.13% Coke 24.04 +1.29% coke 23.72+ 1.64% coke 23.70+1.84% coke | 30.95% 32.11% 31.43% 29.69% 30.07% 34.47% 35.51% 36.39% |
| [127] | RS -Banagladish- 300 to 1180 µm size – sand of 181 µm diameter | Fluidized bed pyrolysis unit | Fast pyrolysis | 400 -500 oC – N2 = 23 to 39 L/min at interval of 4 ml/min | N2 at 31 L/min: 500 oC:30% 475 oC:36% 450 oC:40% 425 oC:35% 400 oC:31% At 450 oC N2 (SG flow rate, L/min.): 23:29.5% 27:35% 31:40% 35:36% 39:33.5% Residence time (Rt) (s): 3.76:29% 3.20:35% 2.80:39% 2.47:37% 2.22:33.5% | 36% 42% 45% 51% 56% 38.5% 41% 43.5% 49% 53% 31.5% 41% 44% 48% 53.5% | 34% 22% 15% 14% 13% 32% 24% 16.5% 15% 13.5% 38.5% 24% 17% 15% 13% |
| [128] | Rice husk (RH) (20%) +polyethylene (PE) (80%) | 1 liter batch reactor of Hastelloy C276 – GC/MS | Co-slow pyrolysis | HR = 5 to 6 ºC/min –N2 - temperature of 430ºC, initial pressure = 0.2 MPa – Rt= 10 min | At 430 oC, 0.2 MP: 73.8% At 430 oC, 1.0 MP: 73% | 10% 12% | 17% H2:3%, CO:5%, CO2:10%, CH4:12%, CnHm:27% 15% Gaseses: H2:3%,CO:3% CO2:3%, CH4:1%,CnHm:11% |
| [129] | rice straw (RS) - Shenfu bituminous coal (SB), Co-pyrolysis of RS/SB blends (mass ratio 1:4, 1:4, and 4:1) - RS and SB of 250–420 lm and 125–180 lm size range | High-frequency furnace rapid pyrolysis system-heated by a high-frequency alternating magnetic field-GC | Co-fast pyrolysis | 600 to 1200 oC – SGR of Argon = 500 mL/min | For RS:30% at 600 oC to 10% at 1200 oC For SB: 10% at 600 oC to 5% at 1200 oC For RS-SB: (1:4): 20% at 600 oC to 5% at 1200 oC For RS-SB: (1:1): 20% at 600 oC to 2.5% at 1200 oC For RS-SB: (4:1): 28.5% at 600 oC to 2% at 1200 oC | 31.5% at 600 oC to 18.5% at 1200 oC 73% at 600 oC to 57% at 1200 oC 60% at 600 oC to 57% at 1200 oC 53% at 600 oC to 38% at 1200 oC 40% at 600 oC to 39% at 1200 oC | 40% at 600 oC to 70% at 1200 oC 17% at 600 oC to 36% at 1200 oC 21% at 600 oC to 57% at 1200 oC 27% at 600 oC to 58% at 1200 oC 31% at 600 oC to 70% at 1200 oC Gasses: H2:1 to 5%, CO:13 to 60%, CH4: 3-5(800-900 oC)-2%, CO2: 21 to 5% – H2:1.5 to 5%, CO:5 to 28.5%, CH4: 7-8(800-900 oC)-2.5%, CO2: 6.5 to 2.5% – H2:1 to 4%, CO:6.5 to 40%, CH4: 3-3.5(800-900 oC)-2.5%, CO2: 8.5 to 2.5% – H2:0.5 to 2%, CO:12.5 to 59%, CH4: 2.5-3(800-900 oC)-2%, CO2: 14 to 3% – H2:0.5 to 2.5%, CO: 15 to 70%, CH4: 3-6(800-900 oC)-2%, CO2: 19 to 6% -C2H6, C2H4, C3H8, C3H6,C2H2 from 0.5% to 3 % |
| [130] | Kitchen food waste (KFW- 5–10 µm) and rice straw (RS- mean size of 0.9 mm.)- China- 100KFW, 75KFW, 50KFW, 25KFW, and 100RS corresponding to blend ratios of KFW with RS | Microwave reactor 1500 kW - | Micro-wave co-pyrolysis | 700–900 ℃ -N2 = 50 ml/min.- HR = 58.3 and 63.5 ℃/min for 100 RS and 100 KFW | 100KFW: 21.8% 75KFW: 20.83% 50KFW: 19.8% 25KFW: 19.2% 100RS: 17.15% | 33.6% 36.37% 39.4% 41.7% 42.25% | 44.6% 42.8% 40.8% 42.25% 40.6% Gasses 100KFW: 42.5% CO2, 17% CO, 21% H2, 19% CH4 75KFW:25% CO2, 15% CO, 39% H2, 21% CH4 50KFW:26% CO2, 13% CO, 40% H2, 21.5%CH4 25KFW: 18% CO2, 13% CO, 43% H2, 26% CH4 100RS:25.5% CO2, 10% CO, 37.5% H2, 25.5% CH4 |
| [131] | Rice husk (RH) with underutilized biomass, Napier grass (NG) and sago waste (SGW)- particle size of 0.2 mm- Malaysia | Fixed bed reactor –GC/MS | Co-slow pyrolysis | 600 oC, HR =30 oC/min – N2=5L/min - Rt= 60 min. | Pure RH: 31.51 wt% (30.70-aqueous, 0.82-organic) Pure NG: 41.91 wt% (29.56-aqueous,12.34-organic) Pure SGW: 37.98 wt% (36.87-aqueous, 1.11-organic) NG/RH:50:50: 35.86 wt% (32.66-aqueous, 1.11-organic) RH/SGW:50:50: 45.55 wt% (36.60-aqueous, 8.95-organic) NG:RH:SGW:30:40:30: 34.13 wt% (31.98-aqueous, 2.14-organic) | 28.5% 34.5% 12.0% 33% 22.5% 31% | 27.5% 37.5% 50% 33% 35% 35% |
| [132] | RS –torrefied/ pyrolysis - low density polyethylene (LDPE) -ZSM-5 catalytic | Microwave - 1.0KW, 2.45 GHz GC/MS - | Co- slow pyrolysis pyrolysis | N2 = 50 ml/min. – 750 W – 309 to 450 oC | RS/LDPE 29.83% RS(T)/LDPE 22.75% RS(T)/LDPE/ ZSM-5 24.46% | - - - | 46.74% 40.98% 39.71% |
| [133] | RS- 0.4 mm size and discarded polyethylene end up in landfills (0.4 mm size )(LDPE) – Mix (P:R) 1:1, 1:2, 1:3 -catalytic (Portland cement, 2.74 μm) -China | Fixed bed reactor- GC-MS | Co-slow pyrolysis | 600 °C under isothermal condition Rt=30 min – N2= 300ml/min | LDPE/RS: (1:1): 21.3 % (1:2): 19.0% (1:3): 14.16% With catalytic (5%):25.80 % (10%):28.16% (15%):32.5 % | 57.2 % 65.45% 74.18% 52.87 % 51.84% 48.5 % | 21.5 % 15.55% 11.66% 21.33 % 20.0% 19.0% For (0, 5, 10, 15%catalytic): H2 (17.93 to 31.18%), CO (22.95 to 29.04%), CH4 (31.98 to37.38%), CO2 (44.45 to 61.89%), C2H4 (28.11 to 30.2%), C2H6 (15.89 to 16.13%) |
| [134] | RH and (PE) plasticwaste , 5 mm size – RH varied between 10 to 50% in blend | Batch reactor -GC | Co-slow pyrolysis | 350 to 430 °C –Rt = 10 to 60 minutes, initial pressure =0.2 to 1 MPa. | 20 % RH/80 % PE (350 to 430 oC): 0.2 MPa, time, min): 10: 47% to 73% 30: 57% to 70% 60: 75% to 67% 0.6 MPa, time (min) : 10:48% to 74% 30: 57% to 72% 60: 69% to 70% 1.0 MPa, time (min): 10:51% to 74% 30:55% to 73% 60: 62% to 72% |  | 20 % RH/80 %(w/w) PE: At 350oC, 0.2 MPa, 10 min: H2 (2%), CO2 (12%), CH4 (10%), CO (6%), CxHy (23%) At 430oC, 0.2MPa, 60 min: H2 (3.5%), CO2 (9%), CH4 (17%), CO (3.5%) CxHy (33.5%) At 350oC, 0.2 MPa, 60 min: H2 (1.5%),CO2 (8.5%), CH4(17%), CO(4%) CxHy (18.5%) At 390oC, 0.6MPa, 35min: H2 (2%), CO2 (6%), CH4 (8.5%), CO (3%), CxHy (21%) At 390oC, 0.6MPa, 35 min, 30/70: H2 (2.5%), CO2 (10.5%), CH4 (9%), CO (3.5%), CxHy (20%) |
| [135] | RH (0.5-1.0 mm) + plastic (high-density polyethylene (HDPE) RH and recycled HDPE pellet (4 × 4 mm2) | Fixed-bed reactor | Co-slow pyrolysis | 400, 500, 600 °C) – Rt = 15, 30, 45 min – HR =10 oC/min | - | 400 °C- Rt (min): 15: 51.06% 30: 53.5% 45: 53.04% 500 °C- Rt (min): 15: 46.5% 30: 47.54% 45: 45% 600 °C –Rt (min): 15: 43% 30: 55.5% 45: 40.2% | - |
| [136] | RS, wheat straw, ground -nut shells, 8–10 mm size - washed RS by deionized water | A batch reactor - two-step slow pyrolysis |  | A. Bhatnagar et al. Waste Management 138 (2022) 298–307 [36] | Rice straw (RS), groundnut shells (GNS), and wheat straw (WS) - size of 8–10 mm- samples washed with deionized water | A batch reactor was used to perform two-step slow pyrolysis experiments to obtain bio-oil and biochar |  |

Table S2: Proximate, ultimate, and fiber composition analyses of rice residues from different references.

| Ref No. | VM % | FC % | Ash % | M % | C % | H % | N % | O % | S % | HV MJ/kg | Fiber composition % |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 76.85 |  | 9.54 | 13.6 | 50.93 | 6.04 | 0.83 | 41.61 | 0.23 | 16.35 | HC.* | C.* | L.* | RS-Taiwan |
| 2 | 60.84 | 16.61 | 22.55 | 7.3 | 48.75 | 5.98 | 1.99 | 43.28 | - | 13.40 |  |  |  | RS-Indonesia |
| 4 | 66.26 | 16.25 | 14.53 | 2.95 | 35.36 | 4.78 | 0.96 | 0.96 | - | - |  |  |  | RS-China |
| 5 | 71.6 68.9 | 14.5 11.1 | 13.9 20.0 | - - | 44.2 47.4 | 6.2 6.7 | 0.8 0.8 | 48.8 45.1 | - | - |  |  |  | RS RH - Thailand |
| 6 | 66.71 | 13.5 | 14.11 | 5.68 | 47.50 | 6.55 | 1.07 | 44.88 | - | 14.97 |  |  |  | RS- China |
| 7 | 72.20 | 14.44 | 13.36 | 8.25 | 45.41 | 6.28 | 0.99 | 47.11 | - | 15.26 |  |  |  | RS-Taiwan |
| 8 | 66.71 | 13.50 | 14.11 | 5.68 | 47.50 | 6.55 | 1.56 | 44.88 | - | - |  |  |  | China |
| 10 | 72.8 74.7 | 9.3 15.2 | 17.9 10.1 | - | 48.9 45.2 | 6.2 6.5 | 0.8 0.8 | 44.1 47.5 | - | - |  |  |  | RH RS - Thailand |
| 11 | 74.53 | 12.11 | 11.98 | 1.37 | 42.78 | 5.77 | 0.34 | 51.18 | - | 15.75 |  |  |  | RH -Malaysia |
| 13 | - | - | 13.5 | - | 40.24 | 5.44 | 3.40 | 37.22 | 0.17 | 15.69 | 19.6 | 34.4 | 22.9 | RS-China |
| 14 | 71.70 | 18.58 | 9.72 | - | 43.68 | 5.70 | 0.97 | 39.72 | 0.21 | 17.10 | - | - | - | RS-China |
| 20 | 62.61 | 14.96 | 17.06 | 6.73 | 38.22 | 5.88 | 0.68 | 39.48 | 0.07 | 17.91 |  |  |  | RH-Malaysia |
| 21 | 65.71 | 15.13 | 14.29 | 6.41 | 50.59 | 7.02 | 2.55 | 48.1 | - | 20.88 |  |  |  | RS-India |
| 22 | 64.30 | 9.20 | 18.80 | 7.07 | - | - | - | - | - | 13.36 |  |  |  | RH-China |
| 23 | 70.50 | 16.6 | 12.90 | 1.1 | 42.0 | 5.4 | 0.4 | 39.3 | - | 16.8 |  |  |  | RH-Spain |
| 24 | 62.70 | 15.10 | 12.70 | 9.50 | 37.86 | 5.24 | 0.68 | 35.32 |  |  |  |  |  | RH-China |
| 26 | 59.44 | 15.39 | 15.39 | 8.69 | 50.59 | 7.0 | 0.77 | 41.40 | 0.24 | - |  |  |  | RH-China |
| 27 | 72.00 81.10 | 5.50 6.30 | 22.50 12.61 | - - | 35.92 38.02 | 5.05 5.75 | 0.26 0.65 | 58.77 55.58 | - | - |  |  |  | RH RS - India |
| 28 | 77.93 | - | 11.23 | - | 40.09 | 5.34 | 1.07 | 42.27 | - | - | 26.81 | 36.72 | 14.51 | RS-China |
| 29 | 62.43 | 14.98 | 15.43 | 7.16 | 44.82 | 5.08 | 0.92 | 49.18 | - | - | 60.27 |  | 14.07 | RS-Turkey |
| 31 | 78.8 |  | 11.9 | 9.3 | 35.50 | 7.0 | 1.4 | 38.1 | - | - |  |  |  | RH-Tiwan |
| 32 | 74.53 | 12.1 | 11.98 | 1.37 | 42.78 | 5.77 | 0.34 | 51.18 | - | 15.75 |  |  |  | RH-Malaysia |
| 33 | - | - | - | 8.0 | 38.69 | 5.4 | 0.67 | 55.03 | 0.21 | - |  |  |  | RH-China |
| 34 | 69.3 | 9.01 | 21.7 | 9.2 | 36.6 | 4.9 | 0.77 | 31.96 | 0.23 | 14.2 |  |  |  | RS-Texas(USA) |
| 36 | 60.84 | 16.61 | 22.55 | 7.3 | 48.75 | 5.98 | 1.99 | 43.28 | - | 13.45 |  |  |  | RS- Korea |
| 37 | 56.0 | 14.0 | 13.3 | 16.7 | 48.78 | 6.59 | 3.73 | 40.9 | - | 16.15 |  |  |  | RH-China |
| 38 | 66.1 | 15.4 | 5.7 | 12.8 | 37.1 | 5.2 | 0.5 | 44.3 | 0.1 | 12.1 |  |  |  | RS-India |
| 39 | 73.01 | 7.25 | 19.74 | 11.95 | 34.11 | 6.53 | 0.17 | 59.19 | 0.1 | - |  |  |  | RS-India |
| 40 | 78.07 73.41 | 6.93 11.44 | 15.0 15.14 | 11.69 10.89 | 36.07 41.92 | 5.20 6.34 | 0.46 1.85 | 58.01 49.42 | 0.26 0.47 | 14.87 12.87 |  |  |  | RS RH - India |
| 41 | 82.30 | - | 11.2 | 6.48 | 39.2 | 4.84 | 1.6 | 53.69 | 0.67 | - | 32.53 | 54.67 | 12.83 | RS-Korea |
| 42 | 78.84 | - | 15.27 | 6.67 | 39.03 | 5.29 | 0.51 | 55.17 | - | 14.62 | 22.20 | 38.30 | 14.23 | RS-California |
| 43 | 66.89 | 14.57 | 7.56 | 10.8 | 39.98 | 2.54 | 4.34 | 52.61 | 0.53 |  |  |  |  | RS-Malaysia |
| 44 | 73.01 | - | 19.74 | 11.95 | 34.11 | 6.53 | 0.17 |  |  | 13.41 |  |  |  | RS-India |
| 45 | 62.3 67.0 | 15.6 13.0 | 22.1 20.0 | 9.4 7.2 | - | - | - | - | - | 15.1 16.2 |  |  |  | Raw RS- California acid treat RS |
| 46 | 54.51 | 14.14 | 25.32 | 6.03 | 34.33 | 4.98 | 0.38 | 60.12 | 0.19 |  |  |  |  | RS-Australia |
| 47 | 60.45 | 14.84 | 16.41 | 8.30 | 37.35 | 4.49 | 0.22 | 33.19 | 0.04 | 13.67 |  |  |  | RH-China -LHV |
| 50 | 62.68 | 12.85 | 15.86 | 8.61 | 40.7 | 5.24 | 0.47 | 53.59 | - | 15.83 |  |  |  | RH-china |
| 51 | 70.6 | 2.97 | 17.09 | 9.45 | 50.45 | 6.58 | 1.49 | 41.46 | 0.23 | 19.81 |  |  |  | RH-India |
| 52 | 71.1 | 9.9 | 13.0 | 6.0 | 40.26 | 5.36 | 0.33 | 31.02 | 0.058 | 16.49 |  |  |  | RH-Taiwan |
| 53 | 76.36 | 15.35 | 8.29 | - | 34.4 | 5.07 | 0.35 | 37.28 | 0.04 | 15.48 |  |  |  | RH- Indonesia |
| 55 | 65.11 64.22 55.98 55.32 | 15.20 14.18 10.95 13.03 | 12.30 13.27 26.17 24.53 | 7.39 8.33 6.90 7.12 | 39.34 38.52 32.39 32.93 | 5.29 5.43 4.49 4.49 | 0.51 1.27 0.41 0.48 | 54.82 54.68 62.68 62.06 | 0.05 0.10 0.03 0.03 | 17.39 16.54 14.88 15.24 |  |  |  | RH (4 samples) – Thailand |
| 56 | 59.5 | 15.5 | 17.1 | 7.9 | 44.6 | 5.6 | - | 49.3 | - | - |  |  |  | RH -Bangladesh |
| 57 | 83.19 88.43 |  | 16.81 11.57 | - | 46.17 50.02 | 6.29 6.11 | 3.99 5.17 | 43.55 38.71 | - - | - - | 26.89 17.74 | 37.81 44.29 | 13.10 26.20 | RS RH -Vietnam |
| 58 | 61.7 62.61 | 15.96 7.11 | 9.72 17.82 | 12.6 12.46 | 43.68 36.6 | 5.7 6.08 | 0.97 0.24 | 39.72 26.68 | 0.21 0.35 | 16.6 16.8 |  |  |  | RS RH - china |
| 59 | 63.64 | 16.89 | 13.70 | 5.95 | 42.70 | 6.01 | 1.20 | 35.97 | 0.42 | 17.32 | 40.39 | 46.75 | 3.71 | RH-China |
| 60 | 69.6 71.6 | 14.9 13.8 | 15.5 14.2 |  | 42.1 44.8 | 6.1 6.5 | 1.2 1.0 | 34.9 33.4 | 0.2 0.1 |  | 22.8 27.7 | 35.7 46.2 | 28.1 26.1 | RH - Argentina Treated RH |
| 63 | 63.0 | 19.40 | 8.10 | 9.5 | 38.20 | 5.2 | 0.63 | 47.68 | 0.19 | 14.37 |  |  |  | RH-Iran |
| 65 | 79.22 80.45 | 12.27 8.70 | 8.51 10.85 | 9.32 6.34 | 45.76 43.98 | 6.22 5.94 | 0.52 0.40 | 47.50 49.68 |  | 16.16 15.91 | 31.12 28.03 | 38.14 30.42 | 26.35 36.02 | RS RH - Taiwan |
| 66 | 68.20 | 19.30 | 12.50 |  | 41.25 | 5.58 | 0.87 | 52.26 | 0.04 | 12.28 |  |  |  | RS-India |
| 67 | 62.61 | 13.95 | 17.82 | 5.62 | 43.39 | 9.56 | 1.06 | 48.34 | - | 16.68 | 23.54 | 34.56 | 24.63 | RH-China |
| 68 | 67.8 | 16.4 | 12.2 | 3.61 | 40.3 | 5.55 | 1.02 | 37.3 | 0.15 | 16.40 |  |  |  | RS-China |
| 69 | 71.47 | 18.39 | 7.45 | 2.69 | 48.59 | 8.27 | 2.67 | 40.47 | - | 17.21 |  |  |  | RH-China |
| 283 | 52.00 | 5.27 | 34.60 | 8.90 | 30.4 | 4.00 | - | 21.10 |  |  | 16.07 | 28.60 | 7.28 | RH-Brazil |
| 72 | 68.25 | 16.92 | 14.83 | 8.43 | 39.48 | 5.71 | 0.67 | 54.12 | 0.1 | 17.43 | 14.04 | 41.52 | 33.67 | RH-UK |
| 73 | 59.5 | 15.5 | 17.1 | 7.9 | 44.6 | 5.6 | 0.5 | 49.3 | - | - | 29.3 | 34.4 | 19.2 | RH-UK |
| 74 | - | - | - | 8.9 6.5 | 40.64 45.96 | 5.09 5.79 | 0.63 0.56 | 53.64 45.96 |  | 17.02 17.32 | 54.44 71.53 |  | 19.34 20.10 | RS - Korea HF-RS |
| 75 | 66.71 61.23 | 13.50 14.95 | 14.11 17.09 | 5.68 6.73 | 47.50 50.47 | 6.55 6.85 | 1.07 0.59 | 44.88 42.09 |  | 14.97 - |  |  |  | RS RH-China |
| 76 | 82.8 | 1.5 | 8.9 | 6.8 | 53.25 | 5.62 | 2.11 | 48.8 | 0.22 | 16.0 | 25.3 | 37.8 | 23.3 | RS-Korea |
| 77 | 66.31 | 12.2 | 16.57 | 4.92 | 40.81 | 4.87 | 0.68 | 36.47 | 0.11 |  |  |  |  | RS-Italy |
| 78 | 75.32 | 15.11 | 7.12 | 2.45 | 38.25 | 7.02 | 2.91 | 51.10 | 0.72 | 19.25 | 31.15 | 43.32 | 8.17 | RH-Gana |
| 79 | 73.0 | 5.0 | 17.0 | 5.0 | 39.45 | 6.49 | 0.83 | 52.98 | 0.25 |  | 28.0 | 34.0 | 18.0 | RH-India |
| 80 | 65.35 | 12.93 | 12.51 | 8.51 | - | - | - | - | - | - |  |  |  | RH-Brazil |
| 81 | 75.89 | 17.80 | - | 6.31 | 49.01 | 5.87 | 1.07 | 44.05 | - |  |  |  |  | RH-UK |
| 82 | 71.0 79.24 | 17.1 11.23 | 11.9 9.53 | - | 35.44 37.41 | 4.77 5.24 | 0.26 0.19 | 42.41 45.92 | - | 15,76 16,38 |  |  |  | RH - China AWRH |
| 83 | 70.60 | 12.87 | 16.53 | - | 39.37 | 5.13 | 0.32 | 55.18 | - | 16.58 |  |  |  | RH-China |
| 84 | 66.26 | 16.25 | 14.53 | 2.95 | 35.36 | 4.78 | 0.96 | 44.36 | -- |  |  |  |  | RS-China |
| 85 | 73.45 | 14.71 | 11.84 | - | 40.82 | 5.71 | 1.19 | 40.44 | - |  |  |  |  | RH-China |
| 86 | 62.44 | 13.61 | 14.58 | 8-10 | 40.93 | 4.84 | 0.42 | 53.81 | - |  | 20.56 | 36.79 | 14.88 | RH-China |
| 87 | 87.2 |  | 12.8 | - | 41.8 | 5.9 | 0.40 | 51.6 | 0.2-0.1Cl | 16.9 |  |  |  | RS-Taiwan |
| 88 | 55.5 | 15.7 | 16.1 | 12.7 | 45.2 | 5.8 | 1.02 | 47.6 | 0.21 | 15.16 |  |  |  | RH-Indonesia |
| 89 | 60.98 | 14.46 | 12.26 | 12.30 | 40.0 | 5.03 | 0.63 | 29.57 | 0.13 | 14.75 | 23.87 | 37.15 | 12.84 | RH-China |
| 90 | 65.50 | 14.65 | 10.5 | 9.4 | 40.7 | 6.0 | 0.5 | 32.90 | 0.02 |  |  |  | 15.70 | RH-MSc |
| 91 | 80.16 |  | 12.76 | 7.08 | 53.94 | 5.84 | 1.02 | 39.20 | 0.02 | 25.64 | 60.62 | 15.74 | - | RS-Vietnam |
| 92 | 58.47 | 14.33 | 17.93 | 9.27 | 32.8 | 5.2 | 3.4 | 40.57 | - |  |  |  |  | RS-India |
| 94 | 66.09 | 12.51 | 17.96 | 3.43 | 38.43 | 5.44 | 0.71 | 53.63 | 0.19 | - |  |  | 12.35 | RS-Australia |
| 96 | 78.64 79.95 80.36 |  | 12.6 11.26 10.53 | 8.94 8.79 9.11 | 37.88 39.54 39.12 | 5.34 4.75 4.58 | 1.41 0.88 0.91 | 55.31 54.63 55.17 | 0.06 0.20 0.20 | - |  |  |  | RH-Malaysia sizes < 250, 250-500, 500-710 µm |
| 97 | 64.27 | 16.74 | 13.84 | 5.15 | 38.45 | 6.07 | 0.90 | 54.55 | 0.03 | - |  |  | 15.84 | RH-Malaysia |
| 98 | 81.90 |  | 11.71 | 6.47 | 48.69 | 6.97 | 0.37 | 43.94 | - | - |  |  |  | RH-India |
| 99 | 61.69 67.82 | 14.54 13.40 | 16.31 11.52 | 7.46 7.26 | 46.05 52.33 | 5.08 5.00 | 0.63 1.20 | 48.24 41.47 | - | - |  |  | 18.12 17.26 | RH & RS - china |
| 100 | 69.75 | 12.67 | 17.58 | db | 50.20 | 6.47 | 1.05 | 42.16 | 0.12 | 19.8 | 27.2 | 3.3 |  | RS-china |
| 101 | 79.8 |  | 11.7 | 8.5 | 39.6 | 5.8 | 0.7 | 53.7 | 0.2- 0.1Cl | - |  |  | 16.9 | RS-Tiwan |
| 105 | 77.5 | 10.9 | 11.6 | 8.0 | 40.30 | 5.53 | 1.07 | 53.10 | - | - |  |  |  | RS-India |
| 106 | 64.9 65.5 | 11.5 14.6 | 14.7 10.5 | 8.9 9.4 | 58.7 40.7 | 0.5 6.0 | 1.1 0.5 | 16.1 32.9 | <0.02 <0.02 | - |  |  | 18.3 15.7 | RS RH-Portugal |
| 107 | 81.6 80.2 | - | 23.5 19.8 | Db daf | 38.9 36.9 | 5.1 5.0 | 0.6 0.4 | 32.0 37.9 | - | 24.3 22.7 | 31.3 37.0 | 14.3 13.6 | 15.29 16.78 | RH RS -India |
| 108 | 57.89 | 15.47 | 15.92 | 10.48 | 47.28 | 5.25 | 0.58 | 46.66 | 0.23 | - |  |  | 16.67 | RH-Malaysia |
| 109 | 72.81 | 14.28 | 12.91 | - | 40.15 | 5.78 | 0.75 | 40.41 | - | - |  |  | 16.87 | RS-China-db |
| 111 | 76.32 | 13.91 | 9.08 | - | 37.18 | 5.81 | 0.62 | 56.39 | - | - |  |  | 15.76 | RS-India |
| 113 | 63.23 61.80 | 14.47 12.94 | 13.17 12.75 | 9.13 12.51 | - | - | - | - | - | - |  |  | 15.58 14.67 | RH RS-India |
| 114 | 60.66 | 16.56 | 12.71 | 10.07 | 27.42 | 4.7 | 0.7 | 34.3 | 0.16 | - |  |  |  | RS-China. |
| 115 | 66.89 | 14.57 | 7.56 | 10.8 | 39.98 | 2.45 | 4.43 | 52.61 | 0.53 | - |  |  |  | RS- Malaysia |
| 117 | 75.5 | 8.9 | 15.4 | 6.0 | - | - | - | - | - | 25.0 | 40.0 | 8.0 | 14.0 | RS-India |
| 118 | 66.9 | 16.5 | 16.6 | db | 42.4 | 6.4 | 0.6 | 50.6 | - | - |  |  |  | RS-Thailand |
| 119 | 73.6 | 7.9 | 18.5 | db | 38.0 | 5.1 | 1.5 | 36.9 | - | - |  |  | 14.9 | RS pellet- |
| 120 | 58.22 | 8.48 | 24.71 | 8.59 | 34.9 | 5.15 | 0.31 | 59 | 0.64 | 10.07 | 37.34 | 41.08 |  | RH-UK |
| 121 | 57.55 | 22.21 | 14.68 | 5.56 | 38.47 | 5.75 | 1.68 | 54.09 | <0.01 | 18.12 | 36.23 | 24.65 | 15.49 | RH-Malaysia |
| 122 | 64.45 | 12.67 | 13.41 | 0.41 | 36.48 | 3.60 | - | 46.51 | - | - |  |  |  | RH-Bangladesh |
| 123 | 78.07 | 6.93 | 15.0 | 11.69 | 36.07 | 5.20 | 0.64 | 57.83 | 0.26 | - |  |  |  | RS-China |
| 124 | - | - | - | 5.94 | 36.02 | 6.63 | 1.12 | 55.85 | 0.38 | - |  |  | 15.06 | RS-Malaysia |
| 125 | 80.1 | 11.1 | 7.9 | 1.0 | 39.5 | 5.7 | 0.8 | 29.3 | 1.1 | - |  |  |  | RS-China |
| 126 | 63.6 | 17.4 | 14.0 | 5.0 | 39.6 | 5.8 | 2.2 | 52.3 | 0.1 |  |  |  | 13.1 | RS-China |
| 127 | 64.45 | 12.67 | 9.47 | 13.41 | 41.48 | 3.60 | - | 41.51 | - | - |  |  |  | RS-Bangladesh |
| 128 | 67.6 | 6.3 | 16.6 | 9.5 | 49.2 | 2.2 | 0.44 | 48.3 | 0.06-0.08Cl | - |  |  | 19.8 | RH-Portugal |
| 129 | 68.37 | 17.72 | 13.01 | - | 43.27 | 6.13 | 1.3 | 34.37 | 0.72 | - |  |  |  | RS-China-db |
| 130 | 64.47 | 12.56 | 15.09 | 7.88 | 40.07 | 5.52 | 0.87 | 53.40 | 0.132 | - |  |  | 15.33 | RS-China |
| 131 | 72.27 | 14.57 | 13.16 | - | 40.67 | 6.79 | 0.44 | 51.23 | 0.87 | - |  |  | 16.56 | RH-Malaysia |
| 134 | 60.3 | 14.4 | 16.6 | 9.5 | 49.2 | 2.2 | 0.44 | 48.1 | 0.06 | - |  |  | 19.8 | RH- Portugal |
| 135 | 61.7 | 15.31 | 15.95 | 7.04 | 46.75 | 6.66 | 0.66 | 45.94 | - | - |  |  | 15.59 | RH- Thailand |

HC.*: Hemicellulose      C.*: Cellulose      L.*: Lignin

Table S3: Bio-oil compositions from pyrolysis of rice residues.

| Ref. No. | Reactor type, yrolysis types, temperature | Bio-oil compoistion |
| --- | --- | --- |
| [1] |  | Acetic acid (C2H4O2) - Furan, 2,5-dimethyl- (C6H8O) -2-Furanmethanol (C5H6O2)- 2H-pyran, 3,4-dihydro (C5H8O) - 2(3H)-furanone, 5-methyl- (C5H6O2) - Phenol (C6H6O) - 1,2-Cyclopentanedione-3-methyl- (C6H8O2) - Phenol, 2-methoxy- (C7H8O2) - Maltol (C6H6O3) -2-Cyclopentan-1-one, 3-ethyl-2-hydroxy- (C7H10O2) - Phenol, 4-ethyl- (C8H10O) - 1,2-Benzenediol (C6H6O2) - Benzofuran, 2,3-dihydro- (C8H8O) - 1,2-Benzenediol, 3-methyl- (C7H8O2) - 1,2-Benzenediol, 3-methoxy- (C7H8O3) - Phenol, 4-ethyl-2-methoxy- (C9H12O2) - 4-Hydroxy-3-methylacetophenone (C9H10O2) - Phenol, 2,6-dimethoxy (C8H10O3) - Benzaldehyde, 3-hydroxy-4-methoxy (C8H8O3) - Phenol, 2-methoxy-4-(1-propenyl)- (C10H12O2) -Ethanone, 1-(4-hydroxy-3-methoxyphenyl)- (C9H10O3) - 2-Propanone, 1-(4-hydroxy-3-methoxypheny)- (C10H12O3) - Benzeneacetic acid, 4-hydroxy-3-methoxy- (C9H10O4) - Phenol, 2,6-dimethoxy-4-(2-propenyl)- (C11H14O3) |
| [7] | Microwave oven – 300 W- Slow - 400 oC | (1) alkanes (C12 tto C32) as Dodecane -Tridecane -Tetradecane -Pentadecane -Hexadecane -Heptadecane -Octadecane -Nonadecane –Eicosane -Heneicosane -Docosane -Tricosane -Tetracosane -Pentacosane -Hexacosane -Heptacosane -Octacosane -Nonacosane -Triacontane -Hentriacontane –Dotriacontane, (2) polars as Phenol -Methylphenol -Dimethylphenol -Ethylphenol -Trimethylphenol –Trimethylbenzenediol, (3) polycyclic aromatic hydrocarbons (PAHs), 2–3 rings as Naphthalene -Methylnaphthalene -Dimethylnaphthalene -Acenaphthylene -Fluorene –Anthracene. |
| [11] | Drop type fixed bed - Fast - 350–600 ◦C | The catalyzed RH bio-oil is single phase with dark brown color- organic acid e.g. (acetic and formic acids), carbonyls e.g. (cyclopentanone, furfural, furanones), phenols (gusiacol, catechol) anhydrosugars e.g.(levoglucosan) and hydrocarbons. |
| [12] | Pulse current heating apparatus with a graphite die -300 to 800 oC | Toluene – Furfural – Pheno l-Guaiacol – Catechol - m-Cresol Levoglucosan - Tetracosane at 500 oC. Aromatic hydrocarbons (Benzene and Styrene)- polycyclic aromatic hydrocarbons (Naphthalene, Phenanthrene, Anthracene, and Pyrene) -Toluene-Ethynylbenezne- Phenol-o-Cresol- -P-Cresol- Biphenyl- Methylnaphthalene- Accenaphthylene-α-Biphenylenemethane-Phenanthrene - Tetracosane at 800 oC. |
| [22] | Fluidized bed - Fast - 450–550 oC | RH: Formic acid (highest%)-b-Hydroxybutyric acid-Toluene-Benzoic acid, 3-methyl-1,2-Benzenedicarboxylic acid- -2-Cyclopentane-1-one, 3-methyl-4H-Pyran-4-one, 2,6-dimethyl- Acetophenone, 1-(4-hydroxy-3-methoxy) Benzaldehyde- 2-hydroxyl – Benzaldehyde- 3,5-dimethyl-4-hydroxyl |
| [23] | Bench-scale plant equipped with conical spouted bed reactor(CSBR) - Fast – 400 to 600 oC | Acids: Acetic acid - Propanoic acid - 2-Oxopropanoic acid - 4-Oxopentanoic acid Aldehydes: Formaldehyde - Butanedial – Ketones: 1-Hydroxy-2-propanone - 2-Butanone 1,3-Cyclopentanedione - 2-Hydroxy-3-methyl-2-cyclopentenone – Phenols: Phenol - Cresols - Guaiacol - 4-Methylguaiacol - Eugenol - Catechol - Methylcatechol - Ethers - 2,2,4-Trimethyl-1,3-dioxalan-Carboxylic Anhydrides - Furans - Coumaran - Saccharides - Levoglucosan - Nitrogenated compounds Water – undefined. |
| [25] | Fixed bed - Fast - 400–800 oC | Acetic acid (C2H4O2) - Furan, 2,5-dimethyl- (C6H8O) - 2-Furanmethanol (C5H6O2) - 2H-pyran, 3,4-dihydro (C5H8O) - 2(3H)-furanone, 5-methyl- (C5H6O2) - Phenol (C6H6O) - 1,2-Cyclopentanedione-3-methyl- (C6H8O2) - Phenol, 2-methoxy- (C7H8O2) - Maltol (C6H6O3) 2-Cyclopentan-1-one, 3-ethyl-2-hydroxy- (C7H10O2) - Phenol, 4-ethyl- (C8H10O) - 1,2-Benzenediol (C6H6O2) - Benzofuran, 2,3-dihydro- (C8H8O) - 1,2-Benzenediol, 3-methyl- (C7H8O2) - 1,2-Benzenediol, 3-methoxy- (C7H8O3) Phenol, 4-ethyl-2-methoxy- (C9H12O2) - 4-Hydroxy-3-methylacetophenone (C9H10O2) - Phenol, 2,6-dimethoxy (C8H10O3) - Benzaldehyde, 3-hydroxy-4-methoxy (C8H8O3) - Phenol, 2-methoxy-4-(1-propenyl)- (C10H12O2) - Ethanone, 1-(4-hydroxy-3-methoxyphenyl)- (C9H10O3) - 2-Propanone, 1-(4-hydroxy-3-methoxypheny)- (C10H12O3) - Benzeneacetic acid, 4-hydroxy-3-methoxy- (C9H10O4) - Phenol, 2,6-dimethoxy-4-(2-propenyl)- (C11H14O3). |
| [26] | Fixed bed with 3-stage condensation columns – Slow - 400 to 600 oC | RH: acids, furans, ketones (high boiling point components, such as methyl cyclopentenone, 3-ethyl-2-hydroxy-2-cyclopenten-1-one and low boiling point components, as 2-butanone), alcohols, acetates, and phenols (extremely high), cyclopentenones, guaiacols, 2- methoxy-4-methylphenol, 4-ethyl-2-methoxyphenol, 2-methoxy-4-vinylphenol, and water. |
| [28] | Microwave oven - Fast – 400 to 600 oC | RS: Phenol- Catechol, p-Cresol, Furfural, Acetic acid, Phenol, 2-methoxy-, Phenol, 2-methyl-, Phenol, 4-ethyl-,2-Cyclopenten-1-one, 2-hydroxy-3-methyl-, 1,2-Benzenediol, 3-methyl-, 2-Propanone, 1-hydroxy, 2-Cyclopenten-1-one, 3-methyl-, Phenol, 2,6-dimethoxy-, Hydroquinone, 2(5H)-Furanone, 1-Hydroxy-2-butanone, 2 -Cyclopenten -1-one, 2-methyl-, Butanoic acid, Pyridine, Vanillin, 2-Propanone, 1(acetyloxy)-, Ethanone, 1-(2-furanyl)-, 2-Methoxy-5-methylphenol, Stigmasta-3,5-diene, Phenol, 2,4-dimethyl-, 3,4,5-Trimethylpyrazole, 1,2-Benzenediol, 3-methoxy-, 2-Isopropoxyphenol, Phenol, 4-(ethoxymethyl)-2-methoxy-, 2-Cyclopenten-1-one, 2,3-dimethyl- |
| [31] | Fluidized bed - Fast – 400 to 550 oC | RH: Acetic acid, Propanoic acid, 2-Cyclopenten-1-one, 2,5-Dimethyl-furan, 2-Methyl-2-cyclopenten-1-one, 3-Methyl-2-cyclopenten-1-one, 1-(2-Furanyl)-ethanone, 2-Hydroxy-3-methyl-2-cyclopenten-1-one, 2,3-Dimethyl-2-cyclopenten-1-one, (10-Propenyl) thiophene, Levoglucosan, Hexadecanoic acid, Phenol, 2-Methyl-phenol, 4-Methyl-phenol, 2-Methoxy-phenol, 2,6-Dimethyl-phenol, 2,4-Dimethyl-phenol, 3,5-Dimethyl-phenol, 2-Ethyl-phenol, 4-Ethyl-phenol, 3-Ethyl-phenol, 3-Methoxy-2-methylphenol, 1,2-Benzenediol, 4-Vinylphenol, 4-Ethyl-3-methyl-phenol, 4-(2-Propenyl)-phenol, 4-Methyl-1,2-benzenediol, 2-Methyl-6-(2-propenyl)-phenol |
| [32] | Drop type fixed bed - Fast – 350 to 600 oC | For catalytic and noncatalytic RH: Organic acide (acetic and formic acids), carbonyls (cyclopentanone, furfural, and furanones), phenols (gusiacol, catechol) anhydrosugars (levoglucosan) and hydrocarbons. |
| [33] | Fluidized bed - Fast – 600 oC | Formaldehyde, Xylitol, Acetaldehyde, o-Cresol, Methyl acetate, m-Cresol, Glucidol, 2-Methoxy-6-methyl-phenol, Ethyl hydroxyl-acetate, Succinicate ethyl methyl ester, Hydroxyacetaldehyde, 3,4-Dimethyl-phenol, Hydroxypropanone, 4-Ethyl-phenol, Ethyl formate, Lactose, Formic acid, 3-Hydroxy-dodecanoic acid,Acetic acid, 2-Methyl-benzaldehyde, 2-Oxo-butyl acetate, Isoeugenol, Pentanal, Catechol, 2,2-Dimethoxy-ethanol, 3-Methyl-catechol, Propionic acid, Vanillin, Furfural, 4-Methyl-catechol, But-2-en-1-ol, Melibiose, 2,5-Dimethoxy-tetrahydrofuran, 3-Hydroxy-D-tyrosine, 1,3-dihydroxy-propanone 46 4-Ethyl-catechol, Valeric acid 47 3-Hydroxy-tridecanoic acid, 4-Hydroxy-butyric acid 48 3-Methyl-4-ethyl-phenol, 5H-Furan-2-one, 4-(3-Hydroxy-propenyl) - phenol, 2,3-Dimethyl-cyclohexanol, Levoglucosan, 3-Hydroxy-cyclohexanone, 3-(4-Hydroxy-2-methoxy-phenyl)- propenal, 4-Isopropyl-cyclohexanol, D-Glycero-L-gluco-heptose, Allylacetic acid, 2-(2-Isopropyl-phenyl)-propan-1-ol, Corylon, 2-Naphthoic acid, 4-Methyl-5H-furan-2-one, 3-Methoxy-5-methyl-4-nitro-phthalic acid, 4-Methoxy-phenol, 3-Methoxy-2-naphthoic acid |
| [34] |  | For Auger: Alkanes as Tridecane, Dodecane, Hexadecane, etc. – Alkenes as 1-Dodecene, 1-Tetradecene, etc. – Alcohols as Nonanol, 4,8-dimethyl- and2-Furanmethanol, tetrahydro- - Ketones as 2-Cyclopenten-1-one, 2-methyl-, 2-Cyclopenten-1-one, 3-methyl-, et c. – Phenols as Phenol, 2-methyl-, Phenol, 4-ethyl-, etc. – Aromatics as Benzene, 1,2,3-trimethyl-, Benzene, 1-ethyl-2-methyl-, etc. – Benzonitrile For Batch: Alkanes as Nonane, Tridecane, etc. – Alkenes as 1-Decene, 4-methyl-, 3-Tetradecene, (Z)-, etc. – Alcohols as 1,2-Ethanediol, diacetate and 2-Furanmethanol, tetrahydro – Ketones as Cyclopentanone, Cyclopentanone, 2-methyl-, Cyclopentanone,3-methyl-, 2-Cyclopenten-1-one, 2-methyl-, Cyclopenten-1-one, 2,3-dimethyl – Phenol as Phenol, 2-methyl-, Phenol, 3-methyl-, Phenol, 2,4-dimethyl- - Aromatic as Ethylbenzene, Benzene, 1,2,4-trimethyl, Benzene, 1-ethyl-2-methyl-, Toluene – Nitriles as Butanenitrile, 3-methyl-, Pentanenitrile. For FB: acids appears as Acetic acid, methyl ester, Butanoic acid, Propanoic acid, Alkenes, Alcohols, ketones, Phenols, Aromatic, Furfural, Benzofuran, 2,3-dihydro, D-Allose, Butanedial, Hexanedial, and 3-Aceto xybenzaldehyde. |
| [35] | Fixed bed - Fast – 450 to 600 oC | Saccharides (LG- major), Furans, Ketones, Alkohols, Phenols, Esters, and Others (benzene, toluene, xylene, alkenes) |
| [39] | Fixed bed - Slow – 300 to 450 oC | In CO2: 3-Furanmethanol, 2-propyltetrahydrofuran, Phenol, 3-methyl-1,2-Cyclopentanedione, 2-methyl-Phenol 2-methoxy-Phenol, 2-ethyl-Phenol, 2,4-dimethyl –Phenol, 4-ethyl-Phenol, Creosol, 2,3-dihydro Benzofuran, 4-(1-methylethyl)-Phenol, 4-ethyl-2-methoxy-Phenol, 2-Methoxy-4-vinylphenol, 2,6-dimethoxy-Phenol, trans-Isoeugenol, 2,6-dimethoxy-4-(2-propenyl)-Phenol In N2: 2-Furanmethanol, Phenol, 3-methyl-1,2-Cyclopentanedione, 2-methyl-Phenol 2-methoxy-Phenol, 2-ethyl-Phenol, 2,4-dimethyl –Phenol, 4-ethyl-Phenol, 2,3-dihydro-Benzofuran, 4-ethyl-2-methoxy-Phenol, 2-Methoxy-4-vinylphenol, 2,6-dimethoxy-Phenol, 3-methyl 2-Cyclopenten-1-one, 3-ethyl-2-hydroxy-2-Cyclopenten-1-one, 2,5-dimethyl Phenol, Naphthalene, Catechol, 2-methyl-Naphthalene, 2-methyl-1,4- |
| [38] | HTL Reactor - Hydrothermal liquefaction – 300 to 350 oC | RS: simple oxygenates, cyclo-oxygenates (cyclopentanone,2-cyclopentene-1-one, 3-methyl-2-cyclopentene-1-one, 2,3-dimethyl-2-cyclopentene-1-one, 2,3,4-trimethyl-2-cyclopentene-1-one, and 2-acetonylcyclopentanone), aliphatic hydrocarbons, phenolics (phenol, 2-methylphenol (o-cresol), 4-ethylphenol, catechol, guaiacol, 4-ethylguaiacol, alkyl-substituted benzenediols, hydroxyl acetophenone, and syringol), aromatics (aromatic hydrocarbons and aromatic oxygenates), indene derivatives, furan derivatives, and esters. |
| [40] [42] | Fixed bed - Slow – 300 to 450 oC Micropyrolzer - Fast - 450 to 550 oC | Furfural: 2-Furanmethanol, 2-Cyclopenten-1-one, 3-methyl-, 3-Hexen-2-one, 3-methyl- Phenol: 2-Cyclopenten-1-one, 2-hydroxy-3-methyl-, Phenol, 2-methyl-, Phenol, 3-methyl-, Phenol, 2-methoxy-, Phenol, 2,4-dimethyl-, 2-Cyclopenten-1-one, 3-ethyl-2-hydroxy-, Phenol, 2,5-dimethyl-, Phenol, 4-ethyl-, Creosol, Catechol, Benzofuran, 2,3-dihydro-, 1,2-Benzenediol, 3-methyl-, Phenol, 4-ethyl-2-methoxy-, 1,2-Benzenediol, 4-methyl-, 2-Methoxy-4-vinylphenol, Phenol, 2,6-dimethoxy- Benzaldehyde, 3-hydroxy-4-methoxy-, 3-Hydroxy-4-methoxybenzoic acid, 1,2,3-Trimethoxybenzene trans-Isoeugenol, Apocynin, Homovanillyl alcohol, Phenol, 2-methoxy-4-(1-propenyl)-, (Z)-, 5-tert-Butylpyrogallol, n-Hexadecanoic acid, 1,2-Cyclopentanedione, 3-methyl-, p-Cresol, Vanillin, 4-Ethylcatechol, 1-Penten-3-ol, 2-methyl-, Hydrazine, 1-(4-ethylphenyl)-, Octadecanoic acid. Acetic Acid, Furfural, Pyridine, Anisole, m-cresol, Methyl syringol, Syringaldehyde, 2-Butanone, 3-Pentanone, Phenol, 3-methoxycatechol, 2-methoxyphenol, Furfuryl alcohol, Toluene, Eugenol, Acetol, Levoglucosan, d-xylose. |
| [46] | Solar pyrolyzer - 500 to 800 oC | Acids (sorbic, hexanoic, palmitic, dodecanoic etc), alcohols (isobutanol, 2-Methyl-1-butanol, furfuryl, guaiacol etc), phenols (3-ethylphenol, 4-methylcatechol, catechol, cresols etc) and small amounts of esters, ketones as well as aldehydes such as 1-dimethylvinylsilyloxy-3-methylbenzene and vanillin. Isobutanol, 1-dimethylvinylsilyloxy-3-methylbenzeneand hepta-ethylene glycol were the prominent compounds produced at 500 °C. Pentaethylene glycol was dominant compound at 600 °C. High concentrations of isobutanol, 1-dimethylvinylsilyloxy-3-methylbenzene and heptaethylene glycol were detected at 700 °C. As the temperature further increased to 800 °C, the compound 1-dimethylvinylsilyloxy-3-methylbenzene was found to be the most abundant in the bio-oil. |
| [49] | Downdraft circulating fluidized bed – Fast – 550 oC | Bio-oil sample were phenols, ketones and aldehydes. While in No.2 bio-oil sample the most abundant chemical compounds were phenols, ketones and furans. Phenols, ketones and aldehydes were the three highest contents chemical compounds in No.3 sample. |
| [50] | Bubbling fluidized bed - Fast – 400 to 600 oC | Acids: Acetic acid C2H4O2, Propanoic acid C3H6O2, 2-Propenoic acid C3H4O2, Butanoic acid, 4-hydroxy- C4H8O3, Alcohols: Methyl Alcohol CH4O, 2-Propen-1-ol C3H6O, Cycbpropylcarbino C4H8O, 2-Cyclopenten-1-one, 2-hydroxy- C5H6O2, Cyclopentanol C5H10O, Dianhydromannitol C6H10O4, Cyclohexen-1-ol C6H10O, Aldehydes: Formaldehyde CH2O, Acetaldehyde, hydroxy- C2H4O2, Propanal C3H6O, Butanedial C4H6O2, Benzaldehyde, 3-hudroxy-4-methoxy- C8H8O3, 4-Hydroxy-2-methoxycinnam aldehyde C10H10O3, Ketones: 2-Propanone, 1-hydroxy- C3H6O2, 2,3-Butanedione C4H6O2, 2-Butanone, 3-hydroxy- C4H8O2, 1-Hydroxy-2-butanone C4H8O2, 2-Propanone, 1-(acetyloxy)- C5H8O3, 3-Pentanone C5H10O, 2-Cyclopenten-1-one, 2-methyl- C6H8O, 2-Cyclopenten-1-one, 3-methyl- C6H8O, 2-Cyclopenten-1-one, 2-hydroxy-3-methyl- C6H8O2, 2-Butanone, 1-(acetyloxy)- C6H10O3, Ethanone, 1-(2-hydroxy-5-methylphenyl)- C9H10O2, Furans: 2(5H)-Furanone C4H4O2, 2,3-Dihydrofuran C4H6O, Furfural C5H4O2, 2-Furanmethanol C5H6O2, 2,4(3H,5H)-Furandione, 3-methyl- C5H6O3, 2-Furanol, tetrahydro-2-methyl- C5H10O2, 2-Furancarboxaldehyde, 5-methyl- C6H6O2, 2-Furancarboxaldehyde, 5-(hydroxymethyl)- C6H6O3, Benzofuran, 2,3-dihydro- C8H8O, Phenols: Phenol C6H6O, Hydroquinone C6H6O2, 1,2-Benzenediol C6H6O2, Phenol, 2-methoxy- C7H8O2, Phenol, 2-methyl- C7H8O, Phenol, 4-methyl- C7H8O, Phenol, 2,4-dimethyl- C8H10O, Phenol, 4-ethyl- C8H10O,Phenol, 2-methoxy-4-methyl- C8H10O2, Phenol, 2,6-dimethoxy- C8H10O3, 1,4-Benzenedicarboxaldehyde, 2-methyl- C9H8O2, 2-Propenoic acid, 3-(2-hydroxyphenyl)-, (E)- C9H8O3, 2-Methoxy-4-vinylphenol C9H10O2, Phenol,2-methoxy-6-(2-propenyl)- C10H12O2, Phenol, 4-ethyl-2-methoxy- C9H12O2, Phenol, 4-(3-hydroxy-1-propenyl)-2-methoxy- C10H12O3, Phenol, 2-methoxy-4-(1-propenyl)- C10H12O2, Esters: Acetic acid, methyl ester C3H6O2, Butyrolactone C4H6O2, 2-Propenoic acid, ethenyl ester C5H6O2, Propanoic acid, 2-oxo-, methyl ester C4H6O3, Sugar: 1,6-Anhydro-á-D-glucopyranose C6H10O5 |
| [52] | Fluidized bed - Slow - 500 oC | Acetic acid, 2-Propanone, 1-hydroxy, Pentane, 3-methyl, Furfural, Acetic anhydride, 2-Hexene, Phenol, 2-Cyclopenten-1-one, 2-hydroxy-3-methyl, Phenol, 2-methoxy, Phenol, 4-ethyl, Phenol, 2-methoxy-4-methyl, Phenol, 2-methoxy-4-propyl, Phenol, 2-(1,1-dimethylethyl)-, Phenol, 2-methoxy-4-(1-propenyl)- |
| [57] | Fluidized bed - Slow - 500 oC | Acetic acid, Benzene, Toluene, Ethylbenzene, p-Xylene, 2-Methyl-2-cyclopenten-1-one, Aceto, 4-Hydroxy-4 methyl-2-pentanone, Furfural, Furfuryl alcohol, Phenol, o-Cresol, p-Cresol, m-Cresol, 2-Methoxy-4-methylphenol, 2-Ethylphenol, 2,4-Dimethylphenol, 4-Ethylphenol, 2,6-Dimethoxypheno, cis/trans-Isoeugenol, Guaiacol, Levoglucosan. |
| [60] | tubular quartz reactor - Fast –Vacuum condition- 300 to 700 oC | RH and A-RH: aliphatic hydrocarbons (C8–C13 alkanes - minor), aromatic compounds(xylenes, phenol, methyl-phenols, 1,2-benzendiol, 3-hydroxy-4-methoxy-benzaldehyde and guaiacols), furan derivatives (2,3-dihydro-benzofuran (DHBF), 5-hydroxymethyl furfural (HMF) and 4-hydroxy-dihydrofuran-2-one), oxygenates (ketones, aldehydes, carboxylic acids, alcohols and ethers - 3-methylcyclopentane-1,2-dione, cyclohexanone, pentanal, cyclic ethers, acetic acid and C4–C16 carboxylic acids), anhydrosugars (LG, 1,4:3,6-dianhydro-D-glucopyranose (DGP), 2,3-anhydro-D-mannosan (AM) and 1,6-anhydro-D-glucofuranose (AGP) in RH at 500 oC). For reactions of A-RH: levoglucosenone (1,6-anhydro-3,4-dideoxyhex-3-enopyran-2-ulose, LGO and DGP) at 300-400 oC. |
| [63] | Fixed bed - Slow – 500 oC | Hydrocarbon (paraffin, olefin, and aromatic hydrocarbons), phenol, alcohol, acid, aldehyde, ketone, ether, ester, furfural, N-containing compound (amine, amide, nitrile, indole, azole, and nitrogen heterocyclic compounds), and N.O-containing compound (amide, imide, oxime, Pyrrolidinedione). Alcohol, aldehyde, acids, ketone, ether, ester, furfural, and phenol derivatives are known as oxygen-containing species |
| [67] | Fixed bed - Slow – 550 oC | Catalyized and non-catalized RH: organic acids, aldehydes, alcohols, ketones, phenols, guaiacols, furans and anhydrosugars. |
| [68] | Fluidized bed - Slow – 500 oC | RS: Furfural, Acetoxyacetone, 1-hydroxyl, Furfural, 5-methyl, Phenol, 2-Cyclopentane-1-one, 3-methyl, Benzaldehyde, 2-hydroxyl, Phenol, 2-methyl, Phenol, 4-methyl, Phenol, 2-methoxyl, Phenol, 2,4-dimethyl, Phenol, 4-ethyl, Phenol, 2-methoxy-5-methyl, Phenol, 2-methoxy-4-methyl, Benzene, 1,2,4-trimethoxyl, Phenol, 2,6-dimethyl-4-(1-propenyl), 1,2-Benzenedicarboxylic acid, diisooctyl ester, 2-Furanone, Levoglucosan, Phenol, 2,6-dimethoxy-4-propenyl, Furanone, 5-methyl, Acetophenone, 1-(4-hydroxy-3-methoxy), Vanillin, Benzaldehyde, 3,5-dimethyl-4-hydroxyl, Cinnamic aldehyde, 3,5-demethoxy-4-hydroxyl. |
| [69] | Fixed bed - Slow – 400 to 700 oC | RH- ZnO/RH: Alkanes C6H14, Toluene C7H8, Alkenes C7H12, Furan,2,4-dimethyl C6H8O, Toluene,2-methyl C8H10, Styrene C8H8, Phenol,4-methxyl C7H8O, Phenol,2,3,5-trimethyl C9H12, Benzene,1‐propyl C9H12, Phenol C6H6O, Octadiene C8H14, Phenol,2-methyl C7H8O, Phenol,3-methyl C7H8O, Benzoic acid C7H6O2, Phenol,2-methoxy C7H8O2, Phenol,1-methyl-2-ethyl C9H12O, Phenol,2-methoxy-4-methyl C8H10O2, Phenol,2-butyl C10H14O, Phenol,1-ethyl C8H10O, Heptylate C7H14O2, 1,2-Benzenediol,3,4-dimethyl C8H10O2, Phenol,2-ethyl-4-methyl C9H12O, Benzaldehyde,1-methyl C8H8O, Phenol,1-trimethyl C9H12O, 1,4-Benzenediol,3-trimethyl C9H10O2, 1,4-Benzenediol,2,3,5-trimethyl C9H12O2, Naphthalene C10H10, Phenol,2,5-methoxyl C8H10O3, 1H-Inden-1-one,2,3-dihydro-methoxy C10H12O2, Eugenol C10H12O2, Benzoic acid,4-hydroxy-3-methoxy C8H8O4, Phenol,2-methoxy-4-trimethyl C10H14O2, Naphthalene,2,5-dimethyl C12H12, Benzeneacetic acid,4-hydroxy-3-methoxy C9H10O4, Phenol,3,5-dimethoxy-4-(2-propenyl) C11H14O3, 93 Fatty acid methyl esters C17H34O2, 1-Octadecene C18H36, Eicosane C20H42, Docosane C22H46 |
| [70] | Fixed bed - Slow - 0.1 MPa to 5.0 MPa | RH Acetic acid, Methyl acetate, Pyrrolea, Furfural, 2-Furan at 0.1 MPa and 3.0 MPa: methanol, 2-Propanone,1-(acetyloxy)-, 2-Cyclopenten-1-one,2-hydroxy-, 2-Furancarboxaldehyde,5 methyl-, Furan,tetrahydro-2-methyl-, 2H-pyran,3,4-dihydro-, 2 Cyclopenten-1-one,2-hydroxy-, 3-methyl-, Phenol, Phenol,2-methoxy-, Phenol-2-methyl-, Phenol,4-methyl-, Phenol,2-methoxy-4-methyl-, Acetic acid,2-(N-methyl-Nphosphomethyl) amino-, Phenol-4-ethyl, Phenol,4-ethyl-2-methoxy-, Bebzofuran, 2,3-dihydro-, Phenol,2-Methoxy-4-vinyl-, Phenol,2,6-dimethoxy-, Phenol,2-methoxy-4-(1-propenyl)-, Hydroquinone, 2-Propanone, 1-(4-hydroxy-3-methoxyphenyl)-, 2-H-bezopyran-2-one,3,4 dihydro-, 6-hydroxy-, D-gluco-heptulosan ,2-Propenal,3-(4-hydroxy-3methoxyphenyl)-No benzene, toluene and xylene were detected. Acetic acid and its derivatives were the prominent compounds |
| [72] | Fixed bed - Slow- 500 oC - ZSM-5, Al-MCM-41, Al-MSU-F and Brunei rice husk ash (BRHA) were used as the catalysts | RH: Styrene C8H8, Furfural C5H4O2, Tetrahydro-2,5-dimethoxyfuran C6H12O3, 16 1-(Acetyloxy)-2-propanone/ Acetol acetate C5H8O3, Cyclopenten-1-one, 2-methyl- C6H8O, 2-Furyl methyl ketone C6H6O2, 1,2-cyclopentanedione C5H6O2, 5-Methyl-2-furancarboxaldehyde/5-methylfurfural C6H6O2, 2,3-Dimethyl-2-cyclopenten-1-one C7H10O, 3-Methyl-2-cyclopentenone C6H8O, 2(5H)-Furanone C4H4O2, 3-Methyl-1,2-cyclopentanedione C6H8O2, Phenol C6H6O, 2-Methoxyphenol/guaiacol C7H8O2, 2-Methylphenol/o-cresol C7H8O, Maltol/larixic acid C6H6O3, 4-Methylphenol/p-cresol C7H8O, 3-Methylphenol/m-cresol C7H8O, 2-methoxy-p-cresol/p-creosol C8H10O2, 2,4-Dimethylphenol /2,4-xylenol C8H10O, 4-Ethylphenol C8H10O, 4-Ethylguaiacol C9H12O2, 2,3-Anhydro-d-galactosan C6H8O4, 1,4:3,6-Dianhydro—dglucopyranose C6H8O4, o-Coumaric acid C9H8O3, 2-Methoxy-4-vinylphenol/4-vinylguaiacol C9H10O2, Isoeugenol C10H12O2 Isovanillin C8H8O3, Vanillyl methyl ketone C10H12O3, Levoglucosan C6H10O5 |
| [73] | Fluidized bed - Slow - 400, 450, 500, 550 and 600°C - zeolite ZSM-5 catalyst | RH: Aromatic HC: Toluene, Ethylbenzene, Naphthalene, Methylnaphthalenes, Biphenyl, Dimethylnaphthalenes, Acenaphthene, Trimethylnaphthalenes Tetramethylnaphthalenes, Fluorene, Methylfluorenes, Phenanthrene, Anthracene, Methyl-phenanthrenes, Dimethylphenanthrenes, Pyrene, Methylpyrene, Chrysene, Methylchrysene. Oxygenated compounds: Phenol, Cresols, Guaiacol, Ethylphenols, Dimethylphenols, Methylguiacols, Benzenediol, Trimethyl-phenols, Methylbenzenediols, Tetramethylphenols, Syringol, Propenylmethoxy-phenols, Naphthols, Methylnaphthols, Dimethylnaphthols, Trimethlnaphthols. |
| [74] | Fluidized bed - Fast - 350, 420, and 500 oC | RS: Methanol, Glycolaldehyde, Acetic acid, Acetol, 1-(Acetyloxy)-2-butanone, Butanedial, C Furfural, 3-Methyl-2-cyclopenten-1-one, L Phenol, 4-Methylphenol, L Guaiacol, 4-Ethylphenol, L 4-Vinylphenol, 4-Vinylguaiacol, L Syringol, Vanillin, C Levoglucosan, 4-Vinylsyringol (Refs.). L Methoxyeugenol, Acetosyringone Total yield of 40 pyrolytic compoundsc, Carbohydrate derivatives, Lignin derivatives, |
| [76] | Fluidized bed - Fast - 415–540 oC | RS: 2-Furancarboxaldehyde, 2(5H)-Furanone, 5-Methyl-2(3H)-furanone, Acetic acid, Furfural, 3-Methyl-2-cyclopenten-1-one, 2-Hydroxy-2-cyclopenten-1-one, 2-Hydroxy-3-methyl-2-cyclopenten-1-one, Phenol, o-Cresol, p-Cresol, o-Guaiacol, m-Xylenol, o-Xylenol, 4-Ethyl-phenol, Pyrocatechol, 4-Methyl-benzaldehyde, Hydroquinone, 3-Methyl-pyrocatechol, 3-Methoxy-pyrocatechol, 4-Methyl-catechol, Levoglucosan, p-Ethylguaiacol, 4-Methyl-pyrocatechol, p-Vinylguaiacol, Syringol, Eugenol, Vanillin, 4-Hydroxy-benzaldehyde, (E)-Isoeugenol, 2-Methoxy-4-(1-propenyl)-phenol, 2,6-Dimethoxy-4-(2-propenyl)-phenol. |
| [82] | Two-stage - Catalytic fast – 500 oC | RH:Acids: Acetic acid, Propanoic acid, Ketones: 2-Propanone, 1-hydroxy-, 1,2-cyclopentanedione , 2-cyclo penten-1-one, 3-methyl-, 1,2-cyclopentanedione, 3-methyl-, 2-cyclopenten-1-one, 3-ethyl-2-hydroxy-, Furans: Furfural, Furan, 2,5-diethoxytetrahydro-, Phenols: Phenol, Phenol, 2-methoxy-, p-Cresol, Phenol, 2,4-dimethyl-, Phenol, 4-ethyl-, Phenol, 3-ethyl-, Creosol, Benzofuran, 2,3-dihydro-, Phenol, 4-ethyl-2-methoxy-, Resorcinol, 2-acetyl-, 4-Methoxybenzene-1,2-diol, 2-Methoxy-4-vinylphenol, Phenol, 2,6-dimethoxy-, Phenol, 2-methoxy-4-(1-propenyl)-, Vanillin, Benzeneethanol, 3-hydroxy-, Sugars: l-Gala-l-ido-octose, Melezitose, levoglucose |
| [83] | Microwave oven - No catalyst RHC Ni/RHC Fe/RHC Cu/RHC | Acetic acid C2H4O2, 2-Propanone, 1-hydroxy- C3H6O2, Ethane, 1,1-diethoxy- C6H14O2, 1-Hydroxy-2 butanone C4H8O2, 2-Oxo-n-valeric acid C5H8O3, Furfural C5H4O2, Furan, 2,5-diethoxytetrahydro- C8H16O3, Pentane, 1,1-diethoxy- C9H20O2, Phenol, 2-methoxy- C7H8O2, 2-Pentanone, 5,5-diethoxy- C9H18O3, Phenol, 2-methoxy-4-methyl- C8H10O2, Phenol, 4-ethyl-2-methoxy- C9H12O2, 2-Methoxy-4-vinylphenol C9H10O2, Heptane, 1,1-diethoxy- C11H24O2, Benzenemethanol, 3-hydroxy-5-methoxy- C8H10O3, Phenol, 2-methoxy-5-(1-propenyl)-, (E)- C10H12O2, Levoglucosan C6H10O5, d-Mannose C6H12O6. |
| [84] | fluidized bed - Fast – 550 oC - ZSM-5, LOSA -1, Gamma- Al2O3 and FCC catalysts | All products: Aromatics: C2–C4 olefins, Petrochemicals, Methane, CO2, CO, Coke, Unidentified, Aromatic selectivity: Benzene, Toluene, Ethyl benzene, p-Xylene and m-Xylene, o-Xylene, Styrene, Indene, Naphthalene, 1-Ethyl-2-methyl benzene, 1,2,3-Trimethyl benzene, Benzofuran, 1-Ethenyl-4-methyl benzene, 2-Methyl benzofuran, 5-Methyl-1H-indene, 2-Methyl indene, 4,7-Dimethyl-1H-indene, 1-Methyl naphthalene, 2-Methyl naphthalene, 2,7-Dimethyl naphthalene, Olefin selectivity:Ethylene, Propylene, Butenes. |
| [85] | vertical drop fixed bed - Slow- 550 oC | RH: Acids: Acetic acid C2H4O2, Propanoic acid C3H6O2, n-Hexadecanoic acid C16H32O2, Octadecanoic acid C18H36O2, Ketones: 1-Hydroxy-2-butanone C4H8O2, Cyclopentanone C5H8O, 1,2-Cyclopentanedione C5H6O2, 1,2-Cyclopentanedione, 3-methyl- C6H8O2, Aldehydes: 4-Methyl-2,5-dimethoxy-benzaldehyde C10H12O3, 4-Hydroxy-3,5-dimethoxy-benzaldehyde C9H10O4, Esters: Ethane, 1,1-diethoxy- C6H14O2, Pentane, 1,1-diethoxy- C9H20O2, Furans: Furan, 2,5-dimethyl- C6H8O, Furfural C5H4O2, 2-Furanmethanol C5H6O2, 2(5H)-Furanone C4H4O2, 2(3H)-Furanone, 5-methyl- C5H6O2, 2-Furancarboxaldehyde, 5-methyl- C6H6O2, Furan, 2,5-diethoxytetrahydro- C8H16O3, Benzofuran, 2,3-dihydro- C8H8O, Phenols: Phenol C6H6O, Phenol, 2-methyl- C7H8O, Phenol, 4-methyl- C7H8O, Phenol, 2-methoxy- C7H8O2, Phenol, 2,4-dimethyl- C8H10O, Phenol, 4-ethyl- C8H10O, Phenol, 2,3-dimethyl- C8H10O, Phenol, 2-methoxy-4-methyl- C8H10O2, 1,2-Benzenediol C6H6O2, Phenol, 2-ethyl-5-methyl- C9H12O, 1,2-Benzenediol, 3-methoxy- C7H8O3, Phenol, 4-ethyl-2-methoxy- C9H12O2, 1,2-Benzenediol, 4-methyl- C9H12O2, 2-Methoxy-4-vinylphenol C9H10O2, Phenol, 2,6-dimethoxy- C8H10O3, Eugenol C10H12O2, Vanillin C8H8O3, Phenol, 2-methoxy-4-(1-propenyl)-, (E)- C10H12O2, Phenol, 2,6-dimethoxy-4-(2-propenyl)- C11H14O3, Sugars: Levoglucosan C6H10O5. |
| [86] | Bench-scale fluidized bed - Fast - | RH: 3-Hydroxy-2-butanone, 2-Propenoic acid, (E)-3-Penten-2-one, Pyridine, 1-Hydroxy-2-butanone, 1 (Acetyloxy) -2-butanone, Propanoic acid, 2-oxo-, methyl ester, Benzyl methyl ketone, Toluene, Cyclopentanone, Tetrahydro-2-furanol, Butanoic acid, 2-methyl-pyridine, Aniline, 2-Cyclopenten-1-one, Furfural, 2-Butanone, 1,6; 2,3-Dianhydro-4-O-acetyl-.beta.-D-talopyranose, 1-(Acetyloxy)-2-propanone, 2-Amino-3-methyl-2-butenenitrile, Carbamic acid, phenyl ester, 4-Hydroxy-butanoic acid, Butyrolactone, Bicyclo[4.2.0]octa-1,3,5-triene, 2-Methyl-2-cyclopenten-1-one, 1-(2-Furanyl)-ethanone, 2,5Hexanedione, 3-Methyl-2-cyclopenten-1-one, 4-Ethyldihydro-3-methylene-, [3aR-(3a.alpha.,4.beta.,6a.alpha.)]-furo[3,4-b]furan-2,6(3H,4H)-dione, 5-Methyl-2-furancarboxaldehyde, Pivalic acid-2-isopropoxyphenyl ester, Phenol, Benzofuran, Tetracyclo [3.3.1.0(2,8).0(4,6)]-non-2-ene, 3-Methyl-1,2-cyclopentanedione, 2,3-Dimethyl-2-cyclopenten-1-one, Indene, 1-Chloro-2,3-dihydro-1H-indene, Acetic acid-phenyl ester, 2-Methyl-phenol, 3-Methyl-phenol, 4-Methyl-phenol, Azulene, (2-Propynyloxy)-benzene, 2,6-Dimethyl-phenol, 2-Methyl-benzofuran, 2-Ethyl-phenol, 3,4-Dimethyl-phenol, 2-Methylindene, 2,5-Dimethyl-. 3-Methylphenyl ester acetic acid, 3-Ethyl-phenol, 2,3-Dimethyl-phenol, Azulene, 3,4-Dimethyl-phenol, 5,9-Dimethyl-, (E)-5,8-decadien-2-one, 1,2-Benzenediol, 2,3-Dihydro-benzofuran, Resorcinol monoacetate, Diacetate,1,2-benzenediol, 3-(1-Methylethyl)-phenol, 2,3,6-Trimethyl-phenol, 4-Ethyl-2-methyl-phenol, 5-Methylene-4,5,6,6a-tetrahydro-3ah-pentalen-1-one, 4-Ethylphenyl acetate, 4-hydroxy-benzenemethanol, 4-Methyl-1,2-benzenediol, 2,3-Dihydro-1H-indene-1,2-diol, 2,3-Dihydro-1H-inden-1-one, 4-tert-Butoxystyrene, 2-Allylphenol, 4-Methyl-1,2-benzenediol, 1-Methyl-naphthalene, 4-(Borane-dimethylamino) pyridine, 3-Hydroxy-benzenemethanol, 1,4-Dihydro-1,4-methanonaphthalene, 4-Butoxy-phenol, Pivalic acid, 2-isopropoxyphenyl ester, 3-Methyl-1,2-benzenediol, 4-(2-Propenyl)-phenol, 1H-Indenol, 3-Hydroxy-benzaldehyde, Diacetate-1,2-benzenediol, Resorcinol monoacetate, 1,1-Difluoro-2-phenyl cyclo propane, Biphenyl, 4-tert-Butoxystyrene 4-Ethylcatechol 5-(1-Propenyl)-, (Z)-1,3-benzodioxole, 2,3-Dimethoxy-benzenamin,e 5-Pentyl-1,3-benzenediol, 2-Methoxy-5-methylphenol, 1,7-Dimethyl-naphthalene, Bipheny97 Biphenylene, 3-Acetonyl-2-hydroxy-2,4,6-cycloheptatrien-1-one, 1-Hexyl-4-nitro-benzene, 3-Isopropoxy-5-methyl-phenol, 2-Naphthalenol, 1-Naphthalenol, Dibenzofuran, 3-Acetoxydodecane, Acetate-1-naphthalenol, 2-Methyl-1-naphthalenol, Alanine,N,N-dimethyl-3-phenyl-ethyl ester, p-Hydroxybiphenyl, 1-Allyl-1-but-3-enyl-1-silacyclobutane, 2-Methyl-1-decanol, Phenanthrene, Tetradecane. |
| [88] | Benchscale semi-batch pyrolysis reactor - Slow – 300 to 600 oC | Pentane, 3,3-dimethyl-, 1-Hexene, 3,4-dimethyl, Oxirane, 2-3thyl-2methyl-, Hexane, 2-chloro-, Phenol, Phenol, 2-methoxy-, Tridecane, Tetradecane, Dodecane, 2,6,10-trimethyl-, 1-Nonadecene, Pentadecane, Dodecanoic acid, methyl ester, Hexadecane, Nonadecane, 9-methyl-, Octadecane, Pentadecane, tetramethyl-, Octadecane, Nonadecane, Hexadecanoic acid, methyl este,r Eicosane, Heptacosane, Citronellol epoxide, Eicosane, (E)-5-isopropyl-6,7-Epoxy-8-Hydroxy-8-Methylnon-2-one, (Z)14-Tricosenyl formate, Cyclopentane,1-(2-decyldodecyl) - 2,4-dimethyl-, HAHNFETT, Docosane, Heptacosane. |
| [89] | Fluidized bed - Fast – 450 -550 °C | Acetaldehyde, 2(5H)-furanone, 5-methyl-, acetic acid, propionic acid, 2-propanone, 1-hydroxy-, 2-butanone, 1-hydroxy-, 2-cyclopenten-1-one, Furaldehyde, Phenol, 5-hydroxymethyl-2-furaldehyde, phenol, 2-methoxy-, phenol,2,4-dimethyl-, phenol, 2,6-dimethoxy- 1,2-benzendiol, 1,2-benzendiol, 4-methyl-, Vanillin, 1,2benzendiol, 4-ethyl-, 2-cyclopenten-1-one,2-hydroxy-3-methyl-, Eugenol, 1,4-benzendiol, D-glucopyranose, levoglucosan. |
| [97] | Microwave oven - Slow – 500 to 800 oC | RH: Monoaromatic compounds: Benzene, Toluene, Ethyl benzene, m&p xylene, o-xylene, Styrene, PAHs: Naphthalene, Acenaphthylene, Anthracene, Phenanthrene, Phenolic: Phenol, 2,4-dimethylphenol, 2-methylphenol, 3,4-methylphenol. |
| [99] | Spout fluidized bed - Fast – 400 to 580 oC | RS&RH: Acids: Acetic acid, Propanoic acid, Butanoic acid, Butanoic acid, 4-hydroxy-, Carbonyls: Hydroxy-acetaldehyde, 1-Hydroxy-2-butanone, 2-Propanone, 1-(acetyloxy)-, 2-Cyclopenten-1-one, 2-methyl-, 2(5H)-Furanone, 1,2-Cyclopentanedione, 2-Cyclopenten -1 -one, 3-methyl-, 2-Cyclopenten-1-one, 2-hydroxy-3 methyl-, 1,2-Cyclopentanedione, 3-methyl-, 2-Cyclopenten-1-one, 2,3-dimethyl-, 2-Cyclopenten-1-one, 3-ethyl-2 hydroxy-, Benzal-dehyde, 3,5-dimethyl-, Furans: Furfural, 2-Furanmethanol, Furan, 2,5-diethoxytetrahydro-, Benzofuran, 2,3-dihydro-, Phenols: Phenol, Phenol, 2-methyl-, Phenol, 4-methyl-, Phenol, 2-methoxy-, Phenol, 2-ethyl-,Phenol, 3-ethyl-, 1,2-Benzenediol, Phenol, 4-(2-propenyl)-, Substituted phenols:Phenol, 2,4-dimethyl-, Phenol, 2,3-dimethyl-, Phenol, 2-methoxy-4-methyl-, 1,2-Benzenediol, Phenol, 2-ethyl-5-methyl-, 1,2 Benzenediol, 3-methoxy-, Phenol, 4-ethyl-2-methoxy-, 1,2-Benzenediol, 4-methyl-, Hydroquinone, 2-Methoxy-4-vinylphenol, Phenol, 2,6-dimethoxy-, 1,4-Benzenediol, 2-methyl-, 4-Ethylcatechol, 4-Hydroxy-2 methoxy benaldehyde,Vanillin, Phenol, 2-methoxy-4-(1-propenyl)-, Phenol, 2-methoxy-5-(1-propenyl)-, (E)-, Eugenol, Phenol, 5-methoxy-2,3,4-trimethyl,- Phenol, 2,6-dimethoxy-4-(2-propenyl)-, Sugars: 1,4:3,6-Dianhydro-alpha-D-glucopyranose, Levoglucosan. |
| [110] | Fixed bed - slow - catalyst metal salts, oxides, and acidic, ZSM-5, Y-Zeolite, Mordenite, SBA-15-350-500 oC | Catalytic and nocataylticRS: Alkyl phenols: Phenol, Catechol, Phenol, 2-methyl, Phenol, 3-methyl, Cresol p-cresol, m-cresol, 4-Ethylcatechol, Ethanone, 1-(2-hydroxy-5-methylphenyl)-, 5-tert-Butylpyrogallol, 1,2-Benzenediol, 3-methyl, 1,2-Benzenediol, 4-methyl, Guaiacol phenols: Benzaldehyde, 3-hydroxy-4-methoxy-, Phenol, 2-methoxy-, 2-Methoxy-5-methylphenol, Apocynin, Vanillin, Syringyl phenols: Phenol, 2,6-dimethoxy-, Other type compounds: Succindialdehyde, 1,2-Cyclopentanedione, 2-Cyclopenten-1-one, 2-hydroxy-3-methyl, 2-Propanone, 1-(acetyloxy), Pentanal, 2-Propanone, 1-hydroxy, Ethyl diazoacetate, Furan: 2-Furanmethanol, Benzofuran, 2,3-dihydro-, Furfural. |
| [112] | Reactor tube - Slow – 550 oC | Phenol: Phenol, 4-Methyl, Phenol, 2-Methoxy, Phenol, 2,6-Dimethoxy, 1,2-Benzenediol, 1,4-Benzenediol, 1,2-Benzenediol, 4-Methyl, 1,4-Benzenediol, 2-Methyl, Ketones: 2-Cyclopenten-1-One, 2-Hidroxy-3-Methyl, 2-Cyclopenten-1-One, 2-Cyclopenten-1-One, 3-Methyl, 2-Cyclopenten-1-One, 2-Methyl, 2-Cyclopenten-1-One, 3-Ethyl-2-Hidroxy, 2-Propanone, 1-Acetyloxy, 1-Hydroxy-2-Butanone, 2-Butanone, 3-Hydroxy, Furans, 2-Furanmethanol, 2-Furanone, Dihydro, 5-Hydroxymethyldihydrofuran, Tetrahydro-2-Furanylmethanol. Phenol, Phenol, 4-Methyl, Phenol, 2-Methoxy, Phenol, 2,6-Dimethoxy, 1,2-Benzenediol, 1,4-Benzenediol, 1,2-Benzenediol, 4-Methyl, 1,4-Benzenediol, 2-Methyl, Ketones: 2-Cyclopenten-1-One, 2-Hidroxy-3-Methyl, 2-Cyclopenten-1-One, 2-Cyclopenten-1-One, 3-Methyl, 2-Cyclopenten-1-One, 2-Methyl, 2-Cyclopenten-1-One, 3-Ethyl-2-Hidroxy, 2-Propanone, 1-Acetyloxy, 1-Hydroxy-2-Butanone, 2-Butanone, 3-Hydroxy, Furans, 2-Furanmethanol, 2-Furanone, Dihydro, 5-Hydroxymethyldihydrofuran, Tetrahydro-2-Furanylmethanol. |
| [114] | Fixed bed - slow –Catalylytic (K2CO3) – 300 to 700 oC | RS: (1) hydrocarbon (e.g. methoxy-cyclobutane); (2) acid compounds (e.g. acetic acid); (3) alcohol compounds (e.g. 2-furan methanol); (4) aldehydes compounds (e.g. acetamido acetaldehyde); (5) lipid (e.g. 2-oxo-propanoic acid methyl ester); (6) ketones (e.g. pentanone, 1-hydroxy-2-propanone); (7) ethers (e.g. 1,2-dimethoxy-4-propylbenzene); (8) phenols (e.g. phenol, 2-ethyl-5-propylphenol); (9) guaiacols (e.g. guaiacol, 4-methyl guaiacol); (10) furan (e.g. 2,5-dimethyl-furan, 2,4-dimethyl-furan). |
| [123] | Fixed bed - slow – 400 oC | RS: 2-Furanmethanol, 2-Cyclopenten-1-one, 3-methyl-, 3-Hexen-2-one, 3-methyl-, Phenol, 2-methyl-, Phenol, 3-methyl-, Phenol, 2-methoxy-, Phenol, 2,4-dimethyl-, 2-Cyclopenten-1-one, 3-ethyl-2-hydroxy-, Phenol, 4-ethyl-, Catechol, Benzofuran, 2,3-dihydro-, Phenol, 4-ethyl-2-methoxy-, Hexadecane, 2-Methoxy-4-vinylphenol, Phenol, 2,6-dimethoxy-, 1,2-Cyclopentanedione, 3-methyl-, 1-Penten-3-ol, 2-methyl-, Hydrazine, 1-(4-ethylphenyl)-. RH/WH(0.5:0.5): 2-Cyclopenten-1-one, 3-methyl-, 2-Cyclopenten-1-one, 2-methyl-, 2-Cyclopenten-1-one, 2,3-dimethyl-, Phenol, 2-methyl-, Stigma sterol, Phenol, 2-methoxy-, Phenol, 2,6-dimethoxy-4-(2-propenyl)-, Phenol, Furfural, Butylated Hydroxytoluene, 2-Cyclopenten-1-one, 3-ethyl-2-hydroxy-, Ethanone, 1-(2-furanyl),- Phenol, 4-ethyl-, Benzofuran, 2,3-dihydro-, p-Cresol, 2-Cyclopenten-1-one, 2-hydroxy-, Phenol, 4-ethyl-2-methoxy-, 2-Methoxy-4-vinylphenol, 1,6-Dimethylhepta-1,3,5-triene, Phenol, 2,6-dimethoxy-, 2-Cyclopenten-1-one, 3-methyl-, Cyclopentanone, Creosol, 1,2-Cyclopentanedione, 3-methyl-, Butyrolactone, 2-Furanmethanol. |
| [131] | Fixed bed - Slow – 600 oC | 3-cyclohexene-1-propanal C9H14O, 3-cyclohexene-1-methanol-,cis- C7H12O2, cyclobutene, 2-propenylidne- C7H8, bicycle[2.2.1]heptane, 3-furancarboxylic acid, methylester C6H6O3, furan, 2,5-dimethyl- C6H8O, dicyclohexyl-methanol C13H24O, 1,1-divinyl-1-silacyclobutane C7H12Si, l-histidine, 3-methyl- C7H11O2N3, 3-furanmethanol C5H6O2, 2-furancarboxaldehyde, 5- methyl- C6H6O2, n-vinylimidazole C6H6N2, phenol C6H6O, carbonic acid, 2-methoxyethl phenyl ester C10H12O4, 2-ethyl-5-propylcyclopentanone C10H18O, 1,2-cyclopenta-nedione, 3-methyl-C6H8O2, cyclohexanone, 5-methyl-2-(1-methylethyl)-, trans-C10H18O, phenol,2-methyl-C7H8O, benzaldehyde, 2-(2-propnyloxy)- C10H18O2, cyclopentanol, 1,2-dimethyl-3-(1-methylethenyl)-, [1r-(1.alpha,beta C10H18O, 1h-1,3-benzimidazol-7-amine], n-[(4 methoxyphenyl)methyl]-2-methyl- C16H17N3, 2,5-dimethyl- C8H10O6.61, 3-ethyl- C8H10O2, benzofuran, 2,3-dihydro- C8H8O, benzaldehyde, 2-methyl- C8H8O, 3-ethyl-5-methyl- C9H12O, 4-ethyl-2-methoxy- C9H12O2, 2-methoxy-4-vinylphenol C9H10O2, 2,3,5,6-tetramethyl- C10H14O, 2,6-dimethoxy- C8H10O3, 1,2,4-trimethoxybenenze C9H12O3, 2-methoxy-4-(1-propenyl)- C10H12O2, 5,6-dipropyl-4-hexyl-2h-pyran-2-one C17H28O2, 4-ethylbiphenyl C14H14, 5-tert-butylpyrogallol C11H14O3, benzeneamine, 3-ethyl-4-hydroxy- C8H11N, 2,6-dimethyloxy-4-(2-propenyl)- C11H14O3, 1,2,34,7-pentamethyl indole C13H17N, silicic acid, diethyl bis (tri-methylsilyl) ester C10H28O4Si3, cyclotrisiloxane, hexamethyl- C6H18O3Si3, octasiloxane, hexadecamethyl- C16H50O7Si8, heptasiloxane, tetradecamethyl- C14H44O6Si7, 12.37 cyclotrisiloxane, octasiloxane, 1,4-benezene dicarboxylic acid, bis(2-ethylhexyl), ester C24H38O4, 1,3-benzenedi carboxylic acid, hexanedioic acid, bis[2-(2-butoxyethoxy)etyl], di(butoxyethyl)adipate C18H34O6. |
| [133] | Fixed bed - slow – cement catalytic-600 oC | Noncatalytic RS: Phenol, P-cresol, 3-butene-2-one-3-methyl-, Isobutane, Naphthalene, decahydro-2, 3-dimethyl, 1, 3-cyclopentadiene, 1-methyl, Furane, 2, 3, 5-tri-methyl-, 2,4 –hexadienal, Benzene, 1-ethyl-4-methyl, Benzofuran, 2, 4-dihydro, 4-pentene-2-ol, 2-Methylcyclopentene-1, 3-dion, 2-pentanal-2-ethyl, oxalic acid allyl octyl ester, Phenol-2-methoxy, Phenol, 3-ethyl-5-methyl-, Styrene, Phenol, 2-ethyl-5-methyl-, 1H-indene-1-one, 2, 3-dihydro, phenol-3,5-dimethyl, Tetrahydrofuran, Naphthalene, decahydro-1, 5-dimethyl-, 2-Cyclopentene-1-one -3-methyl-. Catalytic: Phenol, Toluene, Phenol-3-methyl, Cyclopentanone-2-methyl, 2- propanone-1-hydroxy P-xylene, Benzofuran-2, 3-dihydro ,4-ethyl benzoic acid, Cyclo-pentane-ethylidene, 2-Naphthalenol, Styrene, 1H-indene-3-methyl-, Benzene 1, 3 dimethyl, Bicyclo [5, 1, 0] Octane, 1-Dococene, Mesitylene, 3-pentane dione, Phenol-2-methoxy6-(1-propynyl), 7-Heptadecene-17-chloro, 1-Nonadecene, 1- Naphthalenol-2-methyl, 7-Hexadecene, 2-Cyclopentene-1-one -3-methyl-. Non catalytic RS/PE: 1-Nonene, 1-Undecene, 1-Tetradecene, 1,12-Tridecadiene 5, 1-Heptene, Cetene, 1-Nonadecene, Toluene, Benze-2-propenyl, Benzene, 5-Eicosene, (E),- Heneicosane, 1,9-Decadiene, Hexacosane, Pentadecane, Octane, Hexadecane, Heptadecane, Tridecane, Tetradecane, Octadecane, 5-Eicosene, (E)-, Benzene, 1,3-dimethyl-, 1-Dodecene, Catalytic RS/PE:1-Decene, Heptacos-1-ene, 2-Tetradecene, (E)-, 1-Tridecene, Benzene, Pentadecane, Toluene, Cetene, Heptadecane, Octadecane, 5-Eicosene, (E)-, 1-Nonadecene, Cyclotetracosane, Nonadecane, 1-Heptene, Undecane, 1,12-Tridecadiene, 1,13-Tetradecadiene, Cyclopropane, 1-methyl-2-pentyl-, 1,19-Eicosadiene, Tridecane, 9-Octadecene, Tetradecane, 1,19-Eicosadiene, Benzene, 1,3-dimethyl-. |
| [136] | Batch reactor – two-step pyrolysis - Slow- washed – 340 to 600 oC | Unwashed RS, RS/GNS, RS/WS: Water, Levoglucosan, Acetic acid, Furfural, Butyrolactone, 2(5H)-Furanone, Phenol, Cyclotene, Guaiacol, p-methyl guaiacol, Catechol, p-ethyl guaiacol, Vanillin, Isoeugenol. Washed RS, RS/GNS, RS/WS: Water, Levoglucosan, Acetic acid, Furfural, Butyrolactone, 2(5H)-Furanone, Phenol, Cyclotene, Guaiacol, p-methyl guaiacol, Catechol, p-ethyl guaiacol, vanillin, Isoeugenol. |