# Supplementary materials

Slow-Pyrolysis of Municipal Sewage Sludge: Biochar Characteristics and Advanced Thermodynamics

Naeimeh Valia*, Samyar Zabihia, Shahin Shamima, Abas Mohsenzadeha and Anita Petterssona*

a: Swedish Centre for Resource Recovery (SCRR), University of Borås, 501 90 Borås, Sweden

* Corresponding author, E-mail: naeimeh.vali@hb.se, https://orcid.org/0000-0001-9443-5547

Figure S1.Lab scale rotating pyrolysis unit and its schematic drawing: 1) Nitrogen, 2) Valve, 3) pressure gage, 4) feeding system, 5) thermocouple, 6) gas burner, 7) gas analyzer.

Table S 1. Utilizing the database Sources as a reference, the elements, solid solutions, and compounds in the thermodynamic equilibrium calculations.

| Databases | Comments |
| --- | --- |
| Elements | H, C, N, O, Na, Mg, Al, Si, P, K, Ca, Fe, Cr, Pb, Ni, Cu, Mn, Zn, Cd, S, Cl |
| FactPS | pure stoichiometric gas and solid phases |
| FToxid | pure stoichiometric solid phases Slag A: (liquid oxide melt): K2O, SiO2, CaO, MgO, P2O5 SPINA: (AB2O4-type cubic spinel solution containing Al-Co-Cr-Fe-Mg-Ni-Zn-O) |
|  | Mull: Mullite (Al, Fe)2(Al, Si, B, Fe) O5 CORU: (Corundum-Al2O3-Cr2O3-Fe2O3-Mn2O3) Feld: NaAlSi3O8 - KAlSi3O8 - CaAl2Si2O8 - SrAl2Si2O8 - BaAl2Si2O8 - NaFeSi3O8 CMPc: K2Al2Si4O12-K2MgSi5O12 M2Pa: (Mg,Ca)2P2O7 |
|  | C3Pb: medium-T solid solution (Ca,Mg)3P2O8 |
|  | C3Pa: low-T solid solution (Ca,Mg)3P2O8 |

Figure S2.Results of the Kissinger-Akahira-Sunose method for various conversions during sewage sludge pyrolysis at different temperatures for a) BSS and b) LSS.

Table S 2. Elemental composition and H/C ratio of biochars at various pyrolysis temperatures.

| Biochar | Results |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | Total-C (wt.%) | Total-H (wt.%) | Total-N (wt.%) | H/C Ratio |
| BSSC 500 ˚C |  | 40.4 | 7.42 | 1.30 | 0.18 |
| BSSC 700 ˚C |  | 44.4 | 7.33 | 1.43 | 0.16 |
| BSSC 900 ˚C* |  | 23.2 | 5.60 | 3.65 | 0.24 |
| LSSC 500 ˚C |  | 43.6 | 6.53 | 1.66 | 0.15 |
| LSSC 700 ˚C |  | 42.4 | 5.10 | 1.23 | 0.12 |
| LSSC 900 ˚C |  | 30.8 | 4.90 | 1.20 | 0.16 |
| * Results taken from an external lab. |  |  |  |  |  |

Figure S 3. Nitrogen isothermal adsorption analysis (ADS).

Figure S 4. The results of TECs showing the main gaseous products during pyrolysis at various temperatures.