Supplementary material

Valorization of rice straw through FeCl3 pretreatment: Experiments- Modelling and Optimization

Dinabandhu Manna1 Ranjana Chowdhury1† Suvi Kuittinen2 Ari Pappinen2

Jouko Vepsäläinen3 Md. Kamrul Hassan2*

1Chemical Engineering Department, Jadavpur University, Kolkata – 700 032, West Bengal, India

2 School of Forest Sciences, University of Eastern Finland, P.O. Box 111, FI80101 Joensuu, Finland

3School of Pharmacy, University of Eastern Finland, P.O. Box 1627, FI70211 Kuopio, Finland

†Research supervisor, Email id: ranjana.juchem@gmail.com

Contact no. +91-9830359430, Telephone/FAX: +91-33-2414 6378

*Corresponding author, Email id: kamrul.hassan@uef.fi

Contact no. +358-504422346

Combined severity 									Page No. S3

List of Tables

| Table | Page No. |
| --- | --- |
| Table S1 Coded levels of independent variables for degradation of carbohydrates | S4 |
| Table S2 Coded levels of variables used for the optimization of yields of xylose, glucose and furfural (g/kg of RS) | S5 |
| Table S3 ANOVA Table for optimization xylan degradation | S6 |
| Table S4 ANOVA Table for optimization cellulose degradation | S7 |
| Table S5 ANOVA Table for optimization of YG,EH | S8 |
| Table S6 ANOVA Table for optimization of YG,C | S9 |

List of Figures

| Figure | Page No. |
| --- | --- |
| Fig. S1 Plot of the natural logarithm of each rate constant, lnki against 1T (Rate constants involved in the xylan conversion) | S10 |
| Fig. S2 Plot of the natural logarithm of each rate constant, lnki against 1T (Rate constants involved in the cellulose conversion) | S11 |
| Fig. S3 Glucose yield after enzymatic hydrolysis of untreated and pretreated rice straw | S12 |

Calculation of lignin degradation								          S13

Combined severity

The R0 and ω, the hydrolysis kinetics of hemicellulose and cellulose can be written as,

-1CXydCXydt= kXy								                                 (S1)

As there is no hydrolysis during the heating up and cooling down period,

-1CXydCXydt=kXy0exp-EXyRT							                                  (S2)

Or-ln1CXydCXydt=kXy0-EXyRT							                                  (S3)

Through Taylor series expansion, neglecting higher terms, around reference temperature TR,

-ln1CXydCXydt=lnkXy0-EXyRTR+EXyRTR2TRT-TR					                                  (S4)

or, 1CXydCXydt=kXy0exp-EXyRTRexp(EXyRTR2T-TR)=kXyRexpT-TRωXy		                                  (S5)

RTR2EXy=ωXy; kXy0exp-EXyRTR=kXyR					                                                  (S6)

Or, CXy0CXydCXyCXy=0tkXyRexpT-TRωXydt=kXyRtexpT-TRωXy=kXyRR0Xy,iso	                                                  (S7)

Where,

R0Xy,iso=texpT-TRωXy=severity factor for xylose degradation under isothermal condition             (S8)

Similarly, for hydrolysis of cellulose,

CCellu0CCelludCCelluCCellu=0tkCellRexpT-TRωCelludt=kCellRtexpT-TRωCellu=kCellRR0Cellu,iso                                              (S9)

R0Cellu,iso=texpT-TRωCellu= severity factor for Cellulose degradation under isothermal condition  (S10)

Table S1 Coded levels of independent variables for degradation of carbohydrates

| Input variables | Unit | Coded variable level |  |  | Model Response |
| --- | --- | --- | --- | --- | --- |
|  |  | -1 | 0 | 1 |  |
| Pretreatment temperature | °C | 150 | 170 | 190 | (i) Xylan degradation (%) (ii) Cellulose degradation (%) |
| Pretreatment time | min | 5 | 10 | 15 |  |

Table S2 Coded levels of variables used for the optimization of yields of xylose, glucose and furfural (g/kg of RS)

| Input variables | Unit | Coded variable level |  |  | Model Response |
| --- | --- | --- | --- | --- | --- |
|  |  | -1 | 0 | 1 |  |
| Pretreatment temperature | °C | 150 | 170 | 190 | (i) Xylose yield (g/ kg of RS) (ii) Glucose yield (g/ kg of RS) (iii) Furfural yield (g/ kg of RS) |
| Pretreatment time | min | 5 | 10 | 15 |  |

Table S3 ANOVA Table for optimization xylan degradation

| Source | Sum of Squares | df | Mean Square | F-value | p-value |  |
| --- | --- | --- | --- | --- | --- | --- |
| Model | 4472.93 | 5 | 894.59 | 75.49 | < 0.0001 | significant |
| A-Temperature | 2651.91 | 1 | 2651.91 | 223.79 | < 0.0001 |  |
| B-Time | 321.10 | 1 | 321.10 | 27.10 | 0.0012 |  |
| AB | 187.69 | 1 | 187.69 | 15.84 | 0.0053 |  |
| A² | 1305.67 | 1 | 1305.67 | 110.18 | < 0.0001 |  |
| B² | 52.61 | 1 | 52.61 | 4.44 | 0.0731 |  |
| Residual | 82.95 | 7 | 11.85 |  |  |  |
| Lack of Fit | 82.95 | 3 | 27.65 |  |  |  |
| Pure Error | 0.0000 | 4 | 0.0000 |  |  |  |
| Cor Total | 4555.88 | 12 |  |  |  |  |

(R2: 0.9818; adjusted R2: 0.9688; Predicted R2: 0.9259)

Table S4 ANOVA Table for optimization cellulose degradation

| Source | Sum of Squares | df | Mean Square | F-value | p-value |  |
| --- | --- | --- | --- | --- | --- | --- |
| Model | 3050.65 | 5 | 610.13 | 586.83 | < 0.0001 | significant |
| A-Temperature | 2232.44 | 1 | 2232.44 | 2147.21 | < 0.0001 |  |
| B-Time | 293.32 | 1 | 293.32 | 282.12 | < 0.0001 |  |
| AB | 110.25 | 1 | 110.25 | 106.04 | < 0.0001 |  |
| A² | 374.53 | 1 | 374.53 | 360.23 | < 0.0001 |  |
| B² | 77.49 | 1 | 77.49 | 74.53 | < 0.0001 |  |
| Residual | 7.28 | 7 | 1.04 |  |  |  |
| Lack of Fit | 7.28 | 3 | 2.43 |  |  |  |
| Pure Error | 0.0000 | 4 | 0.0000 |  |  |  |
| Cor Total | 3057.93 | 12 |  |  |  |  |

(R2: 0.9976; adjusted R2: 0.9959; Predicted R2: 0.9831)

Table S5 ANOVA Table for optimization of YG,EH

| Source | Sum of Squares | df | Mean Square | F-value | p-value |  |
| --- | --- | --- | --- | --- | --- | --- |
| Model | 36.54 | 5 | 7.31 | 44.94 | < 0.0001 | significant |
| A-CS | 13.04 | 1 | 13.04 | 80.23 | < 0.0001 |  |
| B-Enzyme loading | 11.68 | 1 | 11.68 | 71.86 | < 0.0001 |  |
| AB | 3.39 | 1 | 3.39 | 20.82 | 0.0026 |  |
| A² | 0.0095 | 1 | 0.0095 | 0.0582 | 0.8163 |  |
| B² | 8.20 | 1 | 8.20 | 50.43 | 0.0002 |  |
| Residual | 1.14 | 7 | 0.1626 |  |  |  |
| Lack of Fit | 1.14 | 3 | 0.3794 |  |  |  |
| Pure Error | 0.0000 | 4 | 0.0000 |  |  |  |
| Cor Total | 37.68 | 12 |  |  |  |  |

(R2: 0.9763; adjusted R2: 0.9642; Predicted R2: 0.9471)

Table S6 ANOVA Table for optimization of YG,C

| Source | Sum of Squares | df | Mean Square | F-value | p-value |  |
| --- | --- | --- | --- | --- | --- | --- |
| Model | 670.27 | 5 | 134.05 | 30.51 | 0.0001 | significant |
| A-CS | 411.54 | 1 | 411.54 | 93.68 | < 0.0001 |  |
| B-EH | 66.94 | 1 | 66.94 | 15.24 | 0.0059 |  |
| AB | 20.25 | 1 | 20.25 | 4.61 | 0.0689 |  |
| A² | 139.15 | 1 | 139.15 | 31.67 | 0.0008 |  |
| B² | 51.56 | 1 | 51.56 | 11.74 | 0.0110 |  |
| Residual | 30.75 | 7 | 4.39 |  |  |  |
| Lack of Fit | 30.75 | 3 | 10.25 |  |  |  |
| Pure Error | 0.0000 | 4 | 0.0000 |  |  |  |
| Cor Total | 701.02 | 12 |  |  |  |  |

(R2: 0.9652; adjusted R2: 0.9431; Predicted R2: 0.9132)

Fig. S1 Plot of the natural logarithm of each rate constant, lnkiagainst 1T (Rate constants involved in the xylan conversion)

Fig. S2 Plot of the natural logarithm of each rate constant, lnki against 1T (Rate constants involved in the cellulose conversion)

Fig. S3 Glucose yield after enzymatic hydrolysis of untreated and pretreated rice straw

Calculation of lignin degradation

The % degradation of carbohydrate polymer (cellulose, hemicelluloses and lignin) has been calculated based on rice straw fed using the following equation (provided in the manuscript):

Degradation of Carbohydrate polymer %= Mass of Carbohydrate polymer in feed rice straw-Residual Mass of Carbohydrate polymer  Mass of rice straw fed to the reactor ×100                             (20)

At 190°C with 15 minutes pretreatment time and 0.2 M FeCl3, the degradation of lignin (%)

= Mass of lignin in feed rice straw-Residual Mass oflignin  Mass of rice straw fed to the reactor ×100

=1.68-1.4351.68×100=14.58