Supplementary Material

Effect of high gold salt concentrations on the size and polydispersity of

gold nanoparticles prepared by an extended Turkevich-Frens method

Kara Zabetakis, William Ghann, Sanjeev Kumar, Marie-Christine Daniel*

Table S1. Data used in Figure 1 in the text.

| 0.3 mM |  |  | 0.6 mM |  |  | 0.8 mM |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Ct/Au Ratio | PDI |  | Ct/Au Ratio | PDI |  | Ct/Au Ratio | PDI |
| 2.0 | 0.293 |  | 2.0 | 0.283 |  | 3.0 | 0.178 |
| 4.0 | 0.022 |  | 4.0 | 0.021 |  | 4.0 | 0.113 |
| 5.0 | 0.037 |  | 5.0 | 0.036 |  | 5.5 | 0.024 |
| 6.0 | 0.023 |  | 6.0 | 0.014 |  | 7.0 | 0.023 |
| 9.9 | 0.046 |  | 7.0 | 0.013 |  | 8.9 | 0.028 |
| 11.5 | 0.076 |  | 8.0 | 0.035 |  | 11.0 | 0.033 |
| 12.6 | 0.088 |  | 10.5 | 0.041 |  | 13.0 | 0.058 |
| 13.5 | 0.094 |  | 12.0 | 0.056 |  | 14.0 | 0.120 |
| 15.1 | 0.097 |  | 14.0 | 0.080 |  | 16.0 | 0.268 |
| 16.0 | 0.106 |  | 16.0 | 0.059 |  |  |  |
| 17.2 | 0.114 |  |  |  |  |  |  |

Table S2. Data used in Figure 2 in the text.

| 1 mM |  |  | 1.2 mM |  |
| --- | --- | --- | --- | --- |
| Ct/Au Ratio | PDI |  | Ct/Au Ratio | PDI |
| 3.0 | 0.165 |  | 2.0 | 0.277 |
| 4.0 | 0.066 |  | 3.0 | 0.234 |
| 5.0 | 0.028 |  | 4.2 | 0.080 |
| 6.0 | 0.034 |  | 5.0 | 0.048 |
| 7.2 | 0.037 |  | 7.0 | 0.028 |
| 8.0 | 0.040 |  | 10.0 | 0.074 |
| 10.0 | 0.043 |  | 12.0 | 0.124 |
| 12.0 | 0.070 |  | 14.0 | 0.386 |
| 14.0 | 0.268 |  |  |  |
| 1.5 mM |  |  | 2 mM |  |
| Ct/Au Ratio | PDI |  | Ct/Au Ratio | PDI |
| 4.0 | 0.121 |  | 3.6 | 0.165 |
| 5.5 | 0.045 |  | 4.5 | 0.111 |
| 6.0 | 0.030 |  | 5.0 | 0.107 |
| 6.5 | 0.099 |  | 5.5 | 0.087 |
| 7.0 | 0.047 |  | 6.0 | 0.079 |
| 7.7 | 0.055 |  | 6.5 | 0.154 |
| 9.0 | 0.074 |  | 8.0 | 0.214 |
| 10.0 | 0.154 |  | 10.0 | 0.233 |
| 12.0 | 0.225 |  |  |  |

Table S3. Data used in Figure 3 in the text

| 0.3 mM |  |  |  | 0.6 mM |  |  |  | 0.8 mM |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Ct/Au Ratio | Size (nm) | PDI |  | Ct/Au Ratio | Size (nm) | PDI |  | Ct/Au Ratio | Size (nm) | PDI |
| 2.0 | 31.70 | 0.293 |  | 2.0 | 26.52 | 0.283 |  | 3.0 | 21.75 | 0.178 |
| 4.0 | 17.34 | 0.022 |  | 4.0 | 15.57 | 0.021 |  | 4.0 | 15.32 | 0.113 |
| 5.0 | 18.57 | 0.037 |  | 5.0 | 14.83 | 0.036 |  | 5.5 | 14.45 | 0.024 |
| 6.0 | 19.38 | 0.023 |  | 6.0 | 15.43 | 0.014 |  | 7.0 | 14.71 | 0.023 |
| 8.0 | 24.99 | 0.092 |  | 7.0 | 15.62 | 0.013 |  | 8.9 | 14.90 | 0.028 |
| 9.9 | 25.19 | 0.046 |  | 8.0 | 15.45 | 0.035 |  | 11.0 | 15.56 | 0.033 |
| 11.5 | 25.38 | 0.076 |  | 10.0 | 16.90 | 0.081 |  | 13.0 | 17.97 | 0.058 |
| 12.6 | 25.94 | 0.088 |  | 12.0 | 17.55 | 0.056 |  | 14.0 | 18.73 | 0.120 |
| 13.5 | 27.43 | 0.094 |  | 14.0 | 17.54 | 0.080 |  | 16.0 | 23.05 | 0.268 |
| 15.1 | 26.81 | 0.097 |  | 16.0 | 18.29 | 0.059 |  |  |  |  |
| 16.0 | 26.33 | 0.106 |  |  |  |  |  |  |  |  |
| 17.2 | 26.40 | 0.114 |  |  |  |  |  |  |  |  |

Table S4. Data used in Figure 4 in the text.

| 1 mM |  |  |  | 1.2 mM |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Ct/Au Ratio | Size (nm) | PDI |  | Ct/Au Ratio | Size (nm) | PDI |
| 3.0 | 20.90 | 0.165 |  | 3.0 | 22.07 | 0.234 |
| 4.0 | 15.60 | 0.066 |  | 4.2 | 15.30 | 0.08 |
| 5.0 | 14.34 | 0.028 |  | 5.0 | 14.15 | 0.048 |
| 6.0 | 13.89 | 0.034 |  | 6.0 | 13.60 | 0.067 |
| 7.2 | 13.95 | 0.037 |  | 7.0 | 13.48 | 0.028 |
| 8 | 14.38 | 0.040 |  | 8.5 | 14.05 | 0.046 |
| 10.0 | 14.92 | 0.043 |  | 10.0 | 16.21 | 0.074 |
| 12.0 | 16.71 | 0.070 |  | 12.0 | 17.45 | 0.124 |
| 1.5 mM |  |  |  | 2 mM |  |  |
| Ct/Au Ratio | Size (nm) | PDI |  | Ct/Au Ratio | Size (nm) | PDI |
| 4.0 | 18.3 | 0.121 |  | 3.6 | 21.76 | 0.165 |
| 5.5 | 14.2 | 0.045 |  | 4.5 | 17.34 | 0.111 |
| 6 | 13.71 | 0.030 |  | 5.0 | 16.17 | 0.107 |
| 6.5 | 13.84 | 0.099 |  | 5.5 | 15.61 | 0.087 |
| 7 | 13.86 | 0.047 |  | 6.0 | 15.15 | 0.079 |
| 7.7 | 14.93 | 0.055 |  | 6.5 | 15.83 | 0.154 |
| 9.0 | 16.0 | 0.074 |  | 8.0 | 17.39 | 0.214 |
| 10.0 | 17.9 | 0.154 |  | 10.0 | 20.90 | 0.233 |

Table S5. Data used in Figure 5 in the text.

| Ct/Au ratio 2:1 |  |  |  | Ct/Au ratio 3:1 |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| [Au3+] (mM) | size (nm) | PDI |  | [Au3+] (mM) | size (nm) | PDI |
| 0.30 | 31.70 | 0.293 |  | 0.80 | 21.75 | 0.178 |
| 0.60 | 26.52 | 0.283 |  | 1.00 | 20.90 | 0.165 |
| 1.20 | 26.41 | 0.277 |  | 1.20 | 22.07 | 0.234 |
| Ct/Au ratio 4:1 |  |  |  | Ct/Au ratio 5:1 |  |  |
| [Au3+] (mM) | size (nm) | PDI |  | [Au3+] (mM) | size (nm) | PDI |
| 0.30 | 17.34 | 0.022 |  | 0.6 | 14.83 | 0.036 |
| 0.60 | 15.57 | 0.021 |  | 1.00 | 14.34 | 0.028 |
| 1.00 | 15.60 | 0.066 |  | 1.20 | 14.15 | 0.048 |
| 1.20 | 15.30 | 0.080 |  | 2.00 | 16.17 | 0.107 |
| 1.50 | 18.30 | 0.121 |  | 0.3 | 18.57 | 0.037 |
| 2.00 | 21.76 | 0.165 |  |  |  |  |

Table S6. Data used in Figure 6 in the text.

| Ct/Au ratio 6:1 |  |  |  | Ct/Au ratio 8:1 |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| [Au3+] (mM) | size (nm) | PDI |  | [Au3+] (mM) | size (nm) | PDI |
| 0.30 | 19.38 | 0.023 |  | 0.60 | 15.45 | 0.035 |
| 0.60 | 15.43 | 0.060 |  | 0.30 | 24.99 | 0.092 |
| 0.80 | 14.45 | 0.024 |  | 1.00 | 14.38 | 0.040 |
| 1.00 | 13.89 | 0.034 |  | 1.50 | 15.17 | 0.065 |
| 1.50 | 13.71 | 0.030 |  | 2.00 | 17.39 | 0.214 |
| 2.00 | 15.15 | 0.079 |  |  |  |  |
| 1.20 | 13.60 | 0.067 |  |  |  |  |
| Ct/Au ratio 10:1 |  |  |  | Ct/Au ratio 12:1 |  |  |
| [Au3+] (mM) | size (nm) | PDI |  | [Au3+] (mM) | size (nm) | PDI |
| 0.30 | 25.20 | 0.046 |  | 0.30 | 25.38 | 0.076 |
| 0.60 | 16.90 | 0.081 |  | 0.60 | 17.55 | 0.056 |
| 1.00 | 14.92 | 0.043 |  | 1.00 | 16.71 | 0.070 |
| 1.20 | 16.21 | 0.074 |  | 1.20 | 17.45 | 0.124 |
| 1.50 | 17.91 | 0.154 |  | 1.50 | 19.84 | 0.225 |
| 2.00 | 20.90 | 0.233 |  |  |  |  |
| Ct/Au ratio 14:1 |  |  |  |  |  |  |
| [Au3+] (mM) | size (nm) | PDI |  |  |  |  |
| 0.30 | 27.43 | 0.094 |  |  |  |  |
| 0.60 | 17.54 | 0.080 |  |  |  |  |
| 0.80 | 18.73 | 0.120 |  |  |  |  |
| 1.20 | 23.93 | 0.386 |  |  |  |  |
| 1.00 | 19.64 | 0.268 |  |  |  |  |

Table S7. Predicted GNPs diameters (nm) using the original model of Kumar et al.1

Table S8. Predicted GNPs diameters (nm) using the model of Kumar et al.1 with a surface potential increase of 11%.

Table S9. Mean Sizes of GNP solutions from starting [Au3+] of 0.3 mM to 2 mM and using Ct/Au ratios of 4:1 to 10:1. Corresponding TEM images are displayed in Figure 9. Each mean size was calculated based on measurements of more 200 gold nanoparticles from no less than five TEM images.

Table S10. Ranges of pH values corresponding to the ranges of Ct/Au ratios used in this work, for [Au3+] of 0.3 mM to 2.0 mM.

Figure S1. Reproducibility of the reported conditions. Representative examples with starting [Au3+] of 1.5 mM and Ct/Au ratios of 4:1, 6:1 and 10:1. A) Zave sizes obtained for triplicate reactions; B) Graph displaying the mean sizes obtained, with their respective error bars. The dashed line represents the size trend observed in Figure 4 in the manuscript.

Figure S2. Overlays of experimental data and simulations for the sizes of GNPs from 0.3 mM (violet), 0.6 mM (magenta) and 0.8 mM (green) initial [Au3+]. (     ) Experimental data; (    ) Predictions using the Kumar’s model in which the zeta potential was increased by (A) 5.5% and (B) 11% for GNPs from 0.6 mM and 0.8 mM; in both (A) and (B), the Kumar’s model was used as is for GNPs from 0.3 mM [Au3+]. The residuals (        ) have been calculated as the difference between the experimental values and the theoretical ones. In order to determine the residuals, a spline curve-based extrapolation2 has been applied to both experimental and theoretical set of data. The lines are guides for the eye.

(1)	Kumar, S.; Gandhi, K. S.; Kumar, R. Ind. Eng. Chem. Res. 2007, 46, 3128-3136.

(2)	Press, W. H.; Teukolsky, S. A.; Vetterling, W. T.; Flannery, B. P. Numerical Recipes in C. The Art of Scientific Computing; Second Edition ed.; Cambridge University Press, 2002.