Table S1: Data of AuNPs obtained in THF solution under different experimental conditions.

|  | Au@OA | Au@OA | Au@OA | Au@OA10 | Au@HDA | Au@HDA2 | Au@HDA10 | Au@DDA2 | Au@DDA10 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Ligand | OA | OA | OA | OA | HDA | HDA | HDA | DDA | DDA |
| Molar ratio | 2-10 | 2-10 | 2-10 | 10 | 2 -10 | 2 | 10 | 2 | 10 |
| Gas | H2 | CO | CO | CO | CO | CO | CO | CO | CO |
| Temperature | 70°C | r.t. | r.t. | 70°C | r.t. | 70°C | 70°C | 70°C | 70°C |
| Time | Overnight | Overnight | 20 min. | 20 min. | Overnight | Overnight | Overnight | Overnight | Overnight |
| Colour | Light pink |  | Violet/blue | Ruby red | Blue | Ruby red | Ruby red | Ruby red | Ruby red |
| Size (nm) | 2 and 10-50 | aggregate | 2 and 10-50 | 9 and 10-50 | 5-50 | 7,2 | 4,7 | 7,4 | 6,1 |
| Shape | Polymorph |  | Sphere and polymorph | Sphere/polymorph | Polymorph | Sphere | Sphere | Sphere | Sphere |
| Stability in Ar | Few days |  | Few days | Months | Months | Months | Months | Months | Months |
| Stability in air | 2 hours |  | 2 hours | Months | Months | Months | Months | Months | Months |