Appendix A

App. A. Examples of simplex lattice designs with three and four components

Appendix B

Mass ratio of the coals and biomass

| No of experiments | Coal 1 | Coal 2 | Biomass 1 | Biomass 2 |
| --- | --- | --- | --- | --- |
|  | Percentage of ash in mixture |  |  |  |
| 1 | 1.0 | 0.0 | 0.0 | 0.0 |
| 2 | 0.0 | 1.0 | 0.0 | 0.0 |
| 3 | 0.0 | 0.0 | 1.0 | 0.0 |
| 4 | 0.0 | 0.0 | 0.0 | 1.0 |
| 5 | 0.5 | 0.5 | 0.0 | 0.0 |
| 6 | 0.5 | 0.0 | 0.5 | 0.0 |
| 7 | 0.5 | 0.0 | 0.0 | 0.5 |
| 8 | 0.0 | 0.5 | 0.5 | 0.0 |
| 9 | 0.0 | 0.5 | 0.0 | 0.5 |
| 10 | 0.0 | 0.0 | 0.5 | 0.5 |
| 11 | 0.7 | 0.1 | 0.1 | 0.1 |
| 12 | 0.1 | 0.7 | 0.1 | 0.1 |
| 13 | 0.1 | 0.1 | 0.7 | 0.1 |
| 14 | 0.1 | 0.1 | 0.1 | 0.7 |
| 15 | 0.25 | 0.25 | 0.25 | 0.25 |

Appendix C

Results of proximate and ultimate analysis

| Parameter | Ad | Vd | Qsa | Qir | Ctd | Htd | Nd | Sta | Ota |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Unit | % | % | J/g | J/g | % | % | % | % | % |
| Mu | 0.2 | 0.54 | 201 | 210 | 0.6 | 0.32 | 0.05 | 0.12 | - |
| 1 | 3.73 | 32.29 | 33266.48 | 30891.95 | 82.50 | 4.83 | 1.33 | 0.22 | 6.92 |
| 2 | 3.79 | 32.51 | 32333.76 | 30511.01 | 82.28 | 4.50 | 1.34 | 0.21 | 8.47 |
| 3 | 0.49 | 82.78 | 20291.10 | 16737.28 | 49.43 | 5.98 | 0.30 | 0.03 | 43.20 |
| 4 | 4.60 | 77.83 | 18486.99 | 15815.51 | 46.52 | 5.86 | 0.47 | 0.12 | 43.68 |
| 5 | 3.70 | 31.40 | 32343.05 | 30584.82 | 83.01 | 4.63 | 1.30 | 0.21 | 7.62 |
| 6 | 2.78 | 36.55 | 27466.61 | 25656.65 | 70.38 | 4.50 | 1.05 | 0.17 | 11.63 |
| 7 | 3.38 | 36.18 | 27921.85 | 26001.39 | 68.92 | 4.57 | 1.05 | 0.18 | 11.45 |
| 8 | 2.93 | 37.17 | 26551.40 | 24954.00 | 69.88 | 4.30 | 1.02 | 0.16 | 12.63 |
| 9 | 3.53 | 35.45 | 26966.93 | 24989.55 | 68.61 | 4.38 | 1.06 | 0.18 | 12.99 |
| 10 | 2.57 | 81.84 | 19465.50 | 16739.04 | 48.47 | 5.91 | 0.38 | 0.07 | 43.33 |
| 11 | 3.58 | 37.31 | 31778.21 | 29139.80 | 77.64 | 4.87 | 1.24 | 0.20 | 10.98 |
| 12 | 3.55 | 36.29 | 30415.43 | 28994.67 | 77.77 | 4.80 | 1.25 | 0.20 | 11.45 |
| 13 | 3.29 | 42.43 | 30176.03 | 28667.24 | 76.85 | 5.07 | 1.12 | 0.18 | 14.79 |
| 14 | 3.66 | 41.24 | 29573.04 | 27412.14 | 74.97 | 4.83 | 1.12 | 0.19 | 15.02 |
| 15 | 3.46 | 41.11 | 30155.55 | 28445.39 | 76.01 | 4.93 | 1.15 | 0.19 | 14.98 |

Appendix D

Results of characteristic melting temperature [ºC] of ashes from studied fuels

| Parameter | ts(O) | tA(O) | tB(O) | tC(O) | ts(Or) | tA(Or) | tB(Or) | tC(Or) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Mu | 30 | 20 |  |  | 30 | 20 |  |  |
| 1 | 1060 | 1340 | 1350 | 1350 | 850 | 1310 | 1320 | 1330 |
| 2 | 1190 | 1270 | 1310 | 1320 | 1070 | 1160 | 1200 | 1210 |
| 3 | 1280 | 1360 | 1360 | 1370 | 1110 | 1310 | 1320 | 1340 |
| 4 | 680 | 840 | 1220 | 1280 | 670 | 810 | 1290 | 1360 |
| 5 | 1100 | 1290 | 1310 | 1320 | 1120 | 1270 | 1280 | 1290 |
| 6 | 1040 | 1340 | 1350 | 1350 | 890 | 1310 | 1310 | 1320 |
| 7 | 1060 | 1300 | 1300 | 1310 | 850 | 1260 | 1280 | 1280 |
| 8 | 1190 | 1260 | 1290 | 1300 | 1050 | 1160 | 1210 | 1220 |
| 9 | 1140 | 1230 | 1260 | 1270 | 1070 | 1140 | 1170 | 1180 |
| 10 | 710 | 1200 | 1220 | 1220 | 700 | 1180 | 1200 | 1210 |
| 11 | 1110 | 1300 | 1310 | 1310 | 1130 | 1260 | 1290 | 1300 |
| 12 | 1120 | 1260 | 1270 | 1280 | 1080 | 1190 | 1220 | 1230 |
| 13 | 1090 | 1300 | 1300 | 1310 | 1120 | 1260 | 1290 | 1300 |
| 14 | 1120 | 1230 | 1240 | 1240 | 1090 | 1170 | 1210 | 1220 |
| 15 | 1120 | 1260 | 1270 | 1270 | 1070 | 1180 | 1230 | 1240 |

Appendix E

Chemical composition of ashes [%] from studied fuels

| Parameter | SiO2 | Al2O3 | Fe2O3 | CaO | MgO | P2O5 | SO3 | Mn3O4 | TiO2 | BaO | SrO | Na2O | K2O |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Mu | 2.15 | 1.10 | 0.29 | 0.50 | 0.14 | 0.08 | 0.27 | 0.04 | 0.08 | 0.08 | 0.04 | 0.04 | 0.14 |
| 1 | 17.71 | 12.89 | 13.65 | 18.61 | 10.67 | 0.87 | 18.23 | 0.24 | 0.47 | 0.41 | 0.25 | 2.95 | 0.85 |
| 2 | 23.07 | 17.72 | 13.91 | 14.21 | 9.03 | 0.27 | 13.96 | 0.33 | 0.82 | 0.36 | 0.15 | 4.81 | 0.98 |
| 3 | 13.72 | 9.27 | 14.82 | 22.48 | 11.37 | 1.13 | 3.74 | 0.31 | 0.32 | 0.23 | 0.12 | 1.53 | 1.80 |
| 4 | 58.03 | 1.14 | 0.54 | 8.63 | 3.72 | 3.21 | 2.33 | 0.62 | 0.08 | 0.06 | 0.03 | 0.24 | 10.94 |
| 5 | 20.34 | 15.28 | 14.10 | 16.43 | 9.81 | 0.56 | 16.05 | 0.28 | 0.64 | 0.39 | 0.20 | 3.84 | 0.90 |
| 6 | 15.32 | 11.25 | 12.60 | 17.35 | 9.74 | 0.81 | 14.02 | 0.23 | 0.41 | 0.34 | 0.21 | 2.39 | 0.91 |
| 7 | 21.62 | 9.92 | 10.15 | 15.67 | 8.51 | 1.12 | 13.65 | 0.28 | 0.36 | 0.32 | 0.19 | 2.22 | 2.33 |
| 8 | 19.05 | 14.37 | 12.75 | 14.29 | 8.42 | 0.37 | 10.79 | 0.30 | 0.66 | 0.31 | 0.13 | 3.87 | 1.01 |
| 9 | 25.91 | 13.04 | 10.91 | 11.94 | 7.13 | 0.68 | 10.60 | 0.33 | 0.61 | 0.27 | 0.12 | 3.67 | 2.38 |
| 10 | 35.46 | 5.32 | 7.58 | 15.51 | 7.57 | 2.16 | 3.04 | 0.47 | 0.20 | 0.15 | 0.07 | 0.88 | 6.47 |
| 11 | 20.73 | 13.67 | 13.24 | 17.45 | 9.87 | 0.82 | 15.17 | 0.29 | 0.54 | 0.37 | 0.20 | 3.34 | 1.44 |
| 12 | 22.51 | 15.20 | 13.20 | 15.98 | 9.45 | 0.63 | 13.80 | 0.32 | 0.64 | 0.35 | 0.18 | 3.85 | 1.49 |
| 13 | 20.44 | 13.05 | 13.37 | 17.49 | 9.85 | 0.84 | 13.86 | 0.29 | 0.53 | 0.36 | 0.19 | 3.10 | 1.54 |
| 14 | 26.01 | 13.38 | 11.96 | 15.01 | 8.85 | 0.95 | 12.82 | 0.34 | 0.56 | 0.32 | 0.16 | 3.39 | 2.51 |
| 15 | 23.16 | 13.34 | 12.64 | 16.25 | 9.22 | 0.88 | 13.20 | 0.32 | 0.54 | 0.34 | 0.17 | 3.28 | 2.01 |

Appendix F

Slagging hazard determination

| Parameter | B/A | Rs | Fe-Caratio | Fe&Ca | Fu | SR |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 1.50 | 0.32 | 0.96 | 26.29 | 5.80 | 29.17 |
| 2 | 1.05 | 0.22 | 1.20 | 31.60 | 5.92 | 38.19 |
| 3 | 2.26 | 0.07 | 0.65 | 24.09 | 7.56 | 21.43 |
| 4 | 0.40 | 0.05 | 2.06 | 1.71 | 5.19 | 82.12 |
| 5 | 1.25 | 0.27 | 1.11 | 29.66 | 5.93 | 33.03 |
| 6 | 1.60 | 0.27 | 0.91 | 23.77 | 5.41 | 27.62 |
| 7 | 1.20 | 0.22 | 0.97 | 20.46 | 5.62 | 39.10 |
| 8 | 1.14 | 0.19 | 1.14 | 27.11 | 5.60 | 35.97 |
| 9 | 0.90 | 0.16 | 1.23 | 24.08 | 5.43 | 46.38 |
| 10 | 0.92 | 0.07 | 0.68 | 12.79 | 7.18 | 54.06 |
| 11 | 1.28 | 0.26 | 1.04 | 26.87 | 6.19 | 34.20 |
| 12 | 1.14 | 0.23 | 1.12 | 28.80 | 6.07 | 36.75 |
| 13 | 1.32 | 0.24 | 0.99 | 26.74 | 6.37 | 33.53 |
| 14 | 1.06 | 0.20 | 1.10 | 25.58 | 6.28 | 41.34 |
| 15 | 1.19 | 0.22 | 1.03 | 25.68 | 6.43 | 37.53 |

Appendix G

Limiting values for slagging factors

| Parameter | Slagging propensity |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Low | Medium |  | High |  | Severe |
| B/A | <0.4 or > 0.7 |  |  | 0.4 – 0.7 |  |  |
| Rs | <0.6 | 0.6 – 2.0 |  | 2.0 – 2.6 |  | 2.6> |
| Fe-Caratio | <0.3 or >3.0 |  |  | 0.3–3.0 |  |  |
| ΣFe&Ca [%] | <10 |  |  | – |  |  |
| Fu | ≤0.6 |  | 0.6 – 40 |  | >40 |  |
| SR | >72 |  | 72-65 |  | ≤65 |  |

Appendix H

App. H. Changing of the ash fusibility temperatures in an oxidizing atmosphere a function of the coal 1: carbon 2: biomass 2 A - sintering temperature ts(O), B – softening temperature tA(O), C – melting temperature tB(O), D – flowing temperature tC(O).

Appendix I

App. I. Changing of the ash fusibility temperatures in an reducing atmosphere a function of the coal 1: carbon 2: biomass 2 A - sintering temperature ts(O), B – softening temperature tA(O), C – melting temperature tB(O), D – flowing temperature tC(O).

Appendix J

App. J. The change of characteristic slagging hazard coefficients of fuel a depending on the coal 1: carbon 2: biomass 1, A – ratio of basic compounds to acidic compounds, B – slagging (Babcock)—index Rs, C – fouling index Fu, D – slag viscosity index, E – iron-calcium ratio, F – iron plus calcium,

Measurement uncertainty

Measurement uncertainty

Measurement uncertainty