# Supplementary Information

Table S1: Element mass fractions of sewage sludge ash, sewage sludge and samples from lab-scale and pilot-scale experiments (L 1000 = lab scale experiment at 1000 °C, P 750 - P 1000 = pilot-scale experiments at 750-1000 °C, SD = standard deviation, in triplicates), n.d.=not determined)

|  | Ash |  | Sewage sludge |  | L 1000 |  | P 750 |  | P 800 |  | P 850 |  | P 900 |  | P 950 |  | P 1000 |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | mean | SD | mean | SD | mean | SD | mean | SD | mean | SD | mean | SD | mean | SD | mean | SD | mean | SD |
|  | mg/kg |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Mn | 5260 | 45 | 121 | 2 | 2340 | 17 | 2010 | 22 | 2190 | 7 | 2100 | 9 | 2030 | 2 | 2020 | 15 | 2130 | 13 |
| Mo | 16.3 | 3.5 | 6.4 | 1.2 | n.d. |  | 9.1 | 2.6 | 11.0 | 0.5 | 11.2 | 3.4 | 7.6 | 3.3 | 10.8 | 2.2 | 9.8 | 1.2 |
| Sb | 16.3 | 1.4 | 4.0 | 0.8 | n.d. |  | 14.3 | 2.5 | 11.0 | 0.1 | 7.9 | 0.9 | 6.5 | 0.7 | 6.9 | 0.1 | 7.3 | 0.9 |
| Sn | 100.7 | 8.8 | 10.0 | 0.9 | n.d. |  | 67.3 | 2.5 | 68.7 | 1.2 | 63.6 | 5.5 | 57.7 | 1.5 | 60.9 | 1.4 | 48.6 | 2.1 |
| Ti | 3400 | 2 | 1440 | 22 | 3980 | 27 | 3380 | 22 | 3680 | 26 | 3600 | 1 | 3530 | 6 | 3560 | 6 | 3810 | 95 |
| Zr | 245 | 11.6 | 95 | 0.8 | n.d. |  | 161 | 1.9 | 182 | 2.3 | 187 | 16.7 | 174 | 1.8 | 178 | 0.4 | 188 | 2.3 |

Table S2 Element mass balance for matrix and trace elements at different set temperatures (measured temperature in kiln is 15-25 °C lower) for the pilot-scale experiment. Elements are sorted in categories “remain in solid” and “removal via gas phase” depending on temperature. Element mass balance is calculated on element mass fractions (table 1) and weights of SSA (5000 g) and SS (1000 g) in starting material mixtures (8000 g) and product (5930-6804 g).

|  |  | Temperature |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | 750 °C |  |  |  | 800 °C |  |  |  | 850 °C |  |  |  | 900 °C |  |  | 950 °C |  |  | 1000 °C |  |  |
| Starting |  | 8000 g |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Product |  | 6804 g |  |  |  | 6539 g |  |  |  | 6350 g |  |  |  | 6370 g |  |  | 6500 g |  |  | 5929 g |  |  |
| remain in solid |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Al | 91 |  | ± | 2 | 93 |  | ± | 3 | 90 |  | ± | 2 | 87 |  | ± | 3 | 88 | ± | 2 | 84 | ± | 4 |
| Ca | 99 |  | ± | 1 | 103 |  | ± | 1 | 96 |  | ± | 1 | 94 |  | ± | 1 | 96 | ± | 1 | 93 | ± | 2 |
| Fe | 117 |  | ± | 3 | 124 |  | ± | 3 | 118 |  | ± | 3 | 113 |  | ± | 3 | 115 | ± | 3 | 110 | ± | 3 |
| K | 123 |  | ± | 6 | 118 |  | ± | 7 | 112 |  | ± | 7 | 111 |  | ± | 7 | 109 | ± | 8 | 103 | ± | 7 |
| Mg | 101 |  | ± | 1 | 102 |  | ± | 1 | 97 |  | ± | 1 | 99 |  | ± | 1 | 98 | ± | 1 | 95 | ± | 1 |
| P | 88 |  | ± | 3 | 91 |  | ± | 5 | 87 |  | ± | 6 | 84 |  | ± | 6 | 85 | ± | 7 | 80 | ± | 7 |
| Si | 113 |  | ± | 15 | 106 |  | ± | 14 | 112 |  | ± | 15 | 122 |  | ± | 19 | 109 | ± | 14 | 93 | ± | 14 |
| Cu | 4 |  | ± | 8 | -2 |  | ± | 8 | 4 |  | ± | 11 | 6 |  | ± | 8 | 6 | ± | 8 | 12 | ± | 8 |
| Mn | -9 |  | ± | 2 | -14 |  | ± | 1 | -6 |  | ± | 1 | -3 |  | ± | 1 | -5 | ± | 2 | -1 | ± | 2 |
| Ti | -8 |  | ± | 1 | -12 |  | ± | 1 | -7 |  | ± | 0 | -5 |  | ± | 0 | -8 | ± | 0 | -6 | ± | 3 |
| Zn | 11 |  | ± | 2 | 3 |  | ± | 3 | 3 |  | ± | 9 | 13 |  | ± | 2 | 9 | ± | 3 | 15 | ± | 2 |
| Zr | 17 |  | ± | 5 | 10 |  | ± | 4 | 10 |  | ± | 12 | 16 |  | ± | 4 | 12 | ± | 4 | 15 | ± | 4 |
| removal via gas phase |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| As | 98 |  | ± | 21 | 95 |  | ± | 13 | 97 |  | ± | 19 | 85 |  | ± | 12 | 77 | ± | 11 | 69 | ± | 10 |
| Cd | 90 |  | ± | 4 | 89 |  | ± | 7 | 76 |  | ± | 4 | 76 |  | ± | 2 | 71 | ± | 4 | 46 | ± | 3 |
| Mo | 70 |  | ± | 57 | 81 |  | ± | 21 | 81 |  | ± | 48 | 55 |  | ± | 99 | 80 | ± | 37 | 66 | ± | 31 |
| Pb | 96 |  | ± | 5 | 83 |  | ± | 5 | 69 |  | ± | 5 | 72 |  | ± | 6 | 80 | ± | 5 | 68 | ± | 5 |
| Sb | 114 |  | ± | 21 | 84 |  | ± | 8 | 59 |  | ± | 25 | 48 |  | ± | 31 | 52 | ± | 13 | 51 | ± | 29 |
| Sn | 89 |  | ± | 9 | 87 |  | ± | 8 | 79 |  | ± | 12 | 72 |  | ± | 8 | 77 | ± | 8 | 56 | ± | 9 |

Table S3: Mean temperature at the hottest temperature zone of the kiln (mean temperature of measuring points at 1000 mm, 1200 mm and 1400 mm length) compared to set temperature.

| temperature [°C] |  |
| --- | --- |
| set | measured |
| 750 | 757 |
| 800 | 773 |
| 850 | 822 |
| 900 | 887 |
| 950 | 937 |
| 1000 | 990 |

Feeding direction

Fig. S1: Temperature profile in material bed over the length of the rotary kiln in operation during steady state conditions.