Effect of some process parameters on the photodestruction of 2CBP using a heterojunction under simulated sunlight

Photocatalytic mediated destruction of 2-chlorobiphenyl by a ZnO-[10%]BiOI p-n heterojunction: Effect of some process parameters

Darlington .C. Ashiegbu1,* and Herman Potgieter1,2,**

1School of Chemical and Metallurgical Engineering, University of the Witwatersrand Johannesburg, Private Bag X3 PO Wits 2050, Johannesburg, South Africa

2Department of Natural Science, Manchester Metropolitan University, Chester Street M1 5GD, Manchester, UK.

*Corresponding author: E-mail: darlington.ashiegbu@wits.ac.za; darlingtonashiegbu1985@yahoo.com ORCID: 0000-0003-2204-6248 (D.C. Ashiegbu); herman.potgieter@wits.ac.za ORCID: 0000-0003-2833-7986 (H. Potgieter)

SUPPLEMENTARY INFORMATION

f

b

e

d

c

a

i

h

g

Fig. S1 EDS spectra and stoichiometry of: a ZnO; b BiOI; c WO3; d ZnO-[5%]BiOI; e ZnO-[10%]BiOI; f ZnO-[20%]BiOI; g ZnO-[5%]WO3; h ZnO-[10%]WO3; i ZnO-[20%]WO3

a

b

Fig. S2 Absorption spectra and Tauc plots of: a ZnO-[X]BiOI absorbance; b ZnO-[X]BiOI Tauc plots; c ZnO-[X]WO3 absorbance; d ZnO-[X]WO3 absorbance Tauc plots; e ZnO, BiOI and WO3 absorption spectra; f ZnO Tauc plot; g WO3 Tauc plot; h BiOI Tauc plot

Fig. S3 (a) Effect of catalyst dose (b) pseudo-first order plots of effect of catalyst dose

Fig. S4 (a) Effect of pH (b) Pseudo-first order plot for the photocatalytic degradation of 2CBP at pH of 2, 5, 7.2, 9 and 11

Fig. S5  Pseudo-first order plot for the photocatalytic degradation of 2CBP by all the synthesized photocatalysts and heterostructures

Table S1 Apparent first order kinetics data for the photodestruction of 2-CBP.

| S/N | Photocatalyst | K (min-1) | R2(Ln Cb/Cbo) | t1/2 (min) |
| --- | --- | --- | --- | --- |
| 1 | ZnO | 0.0012 | 0.966 | 577.6 |
| 2 | WO3 | 0.0010 | 0.990 | 693.1 |
| 3 | BiOI | 0.0046 | 0.983 | 150.7 |
| 4 | ZnO-BiOI 5% | 0.0005 | 0.983 | 1386.3 |
| 5 | ZnO-BiOI 10% | 0.0054 | 0.964 | 128.4 |
| 6 | ZnO-BiOI 20% | 0.0016 | 0.996 | 433.2 |
| 7 | ZnO-WO3 5% | 0.0036 | 0.987 | 192.5 |
| 8 | ZnO-WO3 20% | 0.0029 | 0.978 | 239.0 |
| 9 | ZnO-WO3 10% | 0.0049 | 0.969 | 141.5 |

Table S2 Effect of catalyst dose on the photodegradation of 2CBP.

| Catalyst dose(mg) | Degradation (%) | Kapp (min-1) | R2 |
| --- | --- | --- | --- |
| 35 | 57 | 0.0054 | 0.964 |
| 70 | 57 | 0.0085 | 0.989 |
| 85 | 71 | 0.0077 | 0.999 |
| 100 | 30 | 0.0013 | 0.997 |
| 150 | 4 | 0.0003 | 0.998 |

Table S3 Effect of pH on the photodegradation of 2CBP.

| pH | Degradation (%) | Kapp (min-1) | R2 |
| --- | --- | --- | --- |
| 2 | 20 | 0.0015 | 0.999 |
| 5 | 34 | 0.0027 | 0.999 |
| 7.2 | 57 | 0.0054 | 0.964 |
| 9.1 | 10 | 0.0007 | 0.995 |
| 11.3 | 5 | 0.0003 | 0.997 |

Table S4 Average crystallite sizes of the bare photocatalysts and heterostructures

| Sample | FWHM | Average crystallite size (nm) |
| --- | --- | --- |
| ZnO | 0.2295 | 37.6 |
| WO3 | 0.6533 | 12.9 |
| BiOI | 0.2068 | 40.0 |
| ZnO-BiOI 5% | 0.5276 | 16.4 |
| ZnO-BiOI 10% | 0.2797 | 31.0 |
| ZnO-BiOI 20% | 0.1887 | 45.0 |
| ZnO-WO3 5% | 0.2441 | 35.4 |
| ZnO-WO3 10 % | 0.1759 | 49.0 |
| ZnO-WO3 20 % | 0.2687 | 31.0 |