Table 1: Summary of the general properties of conventional and synthesized calcium carbonate

| Properties | GCC | PCC | Comment | References |
| --- | --- | --- | --- | --- |
| Chemical properties Purity Physical Properties Particle size Refractive index Surface area Brightness Whiteness Opacity Particle shape Structural properties: particle shape, morphology pH Functional Properties Rheological control | 90 -98 % - Wide range of particle sizes: - Fine powders (< 10 μm): - Fine ground: (70 % < 2 μm) - Ultrafine ground (90 % < 2 μm) 1.48-1.65 5-12 (m2/g) 89-93 % > 94 % High Irregular “blocky” Rhombohedral, irregular, blocky - Controlled through particle size adjustment | > 99 % < 2 μm 1.48-1.7 4-25 (m2/g) 92-95% 92 - 95 % Higher Rosette/blocky Scalenohedral, blocky, needle, rosette shaped 9 in 1 dm3 of solution Controlled through particle size adjustment | GCC has relatively more impurities. A small number of products can reach 95% purity. - Similar refractive index for GCC and PCC Higher surface area can be achieved for PCC Some products can reach 96-97 % whiteness GCC and PCC influence the rheological behavior of materials such as cement during application | (Erdogan and Eken 2017b; LLP 2024; Rothon 2017; Zevenhoven et al. 2010) (Erdogan and Eken 2017a; Mewar Microns 2024a; Seo et al. 2014) (Hubbe and Gill 2016) (Hubbe and Gill 2016) (Daswell 2025; Erdogan and Eken 2017a; Seo et al. 2014) (Daswell, 2022a; Moon et al., 2002) (Group 2023) (Hubbe and Gill 2016) (Erdogan and Eken 2017c) (Mewar Microns 2024b) |