Tailored activation of biochar and bone char for targeted removal of PTE under controlled conditions

Supplementary material

Table S1 ANOVA of fractional factorial experiment design factors for Cu removal from biochar (BC) activation with NaOH

| Source of variation | Degrees of freedom | Sum of Sqr | Mean Sqr | F-value | p-value |
| --- | --- | --- | --- | --- | --- |
| Model | 7 | 18721.055 | 2674.440 | 2.7938 | 0.0282* |
| Thermal treatment | 1 | 16735.957 | 16702.760 | 17.483 | 0.0003* |
| Concentration | 2 | 160.918 | 80.459 | 0.1681 | 0.6854 |
| Impregnation Time | 4 | 10.923 | 2.731 | 0.0114 | 0.9158 |
| Thermal treatment * Concentration | 2 | 10.14 | 5.070 | 0.0106 | 0.9189 |
| Thermal treatment * Impregnation Time | 4 | 103.199 | 25.800 | 0.1078 | 0.7455 |
| Concentration * Impregnation Time | 8 | 934.307 | 116.788 | 0.976 | 0.3330 |
| Thermal treatment * Concentration *Time | 8 | 36.849 | 4.606 | 0.0385 | 0.8461 |
| Error | 24 | 22974.472 | 957.27 |  |  |
| Total | 31 | 41695.527 |  |  |  |

Table S2 ANOVA of fractional factorial experiment design factors for Pb removal from biochar (BC) activation with NaOH

| Source of variation | Degrees of freedom | Sum of Sqr | Mean Sqr | F-value | p-value |
| --- | --- | --- | --- | --- | --- |
| Model | 6 | 1658.529 | 236.933 | 2.8054 | 0.0277* |
| Thermal treatment | 1 | 1069.360 | 16702.760 | 12.6617 | 0.0016* |
| Concentration | 2 | 2.423 | 1.212 | 0.0287 | 0.8669 |
| Impregnation Time | 4 | 10.523 | 2.631 | 0.1246 | 0.7272 |
| Thermal treatment * Concentration | 2 | 27.043 | 13.522 | 0.3202 | 0.5767 |
| Thermal treatment * Impregnation Time | 4 | 73.321 | 18.330 | 0.8682 | 0.3607 |
| Concentration * Impregnation Time | 8 | 402.569 | 50.321 | 4.7666 | 0.0390* |
| Thermal treatment * Concentration *Time | 8 | 277.400 | 34.675 | 3.2845 | 0.0825 |
| Error | 25 | 2026.954 | 84.456 |  |  |
| Total | 31 | 3685.483 |  |  |  |

Table S3 Kruskal–Wallis p-values of fractional factorial experiment design factors for Mn, As, Cd, and Zn removal from biochar (BC) activation with NaOH

| Source of variation | Degrees of freedom | p-value |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  | Mn | As | Cd | Zn |
| Thermal treatment | 1 | 0.9549 | 0.2136 | 0.7063 | 0.8796 |
| Concentration | 2 | 0.1291 | 0.6983 | 0.1338 | 0.2629 |
| Time | 4 | 0.9433 | 0.3759 | 0.5353 | 0.1829 |

Table S4 ANOVA p-values of activation experiment design factors for vermiwash bone char activation

| Source of variation | Degrees of freedom | p-value |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | As | Cd | Cu | Mn | Pb | Zn |
| Vermiwash | 1 | 0.4618 | 0.5464 | 0.7154 | 0.2952 | 0.9606 | 0.5928 |
| Time | 1 | 0.7440 | 0.2700 | 0.1381 | 0.3653 | 0.0767 | 0.4097 |
| Vermiwash * time | 1 | 0.0915 | 0.4016 | 0.5228 | 0.3243 | 0.8390 | 0.3797 |